## Slide 1
The Tipsy single soft photon detector:
A pixelized detector for single free electrons in vacuum
with ps time resolution
Hassan Akhtar, Yevgen Bilevych, Hong Wah Chan, Edoardo Charbon,
Harry van der Graaf, Kees Hagen, Gert Nützel,
Serge D. Pinto, Violeta Prodanović, Daan Rotman, Lina Sarro,
Dennis R. Schaart, Emile Schyns, John Smedley, Shuxia Tao, Annemarie Theulings
MCP Conference
Argonne National Lab
Argonne, Ill, USA
Dec 4, 2014
Alternatives to MCPs

## Slide 3
Tipsy principle use pixel chip as 2D sensitive anode
dynode stack above individual pixel
set of closely spaced transmission dynodes

## Slide 4
A very successful photon detector: the Photomultiplier (1934 -1936)
‘good’ quantum efficiency
rather fast
low noise @ high gain: very sensitive
little dark current, no bias current
radiation hard
quite linear
voluminous, bulky & heavy
no spatial resolution, not even 1D
expensive
quite radioactive
can’t stand B fields
Amplification by multiplication: low noise!

## Slide 5
glass window
photo cathode
1st dynode
2nd – 5th dynode
input pads
pixel chip
Reduce size of dynodes (volume downscaling),
and place set of dynodes on top of pixels of
CMOS chip
keep potentials as they were (Vstep ~ 200 V)
(non relativistic) electron trajectories same
form, but smaller (volume)
multiplication yield: assume SEY ~ 4, typical for PMs
pixel input source capacity: only ~ 10 fF
required gain ~1000 = 2.54 = : 5 dynodes sufficient
VACUUM!
No ‘gas amplification’
1 mm
Apply MEMS Technology:

## Slide 6
Hamamatsu: the first MEMS made μPMT
Small dynode geometry as in Tipsy

## Slide 7
MCP (in
vacuum)
John Vallerga: TimePix + MCPs
We do not know how to make MEMS made MCP.
Problem: aspect ratio of holes
But recently Nicolas Wyrsch (Univ of Neuchatel, Swiss) has success (NDIP 2014, Tours, France)
Use a MicroChannelPlate MCP?
Quantum Limited Imaging Detectors, RIT 2009, John Vallerga, jvv@ssl.berkeley.edu

## Slide 8
New: the Transmission Dynode:
faster
more compact
B compliant
rad hard

## Slide 9
Thin (~10 nm), planar dynodes, spaced ~ 30 μm
CMOS pixel chip, square pitch ~ 55 μm
Electron crossing time ~ 5 ps: straight short path due to homogeneous E-field
With gain of ~ 30 k: digital (1 V) signal on pixel input pad (small source cap)
Very strong electric field between dynodes, but far away from Fowler-Nordheim limit
B-field has little influence since Lorentz force is small wrt. electrostatic force
Signal development on pixel chip defined by crossing of the last gap (~ 2 ps)
No ion feedback (not even a little bit)
Noise-free electron multiplier
No bias current: no bias current noise or bias current dissipation
radiation hard
window + photo cathode
Ultra thin planar dynode membranes
vacuum
CMOS pixel chip
“the best electron is a free electron”

## Slide 10
Competitor:
Si-Photomultipliers (APDs, SPADs, D-APDs)

## Slide 11
Competition: Silicon Photomultipliers Photo Diodes
Avalanche Photo Diodes APD
Single Photon APD SPAD
Digital SPAD
Very popular:
Planar, thin
Cheap
Operate in B-field
Potentially QE = 1
faster than PMTs
But they are:
noisy
have bias current
suffer afterpulsing
hard to pixelize
limited to ~ 40 ps
not so radhard

## Slide 12
Essential difference between SiPMs and Tipsy
noisy <==> free-of noise
SiPM
Tipsy/MEMBrane
1200 V
4 - 40 V
Ee = ~ 250 eV
Ee = 1.2 + Δ eV

## Slide 13
Ultra thin membranes
Delft University of Technology: DIMES
SiliconNitride
Thickness 15 nm!

## Slide 14
window + photo cathode
Ultra thin planar dynode membranes
vacuum
CMOS pixel chip
First (2D) simulations: influence magnetic field
0 Tesla 1 Tesla

## Slide 16
Array of ultra thin domes

## Slide 17
MicroElectronicMechanicalSystems ‘MEMS’ Technology
- ultra thin membranes
Cone shape dynode section:
  focusing electron from above
  focusing emitted electrons
  mechanically robust: larger diameter cones feasible
A new single, free electron detector in vacuum
transmission dynodes
+
pixel chip

## Slide 18
Timed Photon Counter
TiPC, Tipsy
Thin, planar, light single soft photon detector
Electron crossing time tc = D √ (2 m/qV) = 5 ps for V = 150 V, D = 20 μm
Electron path: quite straight line towards next dynode
30 k e- enough for digital signal on pixel input pads: 7 dynodes adequate
Signal response after 7 x 5 ps = 35 ps
Time resolution determined by last electron crossing time: ~ 2 ps
Spatial resolution determined by pixel granularity (55 μm x 55 μm)
No noise from electron multiplier, no bias current from electron multiplier
Radiation hard
Operates in magnetic field
But:
Secondary electron emission yield not known
Very strong electric field between dynodes: Fowler-Nordheim limit (109 V/m)
QE limited by QE of classical photo cathode (20 – 40 %)!
Fast: electron mobility is highest
for free electrons in vacuum
Low noise: no bias current

## Slide 19
Transmission Dynode construction

## Slide 20
First realistation of transmission dynode @ DIMES, Delft University of Technology
dia 25 μm
15 nm thin dynode material
Si Rich SiNitride (SRN)
Fabio Santagata
Lina Sarro
Hong Wah Chan
Violeta Prodanović
DIMES, TU-Delft

## Slide 21
Secondary electron emission yields of SiNitride: Fijol et al.

## Slide 22
Depth-of-penetration of 300 eV electron
in dynode material: ~ 5 nm
from simulations
from SEY of reflective dynodes with different active layer thickness
Expected for
transmission dynodes:
SEY same order as for reflective dynodes
SEY above about equal to SEY below

## Slide 23
Secondary Electron Yield
SEY Measurement 1 in SEM
SEM/TEM to measure reflection/transmission SEY@
Particle Optics Group TU Delft
Dual Faraday Cup in SEM
made at Nikhef

## Slide 24
itop
itmesh
isample
ibmesh
ibot
incoming primary beam
secondary electrons (reflective and tranmission)
backscatter & punch through electrons
Dual Faraday Cup

## Slide 25
Dual Faraday Cup
First preliminary result: SEY (transmission) = 1.3
suffer charge up effects

## Slide 26
electron gun
(Kimball Physics)
TimePix
SEY measurement 2
Set-up at Nikhef
dynode under test

## Slide 28
….with a permanent magnet placed 1 m away…..
60 eV electrons on TimePix (without dynode)

## Slide 29
SEY Measurement 3
Photo emission spectrum (PES) - a new way of measuring SEY in Si3N4 proposed by John Smedley
Photon( about 400eV)  Auger electron( 400 eV) Secondary electron
First round measurements April 2014
@synchrotron rad. beam line NSLS Brookhaven National Laboratory;
Second round proposals @BESSY Berlin & ALS LBNL
obtain energy distribution
by varying inverse bias voltage

## Slide 30
Theoretical support
Solid State Physics (no high energy physics!)
Inpact of ~500 eV e- in matter:
  energy transfer to electrons
  scattering, phonon production
result: distribution of energetic electrons in volume dV
Propagation (diffusion) of energetic electrons to surface
(cross sections, phonon losses)
Electron emission in vacuum: electron affinity (Work Function, Escape Potential

## Slide 31
Fig. 1. Schematics of a transmission dynode. Primary electrons (PE) hit the dynode from the top, secondary electrons (SE) and back scattered electrons (BSE) leave the dynode from the top and forward scattered electrons (FSE) and transmission secondary electrons (TSE) leave the dynode from the bottom.
transmission and forward scattered
electron yield as a function of the
energy of the incoming electron.
Layer thickness 20 nm. An electron
affinity of 1,5 eV was assumed
Low-energy GEANT extensions

## Slide 32
Fig. 4. Measured SE counts for a SRN sample irradiated with 420 eV photons. The sample is biased by -15V.
Fig. 5. Simulated spectrum of the energy distribution of SE’s where the photons create 'primary electrons' of 300 eV in the sample. The electron affinity is taken to be 1.5 eV. The simulated sample is not biased.
Data from NSLS-Brookhaven

## Slide 33
Important results on H termination and alkli
metal and metal oxide
Electron Affinity:
Density Functional Theory DFT Simulations
H termination on diamond
- Negative Electron Affinity
- Enhanced SEY
Vienna Ab-Initio Simulation Program
VASP

## Slide 35
SEY measurements
Density Functional Theory simulations
Monte Carlo simulation
Dynode fabrication
Electronic
structure,
work function,
optical data
Select doping/
coating candidates
SEY
Energy spectrum
Material
Property
Fabrication
Model
validation

## Slide 36
The low-energy simulations seems to agree with the photon test beam data
A clear difference in SE emission was observed from SiNitride samples
unprocessed and H- terminated
Electron affinity can be well calculated using ab-initio simulations.
It has been predicted that H-termination works for SiNitride as well as
diamond (which is known). Li-termination may even be better

## Slide 37
For tracking of fast charged particles (MIPS):
Replace photocathode (depleted Si or gas) by:
electron emission membrane e-brane
e-brane
aluminium foil:
- at least 1 electron is emitted in 2 - 4 % of the cases
energy of electron: 0 – 5 eV
probability depends on surface condition
increase to 6 % if layer of AlOxide is present
Emits (at least one) electron at the
crossing point of membrane surface
and MIP, with a high probability, in vacuum

## Slide 38
electron emission membrane ‘e-brane’
Issue: to reach a high yield (prob. to emit at least one electron) > 50 – 95 %
low work function material (low exit potential)
Plain aluminium foil: 2 – 4 % yield
2. Surface enlargement
Skin effect: only ~ 50 nm
surface layer participates to yield
3. Field assistance
(depletion layer)
4. Strong extracting E-field
…..needs solid state (theoretical) physicists…..
Fractal
nano grass

## Slide 39
Electron Affinity
Interesting: - photo cathodes of PMs (bi-alkali etc)
- coating of dynodes of PMs
What is the yield of a photocathode?
120 GeV pion+
100 % yield, due to Cerenkov photons created in entrance window
With pions+ from opposite direction?

## Slide 40
First test in 120 GeV pion beam (H6B ATLAS/MAMMA), Sept 21 2012.
Second test with photon absorber on window at RD51 testbeam on Nov 12, 2012.
~ 51 Ch photons expected
in 2 mm crown glass window

## Slide 41
Thermal noise: single electrons from photocathode
(naked) PM in Cherenkov mode
Yield: 100 %
(naked) PM in non Cherenkov
mode. Yield: 100 %
(naked) PM in non Cherenkov
mode, with exiting Ch photon
absorber. Yield: 29 %

## Slide 43
Surface enlargement
Skin effect: only ~ 50 nm
surface layer participates to yield
Fractal
Use surface enlargement for high QE photocathodes?
The QE of Tipsy of ~0.3 is its only disadvantage wrt. Si-PMs
Surface roughening: papers + Hamamatsu

## Slide 44
PET scanner
Cherenkov radiation becomes more relevant
PET
0.511 MeV gamma
with Pb glass:
only prompt Ch soft photons
With NaI: Ch + Sci soft photons
use Ch photons for timing
use all photons for energy
granularity: multi single soft photon
detection within event
low noise
Applications of new generic soft photon detector

## Slide 45
Future HEP collider experiment: inner (central) tracker
very low detector mass
Tipsy layer at safe distance from IP
spatial resolution: no extrapolation
The Vacuum Cherenkov Tracker
thin transparent foils
generating Cherenkov photons
Tipsy
Cylindrical layer

## Slide 46
Only one crucial milestone/deliverable:
a MEMS made transmission dynode with a
secondary electron yield (SEY) > 3
for an incoming e- with energy lower than 500 eV

## Slide 47
Hassan Akhtar, Yevgen Bilevych, Hong Wah Chan, Edoardo Charbon,
Harry van der Graaf, Kees Hagen, Gert Nützel,
Serge D. Pinto, Violeta Prodanović, Daan Rotman, Lina Sarro,
Dennis R. Schaart, Emile Schyns, John Smedley, Shuxia Tao, Annemarie Theulings
Thanks to Arjen van Rijn, Michiel Jaspers, Oscar van Petten, Gerrit Brouwer,
Wim Gotink, Joop Rövekamp, Bas van der Heijden, Berend Munneke, Henk Peek