## Slide 1: Updates and status on the next generation of Superconducting RF cavities
7th of March 2013
Argonne National Laboratory
DOE Review 2013
Speaker: Thomas Proslier
DOE Review 2013

## Slide 2: solutions
Here we aim at transformative technology changes in SRF technology
by developing a predictive understanding of the materials
physics issues currently limiting SRF technology and by applying
this understanding to significantly improve cavity performance.
A. Gurevich, APL 88, 012511
DOE Review 2013

## Slide 3
Cavity ALD growth
Max size coupons: 2.5” OD-12” long
Test chamber-coupons growth
ILC shape single cell: ~15” long
Gas Out
Gas in
DOE Review 2013

## Slide 4
Synergy onsite
MSD/HEP
PHYS/APS/HEP
Surface treatments
RF testing
Material science
fundamentals
Single Cell Nb Cavities
FNAL
DOE Review 2013

## Slide 5
First cavity test
But:
Program stopped during deposition
Resist HPR and sonicator
BCP does not work -> tumbling @ Fermi (in line)
DOE Review 2013

## Slide 6
Blind Baseline test ANL
Improper Magnetic shielding.
Valve leaking
New shielding
New valves
PAV002 uncoated: Fermi Baseline Q~ 1010
ANL Baseline Q ~ 109
Re-test: Q~ 1010 , Good calibration Accelerating field.
Coated PAV002 cavity with NbTiN/AlN/Nb
RF test on March 07
Coat Jlab ILC cavity with AlN/MoN/AlN/Nb
  Coating 13th March
DOE Review 2013

## Slide 7
Scares Nb cavities / bottleneck of iterations (Jlab/FNAL …)
RF coupons testing as preliminary measure
DOE Review 2013

## Slide 8: RF testing station for coupons
Network
Analyzer
out
in
Available for this project:
cryostat with 3-axis magnet (9T||z, 1 T ||x,y)
VTI (1.5 K – RT), 2.5”
4”
1.9”
18.7 Ghz <-> 3.4 mm
Accommodates:
resonators patterned from new materials;
custom mounts
small-scale cavities
DOE Review 2013

## Slide 9
Superconductors by ALD (thin films)
DOE Review 2013
MoN
condition ξ< d << λ

## Slide 10: MoN by ALD: Gap
1600 cy = 60 nm
Δ = 2 meV
HPR on Si coupons -> didn’t change
Cu coupons -> changed
AlN/MoN/AlN
TiN/MoN/TiN
DOE Review 2013
-> no change

## Slide 11: MoN in Magnetic filed
MoN
H
HC2 [0K] = 13.5T
ξ [0K] ~ 6 nm
ξ [2K] ~ 6.6 nm
At least 10 x higher than NbTi
MoN 60 nm on 0.6 mm Cu wire
IMAX ~ 1 Amp
Assume
60 nm
Measure by Tunnel diode

## Slide 12: MoN superconducting wires
Cu Stranded wires Coil
260 wires/ 50 μm diameter
IMAX = 8000 Amps
2”
80 nm

## Slide 13: Superconducting undulator
Cooling tube
Beam chamber
SE
Mo
Cu
Testing/collab with Y. Yvanyushenkov
NbTi: 700 Amps

## Slide 14
Synergy deposition techniques: Nb onto Cu
HIPIMS/Berkeley
ALD/ANL
Early career award
ECD/Jlab & Alameda
DOE Review 2013

## Slide 15: Initial surface roughness?
Cu surface: Surface roughness, Sticking onto Cu
μm Sup films <-> roughness
4/HPR, All
3/EP (Able Electro)
2/Mechanical polish
(mirror-intermediate(5μm))
1/Machining
AlN/MoN
600nm
~1μm
>30μm
10 coupons
intermediate(5μm)
1 Cu cavity EP
1 Cu cavity Pol + EP
Nb/ Cu cavity
from Jlab
DOE Review 2013
APS optic shop

## Slide 16: Sticking/diffusion barrier
Nb on Cu
High RRR for T >~ 400 C
BUT! delamination occurs
Solution: seed layer/diffusion barrier
ALD can Help:
Nitrides
TiN, AlN, MoN/TiN coating works
DOE Review 2013
Send coupons to HIPIMS/Alameda/Jlab
RF tested @ Jlab (end of March)
Send EP Cu Cavity to Alameda (20 march)
Dep of Nb @ 450C and above.
HPR 2000 psi
AlN/NbTiN
600 nm
HPR 2000 psi
AlN/MoN/AlN
900 nm
Nb sputt @ ANL @ 450C in 10-7 Torr

## Slide 17
HIPIMS (High Impulse Magnetron Sputtering)
DOE Review 2013

## Slide 18
HIPIMS of Nb/Cu or Al: Superconductivity @ ANL
High Quality Nb/Cu or Al
 bulk Nb
Resist HPR test
Mix Nb-Cu
DOE Review 2013

## Slide 19
Cavities test  Uniformity
Test Cavity-coupons Jlab (Kneisel)
Uniform cavity heating in HIPIMS chamber
Fast heating + UHV compatible: IR solution (Heraeus)
Varying the speed of the magnetron arm
-> control on uniformity
2” OD magnetron do not ignite (e mfp interrupted)
1” OD -> ignite inside the cavity tube/ small I
DOE Review 2013

## Slide 20: Point contact
DOE Review 2013
Very low gap -> proximity effect?
X-ray on coupons at IIT -> Nb2N phase (no NbN)
1/ ANNEALING IN N2 (FERMI)

## Slide 21: Point contact
2/ ANNEALING of Nb IN UHV (JLAB)
DOE Review 2013
Correlation with Cavity results:
1400 C heat treatment homogenized gap
To bulk Nb.
Ongoing temp for higher temp treatment

## Slide 22
MSD ALD-PCT-characterization
J. Klug, N. Groll,
N. Becker, C. Cao
HEP support-funding
Th. Proslier
Collab
Berkeley, FNAL, JLAB
A. Anders, R. Mendelsberg
A-M. Valente, Kneisel, Giovati
PHYS-APS Testing
M. Kelly
DOE Review 2013

## Slide 23
Conclusion
Opportunities Coils
Cu Cavity/Nb cavity coating tests
    Multilayers
    Seed layers
    Not enough Nb cavity!
DOE Review 2013

## Slide 24: PCT Spectrum Dependence on Junction Resistance
NbO
Nb
High Z junction
Low Z junction
Au Tip
Depairing region
NbO2
Nb2O5

## Slide 25: Γ collapses for Z < 1.5
Au tip scraping through surface oxide removes depairing

## Slide 26: Fermi lab cold spot
Significantly lower Γ values

## Slide 27
28nm Nb0.8Ti0.2N (without AlN layer)
Tc= 8.3K
by SQUID
Δ(meV)
Γ(meV)