## Slide 1
Ultra-Fast Silicon Detectors
Applications
Principle of UFSD
Time resolution
Segmented UFSD
Hartmut F.-W. Sadrozinski
SCIPP, Univ. of California Santa Cruz, CA 95064, USA
for the
UFSD Group
UCSC – Torino – CNM Barcelona – IJS Ljubljana- LPNHE

## Slide 2
Ultra-Fast Silicon Detectors (UFSD)
Since 2012, we have been developing a new type of sensor and its associated readout electronics, called an ultra-fast silicon detector (UFSD), allowing detection of charged particles over large areas, with very high data rates, and very high spatial precision and time resolution.
The sensor is based on a silicon detector (Low-gain avalanche detector = LGAD) with a new implantation scheme during the sensor fabrication to achieve internal gain without electrical breakdown. It allows an improvement of the time measurement for large area detector arrays by about a factor of 1000 from ~ 10 nano-seconds to ~ 10 pico-seconds.
We expect profound impact in many fields where the timing of charged particles is important.
To name a few:
Tracking: Reduction of random coincidences, by adding a 4th dimension (time).
Vertex Locator: Forward physics in AFP2, HGTD (ATLAS), CT-PPS (CMS)
Time of Flight (ToF): Mass Spectroscopy, Particle ID, Remote Vision
Particle counting: Dose in hadron beams
Energy of low-energy protons: Proton CT (pCT) and Interaction Vertex Imaging (IVI) in hadron therapy
Hartmut Sadrozinski, “Exploring charge multiplication for fast timing with silicon sensors”, 20th RD50 Workshop,
https://indico.cern.ch/getFile.py/access?contribId=18&sessionId=8&resId=1&materialId=slides&confId=175330

## Slide 3
Applications of UFSD in HEP
Several potential applications for UFSD are proposed for instrumentation at particle colliders.
Time-of-Flight (ToF)
ToF will measure the flight path for relativistic particles of a known start time to a few millimeters along the flight direction, in systems with fine granularity in the two perpendicular directions. This offers a significant new capability for large detectors where measurements of the flight path have typically been too coarse to be useful.
Alternatively, for a known path length, the timing measurement can be used to very accurately measure the particle velocity, a classic method to identify the particle mass when combined with a momentum measurement (“Particle ID”).
Advantage: thin ToF sensor.
Coincidence timing to suppress accidental coincidence
For groups of particles hitting an UFSD array, the timing can be used to combine particles with near simultaneous arrival times to distinguish signals from out-of-time backgrounds. In the past this has been used on the level of 10’s of ns to identify the beam crossing, while UFSD will enable us to look into the substructure of an event and associate particles coming from the same z- vertex.

## Slide 4
Identification of the Longitudinal Vertex
ATLAS High-Granularity Timing Detector HGTD
4 active layers per side (~10 m2 in total) in front of FCAL
HGTD baseline dimensions:
Z =[3475, 3545] mm ; ΔZ=70mm
Rmin ~ 90 mm (ηmax≃4.3), Rmax ~ 600 mm (ηmin≃2.4)
Possible to extend η=5.0 (Rmin ~ 50mm)
Required timing resolution: 50 – 100 ps
There are several (6?) technologies being considered.
Radiation Levels: (scaled to 3000 fb-1):
- (1-3)x1015 n/cm2
- (0.3-2.4)x1015 hadrons/cm2 (>20MeV) ~100 Mrad
A challenging project for the radiation resistance of UFSD.
CNM started to work on the UFSD Implementation
2x2 array with 1 ASIC
Thinned 50 µm SoI

## Slide 5: PPS by CMS & TOTEM = CT-PPS
A Totem-CMS combined spectrometer to detect
high momentum – high rapidity protons.
CMS ip5
RP + 200 m
RP – 200 m
Timing
Timing
Tracking
Tracking
Tracking and timing
detectors positioned
inside Roman-pots.

## Slide 6: CT-PPS Basic Design: Timing
Vertex z-by-timing: ~ 2 mm:
Time resolution ~10 ps
Segmentation: 1 - 3 mm
Edgeless, active to ~ 200 micron from edge
Radiation hard:
Lifetime > ~ 1 year at LHC at 1034 (~5*1015 p/cm2)
Rate: 25 ns sensitivity
        Current solution: quartz bars
        Upgrade solution: UFSD
Segmented LGAD,
with pad/pixel size
varying with distance
from the beam.
LGAD and readout
ready for beam test.

## Slide 7
Low-Gain Avalanche Detectors (LGAD)
Low-Gain Avalanche Detectors (LGAD) are based on the principle of SiPM or APD, but with moderate internal gain (10 – 20) and analog response.
Adding a thin p-layer to a n-on-p silicon sensor to increase the E-field and deep n-implants at the edges generate moderate charge multiplication without breakdown.
G. Pellegrini, et al., Nucl. Instrum. Meth. A765 (2014) 12.
The technology is being developed as a RD50 Common Project.
After 7+ manufacturing cycles at CNM (Barcelona) addressing general issues like gain variations, bias voltage reach, leakage current reduction, segmented sensors etc. we now have submissions targeting specific applications mentioned previously.
A second supplier, FBK (Trento), is starting fabrication with mainly INFN funding.

## Slide 8
Gain Calibration with a’s from Am(241)
“Electron injection” with a’s from Am(241) or with red laser illuminating the back side, range ~ few um’s, electron signal drifts and is then amplified in high field, holes drift back.
a’s
Colin Parker, M.S. Thesis UCSC
Large bias voltages reach.
Gain of 15, can be tuned within factor 2x with bias voltage.
2x
Initial e-
e- & h+ from multiplication
Pulse shapes for high-gain (red), low-gain (blue) LGAD and no-gain sensor (yellow)

## Slide 9
Signal Characteristics vs. UFSD Thickness & Gain
No-gain sensors:
rise time and pulse height independent
of thickness
LGAD:
pulse height independent of thickness
thickness determines peaking time (~ electron collection time) and slew-rate
Pulse duration scales with thickness due to saturated drift velocity in high fields
Gain = 10
Gain = 1
50 µm
Gain = 1
Weightfield 2
(WF2)
Simulations
F. Cenna, et al., Nucl. Instrum. Meth. A796 (2015) 149

## Slide 10
Time Resolution and Slew Rate
The time resolution σt depends on the rise time τr i.e. the collection time (~ detector thickness) and signal amplitude S. It has 3 terms:
time walk due to amplitude variation, time jitter due to noise N, and binning resolution:
introducing the slew-rate signal/rise time S/τr = dV/dt.
For constant noise N, to minimize the time resolution, we need to maximize the slew-rate dV/dt of the signal. Need both large and fast signals.
Dependence of the slew-rate dV/dt on the LGAD thickness and gain
50 micron:
~ 3x improvement with gain = 10
Large slew rate, good time resolution
Significant improvements in time
resolution require thin and small sensors
WF2 Simulations

## Slide 11
Measured Time Resolution of UFSD: IR Laser
IR Laser irradiating 300 µm sensors to measures the intrinsic time jitter, of both LGAD and no-gain diode (PIN).
11
For 1 MIP, an UFSD with gain ~ 6 shows a factor of 3 better time resolution than PIN diodes: 70 ps vs 200 ps
For many MIPS the difference is decreasing (important for timing calorimeter)
(7859 W1E10-3)
Hartmut F.-W. Sadrozinski, Ultra-Fast Silicon Detectors. CPAD

## Slide 12
BT Timing Resolution I (Fixed Threshold)
Analysis: Chi Wing Ng (Tom) & Sze Ning Mak (Hazel)
1 MIP
CERN 2014 Beam Test of FZ LGAD 300 µm, C = 12 pF, G=10, BB
Bias 1000V, fixed threshold = 10 mV, filtered with 20 bins
Time walk is large
~ 400ps for MIPs
Resolution:
150 – 200 ps
Precise time walk correction looks non-trivial to incorporate into an ASIC.
Beam tests (BT) data aid in the development of the readout electronics.
Record signal waveforms with 50 ps sampling and analyze off-line.

## Slide 13
BT Timing Resolution II (Constant Fraction Disc.)
Abe’s unified pulse shape indicates uniformity of pulse shapes.
A low CDF has best resolution.
Analysis: Abe Seiden, Natasha Woods, Ben Gruey
CDF = 20% has no time walk
Timing resolution vs. CFD threshold for varying BW cut-off. Optimize the filter (i.e. shaping time) for each CFD threshold
Best time resolution (160 ps)
at low CFD threshold
CFD =20% Time
CFD is easily incorporated
into an ASIC.

## Slide 14
BT Timing Resolution III (Lower Capacitance)
July 2015 beam test, 2 FZ LGAD 300 µm, C = 4 pF (instead of 12 pF before), G=10 & 6, BB
Bias: 900V, CFD: 0->100%, filtered with variable BW.
Resolution: Time difference between two channels divided by sqrt(2).
Analysis: Abe Seiden, Natasha Woods, Ben Gruey
Best resolution 120 ps with CFD @ 8 -15% with BW cutoff ≈ 0.8 GHz
(c.f. 100 MHz for 3.5 ns rise time)
The two LGADs used have different gain. It's difficult to assign correctly the two time resolutions, but using simply the inverse of the gain G, we get:
σ(G = 6) =140 ps, σ(G = 10) = 80 ps

## Slide 15
Timing Resolution of UFSD (Laser, BT, WF2)
Up to now the only MIP data available are for 300 µm LGAD.
Good agreement between data (beam test & laser) and simulations (WF2).
Laser data have no time walk.
Improvements are due to reduction of capacitance which increases the pulse height and reduces the noise.
Prediction: resolution of 30 ps for 50 µm LGAD with gain of 10, needs ASIC
Reduction
of noise
No
time walk
Reduction
of capacitance

## Slide 16
Thin LGAD
MIP’s Pulse shape C = 34 pF, Gain = 3
Simulation of pulse shape (gain = 10)
Capacitance C [pF] | Rise time [ps] | Amplitude [mV] | dV/dt (relative) | Noise [mV]
34 | 710 | 7 | 1 | 3
2 | 390 | 24 | 5.2 | ALARA
Predicted improvement with reduced capacitance (50Ω input, Cividec Amp))
Beam test data provide reality checks for 10 ps electronics development.
We are starting to investigate options for the electronics chain for UFSD including the front-end parameters (shaping time, noise, architecture) on-chip data reduction, data transmission, ASIC technology, power consumption, etc.
We hope to organize a mini-workshop for these topics before the end of the year.

## Slide 17
WF2 Simulation: Radiation Damage (Trapping)
Weightfield 2 (WF2) Implementation and Simulation: Bianca Baldassari
300µm,
NO Gain
300µm,
Gain=10
50µm,
NO Gain
50µm,
Gain=10
The radiation induced change of the peaking time of thick (300µm) sensors bodes ill for timing.
The peaking time (and CFD time) of thin sensors is reasonably stable with radiation.
The rising edge of thin sensors is insensitive to trapping.
Effect of trapping in thick and thin detectors at large fluences is different since the trapping distance is ~ 50 µm.

## Slide 18
Radiation Damage in UFSD
Measurements of collected charge (CCE) with MIP’s done on 300 µm LGAD have confirmed the larger CCE degradation wrt no-gain diodes, as expected since the gain signal is in large part due to late drifting holes which have large trapping effects.
An additional effect resulting in a decrease in gain beyond trapping has been reported in 300 µm LGADs and needs investigation. The fact that this is observed mainly in high-gain LGAD and is leveling off at higher fluence is hard to explain in terms of “Acceptor Removal”.
An interpretation of the data in terms of modification of the field by trapped holes (“Double Junction”) impacts much less the collected charge in thin detectors since both the number of holes and the trapping are much smaller there.
Important to measure the gain (with electron injection by red laser) of thin LGAD with different gains (include no-gain diodes) as a function of fluence, temperature and laser intensity.
Investigate restoring gain loss after irradiation with increasing the bias voltage.
Pursue program to improve radiation tolerance by replacing Boron with Gallium.
Simulation of trapping:
overlap up to 2*1015 neq/cm2 with measurements and agree for low-gain LGAD.
At a fluence of 4*1015 neq/cm2
the 50 µm LGAD is predicted to
yield > 50% of the initial charge.

## Slide 19
Segmented LGAD I: Pixels/Strips
Electrode segmentation makes the E field very non uniform, and therefore ruins the gain and timing properties of the sensor
Non uniform E field
and Weighting field
Separation Timing and segmentation leads to p-on-p LGAD
Un-segmented gain layer (resistive sheet) with AC coupling
Reversed–LGAD design:
the gain is on the opposite
side of the read-out
We need to find a design that produces very uniform E field, while allowing electrode segmentation.
G.-F. Dalla Betta, et al., Nucl. Instrum. Meth. A796 (2015) 154

## Slide 20
Segmented LGAD II: Separate Functions
Large pads for time measurements
Small pixels for position determination
Gain layer
Reading from both sides gives the best of both environments:
      Position determination:
    finely pixelated electrodes, opposite to the gain layer.
    It can use present chips, for example PSI46, FEI4
      Time determination:
larger pads, near the gain layer
much fewer channels (~1/10)

## Slide 21
Segmented LGAD III: p-on-p
Thin p-in-p LGAD has a
very fast slew rate, comparable to n-in-p
Thick p-type LGAD relies
on late hole collection:
p-in-p not viable.
Will p-on-p work since holes are collected which are slower?
Yes, for thin LGAD!

## Slide 22
gain layer p+
AC coupling
n++ electrode
In the n-in-p design, the resistivity of the sheet is hard to control, as the doping of the n++ and p+ layers determine the gain, so the values cannot be chosen as we like.
p++ electrode
Gain layer p+
AC coupling
n++ electrode
In the p-in-p design, the resistivity of the p++ sheet is easier to control
p++ electrode
Resistive Sheet with AC-coupled Pixels

## Slide 23
Conclusions
Ultra-Fast Silicon Detectors promise excellent position and time resolution
Present proposals for their use deal mainly with the suppression of accidental background from different z-vertices in the same LHC event.
We made progress in understanding the principle and the expected performance of UFSD. Manufacturing is approaching maturity.
Simulations with Weightfield 2 (WF2) confirm timing resolutions extracted from beam and laser tests for 300 µm thick LGAD. WF2 is ready to be used to extrapolate to thin sensors.
Thin sensors are predicted to have many advantages. We expect results from UFSD with thickness down to 50µm later this year.
Need to start on frontend electronics and readout system for the first applications of LGAD at the LHC.
Part of this work was carried out in the framework of RD50 Common Projects and was funded by the US Dept. of Energy, the Spanish Ministry of Education and Science and INFN Italy.

## Slide 24
A. Anker, V. Fadeyev, P. Freeman, Z. Galloway, B. Gruey, H. Grabas, Z. Liang, S. N. Mak, C. W. Ng, Hartmut F.-W. Sadrozinski, A. Seiden, N. Woods, A. Zatserklyaniy SCIPP, Univ. of California Santa Cruz, CA 95064, USA
B. Baldassarri, N. Cartiglia, F. Cenna, M. Ferrero
Univ. of Torino and INFN, Torino, Italy
G. Pellegrini, S. Hidalgo, M. Baselga, M. Carulla,
P. Fernandez-Martinez, D. Flores, A. Merlos, D. Quirion
Centro Nacional de Microelectrónica (CNM-CSIC), Barcelona, Spain
M. Mikuž, G.Kramberger, V. Cindro, I. Mandić, M. Zavrtanik
IJS Ljubljana, Slovenia
Author List

## Slide 25
Ultra-fast silicon detectors (UFSD) afford very good time resolution for low-energy proton (or ions) since they have very high slew-rare.
The large slew rate due to the high specific energy loss of low-energy protons is enhanced by a factor 3 when a UFSD with gain = 10 is used. Timing resolution of < 10 ps for protons with E < 200 MeV are predicted.
The fact that UFSDs have their best timing capability when the sensor is thin (< 50 um) goes hand-in-hand with the fact that tracking of low-energy protons need thin sensors to reduce MCS (Multiple coulomb scattering).
Smaller UFSD with 200um thickness and 50um thickness are being produced at CNM.
UFSD for Low-Energy Protons

## Slide 26
Range straggling limit for 200 MeV p
4-D Ultra-Fast Si Detectors in pCT
Protons of 200 MeV have a range of ~ 30 cm in plastic scintillator. The resulting straggling limits the WEPL resolution.
Replace calorimeter/range counter by UFSD:
Combine tracking with WEPL measurement where the ToF of the proton measures the residual energy., with comparable or better resolution than the scintillator.
In support of Hadron Therapy, the relative stopping power (RSP) is being reconstructed in 3D.
The UCSC-LLU pCT scanner uses Si strip sensors to locate the proton and heavy scintillator stages to measure its energy loss (WEPL).
Light-weight,
all silicon
construction
ideal for
installation
Into the gantry

## Slide 27
Direction and energy of (low-energy!) secondaries are measured in telescopes of UFSD and projected back to identify the beam location.
D = 30 cm
UFSD: 50 um thin, pixels 300um x 300 um,
Time resolution of 30 ps,
i.e. (“100ps & Gain = 10”)
allows energy measurement by TOF
Energy resolution on secondaries:
100 MeV pions: 16%
100 MeV protons : 4%
UFSD can operate at 10+ MHz rate and provide real-time beam diagnostics.
Protons
Interaction Vertex Imaging (IVI) with UFSD
Head phantom
Hadron beam
Longitudinal distribution of energy deposition
(Bragg peak) and number of secondaries

## Slide 28
Resistive sheet with AC-coupled Pixels
gain layer
AC coupling
n++ electrode
The AC read-out sees only a small part of the sensor:
small capacitance and small leakage current.
p++ electrode
The signal is “frozen” on the resistive sheet, and it is AC coupled to the electronics
 E and Ew fields are very regular
Segmentation is achieved via AC coupling

## Slide 29
Details of AC coupling - I
Additional Rise time
RAmpl * Cdetector ~ 100 W * 1pF ~ 100 ps
Detector
Detector
Detector
Detector
Detector
Detector
C AC
RAmpl
RSheet
Freezing time
RSheet * CAC ~ 1kW * 100pF ~ 100 ns
Only a small part of the detector is involved
Resistive sheet with AC-coupled Pixels