## Slide 1: JCESR’s search for transportation batteries beyond lithium-ion
Kevin Gallagher
September 17th, 2015

## Slide 2: Electric Vehicles – Niche today…
California Market

## Slide 3: A better battery is one big requirement for larger EV market penetration
Good News:
Lithium-ion is pretty great
and it is getting better
Nykvist and Nilsson Nat. Climate Change (2015)
DOI: 10.1038/NCLIMATE2564
Battery $/kWh
Year

## Slide 4: The challenge: traditional Li-ion is unlikely to reach automaker goals for mass market
Cell level criteria from D. Andre et al, J. Mat. Chem. A, 3, 6709 (2015)

## Slide 5: How do we discover and develop a new battery with a lower cost curve?
1) Identify what success looks like…materials & system
via Techno-economic modeling
2) Determine guiding design rules for challenge
combining atomic & molecular level understanding to create intuition -> discovery
3) Refine
Remember:
JCESR is an experiment!

## Slide 6: Techno-economic modeling: Building a battery on the computer
Connects system level goals to materials challenges
Power
Energy
Depreciation, Overhead, ROI
System

## Slide 7: System Level Volume and Mass Predictions
7
Li-metal
Si anode
Higher
voltage

## Slide 8: System Level Volume and Mass Predictions
8
Magnesium?

## Slide 9: Battery price scales with mass and volume
9
$/kWh =
Processing costs also scale with size
Increase energy density!
($/kg)
(kWh/kg)
3 cell couples with potentially <$100/kWh and >400 Wh/l
Magnesium/Metal-Oxide
Lithium/Sulfur
Lithium/Metal-Oxide
Mg++
e
e
Li+
Li+
e
Mg metal anode
Metal oxide cathode
Li metal anode
Li metal anode
Sulfur
cathode
Metal oxide cathode

## Slide 10: Li-S: discovery of new electrolyte required
10
Liang et al Nat. Comm.10.1038/ncomms6682 (2015)
Current approach requires 10x excess of electrolyte for long life
Eroglu et al, J. Electrochem. Soc. 162 (6), A982 (2015) DOI: 10.1149/2.0611506jes
Low electrolyte volumes in Sulfur electrode result in Li2Sx disproportionation and passivation (poor performance)
Decreasing electrolyte

## Slide 11: Learn from the past: sparingly soluble reactant
Pb
PbSO4
Pb2+
commercial
Lead acid
1 mg/l
S
Li2S
Sx2-
Li2Sx
S62-
JCESR
status quo
Li2Sx fully solubilized
106 mg/l
Notes: understanding mechanisms allows JCESR to unravel the design rules and apply these to the development of performance enhancing electrolytes

## Slide 12: Towards design rules for sparingly soluble
12
Developing an electrolyte that conducts Li+ without dissolving Li2Sx
H.-L. Wu et al., ACS Appl. Mater. Interfaces 2015, 7, 1709−1719
K.C. Lau et al (2015)
Cuisinier et al Energy Environ. Sci. (2014)

## Slide 13: Mg… the indispensable battery of the future?
13
Mg is critical divergent research because we may never solve Li-metal challenge
This is challenging – effort has large computational component to held build intuition through iteration with experiment
Genomic Search
Mg Diff.
Mg NMR
APS/ALS

## Slide 14: Mg metal plating/stripping shows strong structure activity relationship
14
~100% Coulombic efficiency possible! Subtle chemistry requires careful control
cycling in a Mg chloroaluminate
500 nm
-
-
-
-
-
-
-
-
-
-
-
-
100
99
98
coulombic efficiency
500 nm
2 mm
pseudoepitaxy
re-nucleation
porosity
N. Hahn et al J. Phys Chem C submitted (2015)

## Slide 15: To conclude… new materials required for “true” mass market electric vehicles
Metal anodes with high energy cathodes are promising path to <$100/kWh and >400 Wh/l
T-E Modeling used to identify what success looks like at system and materials levels
Integrated characterization, synthesis, & computation efforts to overcome identified challenges