Analysis of Secondary and Field Emission Inside of a

1.3GHz Radio Frequency Electron Gun

Robert Inzinga

Illinois Wesleyan University, Bloomington, Illinois 61701

Raymond Fliller

Fermi National Accelerator Laboratory, P.O. Box 500, Batavia, Illinois 60510

Instances of secondary emission occurring at the photocathode region of a 1.3GHz RF electron gun were investigated by performing phase scans through one RF cycle.  Data sets obtained were compared to simulations performed in ASTRA.  By identifying the secondary emission in the data, the particular secondary emission parameters for the photocathode can be obtained.  In addition, simulations of field emission performed in ASTRA show that only a small amount of field emitted electrons emitted from the irises collide with the photocathode region.

I.  Introduction

This paper looks to identify the circumstances under which secondary emission occurs on a Cesium Telluride, Cs2Te, photocathode inside of an RF gun.  Secondary emission occurs when a primary electron collides with the photocathode and upon impact causes other electrons to be ejected from the surface.  These secondary electrons are then free to be accelerated by the electric field in the cavity.

Instances of recurring secondary emission at the photocathode can lead to multipacting inside of the cavity and cause undesirable damage to the photocathode.  Multipacting occurs when electrons repeatedly strike the photocathode surface, releasing secondary electrons which also impact the photocathode causing an avalanche of electrons.  This is found in the A0 Photoinjector at FNAL. It is believed that secondary emission from the photocathode feeds this multipacting and this study aims to understand the properties of secondary emission at the photocathode.

To look for evidence of secondary emission, we varied the phase of the RF relative to the laser pulse which causes photoemission.  The charge exiting the gun is measured on a faraday cup.  This is called a phase scan.  Data taken with the A0 Photoinjector 1.3GHz RF gun was compared to simulations performed in ASTRA in order to identify areas where secondary emission was present.  The results allow us to characterize the secondary emission of our photocathode.

II.  Theory

The amount of secondarily emitted electrons that may come off a surface as a result of the impact is dependent upon the kinetic energy of the colliding electron and the bulk and surface properties of the material.

Secondary emission is parameterized by

(1)

where is the maximum yield of secondary electrons, Ep,max is the impact energy for maximum yield, and s is a fit parameter for the material.  Figure 1 shows a plot of the secondary electron emission yield for several materials.  By obtaining a plot similar to Figure 1 for a particular photocathode it becomes possible to approximate the amount of secondary electrons that may be emitted from the photocathode.

Figure 1: Examples of secondary emission yield curves as a function of the colliding electron’s impact energy (from Ref. [3])

III.  Experimental Setup

The gun in the A0 Photoinjector Lab has a 1.625 cell RF cavity operating at 1.3GHz. Inside the cavity, a molybdenum plug is coated with a film of Cs2Te; this area is designated as the photocathode.  The photocathode is located at the back of the cavity.  When the laser is shone onto the photocathode, electrons are ejected from the Cs2Te surface.

Figure 2: A0 1.3GHz RF Gun Schematic

Figure 2 shows a schematic of the RF gun used for data taking.  The bucking, primary and secondary solenoids are all shown.  The bucking and primary solenoids are configured such that the photocathode sits in the small gap between them and when both solenoids are given the same amount of current, there is no axial magnetic field at the photocathode.  The secondary solenoid is placed near the end of the RF cavity.  To study the effects of the magnetic field in our data, a variety of solenoid configurations were chosen.  A round beam solenoid configuration provided each solenoid with the same amount of current, in this case 255A.  This configuration makes the axial magnetic field at the photocathode equal to zero and typically provides the best beam properties.  The flat beam configuration sets the bucking, primary and secondary solenoids at 0, 170 and 70A, respectively.  With these currents, the axial magnetic field at the photocathode is no longer 0 which is useful for some beam manipulations.  The no solenoid configuration provides zero current to all of the solenoids and no magnetostatic field in cavity.

An off-axis mirror in the beam pipe aims the laser at the photocathode.  A UV laser produces 2.4ps pulses that come in bunches of ten, each spaced 1µs apart.  This train of ten pulses enters the RF cavity once every second.

The waveguide feeds into the top of the cavity and fits between the primary and secondary solenoids.  The waveguide provides the electric field to the gun to accelerate any particles inside.

All data and simulations were performed with very low charge (~15-20pC per bunch) so that there is little effect from space charge and image charge on the electrons that are secondarily emitted from the photocathode.  A faraday cup is placed 0.63m downstream from the photocathode and measures the amount of charge that exits from the gun.  The amount of charge exiting the cavity is measured at each one degree increment.  A plot of the amount of charge as a function of the phase of the cavity can then be attained from the phase scan.  Once a series of five phase scans are recorded, the charge is averaged for each degree of phase in an attempt to lessen the amount of noise that is present in the final result.

IV.  Simulating Phase Scans

Phase scans taken at A0 could be compared to simulations of phase scans done in ASTRA.  ASTRA enabled us to change the electric field strength at the photocathode as well as the solenoid configurations.  Since the amount of charge in the simulations was also kept to a very small amount to match the data, space charge in the simulations was excluded.  The secondary emission parameters can also be changed in ASTRA.  As a result, the amount of secondarily emitted electrons can be varied, or even eliminated entirely to better identify areas of data with secondary emission.

Figure 3: Phase scan with round beam solenoid settings and 15MV/m cathode gradient

Figure 3 shows a phase scan.  The ideal phase for beam emission indicates that when electrons are ejected from the photocathode via photoemission from the laser, these electrons will experience the maximum amount of acceleration and also the best emittance.

The laser produces pulses spaced at 12ns apart from each other.  The pulses are then fed into a pulse picker which removes unwanted pulses.  The remaining pulses are spaced 1µs apart.  Fellow traveler pulses are not completely extinguished at the pulse picker so that after the signal has been amplified, smaller pre and post pulses are still present.  The post pulse is shown in the phase scan in Figure 3.

The area of secondary emission is the emphasis of our study.  This area will be explained further in the results section.

V.  Results

The phase scans were performed while varying the electric field in the gun as the solenoids stayed at the round beam configuration.  Then the gun gradient was fixed and phase scans were performed while changing the solenoid configurations.

Figure 4: Simulation with round beam solenoid settings and gun gradient at 15MV/m

Figure 4 shows phase scans where the electric field in the gun is set to 15MV/m and the solenoids are in their round beam configuration.  In the above plot, it is clear that the large spike in the data is not present in the simulation with no secondary emission.  However, the simulation with secondary emission at the photocathode fits the data well.  We can see from this set of data and simulations that the spike in the data is a result of secondary emission coming from the photocathode.  The maximum yield parameter that is part of the ASTRA simulations was adjusted here to make the spike in the simulation match the spike in the data due to secondary emission.  The maximum yield was set to 12.0 while the kinetic energy for maximum yield was set to 2.0keV.

Figure 5: Phase scans with round beam settings and 35.4MV/m.

Figure 5 shows a phase scan after increasing the gun gradient to 35.4MV/m.  Notice there are two spikes, but the first is not the result of secondary emission.  This first spike is a result of electrons being ejected into the cavity, starting to return to the photocathode but then making a loop and exiting the cavity.  This activity is shown in Figure 6.

Figure 6: Trajectory of an electron making a loop and exiting the cavity

Figure 6 shows why the first spike is present in both simulations and also gives way to showing that at nearby phases there are electrons that have small kinetic energies as they almost perform a loop, but then collide with the photocathode.  These electrons are now traveling with a low enough kinetic energy such that secondary emission is possible.  The simulation with the secondary emission in Figure 5 contains a second spike that is the result of secondary emission from the photocathode.  The addition of the secondary emission at the photocathode serves to improve the agreement between the simulation and the data.  The parameters for secondary emission at the photocathode are identical to those used in Figure 4 and yet we see that there is far less secondary emission at the higher gun gradient than at the lower.

This characteristic can be attributed to photoemitted electrons at the higher gradient having higher impact energies upon returning to the photocathode.  Since the optimal impact energy is a relatively small kinetic energy, the slower moving electrons in the scenario set at 15MV/m are more likely to cause secondary emission at the photocathode. Hence there is a much larger spike for the lower gradient.

In order to accurately establish the correct parameters for the secondary emission, the plot in Figure 1 must be determined for the photocathode so that it may fit for the variety of the gun gradients.  Knowing this dependence upon the gun gradient, we have chosen to keep the parameters for secondary emission according to Figure 4.

In the remaining data the electric field will remain at 35.4MV/m and the magnetic field configurations will change.

Figure 7: Phase scans with flat beam solenoid settings and 35.4MV/m

At the flat beam solenoid settings for the full gun gradient, the phase scan in Figure 7 is very similar to the results found with the round beam settings.  The spike from electrons traveling in a loop and the small shoulder that is a result of the secondary emission are again present.  The range of phases from the data where a substantial amount of charge coming from photoemission is measured on the faraday cup is slightly narrower than in the simulation.  Thus the first spike in the data and simulation do not match exactly.  Nevertheless, the secondary emission in the simulation appears to match the phases where secondary emission occurs in the data despite the mismatch in the first spike.  We also see that the shoulder from the secondary emission is much smaller in the simulation than in the data.  This is likely to be the result of inaccurate parameters for the secondary emission.

Figure 8: Phase scans with no solenoids and 35.4MV/m

The no solenoids phase scan in Figure 8 is different from the previously viewed phase scans.  The rise and fall of the pulse is very steep and when secondary emission is included in the simulation, the secondarily emitted electrons found on the faraday cup are released at the same phase as the looping electrons.  This is the only solenoid configuration where we have observed this activity.  The random scatter of secondary electrons coming from the nearly looping electrons causes an abundance of secondary electrons to exit the RF cavity.

VI.  Conclusions of Secondary Emission at the Photocathode

Comparisons of the data with simulations occurring at the photocathode are very promising.  We can see that the simulations can correctly identify the areas on the phase scans where there should be secondary emission occurring at the photocathode.  These results can be used to establish parameters for our particular photocathode.  We can also see that this secondary emission occurring at the photocathode feeds multipacting inside of the RF gun as well as become a source of dark current coming from the gun.

VIII.  A Brief Study on Field Emission

Field emission occurs when an electron is emitted from a surface due to a high electric field.  The amount of current released through field emission is described by the Fowler-Nordheim equation

(2)

where IF  is field emission current in Amps, E is the average electric field on the surface in V/m, β is the enhancement factor and  is the work function of the emitting material in eV.  The enhancement factor represents areas of the cavity that are not perfectly smooth and have imperfections in them, such as sharp areas or scratches.  At these areas, the actual electric field is greater than the average electric field, E.

The Fowler-Nordheim formula predicts that field emission is most likely to occur at areas of high electric fields like the photocathode or irises.  The electric field is much higher at the irises than at other surfaces inside of the cavity because of the geometry.  Field emission is a source of electron back bombardment onto the photocathode region which can cause damage to the photocathode.  Also, field emission can become a source of dark current if field emitted electrons exit the cavity.

IX.  Simulating Field Emission

Although it is not possible to directly measure the effect of field emission on the photocathode inside of the 1.3GHz RF gun at A0, it is possible to do simulations in ASTRA and track the trajectories of particles starting at the irises.

Electrons are started at the iris.  The trajectories of these electrons are logged with their final positions inside of the cavity and kinetic energies.  The phase of the RF cavity is varied to simulate the paths of electrons emitted at any RF phase.

Figure 9: Trajectories of field emitted electrons at an RF phase of +170.

Figure 9 shows an ASTRA simulation of the trajectories of electrons emitted from the near iris.  The simulations of field emission from the irises were performed for all three solenoid configurations.  For most cases, electrons did not strike within 20mm of the axis of the RF cavity (photocathode has a radius of 2.5mm).  In very few cases, the electrons did come within 10mm of the axis when emitted from the near iris.  However, it should be noted again that secondary emission from the aperture is not included.  Otherwise, when these field emitted particles strike the back plate of the cavity, secondary emission would be possible and secondarily emitted electrons could strike the photocathode region.  Sources of dark current coming from the near iris are small since many electrons trying to exit the gun eventually collide somewhere in the full cell as seen in Figure 9.

Simulations done at the far iris, as in Figure 10 below, were performed in the same fashion.  A distribution of electrons was produced around the far iris and run through a series of RF phases.  Then the trajectories of all the electrons in the distribution were logged and observed.  Similar to the results found with trajectories starting at the near iris, only a small amount of electrons starting at the far iris collide near the photocathode region of the back plate.

Figure 10: Trajectories of field emitted electrons at an RF phase of +0.

As seen in Figure 10, many electrons collide at radii greater than 15mm away from the axis.  It is important to note that the absence of secondary emission is not necessarily a factor in the accuracy of the simulations.  The impact energy for maximum yield of secondary electrons is usually on the order of a few hundred eV.  However, when electrons coming from the far iris collide with the back plate, their kinetic energies are high enough that they are very likely to penetrate the surface and not cause any significant amount of secondary emission.  Figure 11 shows a distribution of impact energies for electrons that strike near the photocathode.

Figure 11: Distribution of impact energies of electrons colliding with photocathode region

X.  Conclusions for Field Emission

The electrons coming from the irises tend to strike on areas of the back plate rather than at areas near the photocathode.  Also we have evidence in the simulations that there is a small effect from field emitted particles at the irises on the amount of dark current.  Further analysis is required to determine a better understanding of the effects of field emission on the photocathode.

References

[1]	Bluem, Hans P., Charles K. Sinclair, and Thomas J. Schultheiss. Exploration of Long-Life Polarized Electron Sources. 11-25.

[2]	Flöttmann, K., ASTRA User’s Manual, http://www.desy.de/~mypflo/Astra_dokumentation.

[3]	Han, Jang-Hui. Dynamics of Electron Beam and Dark Current in Photocathode RF Guns. University of Hamburg. 2005.

[4]	Han, Jang-Hui., and M. Krasilnikov. Secondary Electron Emission in a Photocathode RF Gun. DESY. American Physical Society, 2005.

[5]	Lewellen, John W. Ion Tracking in Photocathode RF Guns. Argonne National Laboratory. Argonne, IL: American Physics Society, 2002.

[6]	Suberlucq, G. Development and Production of Photo Cathodes for the CLIC Test Facility. CERN. Geneva, 1997.

[7]	Wang, J. W., and G. A. Loew. Field Emission and RF Breakdown in High-Gradient Room Temperature Linac Structures. SLAC. Stanford, CA, 1997. 1-7.

# Text boxes

R position (mm)

R position (mm)

z position (m)

z position (m)

Laser

Ideal phase for

beam emission

Far Iris

Post pulse

Simulations

Pink (no secondary emission)

Green (secondary emission)

Data

Blue

Secondary

Emission

Secondary Emission

Simulations

Pink (no secondary emission)

Green (secondary emission)

Data

Blue

Simulations

Pink (no secondary emission)

Green (secondary emission)

Data

Blue

z position (m)

R position (mm)

near iris

far iris

far iris

Faraday Cup

Waveguide

Near Iris

Cs2Te Photocathode

Full Cell

Half Cell

Secondary Solenoid

Primary Solenoid

Bucking Solenoid

Simulation

Pink (no secondary emission)

Green (secondary emission)

Data

Blue