## Slide 1: MULTILAYER films applied to SRF
Anne-Marie VALENTE-FELICIANO
On behalf of the
HEPTHF Collaboration

## Slide 2: SRF Thin Films Collaboration
Under DOE HEP Grant ARRA & U.S. DOE Contract No. DE-AC05-06OR23177
Films creation:
Jlab: A-M Valente-Feliciano, J. Spradlin, L. Phillips
W&M: A. Lukaszew, D. Beringer
Material and RF characterization:
Jlab: A-M Valente-Feliciano, J. Spradlin, L. Phillips, X. Zhao, B. Xiao, A. Wu
W&M: A. Lukaszew, D. Beringer, S. , R. Outlaw, O. Trofinova
NSU: K. Seo
ODU: H. Baumgart, D. Gu
Black Labs LLC: R. Crooks

## Slide 3: Thin Films: SIS Multilayers
Alex Gurevich, Appl. Phys. Lett. 88, 012511 (2006)
Higher Tc thin layers provide magnetic screening of the Nb SC cavity (bulk or thick film) without vortex penetration
Multilayer coating of SC cavities:
alternating SC and insulating layers with d < 
Nb
Insulating
layers
Higher-TcSC: NbN, Nb3Sn, etc
Strong increase of Hc1 in films allows using RF fields > Hc of Nb, but lower than those at which flux penetration in grain boundaries may become a problem
Strong reduction of BCS resistance because of using SC layers with higher  (Nb3Sn, NbN, etc)
Possibility to move operation from 2K to 4.2K
Taking advantage of the high –Tc superconductors with much higher Hc without being penalized by their lower Hc1…

## Slide 4: Thin Films applications: Nb, Alternative Materials & Multilayers
Use of SRF Thin Films
Bulk Nb
Nb film (>1mm thick)
Multi-Layers
S-I-S-I-S
Substrate
Substrate
Cu, Al …
Single Layer
Nb, high k
Bulk-like performance Nb film
major system simplifications.
highest level of quality assurance and reliable performance.
Use of substrates with higher thermal conductivity
  NbN, Nb3Sn, MgB2, S-I-S-I-S…
  Accessible almost only via deposited or synthesized films.
high k superconducting films
function at higher temperatures or higher fields
Suppression of vortex entry in multilayer structures
for cavity operation at 4.2K or higher

## Slide 5: Approach
SIS Multilayer Structures:
Nucleation studies of NbTiN, NbN on dielectrics like MgO, Al2O3 and reciprocately.
Creation and characterization of a set of NbTiN , NbN…/insulator/Nb samples by UHV multi-target energetic ion deposition with well-controlled, incremented thickness. The variation of rf field properties with temperature as a function of thickness of the superconducting overlayer will provide a direct test of the Gurevich delayed flux entry model.

## Slide 6: Tailoring for optimum RF performance
Careful characterization of the attained composition and microstructure
Close association with resulting rf surface impedance and superconducting properties

## Slide 7: Connecting Structure & Performance for SRF Surfaces
Deposition Control
involves understanding of
The chemistry of the involved species
  Reactivity
  Stoichiometric sensitivity
  Reaction process temperatures
Crystal structure dependence on substrate structure
Influence of deposition energy on resulting structure
Sensitivity to the presence of contaminating species
Stabilization of desired film against subsequent degradation
Characterization of deposited film surfaces
In-situ crystallographic structure characterization – Reflection high-energy electron diffraction (RHEED), Scanning Tunneling Microscopy (STM)
Large area crystallographic structure – X-ray diffraction (XRD)
10 nm-scale crystallographic texture within ~ 50 nm of surface – Electron backscatter diffraction (EBSD)
Topography – stylus profilometry, atomic force microscopy (AFM), optical profilometry
Near surface (< 8 nm) chemistry – X-ray photoelectron spectroscopy (XPS)
Micro-contaminant defects – Secondary ion mass spectrometry, with standards (SIMS)
Structural cross-section of film – Transmission electron microscopy (TEM), Focused Ion Beam (FIB)

## Slide 8: Connecting Structure & Performance for SRF Surfaces
MATERIAL PROPERTIES
Measurement with the SIC cavity
(TE011 sapphire-loaded cylindrical Nb cavity) Surface impedance as a function of magnetic field and temperature from 1.9 K to 4.8 K.
Normal state surface impedance at 10 K, from which the surface value of electronic mean free path and surface Hc1 can be determined.
Superconducting penetration depth, λ, at low field will be measured by carefully tracking the cavity frequency with temperature as the sample temperature is swept slowly back and forth across the transition temperature (SIC sensitivity: 30 Hz/nm) while the rest of the cavity is held at 2 K.
Tc – easy coarse measure of intragrain quality of the film
RRR – convenient assessment of aggregate defect density

## Slide 9
NbTiN, NbN, Mo3Re, V3Si coatings
with Reactive Sputtering and
High Power Pulse Magnetron Sputtering in self-sputtering mode
& MgO coating with RF sputtering
New UHV Multi-technique deposition system under commissioning @ JLab
A unique, versatile thin film deposition system
enabling multiple coating techniques in-situ
Designed to enable rapid exploration of the production parameter space of:
              Nb films
              Alternative material films like NbN, NbTiN
              S-I-S multilayer structures based on these compounds

## Slide 10: Thin Films: Alternative Materials
Substrates
Base pressure without baking
2x10-9Torr
UV desorption system
NEG chamber
3 magnetrons (DC, RF)
Self-sputtered magnetron
Ion source
RGA chamber with differential pumping
Thickness monitors

## Slide 11
Alternative Materials:
NbTiN, NbN
Nb3Sn, V3Si, Mo3Re
Substrates :
Single crystal Nb
Poly crystalline Nb
thick Nb/Cu films
Insulator:
Al2O3, MgO, AlN
according to
lattice mismatch
between
I and S materials
Multilayer: S/I/Nb and S/I/S/I/…/S/I/Nb
Study of growth modes of
Superconductor/ Insulator
&
Insulator/superconductor
Multilayers & Alternative Materials