## Slide 1: LQ Goals and Plans Giorgio Ambrosio Fermilab
BNL - FNAL - LBNL - SLAC
Task Leaders:
Fred Nobrega (FNAL) – Coils
Jesse Schmalzle (BNL) – Coils
Paolo Ferracin (LBNL) – Structure
Helene Felice (LBNL) – Instrumentation and QP
Guram Chlachidize (FNAL) – Test preparation and test
LARP Collaboration Meeting 14
Fermilab
April 26-28, 2010
Notes: 1

## Slide 2: GOALS
Next LQ models goals:
  Achieve short-model performances
    LQS01b/LQS02  TQS02 gradient at 4.5K (~220 T/m)
    LQS03  TQS03 gradient at 1.9K (~240 T/m)
  Demonstrate reproducibility & memory
    LQS02 ≥ LQS01/b
  Demonstrate accelerator-quality conductor & cable insulation
    LQS03  Smaller voltage spikes & no length issues
Need still some R&D:
  Reliable solution for protection heaters on inner layer

## Slide 3: Coils after Test
Delamination on coils Inner Diameter
  Heater – coil
  Insulation – heater
  Insulation – coil
  Also one heater-coil short
Possible causes:
  Superfluid helium + quench
    Seen in TQ coils
  Heat from heaters on ID
    Only in LQ coils
Plans:
  Strengthen insulation
    Not good for cooling
  Change heater location
    Best solution

## Slide 4: Intra-Layer Heaters
Set heaters between inner and outer layer
  Glued by ceramic binder in a sandwich between two S2 or ceramic cloths
Could be developed and demonstrated in single 1m coils (TQ/HQ) tested in mirror structure

## Slide 5: Plans
LQS01b with LQS01 coils
  GOAL: reproduce TQS02 performance
    Check shims
    Check effects of “TQS03b-preload”
    Perform Quench Protection studies (possibly disruptive)
LQS02 with 4 new coils (54/61 strand)
  GOAL: reproduce TQS02 performance
    Address reproducibility
    Effect of thermal cycle
LQS03 with 4 new coils (108/127 strand) and new cable insulation (glass tape)
  GOAL: reproduce TQS03 performance
    Smaller Voltage Spikes
    Better 1.9 K performance
2nd half of May
November 2010
June 2011
Additional reassemblies based on results

## Slide 6: Schedule
LQS03
LQS02
LQS01b
LQS03
LQS02b

## Slide 7: Conclusions
Next LQ models aim at:
  Achieving short-model performances
    LQS01b/02/03
  Demonstrating reproducibility & memory
    LQS02/03
  Demonstrating accelerator-quality conductor and cable insulation
    Smaller voltage spikes & no length issues
    LQS03
Need still some R&D:
  Protection heaters for inner layer
    LQS02 coil #13 with reinforce ID insulation
    TQ/HQ coil in mirror structure