## Slide 1: View from CERN/CERN Schedule Gijs de Rijk on behalf of Lucio Rossi and the Upgrade study working group

## Slide 2: Content
Luminosity...
PhaseI project
The new upgrade plan HL-LHC
Hardware needed for the upgrade
HE-LHC

## Slide 3: Luminosity...
Constants Beam intensity Beam focusing
Beam intensity
    Nb: number of particle per bunch [1.15 1011]
    nb: number of bunches [2808]
Beam focusing
    b*: beta function in the IP (transverse size of the beam) [55 cm]
    F: geometrical loss reduction factor [0.86]
Nominal Luminosity
1· 1034 cm-2s-1
The experiments are though only interested in
Integrated Luminosity
Peak luminosity is posing problems when very high (pileup)

## Slide 6: Main Magnets : MQXC
Coil aperture 120 mm
Gradient 127 T/m
Operating temp 1.9 K
Current 13.8 kA
WP on load-line 85%
Inductance 5.2 mH/m
Yoke ID 260 mm
Yoke OD 550 mm
Magnetic length 9160 mm (Q1,Q3)
7760 mm (Q2)
LHC cables 01 and 02
Porous cable polyimide insulation
Yoke OD identical to MB
Self-supporting collars
Single piece yoke
Welded-shell cold mass

## Slide 7: New features : porous cable insulation

## Slide 8: Porous inter-layer insulation
Conventional ground insulation
Open KCS ground insulation

## Slide 9: Phase I : performance possibilities
More aperture to reach Nominal Luminosity
  or
Lower b* (> 30 cm) for twice peak nominal Luminosity (2.1034 cm-2s-1)
and
New IR quads to replace old ones which reach radiation limits (correctors most affected)
But
Optically a completely new machine
Chromaticity correction is limited
Matching section the next aperture limit
Integrated Luminosity per year gain risks to be limited (20% - 35% ?)

## Slide 10: Luminosity increase : plan Spring 2010 (BC)
Chart: Luminosity [cm-2s-1]
| 2010.0 | 2011.0 | 2012.0 | 2013.0 | 2014.0 | 2015.0 | 2016.0 | 2017.0 | 2018.0 | 2019.0 | 2020.0
to nominal - lumi | 1e+32 | 1.2e+32 | 0 | 1.2e+33 | 2.3e+33 | 6e+33 | 1e+34 | 1e+34 | 1e+34 | 1e+34 | 1e+34
to ultimate - lumi | 1e+32 | 1.2e+32 | 0 | 1.2e+33 | 2.3e+33 | 6e+33 | 1e+34 | 1.2e+34 | 1.4e+34 | 1.6e+34 | 2e+34
hf.2 - lumi | 1e+32 | 2e+32 | 0 | 9e+32 | 1.7e+33 | 3.6e+33 | 6.2e+33 | 1e+34 | 1e+34 | 1e+34 | 1e+34
to ultimate | 0.1 | 1 | 1 | 6.4 | 19 | 37.4 | 89.4 | 149.4 | 219.4 | 299.4 | 399.4
to nominal | 0.1 | 1 | 1 | 6.4 | 19 | 37.4 | 89.4 | 141.4 | 193.4 | 245.4 | 297.4
hf.2 - int | 0.1 | 1.1 | 1.1 | 3.8 | 9.1 | 17.1 | 46.1 | 88.1 | 130.1 | 172.1 | 214.1

## Slide 11: Phase I and schedule
Before 2018 2 long shutdown periods needed for collimation and splices(to go to 7 TeV) : no time for anything else
Because of new schedule radiation damage is not an issue until 2020
In the new schedule the Triplet cannot be built before 2016 at best.
A year long shutdown is needed to install the new triplets
Phase I might only give at maximum a yearly integrated Lumi +35%
Conclusions: no integrated Luminosity gain with Phase I

## Slide 12: The new upgrade plan, HL-LHC
Task force recommendation (L. Rossi et al):
  Stop the phase 1 project
  Keep going with the R&D of Phase 1 which is necessary because of long lead time development;
  Decision in 2013/2014, after LHC behaviour near nominal will be known, the best technology for upgrade. Decision in 2013/2014 to have it by 2018-2020.
  Put the IT upgrade in a global pictures, preceded by all consolidation or improvement needed to make it most effective and compatible with other equipment. Aim for Lpeak= 5 .1034 cm-2s-1
APUL D1: hibernation of the project is the correct choice, if we need the fallback solution of Nb-Ti we probably need them again

## Slide 13: What could be needed for L= 5 .1034 cm-2s-1 ? (1)
  High Gradient/Large Aperture Quads, with Bpeak 13-15 T.
    Higher field quadrupoles translate in higher gradient/shorter length or larger aperture/same length or a mix.
     as small as 22 cm are possible with a factor 2.5 in luminosity by itself,
    Necessarily coupled with a mechanism to compensate the geometrical reduction.
    If a new way of correcting chromatic aberration could be found,  as small as 10-12 cm can be eventually envisaged

## Slide 14: What could be needed for L= 5 .1034 cm-2s-1 ? (2)
  Crab Cavities:
    best candidate for exploiting small  (for  around nominal only +15%).
    However today Crab Cavities are not validated for LHC , not even conceptually: the issue of machine protection should be addressed with priority.
    Global Scheme. 1 cavity in IP4, Proof on LHC, good for 1 X-ing. Semi-global; it may work! (JP Koutchouk)
    Local scheme; 1 cavity per IP side. Maybe local doglegs needed.
  D1: 8 T , 3.5 m long , 150 mm aperture
  Early Separation Scheme could be an alternative (or a complement)
  SC links to replace at the surface electronic equipment today in the tunnel and exposed to high radiation
  New Cryoplants in IP1 & IP5: for power AND to make independent Arc- IR: 2.8 kW @ 1.8 K scales as 5.2 kW @ 2 K (for 1 set of cold compressor)

## Slide 15: What could be needed for L= 5 .1034 cm-2s-1 ? (3)
  Improve some correctors
  Commissioning the lattice sextupoles @ 600-650 A
  New MQT corrector scheme using existing spare 600 A bus bars
  Re-commissioning DS quads at higher gradient
  Review MSs
  Change of New Q5/Q4 (today 2x70 mm : we need larger aperture!), with new stronger corrector orbit, displacements of few magnets
  Larger aperture D2
  (may be other actions, more quads in points 6 and 7)
  Displacement of Power Converters & DFBs at least of Inner Triplets but also of OTHER equipment on surface by means of SC links.
  Cryo-plant for RF in point 4 : 5-7 kW @ 4.5 K
  For extra collimators: 11 m, 11T DS dipoles

## Slide 16: « Coupling » between HG Quad magnets and Crab Cavities

## Slide 17: Hardware shopping list for the upgrade.
A selection of the most important items. (with an eye on collaborations...)
IT Quadrupoles
  IR 1 and 5
11 T – 11 m Twin Dipole for Dispersion suppressor
  IR 3, 7 and 2 To make space for additional (cryo) collimators
Crab Cavities
  Local (IR 1 and 50 or global
Early separation dipole
  IR 1 and 5
Superconducting current links
  IR 1 and 5 (3 & 7)
Q4/Q5 twin aperture Quadrupoles
  IR 1 and 5

## Slide 18: IT Quadrupoles
Ongoing LARP development. Crucial for Nb3Sn option for the upgrade << the LARP quadrupole program has to succeed for the upgrade>>
We (CERN) count on this
The final parameters for the IT quad can only be stated when we have experience with 2808 Nominal bunches per beam at 7 TeV (after the startup in 2013)
A preliminary specification can be given keeping some parameters open
Assumptions:
  The experiments expect a final integrated Luminosity for the full LHC lifetime of 3000 fb-1
  Similar magnet lengths and positions as for PhaseI
  Radiation and heat load studies scaled up from PhaseI

## Slide 19: HF Nb3Sn Quad
Nb3Sn is becoming a reality (first LQ long -3.6 m – quad 90 mm)
This year we expect a second test of LQ-1 and test of LQ-2
4.5 K
~3 K
1.9 K
Note: LQS01 & TQS02
use same strand design
(RRP 54/61)
200 T/m

## Slide 20: NB3Sn : HQ
HQ: a 1 m long - 120 mm aperture model
whose second test is under way

## Slide 21: First HQ test
already above the minimum goal (Phase-1)
Max critical current
Goal Phase 1 (G=127 T/m)
Goal HL-LHC (G=180 T/m)

## Slide 22: IT quadrupole preliminary specification (1)
Aperture A = 120 mm – 150 mm (t)
Gradient G = 175 T/m – 140 T/m (t)
Cold mass length 8 m – 10 m (t)
Maximum cold mass outer diameter = 600 mm (s)
Operation temperature 1.9 K (option 4.4 K) (t)
Operational current ≤ 13 kA (s)
Angular straightness (tilt) 1 mrad rms
Radiation hardness for (e) (with shielding):
  50 MGy
  2.1016 protons/cm2
  3.1018 neutrons/cm2
Maximum heat load
  Local 15 mW/cm3 in 10 cm length parts
  Global 50 W/m
Cold mass pressure tested at 26 bars (NB: t = tbd later, s = soft, e = estimate)

## Slide 23: IT quadrupole preliminary specification (2)
Integrated gradient spread between magnets = ±20 units (e)
Gradient delay during ramp @15 A/s DG = 10 units (e)
Multipoles (s) (see ref)
Ref: Electromagnetic Design of the 120 mm Aperture Quadrupole for the LHC Phase One Upgrade,
F. Borgnolutti, P. Fessia and E. Todesco, sLHC Project Report 0001, 18 May 2009

## Slide 24: IT quadrupole: acceptance criteria and scenarios
Acceptance criteria: (what do we call success ?) (t)
  < 3 quenches to reach nominal gradient
  < 10 quenches to reach 110% of nominal gradient
  Maximum 1 quench after thermal cycle to reach nominal gradient
Scenario for IT Quad
  HQ 1 m short models (ongoing)
  (3.4 m or) 6 m long models by mid 2013
  8 m or 10 m production readiness by end 2014 (1+ working magnet)
  Production between ½ US , ½ CERN or 100% US (t)
    CERN wants to master the technology in any case
  String test at CERN needed (preferably all CM tested at CERN) (t)
  HW ready for installation by 2018

## Slide 25: 11 T – 11 m Twin Dipole for DS
Shift in the magnet position requires to make room for collimators (red squares).
Alternative option based on stronger and shorter magnets (blue rectangles).

## Slide 26: Crab Cavities
qc
Elliptical 800 MHz not far from being designed. Require 400 mm beam-beam
400 MHz small cavity under conceptual study, they can (?) fit in 194 mm beam-beam. Required for final solution
Ref. : F. Zimmermann, Ed Ciapala

## Slide 27: Early separation scheme possible alternative/complement
Nb3Sn at 8.5 T to have margin for heat deposition
13 m from IP
Integration difficult but not impossible
Leveling very easy…
Ref. :
JP Koutchouk and G. Sterbini

## Slide 28: SC link to remove Po.Conv. from H.Rad.
Semi-horizontal link (100-700 m)
Vertical link
H = 100 m
1.1 mm
MgB2 wire

## Slide 29: SC link scheme
220 mm
He
Thermal shield
He
Vacuum insulation
plus MLI
Superconducting 200 kA MgB2 multi-circuit assembly (est60 mm)
100 electrically insulated cables 120 A, 600 A and 7000 A
MgB2 strand
Cu stabilizer

## Slide 30: HE-LHC
Nb3Sn + HTS
magnets
transmission
line magnets
of new injector
P. McIntyre, Texas A&M, 2005
The High Luminosity LHC or HL-LHC is the route that will enable the way to the Farthest Energy Frontier : an HE-LHC based on 20 T magnets for a 33 TeV c.o.m. collider
HE-LHC Workshop 14-16 October in Malta