## Slide 1: HQ Status and Test Results
Shlomo Caspi
LBNL
LARP Collaboration Meeting – CM16
BNL
Montauk May 16-18, 2011
BNL
Jesse Schmalze
Mike Anarella
Peter Wanderer
Arup Gosh
FNAL
Rodger Bossert
Dariusz Bocian
Guram Chlachidze
Giorgio Ambrosio
Emanuela Barzi
Sasha Zlobin
LBNL
Helene Felice
Paolo Feracin
Dan Dietderich
Ray Hafalia
Dan Cheng
John Joseph
Juan Lizarazo
Maxim Martchevskii
Xiaorong Wang
GianLuca Sabbi

## Slide 2: Outline
The HQ program and Target
Past Test summary– HQ01- a, b, c
Recent Test summary – HQ01- d
Future plans

## Slide 3: HQ Program & Targets
  Program
  Part of the US LHC Accelerator Research Program (LARP)
  Develop Nb3Sn quadrupole magnet for the LHC luminosity upgrade.
Magnet
Extend Nb3Sn magnet technology:
  TQ, 1 m long, 90 mm bore, 13T (1.9K) -> without field quality
  LQ, 4 m long, 90 mm bore, 13T (1.9K) -> without field quality
  HQ, 1 m long, 120 mm bore, 15T (1.9K) -> with field quality
HQ program target:
  160 (T/m) at 4.4K (HQ01d reached 170 T/m, 11.8T)
  175 (T/m) at 1.9K
  Good memory – no retraining
A collaboration between BNL/FNAL/LBNL and CERN:

## Slide 4
HQ Progress
2008 July Selection of 120 mm quadrupole aperture for Phase 1
Sept. Cable and coil cross-section geometry finalized
2010 Apr. HQ01a test coils 1,2,3,4
71%-79%,141-157T/m (unusual ramp rate performance)
June HQ01b test coils 1,4,5,6
77%,153 T/m (electrical breakdown)
Oct. HQ01c test coils 1,5,7,8
      70%-138T/m (unusual ramp rate performance)
2011 Apr. HQ01d test coils 5,7,8,9
      86%, 170 T/m (mechanical limit)
Status: 13 coils completed , 4 HQ tests completed, 1 mirror test underway

## Slide 5
LARP – HQ Magnet
0.8 mm strand
15 mm wide cable
120 mm bore
4.4 K/1.9 K -195/214 T/m
4.4 K/1.9 K – 13.7/14.9 T

## Slide 6
HQ01a,b,c,d - Test Results

## Slide 7: HQ01 Training quenches (4.4K)
HQ01a
13683A (157T/m, 79% of ss)
coils 1,2,3,4
HQ01b
13308A (153T/m, 77% of ss)
coils 1,4,5,6
HQ01c
11953A (138T/m, 70% of ss)
coils 1,5,7,8
HQ01d
14983A (170T/m, 86% of ss)
coils 5,7,8,9

## Slide 8: Ramp-rate dependence

## Slide 9
HQ01d Test Results

## Slide 10
Quench Location*
HQ01d – test results
* details and discussion by Maxim Marchevsky

## Slide 11
HQ01d – quench location summary
9
1
2
1
1
Inner layer
2
1
1
1
Outer layer
7
8
5
9
5 mid-plane quenches
First coil 7 followed by 8
Quench velocity ~11.4 m/s ,
tt-t = 5.2 ms

## Slide 12
Magnetic Measurement*
HQ01d – test results
* details and discussion Xiaorong Wang

## Slide 13: HQ01d magnetic measurement
n | Normal (bn) | Skew (an)
3 | 0.21 | -3.17
4 | -0.63 | -4.16
5 | 0.93 | 0.33
6 | 5.61 | -0.17
7 | 0.96 | -0.57
8 | 0.44 | 0.02
9 | -0.12 | 0.30
10 | 1.88 | 4.23
Harmonics at 120 T/m (average up-down ramp)
Measuring coil radius and length = 21.55 mm, 100 mm long
Data shown at a reference radius = 40 mm, 2/3 bore
Continuous ramping up at 10 A/s
b6

## Slide 14
Structure*
HQ01d – test results
* details and discussion Paolo Ferracin

## Slide 15: Coil azimuthal stress during excitation
Pre-stress intentionally low (reduce strain from high coil compaction)

## Slide 16: Next Step - improving stress uniformity HQ01d to HQ01e
ANSYS model for uneven keys
Fine tuning of stress
Need cold data
Need impact on field quality
Nomenclature

## Slide 17
Heater studies*
HQ01d – test results
* details and discussion Helene Felice, Tina Salmi

## Slide 18
Protection heater studies
Stainless steel protection heater strip on the outer layer
Study delay time to quench
Study deposited energy

## Slide 19
Summary of HQ Performance
And next step

## Slide 20: HQ coils are under excessive compaction
Jesse Schmalzle
HQ13
Coil springing out of reaction tooling
LQ 16
Coil remains in reaction tooling
HQ coils tend to spring out from their reaction tolling
Even with one turn less HQ coil #13 still tends to spring out

## Slide 21: Consequences of excessive compaction
21
HQ01b (coil 6 layer to layer and end-shoe)
HQ01a
HQ01a (coil 2 to protection heaters)
Insulation fragmentation after reaction
Broken strands during reaction
Notes: 5/13/2011
s_caspi@lbl.gov
21

## Slide 22
Performance Assessment
Observed limitations and deficiency:
Voltage breakdown (HQ01a,b tests)
Insulation damage (HQ01a,b tests)
Broken strands (coil #10)
Spring-back after reaction
Unusual ramp rate performance (HQ01c tests)
Low plateau magnet performance (HQ01c test)
A common cause –
Coils are under excessive compaction during curing and reaction

## Slide 23
Reducing Coil Compaction *
* details and discussion Helene Felice
Future Plans

## Slide 24
Reducing coil compaction
Near term : Coil #12 - last turn below mid-plane (mirror test underway)
(details and discussion Guram Chlachidize)
Coil #13 – removed one turn (next mirror test)
  Next step :
  Keep existing cross-section and HQ tooling
  Reduce strand diameter from 0.800 mm to 0.778 mm
  Reduce cable size
Allow expansion during reaction 5.6%-6% thickness and 1%-2% in width

## Slide 25: HQ Summary
A 120 mm bore, Nb3Sn quadrupole is underway construction and testing
  4 tests (HQ01a/b/c/d)
HQ01d reached 86% (4.4K) of short-sample (170T/m)
Coil compaction cause of performance limitation:
  Excessive strain puts coils at risk but some can perform
Future plans:
  Test special single coils in mirror configuration
  Reduce strand diameter and cable size
  Optimize and fine tune coil stress
  Test at 1.9K (FNAL, CERN)
  Revise protection heaters design and coil-end spacers