## Slide 1
Nikolay Solyak
Coupler collaboration meeting
(https://indico.fnal.gov/event/43726/)
03 June 2020
TiN coating on coupler window

## Slide 2: TiN coating of ceramic hints
7-14 nm kind of optimal thickness of TiN. If thickness < 4nm – high SEY, >15nm – high electrical conductivity – losses/heating
Advantages:
  Reduce SEY from from 8 to 1  suppress MP activity in window
  electrical conductivity help for charge removal to prevent sparks, discharge, breakdown (operation with beam)
Disadvantages/Issues
  Extra Cost: estimation 5-10% of coupler cost (CPI,…)?
  Control uniformity, thickness, resistivity of TiN - samples
  Effect of Oxidation (exposure to air)
  Possible degradation during processing and operation (bursts, breakdown)

## Slide 3: Questions
Today TiN (TiO, Cr2O3) coating of coupler ceramic is using in many couplers (pulse and cw)
How stable and reproducible the technology?
Optimal thickness, what typical thickness variation vendor can provide? CPI/Thales/RI/…
Existing experience; including processing and beam operation
  Are any difference between Electron and Proton machines?
  Performance with and without DC bias?
  Most common failures of the ceramic (crack and vacuum leak), increase ceramic heating (MP start, electrical conductivity, ceramic loss)?

## Slide 4: Some experience with TiN coated window
Positive
  EXFEL, ESS, SNS, … - easy processing?, working w/o DC bias in operation?
Negative
  FNAL RFQ coupler; grey color and high bias current (high electrical conductivity) after few ~ 1 month of operation.
  China ADS front-end (HWR): in 2 months 4 couplers (out of 12) were broken (10kW)  replaced with 2-window design

## Slide 5: Experience with TiN coating-free ceramic
KEK/STF-2 coupler, no bias. Processed w/o bias (?), no MP. - ILC R&D
  New development: conductive ceramic (cost reduction ILC R&D)
FNAL;
  SSR1 coupler was processed with DC bias  no MP (few bursts during processing) – few windows developed leak after processing (brazing issues), 1 leak (out of 10) after cold test
  650 MHz coupler was processed with and w/o DC bias (4 couplers). No MP after processing (bias), small residual activity after processing w/o bias
  Euclid Techlab (SBIR project)– conducting ceramic development (650MHz coupler) will be tested in August

## Slide 6: Summary
TiN coating of ceramic is challenging but known technology, many coupler vendors do this.
  Helps to suppress MP, also remove charge from ceramic due to electrical conductivity
  Used for many built couplers (vacuum side), but
    - can be destroyed by bursts during conditioning/operation (China ADS).
Positive experience with TiN coating-free ceramic:
    KEK/STF-2 coupler (no bias?),
    FNAL: SSR1 coupler with bias (warm and cold). 650MHz coupler (processing with and without bias). No beam operation yet.
DC bias suppress MP completely, but
  - Vacuum bursts during conditioning/operation are possible - vacuum leak (design issue?)
  Ceramic charging during operation may cause discharge/arc and destroy ceramic
  More data will be available after testing modified designs (325 and 650)

## Slide 7: Plans for TiN coating studies for PIP-II couplers (under discussion)
  Use existing SSR1 ceramic disc (~10) for TiN coating and measurements:
    TiN thickness and resistivity, deposition contents (vs. thickness)
    Loss factor measurements
    Charge removal rate (electron microscope)
CPI – interested to do TiN coating, we are discussing details (meeting)
Euclid Techlab: has experience, qualified personnel, TiN coating chamber, tools (electronic microscope, thickness measurements, etc.)