## Slide 1: Silicon Detectors Frank Hartmann

## Slide 2: Historical aspects – Why use silicon?
Since 50ies large crystals for energy measurements
Need for fast and precise position measurements
  80ies charm quark tagging
  Late 80ies LEP experiments, vertex tracker
  90ies in hadron machines FERMILAB
  Today in all LHC experiments
Where are silicon sensors better suited than gas detectors?
Fast ~O(10ns); Precise O(5µm); very good energy resolution ~O(eV)
Silicon detectors gives momentum & vertexing,
which gives
b tagging
lifetimes
mixing background suppression
…… and a lot of great physics!
  Why wasn’t silicon used earlier?
    Needed micro-lithography technology  cost
    Small signal size (need low noise amplifiers)
    Needed read-out electronics miniaturization
      (transistors, ICs)
Take home

## Slide 3: Historical aspects II – Why use silicon?
In the post era of the Z and W discovery, after the observation of Jets at UA1 and UA2 at CERN, John Ellis visioned at a HEP conference at Lake Tahoe, California in 1983 “To proceed with high energy particle physics, one has to tag the flavour of the quarks!”
CDF; top quark discovery
LEP
Background reduction
10 cm
200 collisions / 40M/s
Resolution to resolve this

## Slide 4: Content
Material Properties – ‘get the numbers’
Detector Structures – strips, pads and pixel - workhorse
What can go wrong – rushed examples
Performance – very short
Radiation – very brief
More Detector Concepts
Detector systems
What can go wrong – rushed examples
Homework – learn about signal formation
Shockley-Ramo
Today
Tomorrow

## Slide 5
Material Properties

## Slide 6: Material Properties Energy bands: isolator–semiconductor–metal
In an isolated atom the electrons have only discrete energy levels. In solid state material the atomic levels merge to energy bands. In metals the conduction and the valence band overlap, whereas in isolators and semiconductors these levels are separated by an energy gap (band gap). In isolators this gap is large.
Notes: Ask the question: What is the difference between insulator and semi-conductor?
Nothing fundamental thus the gap size. Mind diamonds ran under semi-conductor sensors but are insulators.

## Slide 7
n-Doping - donor
T = 0 K
Conduction electron
Valence electron
T > 0 K
p-Doping - acceptor
Intrinsic
Extrinisic = doped
Typical doping concentrations for Si detectors are ≈1012 atoms/cm3
(1014 und 1018 atoms/cm3 for CMOS elements)
@ RT Approximately 1.45·1010 cm-3 intrinsic carieres with 1022 Atoms/cm3 about 1 in 1012 silicon atoms is ionised

## Slide 8: Material Properties Drift velocity and mobility
Drift velocity v
For electrons: and for holes:
Mobility m
For electrons: and for holes:
e … electron charge
e … external electric field
mn , mp …effective mass of e- and holes
tn , tp …mean free time between collisions
for e- and holes
Source: S.M. Sze, Semiconductor Devices , J. Wiley & Sons, 1985
µn(Si, 300 K) ≈ 1450 cm2/Vs
µp(Si, 300 K) ≈ 450 cm2/Vs
CMS
Delphi
Take Home
e 3 times faster then h
Notes: Hier: Speed
\mu also dependent on doping but pretty much constant for values we care
\mu electrons starts to decrease at E16 and holes at E17 and less then for electrons

## Slide 9: Constructing a Detector Estimate Signal to Noise Ratio SNR in an intrinsic silicon detector
Let’s make a simple calculation for silicon: Mean ionization energy I0 = 3.62 eV, mean energy loss per flight path of a mip (minimum ionizing particle) dE/dx = 3.87 MeV/cm (rf. Bethe)
Assuming a detector with a thickness of d = 300 µm and an area of A = 1 cm2.
 Signal of a mip in such a detector:
Charge carrier have to be removed!
 Depletion zone in reverse biased pn junction
 Intrinsic charge carrier in the same volume (T = 300 K):
 Number of thermal created e–h+-pairs is four orders of magnitude larger than signal!!!
Notes: Hier: density – large energy deposition
Could be achieved by cool down but technically non-elegant method and difficult for large volume
BTW, mean not MPV

## Slide 10: The p-n Junction Creating a p-n junction
At the interface of an n-type and p-type semiconductor the difference in the fermi levels cause diffusion of surplus carries to the other material until thermal equilibrium is reached. At this point the fermi level is equal. The remaining ions create a space charge and an electric field stopping further diffusion.
The stable space charge region is free of charge carriers and is called the depletion zone.
Voltage
Notes: Ask students how many free charges we have in the depleted volumes
And where does the space charge comes from?

## Slide 11
The p-n Junction Electrical characteristics
Poisson Equation:
r (charge density) is constant in (+/-) depletion zones
w=width of depletion zone
Take home:
Fields completely defined by doping concentration (& voltage)
Notes: Mind p (doped zone) has a negative space charge!! And vice versa!
Mind to think if \rho mean resistivity or density. It means density charge density on this slide
Vdiffusion is ~O(mV), w ~O(µm)

## Slide 12: The p-n Junction Operation with reverse bias
p-n junction with reverse bias
Applying an external voltage V with the cathode to p and the anode to n e- and holes are pulled out of the depletion zone. The depletion zone becomes larger.
 That’s the way we operate our semiconductor detector!
Take home:
Fields and potentials completely defined by doping concentration & voltage
Notes: It’s dynamic!!!

## Slide 13: Detector Characteristics Capacitance and Depletion Voltage of a detector
r … specific resistivity of the bulk
m … mobility of majority charge carrier
V … bias voltage
A … detector surface
D … detector thickness
For a typical Si p-n junction (Na >> Nd >> ni) the detector capacitance is given as:
Measured detector capacitance as a function of the bias voltage, CMS strip detector:
Depletion voltage VFD is the minimum voltage at which the bulk of the sensor is fully depleted. The operating voltage is usually chosen to be higher (overdepletion).
- High resistivity material (i.e. low doping) requires low depletion voltage.
Notes: Depletion voltage the main topic these days, becoming an academic concept in the HL-LHC case
CV also reflects the doping profile; meaning ‘features’ hint to strange things; e.g. interfaces or changes due to radiation.
Look a the CVs shown here; after radiation you wish for something that nice and clear.
Plattenkondensator C=epsilon A/d

## Slide 14: The p-n Junction Width of the depletion zone
Example of a typical p+-n junction in a silicon detector:
Effective doping concentration Na = 1015 cm–3 in p+ region and Nd = 1012 cm–3 in n bulk.
p+n junction
Without external voltage:
  Wp = 0.02 µm
  Wn = 23 µm
Applying a reverse bias voltage of 100 V:
  Wp = 0.4 µm
  Wn = 363 µm
with
V … External voltage
r … specific resistivity
… mobility of majority charge carriers
Neff …effective doping concentration
Width of depletion zone in n bulk:
  300 µm
  1 µm
Notes: In sensors, p thin but far reaching
N BULK of volume thus bulk doping …

## Slide 15: The p-n Junction Current-voltage characteristics
Typical current-voltage of a p-n junction (diode): exponential current increase in forward bias, small saturation in reverse bias.
S.M. Sze, Semiconductor Devices , J. Wiley & Sons, 1985
Operation mode
Notes: We come back to breakdown regime with SIPMs

## Slide 16: Detector Characteristics Leakage Current
Measured detector leakage current, CMS strip detector (measurement at room temperature):
A silicon detector is operated with reverse bias, hence reverse saturation current is relevant (leakage current).
This current is dominated by thermally generated e-h+ pair (totally dominated by defects). Due to the applied electric field they cannot recombine and are separated. The drift of the e- and h+ to the electrodes causes the leakage current.
Backplane
Voltage source
Amp meter
Notes: Forget about random walk as you read in text books (in a depleted sensors is only ONE zone)
You do not really care unless you cannot supply it – power; thermal runaway!

## Slide 17
Detector Structures

## Slide 18: Pad Detector
The most simple detector is a large surface diode with guard ring(s).

## Slide 19: Microstrip Detector DC coupled strip detector
p+n junction: Na ≈ 1015 cm-3, Nd ≈ 1 - 5·1012 cm-3
n-type bulk: r > 2 kWcm  thickness 300 µm
Operating voltage < 100 - 600 V .
n+ layer on backplane to improve ohmic contact
Aluminum metallization
Traversing charged particles create e-h+ pairs in the depletion zone (about 30.000 pairs in 300mm thickness). These charges drift to the electrodes. The drift (current) creates the signal which is amplified by an amplifier connected to each strip.
A typical n-type Si strip detector:
Notes: Question: why a deep difussion – all edges, cuts interfaces have defects – increase distance of defects to active volume – deep diffusion; guard ring; active edge

## Slide 20: Microstrip Detector AC coupled strip detector
Integration of coupling capacitances in standard planar process.
Deposition of SiO2 with a thickness of 100 - 200 nm between p+ and aluminum strip
Depending on oxide thickness and strip width the capacitances are in the range of 8–32 pF/cm.
Problems are shorts through the dielectric (pinholes). Usually avoided by a second layer of Si3N4.
AC coupled strip detector:
AC coupling blocks leakage current towards the amplifier.
However, the dielectric cuts the bias connection to the strips!
Several methods to connect the bias voltage: polysilicon resistor, punch through bias, FOXFET bias.

## Slide 21: Microstrip Detector a real life case - p-in-n

## Slide 22: n-in-p sensor (for Phase 2 aka HL-LHC)
Invert everything
... and add channel isolation (here p-stops)

## Slide 23: Electrical Field Configuration of a Strip Sensor p-in-n

## Slide 24: Electrical Field across a Strip
Electrical Field [ V/cm]
Increase near strip electrode
Linear

## Slide 25: Simulated Current Density Ionizing particle with 45o angle t=0 s
Simulation Thomas.Eichhorn
|Absolute values|
p-in-n

## Slide 26
2.2. Simulated Current Density Ionizing particle with 45o angle t=1 ns
1ns

## Slide 27
1.1ns

## Slide 28
1.2ns

## Slide 29
1.3ns

## Slide 30
1.4ns

## Slide 31
1.5ns

## Slide 32
1.6ns

## Slide 33
1.7ns

## Slide 34
1.8ns

## Slide 35
1.9ns

## Slide 36
2 ns

## Slide 37
3 ns

## Slide 38
4 ns

## Slide 39
5 ns

## Slide 40
6 ns

## Slide 41
Mind:
all electrons collected
7 ns

## Slide 42: Hole Charge Collection (strip & time resolved)
2,27e-15C
3,27e-15C
3,04e-15C
1,08e-15C
Simulation Thomas.Eichhorn

## Slide 43: Induced current– Shockley-Ramo
Si Signals are fast T<10ns.
In case the amplifier peaking time is >20-30ns, the induced current signal shape doesn’t matter.
The entire signal is integrated.
EW is called weighting field – geometry
(distance, capacitance, shape)
From G. Lutz
p-in-n
20% over-depletion
µn(Si, 300 K) ≈ 1450 cm2/Vs
µp(Si, 300 K) ≈ 450 cm2/Vs
Gas detector work the same, though the electric field in gas is constant and in Silicon is linear
Take home: All signals in particle detectors are due to induction by moving charges.
Once the charges have arrived at the electrodes the signals are ‘over’.
The drift is recorded - the height of the signal is linear proportional to the velocity of the charge
Start: mid-sensor
Notes: Ask about the fiedl? High at p electrode side!!

## Slide 44: Signal Formation – weighting field ~ geometry
An interesting fact is that for diodes (or large pad detector) with an entirely linear field
  electrons and holes contribute the same to the electrode (pad)
For fine segmented sensors pixel and strip one charge type contributes much more; because the electrical fields concentrate at the electrodes;
  the drift velocity there is much higher thus the induced signal is much higher
  Weighting field EW is higher too
    We therefore often say we collect holes, or we collect electrons 
The future CMS High Granularity Calorimeter will register both electrons and holes
  Basically a pad detector (with many pads)
The future HL-LHC tracker will register electrons (mainly)
  The current strips registers holes (the pixels electrons)
The weighting field EW
Notes: Say something about weighting fields

## Slide 45: Strip Sensor to Module

## Slide 46: Strip vs. Pixel Detectors
A strip detector measures 1 coordinate only. Two orthogonal/angled arranged strip detectors could give a 2-dimensional position of a particle track. However, if more than one particle hits the strip detector the measured position is no longer unambiguous. “Ghost”-hits appear!
Pixel detectors produce unambiguous hits!
True hits and ghost hits in two crossed strip detectors in case of two particles traversing the detector:
Measured hits in a pixel detector in case of two particles traversing the detector:

## Slide 47: Hybrid Pixel Detectors Principle
Detail of bump bond connection. Bottom is the detector, on top the readout chip:
“Flip-Chip” pixel detector:
On top the Si detector, below the readout chip, bump bonds make the electrical connection for each pixel.
L. Rossi, Pixel Detectors Hybridisation,
Nucl. Instr. Meth. A 501, 239 (2003)
Drawback of hybrid pixel detectors: Large number of readout channels
Large number of electrical connections and large power consumption.

## Slide 48: Hybrid Pixel Detectors Bump bonding process
Electron microscope pictures before and after the reflow production step.
In bump, The distance between bumps is 100 μm, the deposited indium is 50 μm wide while the reflowed bump is only 20 μm wide.
C. Broennimann, F. Glaus, J. Gobrecht, S. Heising, M. Horisberger, R. Horisberger, H. Kästli,J. Lehmann, T. Rohe, and S. Streuli, Development of an Indium bump bond process for silicon pixel detectors at PSI, Nucl. Inst. Met. Phys, Res. A565(1) (2006) 303–308 82

## Slide 49
Hexagonal sensors to maximize use of wafer area
120, 200, 300 mm thick n-in-p pad sensors
  Thickness defines radiation tolerance
Cell size ~0.5 or ~1 cm2
  Smaller cell size in central region
    High occupancy and noise reduction
Cells are wire-bonded to a PCB on top with holes
120mm thick with 0.5cm2 cells
200mm thick
300mm thick
8” prototype
8” – a first in HEP High Energy Physics
n-in-p more radiation tolerant than p-in-n; thinner = radiation tolerant
Higher radiation at lower radius
Silicon Pad detectors – for calorimeter CALICE & CMS HGCAL
Notes: We learn from the bees
Signal from e and h

## Slide 50: Cautionairy tales of things going wrong - Sensors
No time – I will rush through 

## Slide 51: Evil plastic

## Slide 52: Processing
Dicing
Residues

## Slide 53: Faults - Some are visible
Open Strip:
Shorted Strip:
“Pinhole” (short between
implant and metal):
Open bias resistor:
Open implant at via:
Open implant:

## Slide 54:  High leakage Current Guess where!

## Slide 55: How to break it systematically?
Choose a package, where the sensor moves in the order of 1mm freely!

## Slide 56: Corrosion

## Slide 57
600V
22°C ~50% RH
Corrosion

## Slide 58
600V
22°C ~50% RH
after 17 h

## Slide 59
22°C ~50% RH
after 65 h

## Slide 60
600V
22°C ~50% RH
after 92 h

## Slide 61
600V
22°C ~50% RH
after 162 h

## Slide 62
Aluminum corrosion
Aluminum (2 µm)
Passivation (1 µm)
Triple oxide layer (1.5 µm)
Need voltage and RH in air
Oxidation of Al  insulating
  Goes several mm deep
Insufficient cleaning left Pottassium

## Slide 63: Charge up

## Slide 64: Give your sensors a bath!

## Slide 65: Why? - Charge-up!
I experienced several cases
Processing
Shipping in non lint-free envelopes
Antireflective coating for ‘alignment’ sensors with holes
Bathing in de-ionized water helps but is super delicate

## Slide 66
Performance

## Slide 67: Signal to Noise Ratio
The signal generated in a silicon detector depends essentially only
on the thickness of the depletion zone and on the dE/dx of the particle (see Bethe).
The noise in a silicon detector system depends on various parameters: geometry of the detector, the biasing scheme, the readout electronics, etc.
  Noise is typically given as “equivalent noise charge” ENC. This is the noise at the input of the amplifier in elementary charges.
Landau distribution
with noise
noise distribution
Take home: No charge amplification as in gas detectors

## Slide 68: Signal to Noise Ratio Noise contributions
Leakage current (ENCI)
Detector capacity (ENCC)
Det. parallel resistor (ENCRp)
Det. series resistor (ENCRs)
The overall noise is the quadratic sum:
Alternate circuit diagram of a silicon detector.
e .… Euler number (2.718...) tp …Integration time in µs
e … Electron charge RRs …Series resistor in W
C .…Detector capacity in pF RRp …Parallel resistor in W
Typical values for SNR are 15 to 40.
Notes: Mind, b in ENC_C is strongly t_p dependent
Mind, even DC coupled sensor have a metal line to reduce series resistance!!
1 and 3 relevant for DELPHI; 2 and 4 for LHC
C bei LEP 15 C bei LHC 64!!

## Slide 69: Signal to Noise Ratio Summary
Low detector capacity (i.e. small element size)
Low leakage current
Large bias resistor
Short and low resistance connection to the amplifier
Long integration time
To achieve a high signal to noise ratio in a silicon detector system the following conditions are important:
Obviously some of the conditions are contradictory. Detector and front end electronics have to be designed as one system. The optimal design depends on the application.
Take Home

## Slide 70: Position Resolution
Physics processes:
  Statistical fluctuations of the energy loss (Landau)
  Diffusion of charge carriers
External parameter:
  Binary readout (thresh hold counter) or read out of analogue signal value
  Distance between strips (strip pitch)
  Signal to noise ratio
The position resolution – the main parameter of a position detector – depends on various factors, some due to physics constraints and some due to the design of the system (external parameters).

## Slide 71: Position Resolution Threshold (binary) readout versus analogue readout
Analogue readout with interpolation (signal on two strips):
  Position (charge center of gravity):
  resolution:
p … distance between strips (readout pitch)
x … position of particle track
Threshold readout (one strip signal):
  position:
  resolution:
x1,x2 … position of 1st and 2nd strip
h1,h2 … signal on 1st and 2nd strip
SNR … signal to noise ratio
A position resolution of a few µm is achievable with analogue readout !

## Slide 72: Silicon properties – the numbers are simply right
And detector relevant:
Dense: the average energy loss and high ionized particle number with 390eV/μm ∼ 108 (electron–hole pairs)/μm is effectively high due to the high density of silicon.
  No charge amplification needed
very good intrinsic energy resolution: for every 3.6 eV released by a particle crossing the medium, one electron–hole pair is produced. (30 eV to ionize a gas molecule)
Very fast O(10ns)
Mechanical stability
  Self supporting

## Slide 73: Radiation damage in silicon sensors
A very very brief glimpse

## Slide 74: Examples of crystal defects a defect = ‘energy level in the gap’ ~ dopant
Take home: There is more than Interstitials and Vacancies; especially with impurities present

## Slide 75: Mind ‘the Gap’
Defects are simply add. levels in the band gap
Rule of Thumb:
● Leakage Current - Relevant from E13 1MeVNequiv onwards – LHC
● Depletion voltage - Relevant from E14 1MeVNequiv onwards - LHC
● Trapping - Relevant from E15 1MeVNequiv onwards – HL- LHC
●
●
●

## Slide 76: Some Relevant Radiation Induced Defects
* Point defects
g can only do point defects
From studies of RD50 and WODEAN

## Slide 77: Then there is „diffusion“ (annealing)
The term “diffusion” used here is more a descriptive one combining effects like diffusion, migration, break-up, re-configuration of defects – also often summarized by the term “annealing”

## Slide 78: Macroscopic parameters (in n-bulk FZ sensors)

## Slide 79: Defect Engineering – RD50
Introduced in CMS & ATLAS pixel

## Slide 80: Radiation Damage – Trapping
Trapping teff changes with Feq
Different materials behave differently (n, p, FZ, MCz, oxygenated)
Rule of thumb: dominant damage item up to 1016 1MeVeq
t eff (1015 n1 MeV/cm2) = 2 ns: x = (107 cm/s) · 2 · ns = 200μm
t eff (1016 n1 MeV/cm2) = 0.2 ns: x = (107 cm/s) · 0.2 · ns = 20μm
Annealing effect small
signal decreases
Notes: Not a problem for today’s detectors.
Main EVIL for tomorrow

## Slide 81: Is this all on irradiation? Not really.
The content of impurities is important and different particles and different energies damage differently wrt VFD / E-field
  create also donors, not only acceptors
When trapping becomes the dominant factor, the field becomes parabolic (was linear).
You need high field to get a signal, thinner sensor help (~d2)
n-in-n or n-in-p sensors ‘register’ electrons which are faster and the electric and weight field is higher at the n-electrode  larger signal

## Slide 82: Origin of the double junction
You need:
  Traps and thermal current generators!
Holes / electrons travel to p-electrode / n-electrode – ASYMMETRIC
They are trapped THERE  change effective space charge Neff - ASYMMETRIC
Space charge Neff defines the fields
  Dynamic situation
    generation – trapping – de-trapping
Below depletion voltage, the un-depleted zone is in the middle of the sensor

## Slide 83: Everybody still alive? Ready for coffee?

## Slide 84: The ART of sensor defects
Leaky strip
pinhole
nothing
?
back