## Slide 1: Long Quadrupole Giorgio Ambrosio DOE Review of the LARP Program June 2nd, 2011
LQ Task Leaders:
Fred Nobrega (FNAL) – Coils
Jesse Schmalzle (BNL) – Coils
Paolo Ferracin (LBNL) – Structure
Helene Felice (LBNL) – Instrumentation and QP
Guram Chlachidize (FNAL) – Test preparation and test
BNL - FNAL - LBNL - SLAC
Notes: 1

## Slide 2
Magnet Development Chart
Completed
Ongoing
Starting

## Slide 3: Long Quadrupole†
Main Features:
Aperture: 90 mm
magnet length: 3.7 m
Target:
Gradient: 200 T/m
Goal:
Demonstrate Nb3Sn magnet scale up:
  Long shell-type coils
  Long shell-based structure (bladder & keys)
  Deadline: by the end of 2009
† LQ Design Report available online at:
https://plone4.fnal.gov/P1/USLARP/MagnetRD/longquad/LQ_DR.pdf
LQS01 S.S.L. | 4.5 K
Current | 13.7 kA
Gradient | 240 T/m
Peak Field | 12.25 T
Stored Energy | 460 kJ/m

## Slide 4: LQ Fabrication Process
Cable:
  Cabling: LBNL
  Qualification tests: BNL, FNAL, LBNL
Coils:
  Wind & curing: FNAL
  Reaction & impregnation, BNL, FNAL
  Instrumentation: BNL, FNAL, LBNL
Structure:
  Pre-assembly & magnet assembly: LBNL
Test:
  Warm and cold test: FNAL

## Slide 5: LQ Structure†
LQS is based on TQS (1m model)
and Long Racetrack (4m)
  Segmented shell (4)
TQS Modifications:
  Added masters
  Added tie-rods for yoke & pad laminations
  Added alignment features for the structure
  Rods closer to coils
  Rods made of SS
† P. Ferracin et al. “Assembly and Loading of LQS01, a Shell-Based 3.7 m Long Quadrupole Magnet for LARP” to be published in IEEE Trans. on Applied Superconductivity.
Aluminum shell
TQS
LQS

## Slide 6: LQ Coils†
Fabrication technology:
  From 2-in-1 (TQ coils) to single coil fixtures (LQ)
  Mica during heat treatment
  Bridge between lead-end saddle and pole
Coil design:
  LQ coils = long TQ (1m) coils with gaps to accommodate different CTE during HT
Cross-section of TQ/LQ coil
LQ Coil Fabrication:
5 practice coils (1 Cu and 4 Nb3Sn)
coils #6-#9  LQS01
coils #10-#13  LQS02
Note: coils #6-#9 had 3 severe discrepancies
† G. Ambrosio et al. “Final Development and Test Preparation of the First 3.7 m Long Nb3Sn Quadrupole by LARP” to be published in IEEE Trans. on Applied Superconductivity.

## Slide 7: Scale up Lessons Learnt
Coil #02 (1st Nb3Sn): bowing after HT
  added mica (less friction) and stiffener plate (more rigid tooling)
Coil #03: longitudinal tension in coil by pole
  added longitudinal gaps (accommodate coil contraction during HT and different CTE coil-pole)
Coil #04 & #05:
  fine tuning of longitudinal gaps
Coil #06: incomplete impregnation
  added soak time to potting cycle
Coil #07: stopped argon flow due to power outage
  modified argon supply line
Coil #08: No major issues
Coil #09: Midplane insulation stuck to potting fixture
  changed mold-release
Coil #10-18 (in progress) : No major issues
LQS01
Practice

## Slide 8: LQS01 Internal Readiness Reviews
GOAL: Assess readiness for LQS01 assembly (by evaluating: choice of coils, structure, target pre-stress and assembly procedure) and test (test facility and test plan)
#1: “LQS structure and target pre-stress”
  April 7, 2009 at LBNL with video-link
#2: “LQ coil design and fabrication”
  June 17, 2009 at FNAL with video-link
#3: “LQS01 pre-assembly”
  July 28, 2009 at LBNL with video-link
#4: “Test readiness and test plan”
    October 1, 2009 at FNAL with video-link

## Slide 9: LQS01a Load & Cooldown
Pre-load
  Target stress on shell
  Target stress on roads
  Lower stress on coils ID
Cooldown
  Shell: close to target stress
  Rods: close to target stress
  Coil ID: ~ ½ target stress
   Could reach excessive stress on midplanes above 200 T/m
Azimuthal stress (Pa) at 200 T/m

## Slide 10: LQS01a Quench History
Test report available online at:
https://plone4.fnal.gov/P1/USLARP/MagnetRD/longquad/report/TD-10-001_LQS01_test_summary.pdf
200 A/s
SSL at 4.5K : 240 T/m
Target: 200 T/m
Slow start
  First quenches at high ramp rate (200 A/s)
  Slow training at 4.5K
    Due to low pre-load on pole turns
Faster training at 3K
  Reached 200 T/m
Stopped training
  to avoid coil damage and to achieve better performance with optimal pre-stress

## Slide 11: LQS01b (same coils of LQS01a)
More uniform prestress distribution in the coils
  By using thinner coil-pad shims
Higher preload based on 1m models (TQS03 a/b/c)
  Peak load: 190 MPa +/- 30
  No coil-pole separation in LQS01b

## Slide 12
Gradient at 4.4K of all 1m models with RRP 54/61 strand

## Slide 13
LQS01b: 220 T/m
in 4 quenches
LQS01b: 222 T/m
92% ssl based on strand test
(95% ssl based on cable test)
Gradient at 4.4K of LQ & all 1m models with RRP 54/61

## Slide 14: LQS01b Quench History
At 4.5 K: reproducible quenches in coil #8
 Iq/Ic = 92 ssl
At 3 K: variable quench curr. in coil #6
 limited stability of conductor
At 1.9 K: variable quench curr. in coil #9
 limited stability of conductor
SSL at 4.5K : 240 T/m
Target: 200 T/m
227
LQS01b Quench History

## Slide 15: Voltage Spikes
Large voltage spikes
  Due to flux jumps
    Seen in TQ magnets using RRP 54/61
  Larger than in TQs
  Variable quench detection threshold
  Variable ramp-rate during training
    200 A/s  3 kA
    50 A/s  5 kA
    20 A/s  9 kA
    10 A/s  quench
Maximum Voltage Spike amplitude at 4.5 K with 50 A/s ramp rate
RRP 54/61
by OST
Will be eliminated or significantly reduced by using RRP 108/127
RRP 108/127
by OST

## Slide 16: LQS01b Quench Location
Quench # 3:
Coil8_B2_B3
Quench # 9:
Coil 6_B2_B3
9
6
7
8
Most training quenches in Inner Layer pole turn, with a few exceptions
Plateau quenches in pole turn of Outer Layer of coil 8

## Slide 17: Test After Thermal Cycle
Good memory after thermal cycle with limited DT:
  G = 208 T/m in 1st quench after thermal cycle
  G = 222 T/m at 2nd quench after thermal cycle
  DT max = 100 K
Thermal cycle with unrestricted DT planned for LQS02

## Slide 18: Magnetic Measurement
bn an | TQS 1m |  |  | LQS 4m | 
 | calc. | measured |  | calc. | Measured
 |  | 01 | 02 |  | 
b3 | - | -1.46 | 2.98 | - | 3.43
b4 | - | -0.52 | 1.31 | - | 6.20
b5 | - | 3.06 | -1.45 | - | -0.16
b6 | 5.00 | 5.40 | 6.23 | 8.45 | 10.43
b7 | - | 0.07 | 0.05 | - | -0.10
b8 | - | -0.11 | -0.13 | - | -0.58
b9 | - | 0.02 | 0.10 | - | -0.14
b10 | 0.04 | 0.02 | -0.05 | -0.03 | -0.32
a3 | - | 4.41 | 0.66 | - | 2.11
a4 | - | -1.99 | 0.82 | - | 1.34
a5 | - | 0.71 | -1.50 | - | 0.48
a6 | - | -0.37 | 0.12 | - | -0.37
a7 | - | -0.11 | -0.01 | - | -0.30
a8 | - | -0.18 | -0.10 | - | -0.09
a9 | - | -0.02 | 0.02 | - | -0.55
a10 | - | 0.00 | -0.08 | - | 0.24
Magnetic measurement at 4.5K:
  Some are a few units different w.r.t. computed
  Similar to short models †
  Normal octupole (b4) may have been affected by small differences in impregnation molds
    Two molds used
Average harmonics in the TQS and LQS at 45 T/m (~ 2.6 kA) at the ref. radius r0 of 22.5 mm
† G. Velev, et al., “Field Quality Measurements and Analysis of the LARP Technology Quadrupole Models”, IEEE Trans. On Applied Supercond. , vol.18, no.2, pp.184-187, June 2008

## Slide 19: Coils after Test
Some “bubbles” on coils inner layer
  Coil-insulation separation
Possible causes:
  Superfluid helium and heat during quench
    Seen in TQ coils
  Heat from heaters on inner layer
    Only in LQ coils
Plans:
  Strengthen insulation
    coil #13 has 3 materials on ID
  Change heater location

## Slide 20: LQS01b Results
LQS01 reached the best performance of all TQS02 series (1m models with same conductor)!
  With the first four LQ-production coils; three of which had “severe” discrepancies
   We know how to make and fix long Nb3Sn coils
  Al-shell-based structure is providing support (up to 227 T/m and 92% of ssl) with no signs of limitation
   Segmented shell structure can be used for long Nb3Sn magnets with shell-type coils
  Quench protection keeps hot-spot temperature below 260 K
   We have tools (computation & instrumentation) for protecting long Nb3Sn magnets above 2.2K

## Slide 21: Next Steps & Goals
LQS02a with new set of 54/61 coils:
  Demonstrate reproducibility, test memory after unrestricted thermal cycle
LQS02b options:
  Change limiting coil of LQS02a
  Test LQS w 4 coils made with the same mold
    May reduce octupole
  Test use of 4m keys & bladders (for longer magnets)
LQS03a/b with 108/127 coils:
  Demonstrate better performance below 4.5 K, and smaller voltage spikes
Need still some R&D:
  Reliable solution for protection heaters on inner layer at 2 K
LQS02 Readiness Review (October 26, 2010)
OK to use coils #10-13
Slightly smaller pre-stress than in LQS01b

## Slide 22: LQ Schedule
LQ test turn around time: ~ 7 months
LQ test time: 2 months
LQS03 test
LQS02 test
LQS02b test
LQS03 test
108/127 coils
2011 | 2012

## Slide 23: Conclusions
The Long Quadrupole is demonstrating Nb3Sn scale-up to 4 m
  With excellent results so far
  With no significant open issues
  Showing that we are still learning, and nonetheless have reached significant performance with the first LQ model
The next steps of the Long Quadrupole R&D are going to give a large contribution to the Nb3Sn technology demonstration
  Together with other parts of the LARP program (HQ, LHQ  120 mm...),