## Slide 1
Thin straw update
Brendan Casey, July 27, 2020

## Slide 2: ‘Baseline’ straws
We have purchased and shipped material to PPG to try and manufacture ~8 micron thick spiral wound straws
  They have received the material and are working on it
  3 micron mylar x 2 + adhesive
  Mylar is not metalized straws
Goal:
  They say they think they can do it
  They send us some to test (creep, etc…)
  Straws pass those tests
  We purchase material to make a batch of metalized straws
    We want to get the POs in before the end of the fiscal year
  We have them make a batch and then we can do further tests plus start making single straw and few straw prototypes

## Slide 3: Thinner spiral wound straws
Started testing thinner materials.
Have also sent samples of these materials to PPG
  Told them to work on baseline first and then start playing with these
Have done some instron tests

## Slide 4: Pull tests
12 micron mylar
1.5 micron mylar

## Slide 5: Pull tests
Thickness (microns) | Yield strength (sample 1) (kgf/mm2) | Yield strength (sample 2)
1.5 | 0.034 | 0.045
3.5 | 0.078 | 0.079
6 | 0.146 | 0.157
12 | 0.310 | 0.322

## Slide 6: Metal straws
Have one quote from one group to do some R&D on extruding aluminum
  Extrude in multiple stages and then etch outer diameter
I’m evaluating their quote
I need to give them a spec for outer wall surface finish
  My gut feeling is this in not that important if it is below fractions of a micron but I need to think about it a little more.

## Slide 7: Conclusions
Making progress at greater than a snail’s pace.
I’ll try and have at least a little progress at every meeting