## Slide 1: Snowmass’21 Accelerator Frontier AF7 Accelerator Technology Magnet LoI Status and Plans LoI Authors August 27, 2020

## Slide 2: AF7/Magnet LoI Presentations
Regional program overviews
  US (Prestemon); EU (Bottura); Japan (Ogitsu); China (Xu)
Detector Magnets
  FCC-hh, FCC-ee, AMS (Mentink); J-PARC g-2/EDM, COMET-I&II, ILC (Sasaki)
New superconducting wire and cable development
  Ultra thin A-15 (Kitaguchi); PIT-IBS (Ma)
Dipole magnet design and development
  Cosq, CCT, Fast ramping (Fabbricatore); Block (Felice); Common coil (Gupta); REBCO (Wang); Bi-2212 Accelerators (Garcia-Fajardo); Hybrid Nb3Sn/HTS (Ferracin); Bi-2212 Solenoids (Davis);
Special magnets and new fabrication technologies
  Direct wind, high field solenoids (Amm); wind-react-wind (Caspi)
New accelerator concepts
  Collider in the sea (McIntyre)

## Slide 3: US Magnet Development Program

## Slide 4: US Magnet Development Program

## Slide 5: US Magnet Development Program

## Slide 6: US Magnet Development Program

## Slide 7: US Magnet Development Program

## Slide 8: US Magnet Development Program

## Slide 9: High Field Magnet Development for HEP – A Proposal
L. Bottura (CERN), B. Auchmann (CERN), A. Ballarino (CERN), A. Devred (CERN), S. Izquierdo-Bermudez (CERN), L. Rossi (CERN), F. Savary (CERN), E. Todesco (CERN), D. Tommasini (CERN), G. De Rijk (CERN), D. Schoerling (CERN)
H. Felice (CEA), P. Vedrine (CEA)
F. Toral (CIEMAT), L. Garcia-Tabares Rodriguez (CIEMAT), J.-M. Perez (CIEMAT)
P. Fabbricatore (INFN), S. Farinon (INFN), M. Sorbi (INFN)
M. Seidel (PSI), S. Sanfilippo (PSI)
C. Senatore (UniGe)
B. Holzapfel (KIT), M. Noe (KIT), T. Arndt (KIT)
NOTE: draft author list for the moment

## Slide 10: The Status (August 2020)
The HL-LHC Nb3Sn program has set a new benchmark: we have completed the initial model and prototype magnet development for operation in the 11-12 T field range and the next step is to capitalize on it, use this benchmark to develop industrial, robust and efficient techniques
We have a few demonstrators showing that Nb3Sn has the potential to operate at fields beyond 14 T, the next step is to confirm this potential with model magnets and prototypes
We have not yet had the opportunity to explore the potentials of HTS, the next step is to develop and test demonstrators to assess this technology

## Slide 11: HFM Mission Statement (2021-2027)
II
III
I
Push Nb3Sn magnet technology to its practical limit, both in terms of maximum performance as well as production scale
  Demonstrate Nb3Sn full potential in terms of ultimate performance (target 16 T)
  Develop Nb3Sn magnets for collider-scale production, through robust design, industrial processes and cost reduction (benchmark 12 T)
Provide a proof-of-principle for HTS magnet technology beyond the reach of Nb3Sn, and sufficient field quality for accelerator application (target in excess of 20 T)
OMNE TRIVM PERFECTVM

## Slide 12: HFM Mission Statement (2021-2027)
Value-engineered Nb3Sn
Ultimate Nb3Sn performance
HTS target
LHC
HL-LHC
Fresca2
MDPCT1
NOTE: we move in parallel along both fronts !
Next phase

## Slide 13: Future plans
A paper is in drafting phase, shared with the collaborators (description of the HFM program)
Discussions are on-going with present and potential collaborators
The program is intended as a collaborative effort, and will benefit from coordination and communication (worldwide)
  How to build the structure of the program (work packages)
  How to coordinate ands communicate
    A governance ?

## Slide 14: R&D work for Superconducting Magnet for Future Accelerator Applications
Toru Ogitsu1a, Tatsushi Nakamoto1, Ken-ichi Sasaki1, Michinaka Sugano1, Masami Iio1, Kento Suzuki1, Makoto Yoshida2, Satoshi Awaji3b, Naoyuki Amemiya4c, Yusuke Sogabe4;
  1 KEK Cryogenics Science Center, 2 KEK Institute of Particle and Nuclear Physics,
  3 Tohoku University High Field Laboratory for Superconducting Materials,
  4 Kyoto University Graduate School of Engineering Department of Electrical Engineering
Technical Highlights
  High Field Superconducting Accelerator Magnet Technologies
  Radiation Hard Superconducting Magnet Technologies
Technology | Near Term Target | Mid Term Target | Ultimate Target
High Field | High Field High Jc Reinforced Nb3Sn | 12T Large Aperture R&D Dipole | High Field Radiation Hard SC Magnets for Future High Energy and High Intensity Accelerators (FCC, Muon Collider..)
Radiation Hard | Radiation Hard HTS Mag. Technologies | J-PARC MLF 2nd Target | 

## Slide 15: R&D work for Superconducting Magnet for Future Accelerator Applications
High Field Superconducting Accelerator Magnet Technologies
HL-LHC D1 Development
High Field High Jc Nb3Sn R&D (with Mechanical Reinforcement)
FCC D1 Design Study
Strain-Jc Measurement Instruments
Internal Strain Measurement by Neutron Diffraction at J-PARC
12 T large aperture (100mm) Nb3Sn dipole magnet development (FCC D1 Model)
16 T dipole magnet R&D with 4 T Nb3Sn insert
20 T dipole magnet R&D with 8 T HTS insert

## Slide 16: R&D work for Superconducting Magnet for Future Accelerator Applications
J-PARC MLF Second Target with High Intensity Muon Source
COMET Capture Solenoid Development
J-PARC MLF Second Target Design Study
Inorganic Insulation Study
Neutron Irradiation on Superconductor
Gamma Irradiation on Organic Material
Radiation Hard Superconducting Magnet Technologies
SCS4050-AP (SuperPower)
1MW Proton Beam
HTS Quench Protection Study
(Al Stabilizer
See Sasaki’s Proposal)
US-JP R&Ds
High Field Radiation Hard SC Magnet Technologies
FCC IRQ
Muon Collider
Etc..

## Slide 17
Status and Plan of the High Field Magnet R&D for Future Accelerators Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)
6-m width Tunnel for CEPC-SPPC
SPPC Dipole with IBS
SPPC
collider
CEPC
collider
CEPC
booster
Site study of the CEPC-SPPC
SPPC Magnet Design Scope
Field strength: 12-24 Tesla to get 75-150 TeV in a 100-km tunnel
Baseline Iron-Based Superconductor (IBS), Nb3Sn/ReBCO etc. as options
Aperture diameter: 40~50 mm
Field quality: 10-4 at the 2/3 radius

## Slide 18
NbTi+Nb3Sn
2*ф10 aperture
10T @ 4.2K
year
2018
2028
Field (T)
10
20
Nb3Sn+HTS
2*ф30 aperture
15T @ 4.2K
Nb3Sn+HTS or HTS
2*ф45 aperture
20T @ 4.2K
With 10-4 field quality
Status and Plan of the High Field Magnet R&D for Future Accelerators Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)
R&D Roadmap for next years

## Slide 19
Now China has two 5-Year Programs for IBS and high-field magnets, starting in 2018 and 2019, respectively.
Proposal for
Strategic Priority Research Program
of Chinese Academy of Sciences (CAS)
Science and Technology Frontier Research
for High Field Applications of High Temperature Superconductors
Ranked No. 1 in 7 candidates
by Academic Committee of CAS
360M RMB for 2018-2023
Mainly 122 PIT wires & tapes
11 coated conductors
(100 m long fabrication)
International collaboration are welcome!
R&D from Fundamental research, advanced IBS conductors to Magnet & SRF technology
Status and Plan of the High Field Magnet R&D for Future Accelerators Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)

## Slide 20: Superconducting Detector Magnets for High Energy Physics
B [T]
Solenoid
Return yoke
Matthias Mentink, Helder Pais Da Silva, Tim Mulder, Alexey Dudarev, CERN
Technical Highlights:
  FCC-hh baseline detector design comprising superconducting solenoids utilizing aluminum-stabilized Nb-Ti conductor
  FCC-ee “IDEA” baseline detector design, featuring ultra-transparent solenoid utilizing high-stress aluminum-stabilized Nb-Ti conductor
  ReBCO-based ultra-transparent concentric superconducting solenoid for AMS-100 [1,2], also of interest for FCC-ee
FCC-ee “IDEA”baseline design featuring
ultra-transparent Al/Nb-Ti solenoid
In collaboration with: University of Aachen, Paul Scherrer Institute, University of Geneva
S. Schael et al., https://doi.org/10.1016/j.nima.2019.162561
FCC-hh baseline design featuring superconducting Al/Nb-Ti solenoids
AMS-100 featuring ultra-transparent
ReBCO-based concentric solenoid [2]

## Slide 21: Development of Large Scale Superconducting Solenoid Technologies for Future Accelerator Experiments
Ken-ichi Sasaki1, Mitsushi Abe1, Makoto Yoshida2, Masami Iio1, Takahiro Okamura2, Yasuhiro Makida2, Naoyuki Sumi1, Toru Ogitsu1, Hiromi Iinuma3;
  1 KEK Cryogenics Science Center, 2 KEK Institute of Particle and Nuclear Physics, 3 Ibaraki University Graduate School of Science and Engineering,
Technical Highlights
  Technology for high precision magnetic field design, control and mechanical design in 3-D and cryogenic system.
  R&D for advanced Al stabilized superconducting cable
 | Near Term Target | Mid Term Target | Ultimate Target
Design technology | J-PARC g-2/EDM COMET Phase-I | COMET Phase-II J-PARC MLF 2nd Target | ILD for ILC Detector for FCC Magnets for High Intensity Muon source
Al stabilized SC cable | Basic R&D -Advanced NbTi -HTS | Production | 
Notes: (e.g. extended write-ups, collaboration opportunities, open questions for discussion)

## Slide 22
Design technology
COMET Phase-I
COMET Phase-II
ILD
Advanced Al stabilized SC conductor
COMET CAP(2015)
R&D of advanced cable for ILC
ILD for ILC
Detector for FCC
Magnets for High Intensity Muon source
Cryo Sytem for ILD
TOPAZ
Precision Mag. Field Design
Mech. design for strong/complicated mag. force
Sophisticated Cryo system
Basic R&D of Al stabilized HTS
ATLAS
TOPAZ
VENUS
AMY
1980's~1990's
LHC ~2000's
-Ni-doped Al
-Hybrid stabilizer
CMS
- Ultimate target

## Slide 23: Ultra-thin A15 SC wires for future accelerators
Hitoshi KITAGUCHI and Akihiro KIKUCHI (National Institute for Materials Science, Japan)
Technical Highlights: 0.03-0.05mmdia ultra-thin A15 SC (Nb3Al, Nb3Sn) wires → “React and Wind (R&W)” coil fabrication Higher flexibility in cable design & tuning
Example: 0.03mmdia Nb3Al wire

## Slide 24
Rutherford cable for R&W magnets (under development)
Ultra-thin SC strand
1st bundle
2nd bundle
Successful feasibility study for cabling by using 0.05mmdia pure copper strands
37 ultra-thin strands
37x7(259) ultra-thin strands
Final flexible Rutherford cable
(Equivalent to 1 mmdia monolith strand)

## Slide 25
High Tc (55 K), Ultra-high Hc2 (150 T) and High Jc.
Small anisotropy, e.g., 1~2 for 122 type and Large n-value.
Simple fabrication process and good Mechanical properties.
No oxygen environment required, cheap metal sheath material can be used.
20 K, Hc2 ~70 T
Gurevich, Nature Mater. 10 (2011) 255
Putti et al. SuST 23 (2010) 034003
Iron-based
Superconductor
(Tc = 55K)
2008
Advantages of IBS:
IBS Wires Toward High-Field Applications
Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)

## Slide 26
Latest Progress on PIT-IBS wires Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)

## Slide 27: Development of Superconducting Magnets for Future Accelerators
P.Fabbricatore1, E.De Matteis2, S.Farinon1, U.Gambardella3, G.Iannone3, F.Levi1, S.Mariotto2, R.Musenich1, A.Pampaloni1, M.Prioli2, L.Rossi2, M.Sorbi2, M.Statera1, R.U.Valente2 (INFN Genova1, Milano-LASA2 and Napoli-Salerno3)
Technical Highlights
  High Field Nb3Sn dipoles. Based on the cos-theta EuroCirCol design for a 16T dipole, in the framework of a CERN-INFN agreement a short model single aperture (Falcon_D) is under construction in collaboration with industry.
  HTS magnets. First developments of canted cos-theta magnets are going on.
  Pulsed sc magnets. First design of fast cycled magnets for the accelerator chain of a future Muon Collider
  All the above developments are considered a first step toward long R&D activities with construction of many models and prototypes.
Future plans
  Availability to contribute to the extended write-ups.
  Open to other labs to finding common field of interest for specific developments and/or for sharing and complementing knowledges/expertise

## Slide 28: Toward FCC-hh and future colliders: Exploration of high field magnet technology at CEA-Paris Saclay
Hélène Felice, G. Dilasser, Maria Durante, Philippe Fazilleau, Thibault Lécrevisse, Clément Lorin, P. Manil, F. Nunio, Etienne Rochepault, Françoise Rondeaux, Pierre Védrine
Highlights:
  Nb3Sn :
  Demonstrator toward FCC, Multi-scale approach modeling, PhD work on dimensional changes through digital image correlation
  HTS :
  Eucard (5.4 T record), Eucard 2 cosq (assembly stage), Metal-as-insulation double pancakes Nougat (32.5 T), studies of screening currents in REBCO tapes
Next steps:
  Some key topics identified: from modeling to fabrication and test
  Reinforced synergy btw EU development strategy and International labs is required to achieve accelerator ready high field magnets
  One tool: pursuit of topical Workshops such as:
    Workshop on Nb3Sn technology for accelerator magnets, October 2018, Paris, https://indico.cern.ch/event/743626/

## Slide 29: Common Coil Dipole for High Field Magnet Design and R&D
Technical Highlights:
Alternate design to the conventional cosine theta
Goal is to develop a field quality design with a lower cost in a large production with improved technical performance
Design allows a variety of cables, technologies and material
Future Plans:
Make a case for how this design can help future colliders based on high field dipoles and support R&D programs
Prepare a write-up and discuss opportunities to collaborate in demonstrating a collider quality high field dipole
K. Amm1, M. Anerella1, R. Gupta1, P. Joshi1, BNL
More co-authors from other institutions 2 (list still forming)

## Slide 30: Develop high-temperature superconducting REBCO magnet technology for future circular colliders
Members from main REBCO magnet programs support the LoI
  Bosque (ASC/NHMFL); Ben Yahia, Gupta (BNL); Kashikhin, Lombardo (FNAL); and Gourlay, Wang (LBL)
Our message: rapidly develop REBCO magnet technology as a new tool to enable future energy frontier proton and muon colliders
  Key advantages of REBCO: enable a dipole field of 20 T and above. Operation over a wide temperature range (2 – 50 K) and capable to tolerate higher heat loads than LTS
  Significant room for cost reduction; synergy with HTS fusion development
  Boost the US-Magnet Development Program and allied programs to propel REBCO R&D
How can the REBCO R&D better meet/serve future experimental needs?
  Provide more input to Snowmass
  Engage physicists to understand each other and explore ideas/opportunites
CORC® wires, Advanced Conductor Technologies LLC
STAR™ wires, AMPeers LLC
REBCO tapes, SuperPower Inc.

## Slide 31: Very high field superconducting magnet technologies based on Bi-2212 for future proton colliders
E. Barzi (FNAL), E. Bosque (NHMFL), D. Davis (NHMFL), L. Garcia Fajardo (LBNL), Y. Kim (NHMFL), D. Larbalestier (NHMFL), I. Novitski (FNAL), S. Prestemon (LBNL), T. Shen (LBNL), U. Trociewitz, A. Zlobin (FNAL)
Opportunities and technical Highlights: (1) Bi-2212 – the only multifilamentary, twisted, round wire HTS conductor. (2) The conductor technology (wire Je of 1000 A/mm2 achieved at 4.2 K and 27 T in 2017), experience with prototype coils, and CCT and SMCT magnet design provide an opportunity for adding a very high field, potentially quench training free accelerator dipole magnet technology (>15 T).
Need for fabrication and test facility: RENEGADE (1 m x ∅0.25 m) OPHT furnace (being constructed@NHMFL)), hybrid magnet test facility, and high-field, large bore Nb3Sn dipole magnets.
Collaboration opportunities: (1) Rutherford cable engineering and transverse pressure measurement. (2) Conductor development. (3) Hybrid Nb3Sn/HTS magnet design and testing.
LOI in preparation.
Open questions: Are HTS accelerator magnets quench training free? Is the HTS magnet technology scalable?

## Slide 32: 20 T hybrid magnets
Most effective way to achieve very high collision energies in HEP accelerators: very high field dipole magnets -> 20+ T bore field
Beyond 16 T (limit Nb3Sn) -> HTS superconducting materials, but still significant higher cost than Nb3Sn and Nb-Ti
Economically viable option: “hybrid” magnets
R&D on modelling and with short model fabrication and testing to address different challenges: optimum coil and magnet design for both HTS and LTS, mechanical integration, HTS/LTS ratio, peak stresses, protection with all coils in series, testing, cost, industrialization
Development will pave the way towards very high field magnets for the next generation of particle accelerators
(1) Lawrence Berkeley National Laboratory, Berkeley, CA 94720, pferracin@lbl.gov
(2) Fermi National Accelerator Laboratory, Batavia, IL 60511, barzi@fnal.gov
(3) Applied Superconductivity Center, National High Magnetic Field Laboratory, Tallahassee, FL 32310
(4) Brookhaven National Laboratory, Upton, NY 11973

## Slide 33: The time is right for BSCCO 30 T solenoids
E. Barzi (FNAL), E. Bosque (NHMFL), D. Davis (NHMFL), Y. Kim, D. Larbalestier (NHMFL), T. Shen (LBNL) LOI in preparation
Opportunities and technical Highlights:
Bi-2212 – the only multifilamentary, twisted, round wire HTS conductor, 800-1200 m strand lengths
Wire Ag matrix strengthened up to 160 MPa, composite conductor reinforced above 300 MPa, and magnet level reinforcement above 275 MPa under active development.
Stable, training-free test coil operation with conventional quench management.
Rutherford cable based >30 T solenoids are promising for final muon cooling.
Facilities:
Renegade over-pressure furnace (1 m x ∅ 0.25 m now in construction @NHMFL)
Large bore (>150 mm) 8-14 T LTS solenoid test beds, resistive & hybrid facilities at NHMFL
Collaborations:
Conductor development.
Development of 25 T commercial user solenoids
Rutherford test solenoids towards 25 T operation
Proposed 28 T insert towards UHF-NMR development.
Open question: Can we reliably react and reinforce magnets with high current densities under extreme Lorentz stresses?

## Slide 34: Integrated Magnet Development for HEP accelerators
Kathleen Amm, Michael Anerella, Ramesh Gupta, Brett Parker, Piyush Joshi(BNL) Joseph Minervini, John Brisson, (MIT)
Technical Highlights
  Specialty magnets –
    Direct wind(Linear e+e- colliders, electron-ion machines, proton-proton machines, muon colliders)
    New methods for very high energy colliders
  HTS
    solenoids (30-50T small bore for muon collider cooling, >15T large bore for muon collider 6D cooling, >20T for HEP experiments(e.g. Axion search)
    VHF Dipoles (20-25 T) - high energy proton-proton, muon colliders (linear luminosity dependence)
    VHF quadrupoles and multipoles – IR regions for all high energy machines, specialty applications
  Cross cutting applications with other SC applications – EIC, compact fusion, offshore wind. HEP can leverage efforts and expertise – more bang for the buck
Future plans –partnerships with sister magnet teams (FNAL, LBNL, BNL, MIT NHMFL) and industry

## Slide 35: Snowmass 2020 - Wind-React-Wind (WRW)
Shlomo Caspi (LBNL)
SC magnet technology
Nb3Sn magnets, like NbTi magnets, have similar issues that remain unsolved
Good progress in SC Nb3Sn magnet technology has reached a point where it is difficult to progress unless new ways are introduce to understand, explain and avoid magnet training – a critical costly problem.
Ask yourself, in what way the R&D magnet I am building Is going to be different in solving a problem that thousand other magnets were unable to solve. If the answer is pre-stress stop and look for something new.
Future SC magnet technology
Reduced stress in CCT coils did not solve magnet training but suggested an intrinsic mechanisms within turns to be a more likely source – sintering during reaction, the use of epoxy and mismatch between mechanical properties.
Reacted Nb3Sn is brittle but like any other brittle material can maintain a certain degree of elasticity (e.g. fiber optics)
The “Wind-React-Wind” method is a NEW approach for CCT coils:
  Annealed Nb3Sn (650 C) coils retain their annealed form and maintain a degree of elasticity.
  Reacted Nb3Sn conductor is sufficiently elastic when it is removed from a reacted CCT mandrel.
  Placing the removed turns into a similar new unreacted mandrel should be the same.
  Unreacted mandrel has controlled tolerances and can be made from other materials such as Aluminum.
  Mandrels should be insulated or coated (e.g. anodizing) voiding the use of cable insulation.
  Removing impregnation will place liquid Helium within the cable and greatly improve stability
This new R&D study has a steep learning curve on technology the potential for better understanding foundamental training issues, reduce magnet cost and improve safety

## Slide 36
Reacted Nb3Sn cable
in a CCT bronze mandrel
Flexible Nb3Sn cable removed
Turns replaced into a new anodized (black) Aluminum mandrel
Removed Nb3Sn turns

## Slide 37: Collider in the Sea: 500 TeV with High Luminosity
Peter McIntyre, Texas A&M University
Technical Highlights:
  Magnet cost/TeV increases steeply with magnetic field.
  Tunnel cost/TeV increases with size – faults, bad rock.
  Solution: Choose magnetic field for minimum cost/TeV 3-4 T
  No tunnel!: 1900 km circular pipeline at 100 m depth, neutral-buoyant
  C-magnet w/ LN2 side channel for SR: ultimate luminosity
doi:10.1109/TASC.2017.2656157
doi 10.18429/JACoW-NAPAC2016-MOB2CO03
Working group: Collider-in-the-Sea 500 TeV p-mcintyre@tamu.edu
3.5 T NbTi Cable-in-Conduit 3.5 T REBCO NI Conformal Supercritical He 4-6 K NI blocks – LH2 20-30K
Gulf of Mexico

## Slide 38: Additional/Backup Slides

## Slide 39: Nb3Sn magnets

## Slide 40: Best-of-breed LTS magnets
2018: FRESCA2
14.6 T at 1.9 K
100 mm bore
2020: MDPCT1
14.5 T at 1.9 K
60 mm bore
2019: MBHB002
11 T at 1.9 K
60 mm bore
2020: eRMC
16.5 T at 1.9 K
No bore
Each one of these realizations is a 10-years history

## Slide 41: HTS magnets

## Slide 42: Best-of-breed HTS magnets
This is the infancy of HTS accelerator magnets
REBCO tapes
5.37 T
4.7 T
4.2 T
REBCO Roebel

## Slide 43
Status of the High Field Dipole Magnet R&D
10.7 T NbTi+Nb3Sn Common Coil Model Dipole
Status and Plan of the High Field Magnet R&D for Future Accelerators Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)

## Slide 44: Test of the 1st IBS solenoid coil at 24 T and the 1st IBS racetrack coil at 10 T
25T-HM, RT bore Φ38 mm
Very good performance!
Demonstrating that IBS are very promising for high-field magnet applications
Supercond. Sci. Technol. 2020, in press
Supercond. Sci. Technol. 32 (2019) 04LT01
Status and Plan of the High Field Magnet R&D for Future Accelerators Qingjin Xu (IHEP-CAS) and Yanwei Ma (IEE-CAS)