## Slide 1: MQXFA06 Coil Reception Electrical QC Measurements Coils 119, 122, 123, 211
MQXFA06 Coil Selection Review
Dan Cheng, Bob Memmo, Jordan Taylor
9/25/2020
LBNL

## Slide 2: Overview
QXFA Coil 117 had already been approved (see MQXFA05 Coil Selection Review Report in https://indico.fnal.gov/event/22839/ )
LBNL Acceptance Data from Coils 119, 122, 123, 211 presented here
  Coil 123 has only the A1/2 and B1/2 voltage taps, considered a spare
  Coil 211 EQC was performed (no issues), but SeqR measurements need to be repeated, to be updated later
Data is uploaded in Zip file, summarized here

## Slide 3: Electrical Testing Notes
Keithley 2110 Multimeter (Sequential-R Voltage Measurements, Resistance Measurements)
  HP E3610A DC Power Supply (Current Source for Sequential R)
Hypotultra 7805 (Hipot)
LCR Meter
  GW Instek LCR-819
ECG-Kokusai Winding Test DWX-05 (Impulse Testing)

## Slide 4: MQXFA06 Coil Electrical QC Summary
 |  |  | 117 | 119 | 122 | 211 | 123
See DocDB #956 / SU-1010-1903D |  |  |  |  |  |  | 
RLQ |  |  |  |  |  |  | 
 | R | (mΩ) | 614 | 607 | 611 | 600.91 | 608
 | Ls (mH) | 20 Hz | 10.018 | 10.016 | 10.064 | 9.986 | 10.008
 |  | 100 Hz | 6.4188 | 6.441 | 6.4179 | 6.4263 | 6.4155
 |  | 1 kHz | 5.8528 | 5.8255 | 5.8164 | 5.8252 | 5.8388
 | Q | 20 Hz | 1.282 | 1.295 | 1.28 | 1.296 | 1.289
 |  | 100 Hz | 5.587 | 5.529 | 5.497 | 5.564 | 5.61
 |  | 1 kHz | 8.548 | 8.402 | 8.549 | 8.504 | 8.531
QH R (Ω) |  |  |  |  |  |  | 
 | NT | A01 | N/A | N/A | N/A | N/A | N/A
 | T | A02 | N/A | N/A | N/A | N/A | N/A
 | T-P | B01 | 2.3 | 2.03 | 2.02 | 2.31 | 2.13
 | NT-P | B02 | 2.3 | 2.03 | 2.03 | 2.29 | 2.13
 | T-M | B03 | 2.2 | 2.03 | 2.03 | 2.28 | 2.12
 | NT-M | B04 | 2.2 | 2.02 | 2.03 | 2.26 | 2.1
VT R (mΩ) Individual coils |  |  |  |  |  |  | 
@1 Amp |  | A1 | 614 | 606 | 611 | 619 | 608
 |  | A2 | 613 | 606 | 611 | 619 | 607
 |  | A3 | 415 | 410 | 414 | 419 | 
 |  | A4 | 355 | 352 | 354 | 359 | 
 |  | A5 | 355 | 352 | 354 | 359 | 
 |  | A6 | 350 | 345 | 349 | 353 | 
 |  | A7 | 350 | 345 | 348 | 353 | 
 |  | A8 | 344 | 340 | 342 | 347 | 
 |  | B8 | 343 | 340 | 342 | 347 | 
 |  | B7 | 343 | 340 | 330 | 347 | 
 |  | B6 | 338 | 334 | 336 | 341 | 
 |  | B5 | 337 | 333 | 336 | 341 | 
 |  | B4 | 331 | 328 | 331 | 335 | 
 |  | B3 | 187 | 186 | 187 | 189 | 
 |  | B2 | 0 | 2 | 1 | 0 | 0
 |  | B1 | 0 | 1 | 1 | 0 | 0
HIPOT |  |  | OK | OK | OK | OK | OK
IMPULSE |  |  | OK | OK | OK | OK | OK
122 B7 is not sequential, possibly mislabeled wire? Coil Fabrication also shows out of sequence value as well. Needs examination.
211 reception data was not recorded correctly, will repeat and update (VT data shown is BNL pre-shipping data)

## Slide 5: MQXFA06 Coils Electrical QC Summary
Electrical QC measurements of four coils were presented
  Coil 211 reception SeqR data will be retaken and the table will be updated; no issues expected
  Coil 122 seems B7 voltage tap shows an anomaly (also in Fabrication electrical report); will examine and update
Hipot and Impulse tests all passed without issue

## Slide 6: Additional Slides