## Slide 1: Coil 122 VTB07
Followup to MQXFA06 Coil Selection Review
Dan Cheng, Bob Memmo, Jordan Taylor
9/29/2020
LBNL

## Slide 2: MQXFA06 Coil Electrical QC Summary With Updated Coil 211 Data
 |  |  | 117 | 119 | 122 | 211 | 123
See DocDB #956 / SU-1010-1903D |  |  |  |  |  |  | 
RLQ |  |  |  |  |  |  | 
 | R | (mΩ) | 614 | 607 | 611 | 600.91 | 608
 | Ls (mH) | 20 Hz | 10.018 | 10.016 | 10.064 | 9.986 | 10.008
 |  | 100 Hz | 6.4188 | 6.441 | 6.4179 | 6.4263 | 6.4155
 |  | 1 kHz | 5.8528 | 5.8255 | 5.8164 | 5.8252 | 5.8388
 | Q | 20 Hz | 1.282 | 1.295 | 1.28 | 1.296 | 1.289
 |  | 100 Hz | 5.587 | 5.529 | 5.497 | 5.564 | 5.61
 |  | 1 kHz | 8.548 | 8.402 | 8.549 | 8.504 | 8.531
QH R (Ω) |  |  |  |  |  |  | 
 | NT | A01 | N/A | N/A | N/A | N/A | N/A
 | T | A02 | N/A | N/A | N/A | N/A | N/A
 | T-P | B01 | 2.3 | 2.03 | 2.02 | 2.31 | 2.13
 | NT-P | B02 | 2.3 | 2.03 | 2.03 | 2.29 | 2.13
 | T-M | B03 | 2.2 | 2.03 | 2.03 | 2.28 | 2.12
 | NT-M | B04 | 2.2 | 2.02 | 2.03 | 2.26 | 2.1
VT R (mΩ) Individual coils |  |  |  |  |  |  | 
@1 Amp |  | A1 | 614 | 606 | 611 | 604 | 608
 |  | A2 | 613 | 606 | 611 | 604 | 607
 |  | A3 | 415 | 410 | 414 | 409 | 
 |  | A4 | 355 | 352 | 354 | 350 | 
 |  | A5 | 355 | 352 | 354 | 350 | 
 |  | A6 | 350 | 345 | 349 | 345 | 
 |  | A7 | 350 | 345 | 348 | 344 | 
 |  | A8 | 344 | 340 | 342 | 339 | 
 |  | B8 | 343 | 340 | 342 | 339 | 
 |  | B7 | 343 | 340 | 330 | 338 | 
 |  | B6 | 338 | 334 | 336 | 333 | 
 |  | B5 | 337 | 333 | 336 | 333 | 
 |  | B4 | 331 | 328 | 331 | 327 | 
 |  | B3 | 187 | 186 | 187 | 185 | 
 |  | B2 | 0 | 2 | 1 | 0.1 | 0
 |  | B1 | 0 | 1 | 1 | 0.06 | 0
HIPOT |  |  | OK | OK | OK | OK | OK
IMPULSE |  |  | OK | OK | OK | OK | OK
122 B7 is not sequential, Examination follows in next slides
211 data now shown with updated measurements

## Slide 3: Coil 122 Measurement Differential
 | Coil 122 FNAL | C122 FNAL Differential | Coil 122 LBNL retest | C122 LBNL Differential
A1 | 0.4 |  | 0 | 
A2 | 1 | 0.6 | 0 | 0
A3 | 195.13 | 194.13 | 196 | 196
A4 | 254.62 | 59.49 | 256 | 60
A5 | 254.64 | 0.02 | 256 | 0
A6 | 260.21 | 5.57 | 262 | 6
A7 | 260.45 | 0.24 | 262 | 0
A8 | 266.64 | 6.19 | 267 | 5
B8 | 266.25 | -0.39 | 268 | 1
B7 | 277.42 | 11.17 | 280 | 12
B6 | 272.21 | -5.21 | 274 | -6
B5 | 272.9 | 0.69 | 274 | 0
B4 | 279.15 | 6.25 | 280 | 6
B3 | 421.69 | 142.54 | 423 | 143
B2 | 608.5 | 186.81 | 608.872 | 185.872
B1 | 609.4 | 0.9 | 608.93 | 0.058
 | Coil 119 FNAL | C119 FNAL Differential
A1 | 0.5 | 
A2 | 0.5 | 0
A3 | 192.08 | 191.58
A4 | 251.01 | 58.93
A5 | 251.18 | 0.17
A6 | 256.54 | 5.36
A7 | 256.72 | 0.18
A8 | 263.07 | 6.35
B8 | 263.85 | 0.78
B7 | 264.44 | 0.59
B6 | 269.82 | 5.38
B5 | 270.35 | 0.53
B4 | 274.48 | 4.13
B3 | 416.32 | 141.84
B2 | 598.4 | 182.08
B1 | 598.6 | 0.2
Reference Values from Coil 119

## Slide 4: Voltage Tap Mapping
B07 is ~two straight sections away from B08
B07 is ~one straight section away from B06 in the opposite direction
B07 and B04 are very close in value, within ~1 ohm
Conclusion:
  VTB07 is actually not on pole turn, but rather on 2nd turn, between VTB03 and VTB04
 | Coil 122 LBNL retest | C122 LBNL Differential | 
A1 | 0 |  | 
A2 | 0 | A2-A1 | 0
A3 | 196 | A3-A2 | 196
A4 | 256 | A4-A3 | 60
A5 | 256 | A5-A4 | 0
A6 | 262 | A6-A5 | 6
A7 | 262 | A7-A6 | 0
A8 | 267 | A8-A7 | 5
B8 | 268 | B8-A8 | 1
B7 | 280 | B7-B8 | 12
B6 | 274 | B6-B7 | -6
B5 | 274 | B5-B6 | 0
B4 | 280 | B4-B5 | 6
B3 | 423 | B3-B4 | 143
B2 | 608.872 | B2-B3 | 185.872
B1 | 608.93 | B1-B2 | 0.058
~6 ohms, straight section

## Slide 5: Coil Fabrication Intermediate EQC Steps

## Slide 6: Coil 122 LE VTB Wires Soldered
Fred Nobrega
Soldered wires appear to be correctly placed and labeled, per coil fabrication drawing

## Slide 7: VT Flags, Coil 119 and 122
Courtesy of Fred Nobrega
There appears to be a shift of a cable’s width in Coil 122 VTB07 flag

## Slide 8: Summary and Conclusion
Fabrication data shows same out of sequence values from trace installation
Data was remeasured and confirmed at LBNL
Photos presented
Measurement data suggests that the VTB07 VT flag was placed on the 2nd turn from the pole
  Actual order of the outer layer voltage taps are: B01, B02, B03, B07, B04, B05, B06, B08, A08, etc...

## Slide 9: Additional Slides

## Slide 10: Electrical Testing Notes
Keithley 2110 Multimeter (Sequential-R Voltage Measurements, Resistance Measurements)
  HP E3610A DC Power Supply (Current Source for Sequential R)
Hypotultra 7805 (Hipot)
LCR Meter
  GW Instek LCR-819
ECG-Kokusai Winding Test DWX-05 (Impulse Testing)