## Slide 1
Cathode R&D Needs
and Status for European HE-/Nuclear Physics projects
SNOWMASS 2021,
Electron Source workshop
February, 16, 2022
Presented by Kurt Aulenbacher
Thanks to:
Boris Militsyn, Walid Kaabi, David Elsner, Joachim Enders, Jennifer Groth, Rong Xiang, Flo Hug
Supported by German Science ministry, BMBF, through project 05K19UMA

## Slide 2: Outline
Electron accelerators for nuclear physics in Europe – operating & planned
Photocathode research for such accelerators

## Slide 3: Operating/planned European Accelerators with Photoemission sources- Overview
Big research centers: DESY, HZDR, PSI, CERN, Daresbury, INFN many more: e.g., CsTe, and Magnesium photocathodes, also in SRF guns. Also trying to use GaAs in SRF gun at Dresden.
Could be well suited for nuclear/particle physics but – with a few exceptions - only used for applied research.
University based electron accelerators in Germany
–dedicated to nuclear physics: Bonn (ELSA), Darmstadt S-DALINAC, Mainz (MAMI,MESA):
Only Mainz currently operating with spin-polarized source, ongoing basic research at Darmstadt, Bonn not operating photosource, but ready to continue (if needed by hadron physics experiments)
Upcoming machines: See European Strategy for particle physics “Accelerator R&D Roadmap” arxiv_2201.07895: bERLinPRO, MESA, PERLE
PERLE, (later: LheC) plan to use unpolarized electrons, up to 10mA current (ERL!), up 1nC bunch charge may upgrade to polarized, depending o the physics case
Planned projects: ILC, CLIC : polarized

## Slide 4: Upcoming European Accelerators
arxiv_2201.07895
MESA (construction)
bERLinPro
(commissioning)
PERLE
(planning)
MESA is aiming at round the clock operation
for nuclear physics mainly with spin-polarized beam,

## Slide 5: “spin-polarized”-, i.e. GaAs-related cathode research

## Slide 6: “spin-polarized”-cathode research TU-Darmstadt (TU-D)
Accelence: Joint graduate research center “Physics and technology of energy recovery linacs”
(Darmstadt and Mainz)
NF3 and Lithium Co-deposition studies in cooperation with JLAB/UITF

## Slide 7: TU-D Studies with NF3 and Lithium @JLAB/UITF
Quantum efficiency η
Lifetime τ
PhD Thesis Maximilian Herbert

## Slide 8: TU-D: Cryosource
PhD thesis Tobias Eggert/TU-Darmstadt
Create 4K environment for (hotter) GaAs- cathode in DC-gun.
IGP and NEG pump
source chamber
faraday cup
load chamber
alpha magnet
laser fiber

## Slide 9
Picture&lattice layout : D. Simon
MESA (Mainz Energy-recovering Superconducting Accelerator)
- An electron accelerator for nuclear/particle physics at U-Mainz

## Slide 10
Double sided recirculation design with normal-conducting injector and superconducting main linac
Two different modes of operation:
(1300 MHz CW beam) - EB-operation (P2/BDX experiment): polarized beam, up to 150 µA @ 155 MeV - ERL-operation (MAGIX experiment): (un)polarized beam, up to 1 (10) mA @ 105 MeV
Picture&lattice layout : D. Simon
Gun
MELBA
MAMBO
MEEC-1
MEEC-2
Recirculation arcs 1-3-5
Recirculation arcs 2-4
Ext. beamline
ERL loop
155 MeV dump
5 MeV dump
P2
MAGIX
MESA Accelerator Layout

## Slide 11: Uni Mainz : Polarization drift study
Observed drift of beam polarization during measurement
can reach 1%/day, and may depend on photocathode activation ?
Measurements by „conventional“ 3.5 MeV Mott-polarimeter at MAMI

## Slide 12: Uni Mainz : Polarization drift study
So far, Oxygen was used
Now, in dedicated test set up, Oxygen and NF3 can be used, e.g. for alternating activations
Test set up has similar source compared to the one operating at MAMI (“PKA2”)
..and is equiped with Spin rotator and Mott polarimeter
Intention-I: Compare drift of polarization under Oxygen and NF3 activation
Intention- II Compare QE/Lifetime behavior  draw conclusion for MESA operations
PhD thesis started – Jennifer Groth
PKA2

## Slide 13: Uni Mainz : Surface Photovoltage (SPV -long pulse)
Near band-gap excitation may provoque surface photvoltage at surface
 leads to reduced QE because of modified NEA-state

## Slide 14
Small „ThErmalized“ source At MAINZ (STEAM)- long pulse SPV
.
Operation with up to 150keVbeam
and up to 10mA -
Surface photovoltage in NEA GaAs at 10mA leads to Q.E. dependend saturation current density in DC-operation (400mus long pulses, 800nm excitation wavelength )
S Friederich-PhD thesis Mainz, 2019
STEAM (inverted source design,
based on JLAB idea )
installed at test apparatus “MELBA”
December 2021 Commissioning
of STEAM at MESA has started.
Commissioning of injector in 22/23
Beam operations for P2
(150muA average current, P>0.85 )
envisaged for end 2024.
S. Friederich et al .doi:10.18429/JACoW-IPAC2019-TUPGW028

## Slide 15
Commissioning of STEAM and „MELBA 2.0“ for MESA
Demanding beam dynamics when Spin rotators „ON“
(P2 mode -polarized beam from at STEAM)
OPAL simulations: 0.2 pC bunches with good beam quality (enorm<1mm) possible  sufficent for P2
1pC bunches possible without Spin manipulation  MESA stage 1, ERL programme
Due to SPV, „green“ excitation preferable (if unpolarized beam desired by experiment)
> 1pC bunches possible with „robust“ source & shorter beamline
 (unpolarized MESA Injector Source Two, MIST), not funded

## Slide 16: Uni Mainz : Surface Photovoltage (shortpulse)
PhD thesis Nahid Scahill
-self modulation of picosecond pulses at very low QE?
Fits with models based on SPV (inspired by Mulhollan et al.)
Or PEA+thermionic emission
R= I(30ps)/I(0ps)

## Slide 17
GaAs/GaAsP”Strained Superlattice” :
(T. Maruyama et al. Appl. Physics. Lett. 85,13 (2004) 2640)
Study of pulse response
Strained Superlattice-cathode
Peak width dominated by experimental resolution
As expected, Intensity drops into noise floor after a few picoseconds. Parasitic peaks due to double reflexes? (PhD Thesis Nahid Scahill)
Longitudinal Halo Study at Mainz

## Slide 18
Strained Superlattice-cathode
“Polarized” Photocathode acquisition problem
Commercial supplier no longer available
Due to absence of large-scale polarized accelerator activity in Europe liited interest in setting up infrastructure
Investigating possible new suppliers and
Help by government “applied” physics institutes (“Fraunhofer)?

## Slide 19: Conclusion
Upcoming (Planned/discussed) electron machines in Europe for nuclear/particle (N/P)-physics will need high
average current from (probably) unpolarized photosources
 large interest in progress but little research activity so far
Progress with unpolarized cathodes may be achieved at other facilities which are not dedicated to N/P-physics
(bERLinPro, DESY,…. )  relatively easy to transfer results towards N/P-project
“University scale machines” exist and there is high demand for improving conditions, in particular operational lifetime of spin polarized sources
Research in this direction is feasible with university means and will also be used whereever such spin polarized beams are needed.

## Slide 20: Thank you