## Slide 1: EP Process Flow for 1.3 GHz Elliptical Shaped Cavities at the ANL/FNAL SCSPF
Cavity arrives at ANL
Cavity inspection, weight measurement, and ultrasonic thickness measurements
Ultrasonic cleaning (1% liquinox, 120°F, 60 min)
Mount cavity on EP tool and leak check system with water
Electropolishing
Ultrasonic cleaning (1% liquinox, 120°F, 60 min)
High pressure rinsing (2 passes)
1st assembly
High pressure rinsing (3 passes)
Final assembly
Leak check and RGA scan
Cavity leaves ANL for baking, testing, etc.

## Slide 2: Evolution of ANL EP Parameters
Old ANL EP parameters
Constant voltage EP (18 V)
Acid return temperature 30-35°C
Acid recipe (85:10 vol ratio, old siemens recipe) and later standard 9:1 vol ratio (Feb 2010)
Changes made to EP parameters beginning March 2010 based on discussions with FNAL, KEK, J-Lab
Adjusted ANL EP parameters (April 2010)
Constant voltage EP (14.5 V)
Cavity surface temperature at equator of 30-35°C for bulk EP, 25-30°C for light EP
Standard 9:1 vol ratio electrolyte

## Slide 3: Evolution of ANL EP Parameters
Decrease in Qo
Adjusted EP parameters resulted in lower Q values (no longer polishing on plateau of I-V curve)

## Slide 4: Typical EP Process Data Using Current Parameters
Current ANL EP Parameters
Constant voltage EP: 18 Volts
Slow acid flow
Cavity equator temperature
  Bulk EP: 30-35°C
  Light EP: 25-30°C
Cavity surface temperatures
(equator, iris, beam tubes)
Current
Voltage
Acid dump tank temperature
Acid return temperature
Water chiller temperature (return)
Acid flow rate
 | 1-cell TE1CAT003 |  | 9-cell TB9AES013 | 
EP Type | Bulk EP | Light EP | Bulk EP | Light EP
Voltage | 18 V |  |  | 
Average Current Density | 48 mA/cm2 | 35 mA/cm2 | 37 mA/cm2 | 27 mA/cm2
Nb Concentration of the acid | 2.5 g/L | 3.1 g/L | 1.9 g/L | 1.8 g/L
Cavity Equator Temperature | 30-35°C | 25-30°C | 30-35°C | 25-30°C
Acid Temperature (Return) | 24-26°C | 18-21°C | 26-29°C | 21-23°C
EP monitoring data for the bulk (120 µm) EP of TE1CAT003
Before bulk EP
After bulk EP

## Slide 5: 72 MHz QWR EP for ATLAS Intensity Upgrade
Current
Voltage
Acid dump tank temperature
Acid return temperature
Water chiller temperature (return)
Cavity surface temperatures
Benefits of external water cooling:
De-couples temperature control from the acid
Better control of the EP process
Very stable EP

## Slide 6: Recent Cavity Test Results
1.3 GHz Single Cell Cavity
1.3 GHz Bare 9-Cell Cavity
1.3 GHz Dressed 9-Cell Cavity
Best performing cavities:
Single cell: TE1ACC002 – tumbling + light EP (left)
9-cell: TB9RI022 – light EP (center)
Repair cavity: TB9AES002 (right)
Previous good performing bare cavity
Improved performance after dressed EP
Cavity performance recovered after baking