## Slide 1: Advances in SRF Development for ILC
Akira Yamamoto
ILC-GDE and KEK
Prepared for SRF2011, Chicago, July 25, 2011
With sincere acknowledgment for all
ILC-GDE SCRF collaborators and global SCRF industrial partners
Special thanks for M. Ross, N. Walker, and R. Geng

## Slide 2: Design Update in SB2009
RDR  SB2009
Motivation: Cost containment
Single accelerator tunnel
Smaller damping ring
e+ target location at high-energy end,
SCRF: Gradient variation of 31.5 MV/m +/- 20 %,
HLRF: KCS and DRFS with RDR-RF unit as backup

## Slide 3: Global Plan for ILC Gradient R&D
New baseline gradient:
Vertical acceptance: 35 MV/m average, allowing ±20% spread (28-42 MV/m)
Operational: 31.5 MV/m average, allowing ±20% spread (25-38 MV/m)

## Slide 4: Global Plan for ILC Gradient R&D
New baseline gradient:
Vertical acceptance: 35 MV/m average, allowing ±20% spread (28-42 MV/m)
Operational: 31.5 MV/m average, allowing ±20% spread (25-38 MV/m)

## Slide 5: Global Yield of Cavities in 2008 tested at DESY and JLab Originally reported by H. Padamsee
Process Yield: ~ 23 % @ 35 MV/m, based on 48 Tests for19 cavities
Manufactured by ACCEL, AES, Zanon, KEK (Ichiro-type), and JLab
Reported by H. Padamsee at TTC-08 (IUAC), and ILC-08, (Chicago), based on the status in 2008。
50%
5
H. Padamsee, ILC-08 (Chicago)
Definition for production yield, not established yet

## Slide 6: Creation of a Global Database for Better Understanding of “Production Yield”
Global Data Base Team formed by:
  Camille Ginsburg (Fermilab), leader
  Rongli Geng (JLab)
  Zack Conway (Cornell University)
  Sebastian Aderhold (DESY)
  Yasuchika Yamamoto (KEK)
Activity
  July 2009:
  - Determine DESY-DB to be viable option,
  Sept., 2009: (ALCPG/GDE)
  - Dataset, web-based, support by FNAL/DESY,
  Dec., 2009: (SB2009) : 1st update
  March, 2010 (IW-ILC) : 2nd update
  June, 2010 (End TDP-1) : 3rd update
  March, 2011 (ILC-ALCPG): 4th update
  RI, Zanon, AES, MHI manufactured
  Cavity data included.
  (3 region’s data available)
Production yield allowing to:
- include the 2nd chemical process

## Slide 7: Standard Procedure Established for ILC-SCRF Cavity evaluation, in guidance of TTC
 | Standard Fabrication/Process
Fabrication | Nb-sheet purchasing
 | Component Fabrication
 | Cavity assembly with EBW
Process | EP-1 (~150um)
 | Ultrasonic degreasing with detergent, or ethanol rinse
 | High-pressure pure-water rinsing
 | Hydrogen degassing at > 600 C
 | Field flatness tuning
 | EP-2 (~20um)
 | Ultrasonic degreasing or ethanol (or EP 5 um with fresh acid)
 | High-pressure pure-water rinsing
 | Antenna Assembly
 | Baking at 120 C
Cold Test (vertical test) | Performance Test with temperature and mode measurement
Key Process
Fabrication
Material
EBW
Shape
Process
Electro-Polishing
Ethanol Rinsing or
Ultra sonic. + Detergent Rins.
High Pr. Pure Water cleaning
allow twice

## Slide 8: Global ILC Cavity Gradient Yield Updated, March, 2011
Plot courtesy
Camille Ginsburg of FNAL
TDP-2 Goal
TDP-1 Goal
Achieved
> 50 %
35 MV/m usable

## Slide 9: Global ILC Cavity Gradient Yield Updated, March, 2011
Plot courtesy
Camille Ginsburg of FNAL
TDP-2 Goal
> 28 MV/m usable
Effectively
Achieved:
> 70 %

## Slide 10: Impact of Mechanical Polishing progress in Nov, 2010 ~ May, 2011
✔
✔
AES5 After
Mechanical
Polishing
at Cornell
ACC15 after
Mechanical
Polishing
at FNAL
This cavity
AES6 is being
treated with
mechanical
polishing at
FNAL and will
be then EP
processed and
tested at JLAB
88%
JLAB + FNAL
Average gradient 39 MV/m
94% yield at ≥31 MV/m
+ +
Average gradient 38.8 MV/m
Courtesy: R. Geng

## Slide 11: Impact of Mechanical Polishing as of July, 2011
✔
✔
AES5 After
Mechanical
Polishing
at Cornell
ACC15 after
Mechanical
Polishing
at FNAL
This cavity
AES6 is being
treated with
mechanical
polishing at
FNAL and will
be then EP
processed and
tested at JLAB
88%
JLAB + FNAL
Average gradient 39 MV/m
94% yield at ≥31 MV/m
+ +
Average gradient 38.8 MV/m
Courtesy: R. Geng

## Slide 12: SCRF 9-Cell Cavity Highlight: in 2010
Americas:
Niowave-Roark-FNAL: 1st cavity reached 28.8 MV/m.
Jlab set ~ 90% yield @ 35 MV/m (1 vendor, process at JLab
FNAL-KEK: Cavity repaired, G improved from 11 to 30 MV/m
Asia:
IHEP-KEK: 1st cavity (LL, large-grain, no-end) reached 20 MV/m,
PKU-JLab: Cavity (Tesla, fine-grain) reached 28 MV/m,
Hitachi-KEK: 1st cavity (Tesla-like, no-end) reached 35 MV/m
MHI-KEK: Cavity (Tesla-like w/ end-HOM) reached 37 MV/m,
MHI-KEK-S1-Global: cavity (Tesla-like) reached > 35 (40) MV/m
Europe:
E-XFEL / HG-FP7: 600 cavity production order placed (2 vendors)

## Slide 13: SRF Cavity and Gradient Highlights 2010~ 2011
Americas
  FNAL mechanical polishing improved 9-cell cavity ACC15 gradient from 19 MV/m to 35 MV/m
  JLAB started processing and testing DESY seamless 9-cell cavity built from DESY 3-cell seamless units
  6 of AES 3rd production & 4 Niowave-Roark 1st production received by FNAL
Asia
  KEK MHI-12 reached 40.7 MV/m gradient at Q0 6.2E9
  KEK-JLAB: ACD shape cavity ICHIRO7 reached 40 MV/m gradient at Q0 8E9
Europe
  DESY large-grain 9-cell cavity AC155 reached 45 MV/m at Q0 > 1E10, and more reached in the next, …
R. Geng

## Slide 14: Global Plan for SCRF R&D
Year | 07 | 2008 |  | 2009 |  | 2010 |  | 2011 | 2012
Phase | TDP-1 |  |  |  |  |  | TDP-2 |  | 
Cavity Gradient in v. test to reach 35 MV/m |  Yield 50% |  |  |  |  |  |  Yield 90% |  | 
Cavity-string to reach 31.5 MV/m, with one-cryomodule |  | Global effort for string assembly and test (DESY, FNAL, INFN, KEK) |  |  |  |  |  |  | 
System Test with beam acceleration |  |  | FLASH (DESY) , NML (FNAL) STF2 (KEK, test start in 2013) |  |  |  |  |  | 
Preparation for Industrialization |  |  |  |  | Production Technology R&D |  |  |  | 
Communication with industry: | 2009: 1st step: Visit Vender (2009) 2010: 2nd step: Organize Workshop (2010) 2011: 3rd step: Send specification & receive response |  |  |  |  |  |  |  | 
We are here

## Slide 15: Integrated Systems Tests 2009 ~
“9mA experiment”
achieved ~1800 bunches at 9mA in 09.2009
DE/ERMS ~0.5% (@ 0.8 GeV)
~0.1% within pulse
Full systems integration testing
FLASH (DESY)
NML (FNAL)
STF (KEK)
TDP focus
Under construction
Up to 6 cryomodules
Operation: end 2012
“Quantum Beam” experiment 2011
1 CM with beam 2013
7 CM → 1.2 GeV beam
photon user facility
(2 CM 2015)
(3 CM)

## Slide 16: Cryomodule Development & Test
FLASH (DESY)
  <32 MV/m> in CM operation, PXFEL-1
  < 30 MV/m> in FLASH operation
NML-CM1 (Fermi)
  In progress
STF: S1-Global (KEK)
  Global effort
    DESY/INFN/FNAL/SLAC/KEK
  <26 MV/m> in CM operation

## Slide 17
M. Ross

## Slide 18
M. Ross

## Slide 19: Cryomodule-1 Testing at Fermilab
7 of 8 cavities powered,
2 with high heat; no FE?
1 tuner motor failure
Calibrations under study
Preliminary

## Slide 20: S1-Global Assembly/Test with Global Effort
DESY, FNAL, Jan., 2010
INFN
and
FNAL
Feb.
2010
FNAL & INFN, July, 2010
DESY, May, 2010
March, 2010
June, 2010 ~
DESY, Sept. 2010

## Slide 21
S1-Global High Power Test
at STF/KEK, Sep., 2010 ~
With
Denis Kostin
(DESY) Sept. 2010
With
Yuriy Pischalnikov
Warren Schappert
(FNAL) Oct. 2010
Notes: 777
888
21
777
21
888

## Slide 22: S1-Global: Demonstrations/evaluation of Various Couplers and Tuners
Every coupler and tuner demonstrated, as expected, and be applicable for ILC cavities
Finding various subjects to be further investigated and settled

## Slide 23
MHI-09
MHI-07
MHI-06
MHI-05
AES004
ACC011
Z108
Z109
FNAL
DESY
KEK
Comparison of cavity performance
ave. Eacc,max
VT : 30 MV/m
1 cav : 27 MV/m
7 cav : 26 MV/m
D
C
D : Detune
C : Coupler
D
Performance reduction in two cavities and one coupler
Tuner mechanics trouble in two cavities

## Slide 24
Stability in 6300 sec.
LLRF stability study with 7 cavities operation at 25MV/m
Field Waveform of each cavity
- Vector-sum stability: 24.995MV/m ~ 24.988MV/m (~0.03%)
- Amplitude stability in pulse flat-top: < 60ppm=0.006%rms
- Phase stability in pulse flat-top: < 0.0017 degree.rms
vector-sum gradient
amplitude stability in pulse flat-top
phase stability in pulse flat-top
7-cavity operation by digital LLRF

## Slide 25
A. Bosotti, C. Pagani, R. Paparella, P. Pierini,
INFN (Italy)
K. Jensch, D. Kostin, L. Lilje, A. Matheisen, W.-D. Moeller,
M. Schmoekel, P. Schilling, N. Walker, H. Weise,
DESY (Germany)
T. Arkan, S. Barbanotti, M. Battistoni, H. Carter,
M. Champion, A. Hocker, R. Kephart, J. Kerby, D. Mitchell,
Y. Pischalnikov, T.J. Peterson, M. Ross, W. Schappert,
B. Smith
FNAL (USA)
C. Adolphsen, C. Nantista, SLAC (USA)
M. Akemoto, S. Fukuda, K. Hara, H. Hayano, N. Higashi, E. Kako,
H. Katagiri, Y. Kojima, Y. Kondo, T. Matsumoto, S. Michizono, T. Miura,
H. Nakai, H. Nakajima, K. Nakanishi, S. Noguchi, N. Ohuchi, T. Saeki,
M. Satoh, T. Shishido, T. Shidara, T. Takenaka, A. Terashima,
N. Toge, K. Tsuchiya, K. Watanabe, S. Yamaguchi,
A. Yamamoto, Y. Yamamoto, K. Yokoya,
KEK (Japan)
Many Thanks for
Global Collaboration for S1-Global

## Slide 26: Global Plan for SCRF R&D
Year | 07 | 2008 |  | 2009 |  | 2010 |  | 2011 | 2012
Phase | TDP-1 |  |  |  |  |  | TDP-2 |  | 
Cavity Gradient in v. test to reach 35 MV/m |  Yield 50% |  |  |  |  |  |  Yield 90% |  | 
Cavity-string to reach 31.5 MV/m, with one-cryomodule |  | Global effort for string assembly and test (DESY, FNAL, INFN, KEK) |  |  |  |  |  |  | 
System Test with beam acceleration |  |  | FLASH (DESY) , NML (FNAL) STF2 (KEK, test start in 2013) |  |  |  |  |  | 
Preparation for Industrialization |  |  |  |  | Production Technology R&D |  |  |  | 
Communication with industry: | 2009: 1st step: Visit Vender (2009) 2010: 2nd step: Organize Workshop (2010) 2011: 3rd step: Send specification & receive response |  |  |  |  |  |  |  | 
We are here

## Slide 27: SCRF-ML Technology Required
RDR Parameters | Value
C.M. Energy | 500 GeV
Peak luminosity | 2x1034 cm-2s-1
Beam Rep. rate | 5 Hz
Pulse time duration | 1 ms
Average beam current | 9 mA (in pulse)
Av. field gradient | 31.5 MV/m
# 9-cell cavity | 14,560
# cryomodule | 1,680
# RF units | 560
RDR  SB2009

## Slide 28: SCRF Procurement/Manufacturing Model
Regional hub-laboratories responsible to regional procurements to be open for any world-wide industry participation
Regional Hub-Lab:
E, & …
Regional Hub-Lab:
A
Regional Hub-Lab:
B
Regional Hub-Lab:
D
World-wide
Industry responsible to
‘Build-to-Print’ manufacturing
ILC Host-Lab
Regional Hub-Lab:
C: responsible to
Hosting System Test and Gradient Performance
Technical Coordination
for Lab-Consortium
: Technical
coordination link
: Procurement link

## Slide 29: Communication with Industry in 2011
Visit factories, and Request for information
  Based on currently available manufacturing technology and available information with worldwide industry
    Assume the EXFEL ‘build-to-print’ specifications as a common reference, and
    Allow ‘plug-compatible’ alternate designs with the cost equivalent or more effective production and/or better performance
Requests for information to companies
  Cost comparisons: 20/50/100 % in 3 or 6 year production ?
  Factory-site location: company or laboratory ?
  Sharing responsibilities for the cost-effective production ?
  Deliverables with ‘build-to-print’ fabrication?
  Consortium to be considered or not

## Slide 30: Visiting Companies in Progress (and further plan)
 | Date | Company | Place | Technical sbject
1 | 2/8 | Hitachi | Tokyo (JP) | Cavity/Cryomodule
2 | 2/8 | Toshiba | Yokohana (JP) | Cavity/Cryomodule, Magnet
3 | 2/9 | MHI | Kobe (JP) | Cavity / (Cryomodule)
4 | 2/9 | Tokyo-Denkai | Tokyo (JP) | Material (Nb)
5 | 2/18 | OTIC | NingXia (CN) | Material (Nb, NbTi, Ti)
6 | 3/3 | (Zanon) mtg at INFN | Verona (IT) | Cavity/(Cryomodule)
7 | 3/4 | RI | Koeln (DE) | Cavity (Cryomodule)
8 | 3/14, (4/8) | AES | Medford, NY (US) | Cavity (Cryomodule)
9 | 3/15, (4/7) | Niowave | Lansing, MI (US) | Cavity/ (Cryomodule)
10 | 4/6 | PAVAC | Vancouver (CA) | Cavity, EBW-machine
11 | 4/25 | ATI Wah-Chang | Albany, OR (US) | Material (Nb, Nb-Ti, Ti)
12 | 4/27 | Plansee | Ruette (AS) | Material (Nb, Nb-Ti, Ti)
13 | 5/24 | SDMS | Sr. Romans (FR) | Cavity, Vessel, joint
14 | 7/6 | Heraeus | Hanau (DE) | Material (Nb, Nb-Ti, Ti)
15 | 9/14 | Zanon | Verona (IT) | Cryomodule
16 | 11/16 | SST | Munchen (DE) | EBW-machine

## Slide 31: The 2nd workshop on SCRF Technology and Industrialization for the ILC
as a satellite meeting of SRF 2011
Date: July 24, 2011
Place: Chicago
Agenda:
  Introduction
  Reports from SCRF cavity/cryomodule industry
  Reports from SC material vendor
  Comments from Potential Regional Hub-laboratory
  Discussions on the ILC SCRF industrialization model
Note:
  Open for everybody,
  Many Industrial participations acknowledged

## Slide 32: Workshop Objectives
Exchange information:
  efforts on cost-effective SCRF cavity/cryomodule production and quality control
Discuss on:
  optimum industrialization models for ILC including the scale, time, and site,
  sharing responsibilities between industry and laboratories, and/or industry and industry,
  how to manage industrial constraint/regulation and to coordination it in global scale
Provide:
  advices for the ILC TDR and cost-estimate.

## Slide 33: Cavity R&D for ILC 1 TeV-Upgrade (continued)
ILC SRF cavity R&D beyond 2012
  Importance
    Maintain “global” nature for coherence
    Project oriented, targeted R&D, benchmarked progress
    Resource sharing, cross-region experience exchange
  ILC: driver for high gradient SRF cavity technology
    Pursuit of ultimate gradient continues to motivate innovation
    Gradient success continues to benefit SRF based accelerators
year | # of >35 MV/m 9-cell cavities | # of labs capable of 35 MV/m processing | # of Industrial manufacturers capable of 35 MV/m fabrication
2006 | 10 | 1 DESY | 2 ACCEL, ZANON
2011 | 41 | 4 DESY, JLAB, FNAL, KEK and others joining soon | 4 RI, ZANON, AES, MHI, and others joining soon
R. Geng

## Slide 34: Cavity R&D to be extended for possible ILC 1 TeV Upgrade
High gradient
  Shape: LL/ICHIRO, RE, LSF – on going
  Processing: Mechanical polishing – on going
  Material
    Large grain – on going
    Nb/Cu laminate – needs re-start
    Multi-layer and material beyond Nb – to be encouraged
High Q0
  Large grain – on going
  ALD over coating – R&D started
Suppress field emission
  CO2 snow cleaning – on going
  HOM can cleaning – R&D started
M. Ross

## Slide 35: Summary
SRF 1.3 GHz cavity R&D progressed
  9-cell cavity Gradient R&D:
    Maximum gradient reaching > 45 MV/m (w/ large-grain)
    Production-yield progressed in ILC Global data-base:
      ~ 20 % at 35 MV/m in 2008 to ~ 60 % at 35 MV/m in 2011
  Cavity-string performance in Cryomodule
    FLASH/PXFEL-1: reached <32 MV/m>
    NML: in progress
    S1-Global: reached <26 MV/m> with 7 cavity-string
  Superconducting accelerator system test
    FLASH: progressing in acceleration for 9 mA demonstration
Industrialization study in progress
  in close communication with industry
Further high-gradient R&D after TDR being prepared,
  for possible 1-TeV upgrade
Please refer
further ILC related papers
presented in SRF2011

## Slide 36: backup

## Slide 37: Four Cavity Manufacturer Data Now Included for Global Yield Analysis

## Slide 38
Local grinding of quench location
Pit; appeared after bulk EP,
limit to 16MV/m
Bump at heat affecting zone,
limit to 20MV/m
AES003 4-cell equator, t=306 degree
MHI08 2-cell equator, t=172 degree
200um x 600um, depth 115um
600um x 600um, hight ~50? um
30MV/m
local grinding & EP
27MV/m
local grinding & EP
38MV/m
additional EP
34MV/m
additional HPR and bake
Local grinder tool

## Slide 39: ACC15 Reached 35 MV/m after Mechanical Polishing at FNAL
More cavities
by FNAL mechanical
polishing
on the way…

## Slide 40: KEK MHI-12 Exceeded 40 MV/m
MHI-13 reached 36.5 MV/m at Q0 7.5E9 after first-pass processing

## Slide 41: KEK ICHIRO7 Reached 40 MV/m
50 MV/m in perspective as
many ICHIRO
1-cell cavities achieved gradient of > 50 MV/m…
Photo courtesy
Kenji Saito & Fumio Furuta
of KEK

## Slide 42: DESY Large-Grain Cavity AC155 Reached > 45 MV/m at Q0 > 1E10
Heavy BCP + EP + low temperature bake
7 more cavities
on the way…

## Slide 43: Gradient Progress at TTF at DESY ~ 2008
ILC:
  <31.5> MV/m
TTF: ~ 2008：
  <~ 30> MV/m
  >> EXFEL

## Slide 44
Simulation
(time: us from start of fill)

## Slide 45: Achievements: SRF Linac – FLASH (DESY)
High beam power and long bunch-trains (Sept 2009) |  | 
Metric | ILC Goal | Achieved
Macro-pulse current | 9mA | 9mA
Bunches per pulse | 2400 x 3nC (3MHz) | 1800 x 3nC 2400 x 2nC
Cavities operating at high gradients, close to quench | 31.5MV/m +/-20% | 4 cavities > 30MV/m
Gradient operating margins (Feb 2011) |  | 
Metric | ILC Goal | Achieved
Cavity gradient flatness (all cavities in vector sum) | 2% DV/V (800ms, 9mA) | 2.5% DV/V (400ms, 4.5mA) “Methodology established”
Gradient operating margin | All cavities operating within 3% of quench limits | (Focus of early 2012 run)
Energy Stability | 0.1% at 250GeV | <0.15% p-p (0.4ms) <0.02% rms (5Hz)

## Slide 46: New Cryomodule Test Facility (ARRA funded )
New Cryomodule Test Facility
New 500 W 1.8 K refrigerator
(under fabrication in industry)
will be located in CMTF bldg
New Electronics building above tunnel extension
Compressor building

## Slide 47: Production Process/Responsibility
Step hosted | Industry | Industry/Laboratory | Hub-laboratory | ILC Host-laboratory
Regional constraint | no | yes | yes | yes
Accelerator - Integration, Commissioning |  |  |  | Accelerator sys. Integ.
SCRF Cryomodule - Perofrmance Test |  |  | Cold, gradient test | As partly as hub-lab
Cryomodule/Cavity - Assembly |  | Coupler, tuner, cav-string/cryomoduleassmbly work |  | As partly as hub-lab
Cryomodule component - Manufacturing | V. vessel, cold-mass ... |  |  | 
9-cell Cavity - Performance Test |  |  | Cold, gradient test | As partly as hub-lab
9-cell Cavity - Manufacturing | 9-cell, end-group assembly, Chem-process, He-Jacketing |  |  | 
Sub-comp/material - Production/Procurement | Nb, Ti, specific comp. … |  | Procurement | 

## Slide 48: Agenda (a.m.)
08:30 - 08:35 Welcome 05'
Speakers: Mark Champion (FNAL) , Camille Ginsburg (FNAL)
08:35 - 09:15 Introduction 40'
Speaker: Akira Yamamoto (KEK)
09:15 - 12:00 Cavity Industrial Partners
09:15 ILC SCRF Dressed Cavity, An Industrial Cost Estimate Update 25'
Speaker: J. Sredniawski (AES)
09:40 Niowave’s Industrialization Plan 25'
Speakers: T.L. Grimm, C.H. Boulware, A.A. Kolka, and J.L. Hollister (Niowave)
10:05-10:20 Coffee Break--> 15’
10:20 Utilization of Industrial Electron Beam Processing
in Order to Optimize Fabrication of SRF Cavities in Larger Quantities 25'
Speaker: R. Edinger (Pavac)
10:45 Preparing RI for the Mechanical Manufacturing and
Surface Preparation of 300 XFEL Cavities 25'
Speaker: M. Pekeler (RI)
11:10 Study of Industrialization and Factory Layout for SCRF Cavity Production 25'
Speaker: S. Ishii (MHI)
11:35 Study of Industrialization and Factory Layout for Cryomodule Assembly 25'
Speaker: T. Semba (Hitachi)
12:00 - 13:00 Lunch (working lunch served by GDE, Maxine)

## Slide 49: Agenda (p.m.)
13:00 - 14:40 Material Industry Partners
13:00 Niobium from OTIC 20'
Speaker: H. Zhao (OTIC Ningxia)
13:20 Nb-sheet Production Status and Future Prospects 20'
Speaker: H. Umezawa (Tokyo Denkai)
13:40 Status and Future Prospect for Superconducting Material 20'
Speaker: T. Nelson (ATI/Wah Chang)
14:00 Progress and Capability of Nb Seamless Pipe 20’
Speaker: B. Spaniol (Heraeus)
14:20 Progress and Capability of Nb Sheet Production 20'
Speaker: R. Grill (Plansee)
14:40 - 14:50 Coffee Break
14:50 - 15:30 Laboratory
14:50 Industrialization Activities in the Americas 20'
Speaker: Bob Kephart (FNAL)
15:10 Industrialization Studies in the KEK Cavity Fabrication Facility (CFF) 20’ Speaker: Hitoshi Hayano (KEK)
15:30 - 16:00 Summary and Discussion 30'
Conveners: Mark Champion (FNAL) , Camille Ginsburg (FNAL)

## Slide 50: Main Issues at Very High Gradient
Material
Nb: > 2000 Oe (exp.)
2400 Oe (the.)
Nb3Sn: > 4000 Oe (the.)
Cavity shape
Cavity surface chemistry
Cavity surface smoothness
Cavity wall
thermal conductance
Achievable gradient
“Knobs” for improved reproducibility in overcoming local quench at very high gradient of 40-50 MV/m
Alternate cavity shape for reduced Hpk/Eacc ratio. In hand (LL, RE, LSF).
Uniform cavity processing for reduced local “bad” spots. In hand (EP).
Smooth surface for reduced local magnetic field enhancement. In hand(CBP & derivative + EP).
Improved wall thermal conductance for increased local heating tolerance.
  Cavity heat treatment optimization for “phonon peak engineering”
  Use Nb/Cu composite material (such as explosion bonded material)
(5) The game-changing knob is a Nb replacement material (such as Nb3Sn or Mg2B w/ multi-layer).

## Slide 51: Global Plan for SCRF R&D
Year | 07 | 2008 |  | 2009 |  | 2010 |  | 2011 | 2012
Phase | TDP-1 |  |  |  |  |  | TDP-2 |  | 
Cavity Gradient in v. test to reach 35 MV/m |  Yield 50% |  |  |  |  |  |  Yield 90% |  | 
Cavity-string to reach 31.5 MV/m, with one-cryomodule |  | Global effort for string assembly and test (DESY, FNAL, INFN, KEK) |  |  |  |  |  |  | 
System Test with beam acceleration |  |  | FLASH (DESY) , NML (FNAL) STF2 (KEK, test start in 2013) |  |  |  |  |  | 
Preparation for Industrialization |  |  |  |  | Production Technology R&D |  |  |  | 
Communication with industry: | 2009: 1st step: Visit Vendor (2009) 2010: 2nd step: Organize Workshop (2010) 2011: 3rd step: Send specification & receive response |  |  |  |  |  |  |  |