## Slide 1: Stoichiometric Nb3Sn in First Samples Coated at Cornell
Sam Posen
Cornell University
Notes: Thanks, honoured

## Slide 2: Motivation – High Gradients
Nb cavities are reaching fundamental limit
Alternative materials required to reach higher gradients
Nb3Sn 100 MV/m?
From Akira Yamamoto’s talk “Advances in SRF Development for ILC” on Monday

## Slide 3: Motivation – Low Surface Resistance
Nb3Sn has already shown great promise
Great potential of Nb3Sn for moderate field, high Q machines. Modest cyrogenic costs!
  ~1010 at 4.2K! ~1011 at 2K!
Cavities produced by University of Wuppertal

## Slide 4: Nb3Sn Furnace Insert
Nb heat Shields
Power for heater
Copper transition weld from stainless to Nb
Flange to UHV furnace
Coating chamber is inserted into UHV furnace. Separate vacuum system keeps cavity furnace free from tin contamination
UHV Furnace
Top of insert
Notes: Small samples relative to furnace size may help keep temperature more uniform

## Slide 5: Nb3Sn Fabrication at Cornell
UHV Furnace
Nb substrate to be coated
Coating by Vapor Diffusion
Coating procedure follows work of Müller et al., University of Wuppertal in 80s and 90s
W crucible holding 99.999% Sn
1100 C
1200 C
Heater
Temperature monitoring by thermocouples inside furnace. Gradient <1 K across sample

## Slide 6: New Surface Preparation Techniques
Add to Wuppertal procedure new techniques that have increased Q and E values in Nb cavities

## Slide 7: New Surface Preparation Techniques
Add to Wuppertal procedure new techniques that have increased Q and E values in Nb cavities
Nb, 1993

## Slide 8: New Surface Preparation Techniques
Add to Wuppertal procedure new techniques that have increased Q and E values in Nb cavities
Nb, 1993
+ HPR, EP, 120 deg C bake, CBP, single crystal Nb
Nb, 2011

## Slide 9: New Surface Preparation Techniques
Add to Wuppertal procedure new techniques that have increased Q and E values in Nb cavities
Nb3Sn, 1995

## Slide 10: New Surface Preparation Techniques
Add to Wuppertal procedure new techniques that have increased Q and E values in Nb cavities
Nb3Sn, 1995
+ HPR, EP, 120 deg C bake, CBP, single crystal Nb
Nb3Sn, 2012
???
Notes: Improve substrate – maybe push off the onset of Q-drop – increase Hc1?

## Slide 11: First Coated Samples
2 square samples were coated
Coatings were characterized in various ways
One of the samples was anodized in NH4OH at 75V
Nb->blue Sn-> yellow Nb3Sn -> Pink/purple
Uniform coating! No excess tin on surface!
Anodized
Not anodized
1”

## Slide 12: First Coated Samples
2 square samples were coated
Coatings were characterized in various ways
One of the samples was anodized in NH4OH at 75V
Nb->blue Sn-> yellow Nb3Sn -> Pink/purple
Uniform coating! No excess tin on surface!
Anodized
Not anodized
1”

## Slide 13: SEM Images
Cornell, 2011
Wuppertal, 1996

## Slide 14: SEM Images
Cornell, 2011
Wuppertal, 1996

## Slide 15: EDX Analysis
Uniform coating!
24.2±0.5 atomic % Sn!
Tc vs %Sn
Hc2 vs %Sn

## Slide 16: EDX Analysis
Uniform coating!
24.2±0.5 atomic % Sn!
Tc vs %Sn
Hc2 vs %Sn
Increased lattice strain above
24.5 atm%Sn

## Slide 17: EDX Analysis
Uniform coating!
24.2±0.5 atomic % Sn!
Tc vs %Sn
Hc2 vs %Sn
Increased lattice strain above
24.5 atm%Sn

## Slide 18: XPS Analysis

## Slide 19: XPS Analysis

## Slide 20: 4-Wire Resistance Measurement
Tc
Notes: 2 checks

## Slide 21: 4-Wire Resistance Measurement
Tc
Notes: 2 checks

## Slide 22: 4-Wire Resistance Measurement
Tc
RRR
Notes: 2 checks

## Slide 23: 4-Wire Resistance Measurement
Tc
RRR
Notes: 2 checks

## Slide 24: RF Tests of Samples
Already fabricated Nb3Sn bottom plate for Pillbox TE cavity. Anodization, EDX, SEM show similar results. RF testing very soon!
See Yi Xie’s poster THPO050
With Nb3Sn coating
Before coating
Next step: Mushroom TE cavity. Designed to reach >200 mT on sample!
Notes: 4”

## Slide 25: Future Plans
Next few months
  RF tests of samples in TE cavities
2012
  Coat single cell 1.3 GHz cavity
  RF tests with full cavity T-map
Beyond
  At any locations with poor performance, cut cavity and perform surface analysis
  Use RF performance as feedback to guide improvement of coating process

## Slide 26: Acknowledgements and References
Special thanks to my advisor Matthias Liepe for his guidance and insight and to Hasan Padamsee for his knowledge and advice
A. Yamamoto’s “Advances in SRF Development for ILC,” this conference.
G. Müller et al. “Nb3Sn layers on high purity Nb cavities with very high quality factors and accelerating gradients,” EPAC 1996, Barcelona, Spain, pp. 208-2087, 1996.
H. Padamsee, J. Knobloch, and T. Hays, RF Superconductivity for Accelerators, Wiley & Sons, New York, ISBN 0-471-15432-6, 1998.
A. Godeke, “A review of the properties of Nb3Sn and their variation with A15 composition, morphology and strain state,” Supercond. Sci. Technol., 19, R68–R80, 2006.
A. Godeke, “Nb3Sn for Radio Frequency Cavities,” LBNL-62140, 2006.