## Slide 1: Muon Collider 6D Cooling Model Magnets
M. Tartaglia
Technical Division, Magnet Systems Dept.
Fermilab

## Slide 2
Topical Workshop on the Neutrino Factory and Muon Colliders
Colliding Ring/IR Magnets ~10 T, wide aperture/ open midplane
Wide aperture 20 T solenoids
HCC solenoid rings up to 20 T (one of many options-most challenging magnet-wise)
Very High Field Solenoids
Interesting Magnets in Muon Colliders
6-D Cooling Channel
Transverse Cooling up to 50 T

## Slide 3: Helical Cooling Channel
The helical solenoid (HS) concept (FNAL/Muons Inc.) :
    Coils follow the helical beam orbit generating solenoidal, helical dipole and helical quadrupole fields
    Multi-section HCC
  Would require 160 meters of magnets
  Wide range of fields, helical periods, apertures
    Room for RF system
  Field tuning is more complicated at high fields
    NbTi, Nb3Sn/Nb3Al and HTS in final stage (progression of models)
Early Specs, ca. 2006-K. Yonehara, S. Kahn, R. Johnson et al.

## Slide 4: HS Mechanical Concept (FNAL)
Hoop Lorentz forces intercepted by stainless steel rings around the coils
Transverse Lorentz forces intercepted by support flanges
Outer LHe vessel shell provides mechanical rigidity to the structure
The peak stress is ~60 MPa
Two short models built and tested successfully

## Slide 5: HSM01, HSM02 NbTi Model Magnet Design & Documentation
Design, Fabrication, Testing Primary Responsibility
  Program Oversight Mike Lamm
  Sasha Zlobin, John Tompkins
  Magnetic Design Vladimir Kashikhin
  Mechanical Design & Fabrication Sasha Makarov
  Nikolai Andreev, Miao Yu
  Testing & Analysis Mike Tartaglia
  Guram Chlachidze, MTF !
  Documents
    Tiweb.fnal.gov Magnet Description Documents
    TD-09-011 Test of Four Coil Helical Solenoid Magnet HSM01
    PAC’09 Four Coil Superconducting Helical Solenoid For
    MANX
    TD-11-012 HSM02 Magnet Fabrication and Test Summary
    MT-22 Model NbTi Helical Solenoid Fabrication and Test Results

## Slide 6: HSM01, HSM02 NbTi Model Magnet Design Features
4 coil prototype model magnets with large aperture
    1st Two models in planned series: Technology Demonstration
      HSM02 same design with improvements based on HSM01 experience
    Largest diameter that can be tested in VMTF R&D stand (OD ~ 25”)
  “Hard Way Bend” winding of NbTi cable (LHC quad – not optimized)
    Smooth transition without splices between 4 offset coils
    “keystoned” cable hard to wind with high packing factor
      HSM02 cable flattened, improved winding
    Embedded quench protection strip heaters
  Epoxy-impregnated coil package
    Stainless steel rings control hoop Lorentz stresses
      Sharp edges require care with insulation scheme
    but provide no pre-stress on coils to constrain conductor motion
      Next step in the progression will use Aluminum outer rings
  No Iron Flux Return
    Large stray field, forces on SC leads
      SC Lead motion in HSM01 led to some quenches, ground fault

## Slide 7: HSM01, HSM02 NbTi Model Magnet Design
HSM01 Dissection
After Testing

## Slide 8: HSM01, HSM02 NbTi Model Magnet Assembly

## Slide 9: HSM01, HSM02 NbTi Model Magnet Tests
Main Test Goals:
  Measure Mech. Stresses
  Quench Performance
    vs Temperature
    vs Ramp Rate
  Protection Heater Effic.
  Magnetic Field Map
HSM01 tested in Nov/Dec 2008
  TD-09-011, PAC’09
  Ground Insulation issues
  Epoxy voids, packing factor
  SC lead support
  Coordinate System
HSM02 tested in Nov/Dec 2010
  TD-11-012, MT-22
  2 thermal cycles
  (quench re-training)
  LN2 Conduction cooling study

## Slide 10: HSM01, HSM02 NbTi Model Mechanical Stress
Detailed HSM01 mechanical stress analysis made in TD-09-011
  FEM analysis of Cool down (.2-.3%); Lorentz Force <.007%) stresses
  Transverse (radial), Azimuthal, Longitudinal , compensating (T,B) gauges on coils
    Predicted Max On Coils: 13 MPa (T), 10.5 MPa (A), 34.5 MPa (L)
    Predicted Max On Links: 116 (T), 101 (A) , 306 (L)
    “Acceptable” for 304 S.S., “designed far beyond required even for Nb3Sn”
  Hard to measure with any confidence
    Imperfect compensation, gauge calibrations? Debonding from surface
    measured stresses were < or ~ consistent with calculated
    HSM02 has same mechanics
  Instrumented with fewer gauges (4 Azimuthal + 1 comp.)
  Cool down stress analysis not completed –
    inconsistent gauge data (warm/cold) suggests debonding
    Lorentz force stresses were <~0.008%

## Slide 11: HSM01, HSM02 Test Results Quench Studies
Quench Protection
  MIITS calculation (local heat balance), Peak Temperature Rise
    LHC Outer cable (30 0.8mm strand NbTi) max. 11 MIITS; data ~3-4
    Conductor RRR – Copper stabilizer resistance (higher RRR is better)
    HSM01 ~140-155 (same as LQXB) HSM02 ~102 (rather low; why?)
  Magnet Description Document
    Low Inductance ~200 mW, Estored(16kA)~26 kJ
    Dump Resistor energy extraction
      (t~L/Rbus+mag, Vmax=IRdump)
    Rd HSM01 = 10 mW, HSM02 = 60 mW
  Protection Strip Heaters
    Study of inducing quenches (for long magnets)

## Slide 12: HSM01, HSM02 Test Results Quench Performance
Quench Prediction: at 4.5 K, HSM01~16 kA, HSM02 ~ 15 kA
  Magnet Load Line crosses Conductor Critical Current (vs T)
  Peak field is slightly higher on end coils
Somewhat slow quench training to plateau
HSM01 (HSM02) reached 85% (100%) of Ic
Very similar training curves - slightly erratic
  (char. of epoxy-impregnated coils)
Little temperature dependence of training rate (higher Ic, mechanical limitations)
Quenches mostly in end coils for both

## Slide 13: HSM01, HSM02 Test Results Quench Performance
Quench Locations
  Generally only know which coil quenched (one voltage segment across each coil)
    There has been no detailed analysis of quench velocity
  HSM02: Two quenches developed ~ simultaneously in adjacent coils
  presumably originating in transition region between coils

## Slide 14: HSM01, HSM02 Test Results Quench Performance
Quench Prediction: at 4.5 K, HSM01~16 kA, HSM02 ~ 15 kA
  Design would allow at least 15 % current operating margin
Plateau is “remembered” at 4.5 K after reaching highest current at 3.0 K
Fast Re-training of HSM02 after 300K T-cycle
Virtually no ramp rate dependence (both magnets) to quite high ramp rates (600 A/s) … as expected
Quenches 46-51 Dip at 3K:
Allowed 30 minutes recovery between quenches
Quench 52: waited 1 hour

## Slide 15: HSM01, HSM02 Test Results Quench Heater Performance
Quench Protection Heaters
  HSM01 had S.S. strip heaters on Outer Layer of each Coil
    Three were full length, one 6-inch “spot” heater
    Time did not allow exploration of heater parameters
      only one quench induced, at low heater voltage
      HSM02 S.S. strip heaters on mandrel prior to winding of each Coil
        All in parallel, with 4W external resistor ; fixed HFU capacitance
          (to increase range of parameters given heater voltage limits)
          Mapped out Time (heater fired to quench detected) vs {I, Vhfu}
          Still needed: calculate heater power density

## Slide 16: HSM01, HSM02 Test Results Quench Heater Performance
Conduction Cooling Study
  We do not have the facilities to test indirectly cooled magnets
    Need vacuum vessel for insulation
      VMTF is not a good vac. Vessel
    No helium supply to cooling tubes
    Helium vapor-cooled leads for power testing
    We tried a simple thermal test
    Pump out VMTF helium space; we achieved <0.1 Torr
    Connect LN2 to cooling tubing
    Measure T vs time on all four coils with 1 RTD/coil +top, bottom
      Not so great: RTD calibrations are sparse at high T (300, 80K)
      No one has had time to model expectations, compare with data

## Slide 17: HSM01, HSM02 Test Results Quench Heater Performance
Conduction Cooling Study
  We learned one very important Lesson
    Copper tubing wrapped around each coil
    Makes a beautiful 10:1 transformer!
    This is not the right way to design the cooling tube layout

## Slide 18: HSM01, HSM02 Test Results Magnetic Field
Magnetic Field Maps: 3D Hall probe scans, vs 3D model prediction
What are the tolerances
On “field quality”
On ring positions ?
These will be measured
Carefully in HSM02
(better attention to alignment/survey features,
Coordinate systems)

## Slide 19: HSM01, HSM02 Test Results Magnetic Field
Magnetic Field Maps: 3D Hall probe scans
  HSM01 ±10A at 300 K, 2 kA at 4.5 K (in 1.75” warm bore tube)
  HSM02 5 kA at 4.5 K (warm planned)
There is no central axis (offset rings)
  Mechanical center is well defined
  Fiducial marks allow probe positioning
  Make comparison to 3D Model
Cold measurements along a central line
no surprises – Bz/I agrees with warm
Warm measuments
  central line along Z (solenoid dir.)
  Along Z at {R=4cm, q}
Off-axis:
Relating {magnet, probe, model} Coordinate Systems needs a bit more attention (done in HSM02)

## Slide 20: HSM01, HSM02 Test Results Magnetic Field
HSM01

## Slide 21: HSM01, HSM02 Test Results Magnetic Field
HSM02: Still setting up to do warm measurements at ±10A
  Conventional Test Stand B tied up with Accelerator Support projects
  New system development, new 3D Senis Hall probe (vs 3 1D probes)
  Minor complication: steel table (mounted high on Al beam)

## Slide 22: HSM Next Steps Other models in progress, planned
HSM03 – same design but with Aluminum rings for coil pre-stress
HSM04 – Nb3Sn design
  Needed for inserts in higher field cooling regions
  Very different technology (small part of larger High Field magnet program)
Helical solenoids using HTS (BSSCO wire or YBCO tape) conductor
  Also needed for inserts in higher field regions
  New, very different technology –
    collaboration with Muons, Inc. to design, build, test first model
    First YBCO model has been built and tested –
        results for another talk !