## Slide 1: Material characterization for thermal modeling of Nb3Sn Superconducting Magnets by Andrew Davies
the most likely cause of death for a superconducting magnet
Find the temperature margin before the magnet quenches.
Provide a compiled data set for future modeling
Transient heat flow remains un-modeled.

## Slide 2: Electrical description of thermal systems
For one-dimensional heat flow
Transmission line equation
No direct comparison for inductance and the volume element cannot cool itself, L′=0 and G′=0
Kirchhoff “Two different forms of energy behave identically when the differential equations which describe them have the same form and the initial and boundary conditions are identical”

## Slide 4: Network Model

## Slide 6: Material data collection and compilation
Temperature range of 1.0K to 300.0K
The compiled dataset will be used as input to the Network model for Nb3Sn Superconducting Magnets.
Assess the impact of material properties on thermal properties of magnets.
Heat conductivity and Heat capacity.
  Young modulus, density, coefficient of thermal expansion
Assess the impact of magnetic fields on thermal properties. (NbTi, Nb3Sn)

## Slide 7: Material Used in Magnets
Materials
  Polyimide (Kapton)
  G10
    Epoxy CTD-101K
    Ceramic binder CTD-1002X
    Glass fibers S-2 Glass
  NbTi
  Nb3Sn
  Stainless steel 304
  Stainless steel 316LN
  Titanium
  Niobium
  Tin
  Bronze
    Copper

## Slide 10: Material Characterization
The objective was to provide a reliable equations for all materials across the full cryogenic temperature range.
Reference [24] White Tin: Tabulated data from [24] was fitted to the following equations.
Valid for 25<T<300K R2=.999696
Where x= log10(T)

## Slide 11
Chart: Nb3Sn specific heat capacity
| 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Nb3Sn Normal H = 0 T [16] Equation: | 2.1006 | 2.608 | 3.1957 | 3.869 | 4.6319 | 5.4877 | 6.4385 | 7.4855 | 8.6285 | 9.8663
Nb3Sn Normal H = 0 T [16] Equation: | 0.11072 | 0.22145 | 0.3322 | 0.44298 | 0.55379 | 0.66466 | 0.77558 | 0.88656 | 0.99762 | 1.1088 | 1.22 | 1.3313
Nb3Sn [17], Normal Equation: | 0.101 | 0.208 | 0.327 | 0.464 | 0.625 | 0.816 | 1.043 | 1.312 | 1.629 | 2 | 2.431 | 2.928 | 3.497 | 4.144 | 4.875 | 5.696 | 6.613 | 7.632 | 8.759 | 10
[17], Super B = 11T equation | 0.064416 | 0.24594 | 0.66169 | 1.4288 | 2.6643 | 4.4854 | 7.0091 | 10.3527 | 14.6331 | 19.9675 | 26.473 | 34.2668 | 43.4659 | 54.1874 | 66.5485 | 80.6662 | 96.6577 | 114.6402
[17] super B = 2 T equation | 0.027682 | 0.17247 | 0.55149 | 1.2818 | 2.4806 | 4.265 | 6.752 | 10.0588 | 14.3025 | 19.6002 | 26.0689 | 33.826 | 42.9883 | 53.6731 | 65.9974 | 80.0785 | 96.0333 | 113.9789
Nb3Sn [17] T<Tcs Equation CSuper (J/(kg*K) | 1.0432 | 8.3453 | 28.1655 | 66.7627 | 130.3959 | 225.3241 | 357.8063
Nb3Sn[17] Tcs<T<Tc Equation CpTransitionSuper | 357.8063 | 267.2923 | 0.61135
Nb3Sn [17] T>Tc Equation Cnormal | 0.61135 | 0.75475 | 0.91325 | 1.0868 | 1.2755 | 1.4793 | 1.6982 | 1.9322 | 2.1812 | 2.4454 | 2.7246 | 3.019
Nb3Sn Super [27] Equation: | 0.1872 | 0.3996 | 0.6624 | 1.0008 | 1.44 | 2.0052 | 2.7216 | 3.6144 | 4.7088 | 6.03 | 7.6032 | 9.4536 | 11.6064 | 14.0868 | 16.92 | 20.1312 | 23.7456 | 27.7884 | 32.2848 | 37.26 | 42.7392 | 48.7476 | 55.3104 | 62.4528 | 70.2 | 78.5772 | 87.6096 | 97.3224 | 107.7408 | 118.89
Nb3Sn[39] | 1.23 | 2.01 | 2.99 | 4.23 | 8.96 | 17.1 | 28 | 45
Nb3Sn Super H=0 T [16] Superconducting state | 0.072214 | 0.12254 | 0.19299 | 0.28961 | 0.42272 | 0.59382 | 0.81021 | 1.0694 | 1.3738 | 1.7336 | 2.1564 | 2.6445 | 3.1704
Nb3Sn Normal H=0 T [16] Normal state | 0.52085 | 0.6542 | 0.79763 | 0.96873 | 1.1574 | 1.3789 | 1.6229 | 1.8871 | 2.1689 | 2.4658 | 2.793 | 3.1427 | 5.206 | 7.7196 | 10.5981 | 13.7307 | 16.9389 | 20.0237 | 22.9022 | 25.7102 | 28.6189 | 30.9087

## Slide 12: Second order transition in magnetic field

## Slide 13
Chart: G10 Specific Heat Capacity
| 4 | 10 | 20 | 30 | 50 | 77 | 100 | 150 | 200 | 300
[43] G-10CR | 2 | 15.4 | 47 | 81 | 149 | 239 | 317 | 489 | 664 | 999
[39] G-10 | 0.35 | 2 | 4 | 6.89 | 20 | 40.55 | 65 | 89.6 | 131.3 | 189.5 | 281.75 | 386.5 | 456 | 576.3 | 704.3 | 846 | 1022.8 | 1400
[22] G10 | 0.17 | 2.1614 | 2039.2677
[19] Glass Fiber Reinforced Polyester | 300 | 400 | 500 | 1000 | 1500
[43] Glass/resin (s 901Glass/NASA resin 2) | 0.64 | 6.7 | 28 | 50 | 94 | 169 | 262 | 560 | 960 | 1940
[24] SPECIFIC HEAT of VITREOUS SILICA(Silica Class, Quartz Class.) | 4.5 | 12.6 | 24.4 | 37.9 | 51.9 | 80.8 | 111 | 141 | 172 | 204 | 236 | 268 | 331 | 391 | 446 | 497 | 544 | 588 | 629 | 668 | 704 | 738
[43] Epoxy (stycast 2850FT) | 0.5 | 6.3 | 22.6 | 42 | 83 | 154 | 240
[43] Epoxy (CY221) | 22 | 85 | 170 | 270 | 400 | 480 | 1000 | 1300

## Slide 14: End

## Slide 15: Results
Evaluate final results
Propose possible future steps of analysis
Present effects of the input parameters

## Slide 20
Case study: LHC dipole protection
It's difficult! - the main challenges are:
1) Series connection of many magnets
In each octant, 154 dipoles are connected in series. If one magnet quenches, the combined inductance of the others will try to maintain the current. Result is that the stored energy of all 154 magnets will be fed into the magnet which has quenched  vaporization of that magnet!.
Solution 1: put cold diodes across the terminals of each magnet. In normal operation, the diodes do not conduct - so that the magnets all track accurately. At quench, the diodes of the quenched magnet conduct so that the octant current by-passes that magnet.
Solution 2: open a circuit breaker onto a dump resistor (several tonnes) so that the current in the octant is reduced to zero in ~ 100 secs.
2) High current density, high stored energy and long length
As a result of these factors, the individual magnets are not self protecting. If they were to quench alone or with the by-pass diode, they would still burn out.
Solution 3: Quench heaters on top and bottom halves of every magnet.