## Slide 1: Traveling wave SRF for ILC Energy Upgrade
Hasan Padamsee
Cornell University and Fermilab
With Valery Shemelin (Cornell) and Slava Yakovlev (Fermilab)

## Slide 2: Steady Progress In Single and Multi-cell Cavity Gradients Over 4 Decades

## Slide 3: Present Limits of SRF
The Standing Wave (SW) TESLA Niobium-based structure is limited to a gradient of about 50 MV/m by the critical RF magnetic field (200 – 210 mT).
Advanced shape cavities will be limited by the critical RF magnetic field to about 60 MV/m
  Re-entrant, Low-Loss, Ichiro, Low Surface Field
  Here we lower Hpk/Eacc (10-20%) but raise Epk/Eacc (15-20%)
How to break through this gradient barrier with Niobium?
Explore the option of Niobium Traveling Wave (TW) structures

## Slide 4: Animations of TW and SW
Red standing wave – High Peak Fields
Green (acceleration) and Blue (Return) Waves are Travelling Waves - Lower peak fields
Guide blue wave in a return wave-guide to avoid SW peak fields – attached to both ends

## Slide 6: Advantages of TW Structures
Travelling wave (green) structures lower BOTH Hpk/Eacc and Epk/Eacc
  Because RF power returns (blue) not through the accelerating structure (to form a standing wave (red) with harmful peaks)
  But power returns through a separate return Nb waveguide
+ Travelling wave structures offer 2X higher R/Q
  lowers Cryo power and RF power and lower AC power
By choosing the Low-Loss cell shape + reduced aperture (see below) it is possible to lower Hpk/Eacc by 48% over the TESLA structure!
Opening the door to Eacc > 70 MV/m !!
  Hpk = 200 mT, Epk = 120 MV/m
Lower aperture is allowed because bunch charge for 3 TeV will about 3 X less to get acceptable IP background…
Putting SRF on the Road to ILC – 3 TeV with Niobium
  With Capital cost comparable to CLIC 3 TeV and AC power much less than CLIC 3 TeV
Without struggling with exotic new superconductors (sorry!)

## Slide 7: Many Challenges for TW - 1
Requires twice the number of cells per meter to provide the proper phase advance (about 105 degrees)
Cavity fabrication and surface processing procedures and fixtures must deal with (roughly) double the number of cells per structure.
SW TESLA
TW

## Slide 8
A feedback waveguide for redirecting high power from the end of the structure back to the front end of accelerating structure
The feedback requires careful tuning to compensate reflections along the TW ring to obtain a pure traveling wave
Multipacting has been studied - will not be a problem
HOM propagation and HOM damping study started - encouraging
Challenges for TW - 2
3-cell unit prepared at Fermilab by Euclid Corp
– not yet tested

## Slide 9: A Start for Travelling Wave Structures
1-cell prepared by Euclid Corp with Fermilab
Reached 26 MV/m with inferior (easier) treatment of BCP.
Should do better with EP/baking

## Slide 10: Parameters for IlC 3 TeV Explored (Detail Parameters available) Compare to ILC 1 TeV & to CLIC 3 TeV
 |  | ILC1 TeV From TDR | ILC3 TeV From 1 TeV | CLIC 3 TeV
Energy | TeV | 1 | 3.0 | 3.0
Luminosity | X1034 | 4.9 | 6.1 | 5.9
AC Power | MW | 300 | 453 | 590
Cap Cost | BILCU | 13.3 | + 11.5 (24.8 Total) | 24.2 total BCHF
Gradient | MV/m | 45 | 70 | 72/100
Q of new linac | 1010 | 2 | 2 | 5700

## Slide 11
Thank You
Questions?