## Slide 1: Challenges and opportunities of SRF theory for particle accelerators
Alex Gurevich1 and Jim Sauls2
1Old Dominion University, Norfolk VA
2Northwestern University, Evanston, IL
1Supported by DOE under grant DE-SC0010087-020

## Slide 2: Have the best Nb cavities reached theoretical limits?
Can the fundamental limits of Q and H be
increased by materials treatments?
?
?
Are there the fundamental limits of Q(H)
and the breakdown field?
Q(H) and Eacc of Nb cavities have been steadily improving
How close are breakdown fields to the current pairbreaking instability of the Meissner state?
Theoretical limits of H and Q at T << Tc and
GHz frequencies are largely unknown.

## Slide 3: Theoretical challenges
Field limit
The widely used GL theory of dc superheating field Hs(T) is applicable near Tc but not at T << Tc.
Only Hs(0) = 0.84Hc at was calculated (Galaiko 1966, Catelani and Sethna, 2008; Lin and Gurevich, 2012).
at T << Tc and arbitrary GL parameter has not yet been calculated.
Dynamic superheating field Hd(T,f). How different can it be from the static Hs(T) at GHz frequencies?
Recent result: (Sheikhzada and Gurevich, 2020)
Q limit
BCS surface resistance Rs(T) vanishes at T=0. How far can the residual resistance be decreased?
Trapped vortices, subgap quasiparticles and two-level states, proximity-coupled suboxide layers.
Nonequilibrium superconductivity
Nonlinear BCS surface resistance in a nonequilibrium SC under strong rf current. Negative Q(H) slope.
Extreme dynamics and nonlinear losses of trapped vortices driven by strong rf current
Tuning SRF performance by surface nanostructuring
Increase of Hs and vortex penetration field by SIS multilayers and impurity gradients at the surface
Reduction of Rs by optimizing proximity-coupled layers and transparency of grain boundaries

## Slide 4: DC superheating field near Tc
Meissner state becomes unstable at H > Hs as the Cooper pairs reach the critical
pairbreaking velocity and the RF current density Js = H/ at the surface
approaches the depairing current density Jd = Hs/
At T << Tc, only Hs(0) = 0.84Hc at κ >> 1 has been
calculated in the clean limit (Galaiko 1966, Catelani and Sethna, PRB 2008)
and for arbitrary impurity concentration (Lin and Gurevich, PRB 2012)

GL region, T ≈ Tc: (Matricon and Saint-James, 1967, Chapman 1995)
Bs decreases as the GL parameter κ = λ/ξ increases
No microscopic theory of Hs(T) at low T and
Nb
Microscopic theory gives 13% larger Hs(0) than the GL extrapolation

## Slide 5: Surface nanostructuring to increase Bs
Kubo et al, APL, 104, 032603 (2014); SUST, 30, 023001 (2017);
Posen, Transtrum, Catelani, Liepe, Sethna, Phys. Rev. Appl. 4, 044019 (2015); Gurevich, AIP Adv. 5, 017112 (2015)
Nb
dielectric layers
higher-TcSC: Nb3Sn, …
SIS multilayers Gurevich, APL. 88, 012511 (2006)
Smooth increase of the impurity scattering rate in a dirty
surface layer of thickness
Ngampruetikorn and Sauls, Phys Rev Research. 1, 012015 (2019)
Calculations of Hs(T) at low T and large GL parameter
based on the microscopic Eilenberger equations
Calculation of Hs for a
nanostructured surface
as functions of ,
and the impurity m.f.p.
is needed
20-40% increase of Hs
Hm at the optimum thickness exceeds Hs of both Nb and the layer material. mT (dirty Nb layer), mT (Nb3Sn)

## Slide 6: Nonequilibrium SRF
Mattis-Bardeen cannot describe the field-dependent Rs(H) high RF fields
Numerical simulations of time-dependent equations of nonequilibrium BCS
Kinetic equations for quasiparticles and dynamic equations for SC condensate
Time-dependent GL equations for a gapped dirty superconductor
Relaxation time constant of quasiparticles on phonons can be much larger
than the RF period at 1-2 GHz frequencies of SRF cavities,
Sheikhzada and Gurevich, PRB 102, 104507 (2020)
Kramer and Watts-Tobin, PRL, 40. 1041 (1978)
Watts-Tobin, Krahenbuhl and Kramer, JLTP 42, 459 (1980)
Relaxation time of SC condensate:
Relaxation time of quasiparticles due to
inelastic electron-phonon collisions:
For Nb at 7K: ,
Nearly instantaneous reaction of the SC condensate to the RF field
Much slower relaxation of quasiparticles. Quasiparticle relaxation slows down greatly as T decreases

## Slide 7: Dynamic breakdown of superconductivity
SC breakdown above Hd (T,f) which increases with f up to the limit:
SC pairbreaking caused by the time
averaged squared RF field

## Slide 8
Dynamic superheating field
High temperatures: enhancement of Hd due to slow qp relaxation:
Lin and Gurevich, PRB 85, 054513 (2012)
Low temperatures: T < 0.5Tc: the relaxation time increases greatly but the density of quasiparticles decreases exponentially in the dirty limit.
No effect of quasiparticles on SC breakdown if
In the clean limit the quasiparticle gap vanishes at H < Hs,
so the dynamic superheating field may be enhanced by slow relaxation of
quasiparticles
Sheikhzada and Gurevich, PRB 102, 104507 (2020)

## Slide 9: Trapped vortex driven by RF Meissner current
Typical depinning Jc = 10-100 kA/cm2 in Nb are some 4 orders of magnitude lower than Jd = Hc/λ, = 500 MA/cm2
Pinning is too weak to stop the vortex tip above H > 0.01Hc = 2 mT
2
λ
l
H(t)





























λ
A trapped elastic vortex is driven by the Lorentz force balanced by viscous drag and bending stress At Ha = 100-200 mT, J(0) at the surface approaches the depairing limit
:
At H = Hc, the superflow velocity of Cooper pairs reaches the critical pairbreaking value vc = /pF and the velocity of the vortex tip is
This yields v = 10 km/s, which exceeds the speed of sound (2-4 km/s) and vc = /pF = 1 km/s. Vortex velocities 10-20 km/s were observed by SQUID scanning microscopy Embon et al, Nature Comm. 8, 85 (2017)
How can a supersonic vortex tip remain connected to a subsonic elastic vortex line in the bulk?
The vortex tip can move faster than the superfluid velocity of rf current

## Slide 10: What happens to the vortex core at high velocities?
Slow vortex
Fast vortex
v
v
A nearly round vortex core
Cloud of dissipative quasiparticles is
locked onto the moving core
Bardeen-Stephen vortex drag
Velocity-dependent Larkin-Ovchinnikov vortex drag:
TDGL simulations show that the fast vortex core stretches along v
A cloud of nonequilibrium quasiparticles lagging behind the moving core
Decrease of the vortex drag with v causes a jumpwise LO instability as
the local force balance breaks down at

## Slide 11: Manifestations of the LO effects in SRF cavities
What happens to the vortex if its fast tip is LO-unstable while the rest of the vortex is LO-stable?
The effect of LO vortex drag velocity dependence on the field dependence of nonlinear RF losses of trapped vortices
Since the LO critical velocity km/s is 1-2 orders of magnitude smaller than velocities of a vortex tip
at H = 10 -100 mT, the LO velocity dependence of the vortex drag can be essential in SRF cavities.
H(t)
u(z,t)
LO
unstable
LO
stable
experiment
on Nb films
low-T
extrapolation
Leo at al., PRB 84, 014536 (2011)

## Slide 12: Nonlinear dynamics of a trapped vortex in a random pinning potential
Numerical simulation of nonlinear dynamics of a curvilinear elastic vortex driven by strong RF current in a film
Mesoscopic effects in RF response for different pinning configurations
LO instability in the presence of random pinning
Effect of overheating
Pathirana and Gurevich, PRB 101, 064504 (2020)
and unpublished
f0 = 22 GHz for a moderately clean Nb.

## Slide 13: LO mechanism of the low-field Q(H) rise
The surface resistance Ri(H) starts decreasing with the field amplitude as the frequency increases. Calculated for different values of
Fit to the experimental data of for a 1.47 GHz Nb cavity
Ciovati, JAP 96, 1591 (2004)

## Slide 14: Tuning the negative Q slope by impurities
Making the surface dirtier shifts the anomalous drop of the vortex surface resistance Ri(H) to lower fields.
May pertain to the low-field Q(H) drop observed on many Nb cavities
Calculated for

## Slide 15: Residual surface resistance of trapped vortices
Larkin-Ovchinnikov with random pinning
Bardeen-Stephen
Averaging over statistical realizations of the
pinning potential often (but not always) yields
a linear low-field dependence of Rs(H).
0.5-3 GHz
10-30 GHz
0.5-3 GHz
Quasi-static collective pinning:
Liarte et al. Phys. Rev. Appl. 10, 054057 (2018)
1d pinning simulations:
Checchin and Grassellino, Phys. Rev. Appl. 14, 044018 (2020)
LO critical velocities: v0 = 20-100 m/s in the frequency-dependent parameter
Pathirana and Gurevich,
(2020 unpublished)
Pathirana and Gurevich,(2020 unpublished)
v0(T) at low temperatures T << Tc has not been measured, but
it is expected to be much smaller than at 0.5Tc < T < Tc

## Slide 16: Vortex overheating effects
Bardeen-Stephen
1-2 GHz
h = Ri /R0 is proportional to the trapped flux
Quasi-linear dependence caused by heating
High-field upturn of Rs(H)
Larkin-Ovchinnikov
Heating mitigates the negative Q slope
Pathirana and Gurevich (2021 unpublished)

## Slide 17
Current-induced broadening of DOS peaks causes a negative Q(H) slope
Subgap states caused by finite quasiparticle lifetimes.
Surface layer of reduced BCS pairing constant (surface nonstoichiometry)
Proximity coupled thin normal (suboxide) layer on the surface
Small density of magnetic impurities
S
N
magnetic
impurities
Gurevich, PRL 113, 087001 (2014)
Gurevich and Kubo, PRB 96, 184515 (2017)
Kubo and Gurevich, PRB 100, 064522 (2019)
Calculatioins of Rs in the dirty limit
based on the Usadel equations
Optimizing surface resistance by pairbreaking mechanisms
Current-induced DOS broadening
DOS oscillating under RF currents
Reducing Rs by engineering an optimum DOS by surface nanostructuring and impurity management
Surface resistance can be reduced by RF current, surface nanostructuruing and magnetic impurities

## Slide 18
N thickness
barrier between N&S
is an interface resistance
very sensitive to heat treatment
is an N layer thickness
(e.g., thickness of suboxide on the Nb surface)
proximity effect coupling
Field-dependent surface resistance Rs(H0)
different N-layer thickness
No normal layer →

## Slide 19
Tuning Rs by magnetic impurities
is spin flip m.f.p
magnetic
impurities
An optimum density of magnetic impurities can significantly reduce Rs
corresponds to the spin flip m.f.p.
4μm

## Slide 20
Rs can be optimized by tuning the N-layer parameters.
Rs can be smaller than the ideal surface without N layer
Tuning Rs by a proximity-coupled N layer
The resistive barrier between
N&S can be changed significantly by
materials treatments
DOS with subgap states