## Slide 1: Nb3Sn Superconducting Radiofrequency Cavities
Presenter: Ryan Porter1
Authors: S. Posen2, M. Liepe1, G. Eremeev2, U. Pudasaini3, C.E. Reece3
1Cornell University
2Fermi National Accelerator Laboratory
3Thomas Jefferson National Accelerator Facility
SNOWMASS Letter of Interest: SNOWMASS21-AF7_AF0_Posen-086
https://www.snowmass21.org/docs/files/summaries/AF/SNOWMASS21-AF7_AF0_Posen-086.pdf
Notes: How to introduce myself. Feels like I need a grander entry, better at selling. Less introducing us, more salesman

## Slide 2: SRF Introduction
Superconducting niobium RF cavities
  Used to accelerate beams in modern accelerators
  Low losses/high energy efficiency key to modern accelerators
Gold standard for modern HEP accelerators
  LBNF/DUNE, LHC, KEKB, etc.
  Many past machines: LEP, HERA, etc
1m
Key technology for future HEP projects
  ILC, FCC-ee, CepC, HL-LHC, PIP-II,
Used in other major DOE projects:
  LCLS II, Electron-Ion Collider (EIC)
LHC
PIP-II
ILC

## Slide 3: Key Figures of Merit
Accelerating Gradient
Higher Eacc
Higher energy gain
Shorter accelerators
Higher energy reached
Quality Factor
$$$
$
2K
4K
Higher Operating Temperature
More efficient
Lower cost
Operating Temperature
Higher Q
More efficient
Higher duty-cycle
Higher luminosity

## Slide 4: Niobium Cavities Reaching Fundamental Limits
D. Bafia et al. “Gradients of 50 MV/m in TESLA Shaped Cavities via Modified Low Temperature Bake, in proc. of 19th Int. Conf. on RF Superconductivity (SRF2019), Dresden Germany, July 2019
Eacc limit ≈ 50 - 55 MV/m
Q limit = ????
Unknown
Limited to 2 K
operation
Need better materials for future HEP accelerators
Notes: Replace with figure with overlapped AES022 + N-infused/doped cavity with higher Q but lower Eacc

## Slide 5: Best Material for Next-Gen SRF: Nb3Sn
Blue: tin
Red: niobium
Higher critical temperature
→ Operation at 4.2 K
→ More efficient
Higher superheating field
→ Double the limit of niobium
2 μm
1 μm
≈3 μm
RF Surface
1 μm
Nb
Nb3Sn

## Slide 6: Potential of Nb3Sn Cavities
 | Niobium | Nb3Sn
Superheating field | 240 mT | 420 mT
Max. Eacc (theoretical limit) | 55 MV/m | 100 MV/m
Increased Accelerating Field
Higher energy reached
Shorter accelerators
 | Niobium | Nb3Sn
Critical Temperature Tc | 9 K | 18 K
Q0 at 4.2 K | 6 x 108 | 4 x 1010
Q0 at 2.0 K | 4 x 1010 | >1011
Q0 given for 1.3 GHz ILC-shape cavities
Lower Cooling Cost and Complexity
$$$
$
2K
4K
Lower cost
Higher Luminosity
  Longer pulse lengths/bunch train length
  And/or higher rep. rate

## Slide 7: The Rebirth of Nb3Sn SRF R&D
Siemens AG,
K.F Karlsruhe
(Cornell)
U. of Wuppertal
RF testing at JLAB, Cornell, SLAC, CERN…
Nb3Sn Papers at SRF Conference
Cornell
JLAB
FNAL
CERN
PKU, IMP, KEK…
INFN
Early Attempts—Poor Performance
DOE funds small R&D projects
Produces first good results
Notes: 46 contributions at Nb3Sn Workshop

## Slide 8: Current Nb3Sn Cavity Performance
Gradients up to 24 MV/m: exceeds typical operating gradient of current CW machines
4 K operation with unprecedented Q >1010 in CW operation achieved at all 3 labs
4.2 K
G. Ciovati, I. Parajuli, U. Pudasaini
4 K
4.2 K

## Slide 9: Moving to 4.2 K
At 2.0 K, it takes 800 W to remove 1 W of heat
At 4.2 K, you
need 250 W
Operating at 4.2 K
~1/3 power losses for same Q

## Slide 10: Cryo-Efficiency
‘State of the art’ Nb at 2 K
Nb3Sn at 4.2 K
1.3 GHz
More efficient at ILC spec
Q = 4·1010
Q = 4·1010
Niobium Limit
Q = 2·1010
1.5 - 3 x efficient than niobium!
Simpler, cheaper cryogenics at 4.2 K
Notes: Update to include N-infused/mid-T bake type results

## Slide 11: Cryocooled SRF Cavities
No liquid helium
Small, turn-key, affordable
Enables small scale SRF accelerators
  Compact light sources, polymer cross-linking, waste processing, etc
R.C. Dhuley et al, ﻿Supercond. Sci. Technol. 33 06LT01 (2020)
N. Stilin et al, ﻿arXiv:2002.11755v1 (2020)
G. Ciovati et al, Supercond. Sci. Technol. 33 07LT01 (2020)
4K
2K
Turn Key Cooling
High efficiency enables cryocooler operation:

## Slide 12: Increasing Efficiency
0 nΩ
16 nΩ
Not fundamental
Fundamental (BCS) Resistance
Surface resistance at 4.2 K and 10 MV/m (Cornell single-cell)
Q = 2·1010
4·1010+
Can be removed
Further R&D

## Slide 13: Research Highlight I: Quality factor
‘2-Gap’ BCS Analysis:
Sn-Segregation in Grain Boundaries + Vortex Entry:
Material Growth Studies:
Sn Nano Residue:
Coating with different nucleation profiles:
J. Carlson et al, ﻿Phys Rev B 103 024516 (2021)
U. Pudasaini, ﻿” Nb3Sn growth in vapor diffusion: process design for large surface area coatings,” presented at Nb3SnSRF’20, Nov 2020
R.D. Porter et. al., “High Frequency Nb3Sn Cavities,” in proc. of SRF2019, Germany, 2019
U. Pudasaini, ﻿” Nb3Sn growth in vapor diffusion: process design for large surface area coatings,” presented at Nb3SnSRF’20, Nov 2020
R. D. Porter, ﻿” Growth Studies and Optimization of Nb3Sn Coatings,” presented at Nb3SnSRF’20, Nov 2020
Notes: W

## Slide 14: Increasing Eacc
Can reach 24 MV/m Eacc
  Meets spec for many machines!
  Could read 100 MV/m
Before 2013
~ 5 MV/m
2013
15 MV/m
2015
18 MV/m
2030
50 MV/m ???
2020
24 MV/m
Future
100 MV/m
Current
24 MV/m
Steady advancement over last 10 years:
Notes: CBMM-D reaches higher fields after processing, but with a lower Q. I’m not sure whether to list 21 MV/m or 24 MV/m as the usable gradient.

## Slide 15: Research Highlights II: Cavity Quench
Time Resolved Quench Thermometry
Surface Roughness Reduction:
Vortex Nucleation at Grain Boundaries:
Material Growth Optimization and New Processes:
A. R. Pack, M. Transtrum (BYU), SRF2019, MOP017
R. D. Porter, ﻿” Surface Resistance, Frequency Dependence, and Field Limitation in Nb3Sn Cavities,” presented at Nb3SnSRF’20, Nov 2020
Time dependent Ginzburg-Landau Simulation of Vortex Nucleation
Vapor Deposition
Sputtering
Electrodeposition
S. Posen et. al., arXiv:2008.00599 ﻿, Aug 2020
Md. N. Sayeed, Nb3SnSRF’20, Nov 2020
Z. Sun, Nb3SnSRF’20, Nov 2020

## Slide 16: Collaborations
Have built many collaborations
Unlocked skills + tools + knowledge outside our community
  Condensed matter theorists, material scientists, microscopists, chemists, and more
Provides critical expertise needed to succeed

## Slide 17
Single-cell to Multi-cell Cavities
Used for
material
R&D
Usable in real accelerators
Single-cell
Multi-cell

## Slide 18: Multi-cell Coating Nb3Sn Cavities
“Siemens” configuration, i.e., no secondary heater for the tin source
“Wuppertal” configuration, i.e., with secondary heater for the tin source
Soon to be completed!
“Wuppertal” configuration, i.e., with secondary heater for the tin source

## Slide 19: Multi-cell Nb3Sn Cavities for Accelerator Applications
JLAB: 5-cell 1.5 GHz
FNAL: 9-cell 1.3 GHz
Nb3Sn accelerator multi-cell cavities reaching useful gradients as high as 15 MV/m with high Q at 4.4 K!

## Slide 20: Outlook
Higher Energy
  ~2 x higher potential maximum gradients
  Nb3Sn + Traveling Wave + Improved cell shape → Eacc > 140 MV/m (?)
Can be removed
Fundamental
2030
50 MV/m ???
Before 2013
< 5 MV/m
2013
15 MV/m
2015
18 MV/m
2020
24 MV/m
0 nΩ
16 nΩ
Higher Luminosity
  Lower cryogenics loses
  Lower cost
  Longer pulse lengths/bunch train length
  And/or higher rep. rate
Q = 2·1010
4·1010
Accelerating Gradient Improvements
Efficiency Improvements

## Slide 21: Conclusions
SRF key technology for current and future HEP accelerators
Niobium is great, but reaching fundamental limits
Nb3Sn ‘game-changing’ material for SRF and HEP projects
  Meets spec for some current machines
Technology almost ready for real accelerators
  Promising early multicell-cavity results
Snowmass community should strongly endorse continued investment into Nb3Sn SRF cavity R&D