## Slide 1: The ATLAS Material Irradiation Station (amis)
Irradiation Stations and Alternatives
Workshop at FermiLab (virtually)
JUne 17-18, 2021
erhtjhtyhy
Jerry Nolen
Physics Division
Argonne National Laboratory
This work used the resources of the Argonne Tandem Linac Accelerator System (ATLAS), which is a U.S. Department of Energy, Office of Science User Facility supported under contract DE AC02 06CH11357.
The design and construction of the new AMIS facility is supported by the U.S. Department of Energy, National Nuclear Safety Administration (NNSA), under contract DE-AC02-06CH11357.
The AMIS project is managed by Brahim Mustapha of the Physics Division and the Chief Engineer is Albert Barcikowski of the Experimental Operations and Facilities Division.
The materials irradiation research program is led by Abdellatif Yacout manager of the Fuel Development and Qualification group within the Chemical and Fuel Cycle Technologies Division.

## Slide 2
Overview of the Argonne superconducting heavy ion linac ATLAS
The ATLAS Multi-User Upgrade
The ATLAS Material Irradiation Station (AMIS)
  Advantages of heavy ion beams for high DPA studies
  Examples of studies to date at the stand-alone irradiation station
  Design and Status of AMIS
  Prospects for increased beam time for materials irradiation using AMIS
Concept for a dedicated heavy ion linac for in-situ studies at the Argonne APS: XMAT
Outline

## Slide 3
the Argonne Tandem Linear
Accelerator System (ATLAS)

## Slide 4: ATLAS: Argonne Tandem Linear Accelerator System
1st Superconducting ion linac in the world
It has been operating for over 35 years
National user facility serving ~ 400 users per year
1st Multiple charge state acceleration demonstrated in 2000
CARIBU: Pulsed beams of short-lived fission fragments beginning 2016
4

## Slide 5: Simultaneous Multi-Charge State Acceleration
Simultaneous acceleration of multiply charged U-238 ions through a superconducting linac (ATLAS), P. Ostroumov et al, PRL 2001
238U from PII, stripped and injected to Booster
238U Intensity distribution of accelerated Q’s
5
Emittances & Twiss parameters for # Q’s
The broad acceptance of ATLAS together with pulsed beams from a charge breeder
makes possible the delivery of “similar” m/q ion beams to 2 simultaneous users

## Slide 6
the concept of the
ATLAS Multi-user upgrade

## Slide 7
The Need
  Significant competition & increased pressure on ATLAS beam time
  Increasing demand for longer experiments (> 1 week)
  Examples: Low intensity radioactive beams & low cross section reaction channels
  Requested beam time significantly exceeds ATLAS’s ~ 6000 hours/year
  ATLAS PAC is typically over-subscribed by a factor of 2-3 …
The Purpose
  Relieve pressure on beam time and accomplish more physics by serving two users at a time, allow more time for some applications (such as AMIS)
  When running CARIBU Beams, the machine is “empty” ~ 90% of the time while operating CW  Take advantage of that time (Economical!)
The Need & Purpose of the ATLAS MUU

## Slide 8
EBIS beam is typically ~1 ms pulse up to 30 Hz repetition rate  ~ 3 % DF
DC beam from ECR could be injected into ATLAS in the remaining ~ 97% DF
Considering 2 x 1 ms switching time, the useful ECR duty cycle can be ~ 90%
CARIBU beams are typically charge-bred to corresponding A/q ≥ 4, ATLAS accelerates beams with A/q ratios ≤ 7  The useful range of A/q overlap is 4-7
t
t
Radioactive ions from CARIBU-EBIS
Stable ions from ATLAS-ECR
Combined beam structure
~ 3% Duty Factor
~ 90 % Duty Factor
t
The Opportunity with Pulsed CARIBU-EBIS

## Slide 9: ATLAS Multi-User Upgrade
EBIS beams represents 1-3% duty factor
Interleave pulsed EBIS beam with continuous ECR beam
  Enables delivery of beams to 2 users with nearly no loss of intensity
t
Combine beams
Separate beams
EBIS pulse, ~1 ms @ 10Hz
ECR stable beam, ~95 ms
4-7 MeV/u
4-15 MeV/u

## Slide 10
Table shows beams within 1% of A/q ratio
Overlap between stable and RIB beams offers a lot of flexibility
Study of a recent run period showed ~40% potential overlap, limited only by the number of days of CARIBU beams
A/Q | Stable beams | CARIBU beams
4.000 | 20Ne5+, 28Si7+, 36Ar9+ | 84Se21+, 88Kr22+, 92Sr23+, 101Mo25+, 105Ru26+
4.143 | 58Ni14+ | 83As20+, 95Y23+, 104Tc25+, 112Pd27+, 117Cd28+
4.364 | 48Ti11+, 74Ge17+ | 92Kr21+, 105Nb24+, 109Tc25+, 119Pd27+, 149Nd34+
4.538 | 59Co13+ | 91Rb20+, 105Zr23+, 123Cd27+, 131Te29+, 146Pr32+
4.875 | 78Kr16+ | 93Y19+, 102Mo21+, 132Sn27+, 141I29+, 162Eu34+
5.000 | 40Ar8+,60Ni12+, 90Zr18+ | 85Se17+, 110Mo22+, 124In25+, 141I28+, 159Pm32+
5.280 | 132Xe25+ | 105Ru20+, 126In24+, 137I26+, 153Pr29+, 165Tb31+
5.600 | 84Kr15+ | 100Nb18+, 111Tc20+, 117Cd21+, 141Xe25+, 147La26+
5.643 | 79Br14+, 107Ag19+ | 96Rb17+, 107Nb19+, 119Cd21+, 135Te24+, 151Nd27+
5.714 | 80Se14+ | 91Kr16+, 97Zr17+, 109Ru19+, 131Sb23+, 143Ba25+
6.432 | 238U37+ | 83Se13+, 90Kr14+, 97Sr15+, 103Zr16+, 141I22+
6.709 | 208Pb31+ | 88Se13+, 88Br13+, 94Rb14+, 100Y15+, 107Nb16+
6.792 | 197Au29+ | 89Se13+, 89Br13+, 95Rb14+, 102Y15+, 108Nb16+
7.000 | 133Cs19+ | 84As12+, 98Rb14+, …
Combining ECR Stable beams with CARIBU RIBs

## Slide 11
Adding a 3rd switchyard to enable AMIS

## Slide 12
Low-energy heavy ion beams ~ 1 MeV/u effectively emulate material damage in nuclear reactors, in both fuel and structural materials at DPA rates of 2000 per day or more
Irradiations at ion rates up to 1E12/s or more at 1 cm2 – generally limited by sample heating
Irradiation studies that would have taken years at a reactor have been accomplished in a few hours or days at ATLAS: see publications of the Reactors Materials group of Latif Yacout over the past 5 years at a stand-alone station
Ref: M. Pellin et al, Journal of Nuclear Materials 471 (2016) 266-271
Based on this initial success, NNSA has funded an addition to the ATLAS MUU
Radiation damage mechanisms Damage as function of depth Previous Irradiation Station
Material Irradiation Studies for Nuclear Energy

## Slide 13: Typical result from the previous stand-alone irradiation station at ATLAS
UO2 sample irradiated to 1357 dpa at 350 oC with 84-MeV Xe beam
See separate list of publications of this reactor materials group

## Slide 14: Summary of advantages of heavy ion beams for materials irradiation
Ions from protons to uranium are available at ATLAS at energies with ranges of ~10 microns at sample densities ~10 g/cm3
DPA ~2000 per day are easily achieved with either cooled or heated samples and without activation – i.e. immediate PIE is possible
Heavy ions within the range of 10 microns have a large nuclear damage to ionization heat ratio, e.g. the ionization heat per DPA scaled to uranium beam on uranium oxide = 1:
  Uranium 1, Krypton 2, Helium 6, Protons 7
  Heavier ions have both higher dpa rates per ion and less heating per dpa
Beams of all fission fragment elements with appropriate energies ~100 MeV are available, e.g. gases such as Xe and refractories such as Zr
Beams of elements of structural components such as Fe to mimic effects of neutron damage via irradiations such as Fe on Fe
Recent interest expressed for study of W for the SNS second station and the higher power ESS: e.g. W on W irradiations

## Slide 15
Pulsed switching using a pulsed Wien filter magnet will allow more beam time by taking advantage of the ATLAS multi-user upgrade
The new beamline is currently under development, will be commissioned in FY2022
Funded by NNSA’s Office of Defense Nuclear Nonproliferation
AMIS
A dedicated material irradiation station after PII
AMIS: ATLAS Material Irradiation Station (New)

## Slide 16
Thick Septum ~ 5 cm for beam separation
Magnetic shielding to limit effect on straight ATLAS beam
10-deg Pulsed Wien filter magnet 90-deg Septum magnet
Combines E&B fields
Pulsed E-field, DC B-field
E&B add-up to deflect beam to AMIS target
E changes sign to cancel B-field for straight beam
AMIS Beamline: Key Components

## Slide 17
XMAT: a concept for a future dedicated linac at the Argonne aps for in-situ irradiation/examination

## Slide 18: XMAT Layout: beam directed to a sample/target in an x-ray hutch at the Argonne APS for in-situ irradiation & examination via 3D x-ray imaging
Kutsaev, Sergey V., Brahim Mustapha, Peter N. Ostroumov, Jerry Nolen, Albert Barcikowski, Michael Pellin, and Abdellatif Yacout. "Heavy ion linear accelerator for radiation damage studies of materials." Review of Scientific Instruments 88, no. 3 (2017): 033302.
Notes: Note that the APS hutches sit underneath the Ion Source. ANL has built already and recently both an energetic ion beam line (XMAT would utilize the front end of this design) and a hard xray beam line.

## Slide 19: Scale model of XMAT near an APS beam line

## Slide 20
Summary and outlook

## Slide 21
The ATLAS Multi-User Upgrade will relieve the pressure on beam time at ATLAS and enhance the capabilities of the facility
High DPA irradiations by the Argonne Nuclear Engineering group led by Latif Yacout at a dedicated station over the past 5 years have demonstrated the value of heavy ion beams with ranges ~10 microns at DPA rates ~2000 per day or more
NNSA is funding AMIS, a dedicated irradiation station at ATLAS
  AMIS will operate first stand-alone in 2022 and later as part of the ATLAS MUU
  Beam time at AMIS will be allocated when synergistic with the basic nuclear physics research mission of ATLAS on an incremental cost-recovery basis
  Samples are not activated by these heavy ion beams
Pending the success of AMIS, XMAT, a concept for a dedicated heavy ion linac-based irradiation capability located at the Argonne APS with in-situ diagnostics has been developed
  Rough cost estimate 20-30 M$ on the time horizon ~5-10 years
Summary and Outlook

## Slide 22
supplemental slides
See the attached list of publications by the
Argonne nuclear materials research group