## Slide 1: MQXFA10 Coils Acceptance Review QXFA131, and QXFA132
Fred Nobrega, CAM/L3
Miao Yu, Deputy L3
Marcellus Parker, Electrical
Coil Fabrication at FNAL
U.S. HL-LHC Accelerator Upgrade Project
MQXFA10 Coils Acceptance Review
September 8, 2021

## Slide 2: Overview
Discrepancy Reports for QXFA131 and QXFA132
  Typically written against specific step in traveler which conforms to the following documents:
    QXFA Series Coil Production Specification, US-HiLumi-doc-2986
    MQXFA Final Design Report, US-HiLumi-doc-948
    QXFA Series Coil Fabrication Electrical QC Plan, US-HiLumi-doc-521
No items to be addressed from the MQXFA09 Coils Acceptance Review
Appendix
  Critical DR’s with subset of attachments (if applicable)
  Coil data for magnet fabrication report

## Slide 3: DR Summary
Coil # | Total DR’s | Critical DR’s
QXFA131 | 6 | 0
QXFA132 | 4 | 1
Legend
Noncritical DR
Critical DR
Critical DR – affects form/fit/function and needs L2 review
Coil # | W&C Prep | React | Impreg | CMM Interface | Electrical
QXFA131 | 0 | 1 | 2 | 0 | 3
QXFA132 | 0 | 1 | 2* | 0 | 1
Links to all DR’s: (VPN or FNAL services account required)
Discrepancy Reports – QXFA131
Discrepancy Reports – QXFA132
* Critical DR

## Slide 4: QXFA131 DR’s
DR Number | Description | Disposition
12325 Electrical Testing | The B1-B2 values in the calculate table are out of spec. (traveler step 8.1) | DMM measurements were retaken at a later step (13.3) in the traveler with more reliable connections and the value were within range.
12387 Electrical Testing | voltage tap values are out of spec | VTA01 and VTA02 data were input incorrectly into the traveler
12388 Electrical Testing | voltage tap values are out of spec (traveler step 13.3) | DMM measurements were taken using cable terminals that were better equipped for accurate low-level resistance measurements.
Legend
Minor DR
Critical DR
Critical DR – affects form/fit/function and needs L2 review

## Slide 5: QXFA131 DR’s
DR Number | Description | Disposition
12313 Reaction | Per the process capability plots attached to this traveler step, there were 7.6% of the individual thermocouple measurements which were above the upper spec limit for the 395C soak, and 0.6% below the lower spec limit in the 665C soak. | The coil reaction witness sample passes all requirements and is recorded in the coil interface traveler.
12448 Splice / Epoxy Impregnation | 1 layer of Hexcel 4522 (6 mil) was installed instead of 1 layer of BGF 6781 (10 mil thick) as designed. This DR also applies to coils QXFA129, 130, 131 and 132. | CERN has been notified and concurs that the material swap is minor and to use as is. They will write a NCR (level 1, concession). Coils 129 & 130 have passed the coil acceptance review and with coil 130 planned for magnet MQXFA09. The remaining coils are complete and at LBNL.
12348 Splice / Epoxy Impregnation | Using the cutting guide tool to cut the layer of epoxy from the pole of the coil, the tech mistakenly cut across 2 current blocks on his first pass of multiple passes. | Verified that the depth of cut was shallow and did not reach the cable via approved off-normal work plan.
Legend
Minor DR
Critical DR
Critical DR – affects form/fit/function and needs L2 review

## Slide 6: DR12348 QXFA131
Near side
Far side

## Slide 7: QXFA132 DR’s
DR Number | Description | Disposition
12334 Reaction | As per the process capability plots attached to this step, the 665C soak had 0.9% of the data out of spec on the low side. | Witness samples are accepted, as indicated in the coil interface traveler. T/C #10 was recalibrated twice for confirmation, and when using the adjusted offsets the data were all in spec (see the 665C before/after reaction plots in the appendix).
12337 Splice / Epoxy Impregnation | A small section of the blanket was wedged between the mid plane shim and the last turn of the coil. | Installation of SS midplane shim during coil reaction prep pinched the OL S2 glass. A working group meeting agreed to proceed with coil fabrication as is. Presentation attached to DR. No repair is needed.
Legend
Minor DR
Critical DR
Critical DR – affects form/fit/function and needs L2 review

## Slide 8: DR12337, QXFA132 Prep for Reaction; Midplane Shim Installation

## Slide 9: QXFA132 DR’s
DR Number | Description | Disposition
12364 Reaction | Coil short to structure prior to impregnation | 4-wire measurements taken from the coil lead to several locations on the impregnation tooling indicate a ~5 Mohm short. After impregnation, the short did not exist.
12448 Splice / Epoxy Impregnation | 1 layer of Hexcel 4522 (6 mil) was installed instead of 1 layer of BGF 6781 (10 mil thick) as designed. This DR also applies to coils QXFA129, 130, 131 and 132. | CERN has been notified and concurs that the material swap is minor and to use as is. They will write a NCR (level 1, concession). Coils 129 & 130 have passed the coil acceptance review and with coil 130 planned for magnet MQXFA09. The remaining coils are complete and at LBNL.
Legend
Minor DR
Critical DR
Critical DR – affects form/fit/function and needs L2 review

## Slide 10: MQXFA09 Coils Review Recommendations
No issues or recommendations to be address from the MQXFA09 Coils Acceptance Review

## Slide 11: Appendix

## Slide 12: Witness Samples QXFA131 & 132
QXFA132 argon inlet moved to coil LE

## Slide 13: QXFA131 Average Temperature & Dwell Time

## Slide 14: QXFA131 210° C Plateau
T/C #4

## Slide 15: QXFA131 395° C Plateau

## Slide 16: QXFA131 665° C Plateau

## Slide 17: QXFA132 Average Temperature & Dwell Time

## Slide 18: QXFA132 210° C Plateau
T/C #4

## Slide 19: QXFA132 395° C Plateau
T/C #4

## Slide 20: QXFA132 665° C Plateau

## Slide 21: QXFA132 665° C Plateau

## Slide 22: QXFA131 Hi-pot & Electrical Checks
 (revised 5/6/22)

## Slide 23: QXFA131 Impulse Test

## Slide 24: QXFA132 Hi-pot & Electrical Checks (original)
 (revised 5/9/22)

## Slide 25: QXFA132 Impulse Test

## Slide 26: Coil Dimensional Specifications
 | Dimension (mm) | Tolerance (mm)
Inner radius | 74.750 | ± 0.250
Outer radius | 113.376 | ± 0.250
Coil to midplane gap | 0.125 | ± 0.050
Keyway width | 14.00 | ± 0.25
Coil length | 4529 | ± 5
  MQXFA Final Design Report, US-HiLumi-doc-948
Coil tolerances per drawing F10115850.

## Slide 27: Coil Reaction & Impregnation Specifications
Coil Reaction | Step | Description | Average Rate | Time
Step 1 | Ramp | from 20 °C to 210 °C | 25 C/hour | 
Step 2 | Soak | 210 °C |  | 48 hours
Step 3 | Ramp | from 210 °C to 400 °C | 50 C/hour | 
Step 4 | Soak | 400 °C |  | 48 hours
Step 5 | Ramp | from 400 °C to 665 °C | 50 C/hour | 
Step 6 | Soak | 665 °C |  | 50 hours
Step 7 | Ramp | from 665 °C to 20 °C |  | ~ 80 hours
Coil Impregnation | Description | Average Rate | Time | Comment
Ramp | from 20 °C to 110 °C | 10 C/hour |  | Coil Degas
Soak | 110 °C |  | 8 hours | 
Ramp | from 110 °C to 55 °C | 1.7 C/hour |  | 
Soak | 55 °C |  | 4-6 hours | Epoxy Fill
Ramp | from 55 °C to 110 °C | 10 C/hour |  | Epoxy Cure
Soak | 110 °C |  | 5 hours | 
Ramp | from 110 °C to 125 °C | 10 C/hour |  | 
Soak | 125 °C |  | 16 hours | 
  MQXFA Final Design Report, US-HiLumi-doc-948

## Slide 28: Coil Electrical Measurement Range
 | Measurement | Ref. Min-Max
 | Coil Resistance @ 1A | 577.31-614.75 mV
 | Ls @ 20 Hz | 4.56-6.29 mH
 | Q @ 20 Hz | 0.73-1.28
 | Ls @ 100 Hz | 3.16-6.24 mH
 | Q @ 100 Hz | 1.57-5.44
 | Ls @ 1 kHz | 1.77-5.75 mH
 | Q @ 1 kHz | 1.95-8.41
  QXFA Coil Fabrication Electrical QA, US-HiLumi-doc-521

## Slide 29: Coil Length
 | Overall Coil Length (mm)
Pre-Series Requirement | 4532 ± 5.0
QXFA 114 | 4530
Series Requirement | 4529 ± 5.0
QXFA 124 | 4531.1

## Slide 30: Cable Preparation
Re-spool the insulated cable to verify the total length (min. 441 m including the winding lead).
Split into two reels for L1 coil (min. 195 m) and L2 coil (min. 246 m).
Cable length in coil
Cable respooling
 | Cable ID | Total (m) | L1 (m) | L2 (m)
QXFA 131 | 1141 | 450.6 | 204.6 | 246
QXFA 132 | 1146 | 448.9 | 202.9 | 246
 | Cable ID | Total (m) | L1 (m) | L2 (m)
Average (QXFA 104-128) |  | 427.3 | 188.1 | 239.2
QXFA 131 | 1141 | 427.1 | 188.0 | 239.1
QXFA 132 | 1146 | 427.1 | 188.4 | 238.7

## Slide 31: Wedge Length and Gap
Wedge gap: 2 mm 3.75 mm 3.75 mm 3.75 mm 3.75 mm 3.75 mm 2 mm
QXFA 131 & 132

## Slide 32: Pole Gap

## Slide 33: QXFA Production Coil Pole Gap