## Slide 1: Coil ordering in MQXFA10 based on conductor properties
Maria Baldini, Vittorio Marinozzi

## Slide 2: MQXFA07 cables: RRR estimations
COIL | CABLE
129 | P43OL1132
131 | P43OL1141
132 | P43OL1146
220 | P43OL1135
221 | P43OL1143
Rolled and minor edge extracted samples used to estimate RRR of the coil
Each cable: 40 strands in parallels coming from several spools
Spools come from different billets.
Maximum coil to ground voltage at quench with ordering: 353 V (EDMS 1963398, Us-HiLumi Docdb 879)
There is one rolled sample value per billet.
If the Cu/NCu value of the spool used for the cable is not present, the Cu/NCu of a particular spool is estimated averaging data from spools belonging to the same billet.
A weighted mean (weight= # of strands) is used to estimate cable RRR rolled samples and Cu/Ncu values.
Minor and Major edge extracted samples are collected only from the most represented billets. Values are averaged
Witness sample RRR are also collected on representative billets. Data are not measured anymore starting from cable 1134

## Slide 3: MQXFA10 coils
COIL | RRR (rolled) | RRR (minor edge) | RRR (major edge)
129 | 222.1 | 263.2 | 360.2
131 | 232.1 | 305.6 | 353
132 | 248.5 | 264.2 | 352.8
220 | 208.7 | 246.2 | 298.8
221 | 213.97 | 250.2 | 365
COIL | Cu/NCu
129 | 1.147
131 | 1.167
132 | 1.169
220 | 1.170
221 | 1.175

## Slide 4: MQXFA10 coil RRR

## Slide 5: Peak voltages assumptions
Current: 16470
  Old nominal, since electrical design criteria are based on old nominal current
Nominal protection (CLIQ 600 V - 40 mF, OL QH 300 V – 7.05 mF)
Coils are reported in mechanical ordering
Peak voltages have been computed using rolled and minor edge RRR values. All coil orderings resulting in peak voltage to ground less than 353 V with both assumptions and in all failure cases have been identified
P1
P2
P3
P4
Peak voltages computed using STEAM-LEDET app provided by CERN
  All possible combinations of coils are considered (120)
  For each combination, nominal scenario plus 3 failure scenarios are considered
Notes: Need to be u

## Slide 6: Peak voltages report
Old value, since design criteria are based on old nominal current

## Slide 7: Acceptable coil orderings
There are 67 acceptable coil orderings with voltage < 353 V that are common for both rolled and minor edge RRR values (values reported for rolled RRR)
P1 | P2 | P3 | P4 | V
220 | 221 | 131 | 132 | 333
221 | 220 | 132 | 131 | 334
221 | 220 | 131 | 132 | 334
220 | 129 | 131 | 132 | 334
221 | 129 | 132 | 131 | 335
221 | 129 | 131 | 132 | 335
220 | 129 | 221 | 131 | 335
220 | 129 | 131 | 221 | 335
221 | 220 | 131 | 129 | 336
221 | 129 | 132 | 220 | 336
221 | 129 | 131 | 220 | 336
220 | 129 | 221 | 132 | 336
220 | 129 | 132 | 131 | 336
129 | 220 | 221 | 132 | 336
129 | 220 | 221 | 131 | 336
220 | 129 | 132 | 221 | 337
131 | 221 | 132 | 220 | 337
131 | 220 | 132 | 221 | 337
131 | 221 | 132 | 129 | 338
131 | 129 | 132 | 221 | 338
131 | 220 | 132 | 129 | 339
131 | 129 | 221 | 220 | 339
131 | 129 | 132 | 220 | 339
132 | 221 | 131 | 220 | 340
132 | 220 | 131 | 221 | 340
221 | 220 | 132 | 129 | 341
P1 | P2 | P3 | P4 | V
131 | 132 | 221 | 129 | 341
221 | 131 | 220 | 129 | 342
220 | 131 | 221 | 132 | 342
132 | 129 | 131 | 221 | 342
131 | 132 | 221 | 220 | 342
129 | 221 | 220 | 131 | 342
221 | 129 | 220 | 131 | 343
132 | 221 | 131 | 129 | 343
132 | 131 | 221 | 220 | 343
132 | 131 | 221 | 129 | 343
131 | 129 | 221 | 132 | 343
131 | 129 | 220 | 221 | 343
132 | 129 | 131 | 220 | 344
131 | 220 | 221 | 132 | 344
221 | 132 | 220 | 129 | 345
132 | 220 | 221 | 131 | 345
132 | 129 | 221 | 131 | 345
129 | 220 | 132 | 131 | 345
220 | 221 | 132 | 131 | 346
220 | 132 | 221 | 131 | 346
132 | 220 | 131 | 129 | 346
221 | 129 | 220 | 132 | 347
132 | 129 | 221 | 220 | 347
129 | 221 | 220 | 132 | 347
129 | 220 | 132 | 221 | 347
129 | 132 | 220 | 221 | 347
P1 | P2 | P3 | P4 | V
132 | 220 | 221 | 129 | 349
132 | 129 | 220 | 221 | 349
131 | 132 | 220 | 129 | 349
129 | 132 | 220 | 131 | 349
221 | 132 | 131 | 220 | 350
221 | 131 | 132 | 220 | 350
132 | 221 | 220 | 129 | 350
132 | 131 | 220 | 129 | 351
132 | 129 | 220 | 131 | 352
129 | 221 | 132 | 131 | 352
129 | 132 | 221 | 131 | 352

## Slide 8: Backup slides

## Slide 9: MQXFA03-04 Coil RRR: calculated vs measured
MQXFA03 measured coil RRR are more consistent with estimate based on rolled samples
MQXFA04 measured coil RRR are more consistent with estimate based on minor edge extracted samples

## Slide 10: MQXFA05 Coil RRR: calculated vs measured
MQXFA05 measured coil RRR are consistent with estimate based on minor edge extracted samples
Rolled samples data were not used for simulation because there was a different heat treatment for one of the coil
MQXFA06 measured coil RRR are consistent with the lowest value between the edge samples