## Slide 1: Magnets 302.2.02 and 03 – Strand Procurement and Testing Cable Fabrication
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 and CAM)
Elizabeth Lee – LBNL (302.2.03 CAM deputy)
Mike Naus – LBNL (302.2.03 L3 Deputy)
Jonathan Lee – LBNL Intern Student
HL-LHC AUP MQXFA10 Coil Acceptance Review – 08 Sept 2021

## Slide 2: Outline
Cable & Coil Overview
Strand Summary
Cable DR Summary
Discrepancy Reports by Cable

## Slide 3: Cable & Coil Overview
All cables are 2nd generation QXF cables produced under AUP
Coil # | Cable #
129 | P43OL1132
131 | P43OL1141
132 | P43OL1146
220 | P43OL1135
221 | P43OL1143
Previously Approved

## Slide 4: Strand Summary
All strands ordered per the “HiLumi” specification
  AUP
    FNAL 646116 Shipment A
    FNAL 646116 Shipment B
    FNAL 646116 SA1 Shipment B
    FNAL 646116 SA1 Shipment C
    LBNL 7428700 Shipment A
    LBNL 7428700 Shipment B
  LARP
    FNAL 632982 D - Spec 0
Conductor Description:
  Ø0.85 mm, 108/127 stack, Ti-doped, Reduced-Sn

## Slide 5: Cable QC Summary
All cables passed the required quality control testing per US-HiLumi-Doc. 74
Six (6) DRs reported across the four (4) cables

## Slide 6: Cable DR Review

## Slide 7: QXFA-131 / P43OL1141
No Discrepancy Reports for Cable P43OL1141

## Slide 8: QXFA-132 / P43OL1146 Discrepancy Report #12104
Issue: One CME mid-thickness data point below spec by 0.2 µm at 81st meter
Cause: Late thickness adjustment
Acceptance Justification: Single point, only out by small amount and not expected to impact cable viability
(1 of 3)

## Slide 9: QXFA-132 / P43OL1146 Discrepancy Report #12232
Issue 1: TCs outside of calibration window
Issue 2: TC values along the sample length during the heat treatment plateaus varied by more than 2 °C.
210C Plateau: Range = 3.1 °C
400C Plateau: Range = 4.1 °C
665C Plateau: Range = 6.4 °C
Cause 1: Unable to calibrate TC probes in RRR furnace as built
  Now fixed
Cause 2: TC drift coupled with the inability to calibrate.
Acceptance Justification:
  Quartz-encapsulated witness wire RRR was within normal range
    Temperatures were within historical norms
  Average temperatures were on target
  210C Plateau: Average = 209.4 °C
  400C Plateau: Average = 398.9 °C
  665C Plateau: Average = 665.3 °C
(2 of 3)

## Slide 10: QXFA-132 / P43OL1146 Discrepancy Report #12158
Issue: Insulation thickness verification measurement 0.9 mm above spec at 0.159 mm
Cause: Operator error (suspected)
Acceptance Justification:
Subsequent measurement of post-coiling cable drop lengths was on target at 0.145 mm
(3 of 3)

## Slide 11: QXFA-220 / P43OL1135 Discrepancy Report #11915
Issue: Several mid-thickness data points above spec
  0.1 µm to 1.6 µm above USL
Cause: Measurement noise coupled with above target thickness
Acceptance Justification: OOS values are small and not expected to impact cable viability
(1 of 2)

## Slide 12: QXFA-220 / P43OL1135 Discrepancy Report #11920
Issue: Insulation thickness average OOS high by 0.2 µm on LBNL verification sample
Cause: Measurement & raw material variation
Acceptance Justification:
  OOS by very small amount & not expected to impact cable viability.
  Vendor measurement average within specification (0.1493 mm)
(2 of 2)

## Slide 13: QXFA-221 / P43OL1143 Discrepancy Report #12038
Issue: One CME mid-thickness data point above spec by < 1 µm
Cause: Measurement noise coupled with slightly above target thickness
Acceptance Justification: Single point, only out by small amount and not expected to impact cable viability. Potentially within post-coil cable drops
(1 of 1)

## Slide 14: END [Back-Up Slides Below]

## Slide 15: Present strand production data
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h

## Slide 16: Present strand production data
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h

## Slide 17: Present strand production data
Data for 15% rolled strand predicts the RRR at cable sharp bend
Lab: IEC method, Supplier: 20K method
Inter-lab comparisons have validated approaches (see QP)

## Slide 18: P43OL1141 – Cable Date, Lengths
Cable Manufacture Date
  2019 01 07 (Production run)
Cable Length:
  468 m (LBNL, fabricated, including LBNL samples)

## Slide 19: P43OL1141 – Strand and SS Core ID
Spool:
  PO08S00344A04U x 3 ULs,
  PO08S00355A02U x 2 ULs,
  PO08S00456A01U x 2 ULs,
  PO08S00457A05U x 2 ULs,
  PO08S00460A05U x 2 ULs,
  PO08S00461A03U x 1 ULs,
  PO08S00454A09U x 1 ULs,
  PO08S00236B01U x 2 ULs,
  PO08S00453A07U x 2 ULs,
  PO08S00454A08U x 4 ULs,
  PO08S00453A05U x 1 ULs,
  PO08S00369A01U x 8 ULs,
  PO08S00377A03U x 7 ULs,
  PO08S00453A02U x 3 ULs.
Core:
  120L09A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 11 billets

## Slide 20: P43OL1141 Respooling Wire Diameter
Below LSL: 0.01%
Above USL: 0.01%

## Slide 21: P43OL1141 – Cable QC Data Summary
CME:
Residual Twist:
  130°
10-stack:
  Qualification: 1.517 mm
  Production tail end: 1.522 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.2 | 0.409 | 18.169 | 1.526
Average | 17.0 | 0.364 | 18.156 | 1.523
Minimum | 17.0 | 0.321 | 18.149 | 1.519
Sigma | 0.02 | 0.010 | 0.003 | 0.001

## Slide 22
Rollers: P-95 (2019-12-02) and P-96 (2019-12-02)

## Slide 23
Rollers: P-95 (2019-12-02) and P-96 (2019-12-02)

## Slide 24
Rollers: P-95 (2019-12-02) and P-96 (2019-12-02)

## Slide 25: P43OL1141 – Braiding
Fiberglass Lot #100858, 100602
P/I: 18.9
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.148 mm; #2) 0.147 mm; #3) 0.145 mm;
  Mean 0.147 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.149 mm; #2) 0.148 mm; #3) 0.147 mm;
  Mean 0.148 mm
Vector #464342

## Slide 26: P43OL1141 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.851 ± 0.006 mm (LBNL)1
Cu ratio a | 53.9% (OST)
Strand twist pitch a | 19.0mm (OST)
RRR (RW) a | 343 (OST)
RRR (15% rolled) a | 229 (OST)
IC (4.2 K, 15 T) a | 389 A (OST)
IC (4.2 K, 14 T) a | 485 A (OST)
IC (4.2 K, 13 T) a | 593 A (OST)
IC (4.2 K, 12 T) a | 716 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 27: P43OL1141 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 28: P43OL1141 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 29: P43OL1141 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | PO08S00344A04U P43OL1141AE05E | 3 (3) | LRLK200731ALC1 | 353 | 349 | 429 | 415
ID #2 | PO08S00454A08U P43OL1141AE29E | 5 (4) | LRLK200731ALC1 | 353 | 281 | 406 | 443
ID #3 | PO08S00369A01U P43OL1141AE41E | 8 (8) | LRLK200731ALC2 | 364 | 340 | 397 | 431
ID #4 | PO08S00377A03U P43OL1141AE51E | 7 (7) | LRLK200731ALC1 | 386 | 295 | 408 | 434
ID #5 | PO08S00453A02U P43OL1141AE57E | 6 (3) | LRLK200731ALC1 | 309 | 263 | 360 | 375
Vector #464342

## Slide 30: P43OL1146 – Cable Date, Lengths
Cable Manufacture Date
  01 July 2020 (Production run)
Cable Length:
  475 m (LBNL, fabricated, including LBNL samples)

## Slide 31: P43OL1146 – Strand and SS Core ID
Spools:
Core:
  120L04A7322313
    Heat: 844979. Lot: 16-597
    Material: 316L
    Chemical Properties CoT/CoC #172660-1: 0.14 wt% Co
    Core width: 12.0 mm
28 spools from 18 different billets
PO08S00344A01U x 1 ULs | PO08S00355A01U x 2 ULs | PO08S00361A02U x 1 ULs | PO08S00381A05U x 1 ULs
PO08S00344A03U x 1 ULs | PO08S00358A04U x 2 ULs | PO08S00361A03U x 2 ULs | PO08S00382A02U x 1 ULs
PO08S00344A05U x 1 ULs | PO08S00358A07U x 1 ULs | PO08S00362A02U x 3 ULs | PO08S00383A01U x 2 ULs
PO08S00347A02U x 1 ULs | PO08S00359A01U x 3 ULs | PO08S00364A02U x 1 ULs | PO08S00383A02U x 2 ULs
PO08S00347A03U x 2 ULs | PO08S00359A02U x 1 ULs | PO08S00366A02U x 2 ULs | PO08S00383A05U x 1 ULs
PO08S00353A05U x 1 ULs | PO08S00360A01U x 1 ULs | PO08S00367A01U x 2 ULs | PO08S00409A03U x 1 ULs
PO08S00354A03U x 1 ULs | PO08S00360A02U x 1 ULs | PO08S00381A04U x 1 ULs | PO08S00416A02U x 1 ULs

## Slide 32: P43OL1146 Respooling Wire Diameter
Below LSL: 0.003%
Above USL: 0.002%

## Slide 33: P43OL1146 – Cable QC Data Summary
CME:
Residual Twist: 130°
10-stack:
  Qualification: 1.524 mm
  Production tail end: 1.525 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.394 | 18.175 | 1.527
Average | 17.0 | 0.370 | 18.144 | 1.523
Minimum | 16.9 | 0.320 | 18.135 | 1.515
Sigma | 0.01 | 0.012 | 0.005 | 0.002

## Slide 34
Rollers: P-93 (2019 12 02) & P-94 (2019 12 02)

## Slide 35
Rollers: P-93 (2019 12 02) & P-94 (2019 12 02)

## Slide 36
Rollers: P-93 (2019 12 02) & P-94 (2019 12 02)

## Slide 37: P43OL1146 – Braiding
Vector #464342
Insulation Thickness (at 5 Mpa)
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.149 | 0.148 | 0.149
LBNL Verification | 0.147 | 0.145 | 0.144 | 0.145
Fiberglass Lot: #11154
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.

## Slide 38: P43OL1146 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8502 ± 0.0006 mm (LBNL)1
Cu ratio a | 53.89% (BOST)
Strand twist pitch a | 18.7mm (BOST)
RRR (RW) a | 339 (BOST)
RRR (15% rolled) a | 247 (BOST)
IC (4.2 K, 15 T) a | 389 A (BOST)
IC (4.2 K, 14 T) a | 484 A (BOST)
IC (4.2 K, 13 T) a | 591 A (BOST)
IC (4.2 K, 12 T) a | 713 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 39: P43OL1146 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 40: P43OL1146 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 41: P43OL146 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | PO08S00383A01U P43OL1146AE06E | 5 (2) | LRLK201012ALC1 | 332 | 261 | 390 | 384
ID #2 | PO08S00355A01U P43OL1146AE09E | 2 (2) | LRLK201012ALC1 | 361 | 281 | 413 | 409
ID #3 | PO08S00361A03U P43OL1146AE13E | 3 (2) | LRLK201012ALC2 | 330 | 234 | 383 | 388
ID #4 | PO08S00344A03U P43OL1146AE57E | 3 (1) | LRLK201012ALC2 | 350 | 250 | 411 | 404
ID #5 | PO08S00347A02U P43OL1146AE60E | 3 (1) | LRLK201012ALC1 | 391 | 295 | 448 | 438
Vector #464342

## Slide 42: P43OL1146 – Ic, Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00362A02U P43OL1146AE49E | 684 | 571 | 469 | 382
PO08S00366A02U P43OL1146AE01E | 679 | 568 | 466 | 376
PO08S00359A01U P43OL1146AE23E | 670 | 555 | 458 | 369

## Slide 43: P43OL1146 – SSL Plot, Qual Samples

## Slide 44: P43OL1135 – Cable Date, Lengths
Cable Manufacture Date
  2019 07 08 (Production run)
Cable Length:
  471 m (LBNL, fabricated, including LBNL samples)

## Slide 45: P43OL1135 – Strand and SS Core ID
Spool:
  PO08S00452A01U x 5 ULs,
  PO08S00451A01U x 1 ULs,
  PO08S00450A01U x 18 ULs,
  PO08S00451A02U x 16 ULs,
Core:
  120L16A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 3 billets

## Slide 46: P43OL1135 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.00%

## Slide 47: P43OL1135 – Cable QC Data Summary
CME:
Residual Twist:
  125°
10-stack:
  Qualification: 1.532 mm
  Production tail end: 1.529 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.425 | 18.182 | 1.537
Average | 17.0 | 0.403 | 18.152 | 1.530
Minimum | 17.0 | 0.374 | 18.146 | 1.525
Sigma | 0.01 | 0.009 | 0.003 | 0.002

## Slide 48
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 49
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 50
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 51: P43OL1135 – Braiding
Fiberglass Lot #100858
P/I: 18.9
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.151 mm; #2) 0.149 mm; #3) 0.148 mm;
  Mean 0.150 mm (see DR #11920)
LBNL 10-stack verification QC:
  Cycle #1) 0.145 mm; #2) 0.142 mm; #3) 0.141 mm;
  Mean 0.143 mm
Vector #464342

## Slide 52: Discrepancy Report #11920
Average insulation thickness measurement a fraction of a micron oversize
Attributed to measurement uncertainty; should not impact cable readiness

## Slide 53: P43OL1135 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.001 mm (LBNL)1
Cu ratio a | 54.0% (OST)
Strand twist pitch a | 18.7mm (OST)
RRR (RW) a | 376 (OST)
RRR (15% rolled) a | 209 (OST)
IC (4.2 K, 15 T) a | 379 A (OST)
IC (4.2 K, 14 T) a | 475 A (OST)
IC (4.2 K, 13 T) a | 583 A (OST)
IC (4.2 K, 12 T) a | 706 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 54: P43OL1135 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 55: P43OL1135 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 56: P43OL1135 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | P43OL1135AE05E PO08S00452A01U | 17 (9) | LRLK200206ALC1 | 348 | 280 | 377 | 359
ID #2 | P43OL1135AE39E PO08S00451A02U | 17 (8) | LRLK200206ALC1 | 231 | 202 | 297 | 282
ID #3 | P43OL1135AE37E PO08S00451A02U | 12 (7) | LRLK200206ALC1 | 324 | 204 | 343 | 316
ID #4 | P43OL1135AE12E PO08S00450A01U | 12 (5) | LRLK200206ALC1 | 294 | 256 | 388 | 387
ID #5 | P43OL1135AE11E PO08S00450A01U | 11 (5) | LRLK200206ALC1 | 297 | 289 | 353 | 361
Vector #464342

## Slide 57: P43OL1143 – Cable Date, Lengths
Cable Manufacture Date
  27 Jan 2020 (Production run)
Cable Length:
  472 m (LBNL, fabricated, including LBNL samples)

## Slide 58: P43OL1143 – Strand and SS Core ID
Spools:
Core:
  120L07A7322313
    Heat: 844979. Lot: 16-597
    Material: 316L
    Chemical Properties, CoT/CoC #172660-1: 0.14 wt% Co
    Core width: 12.0 mm
From 12 billets
PO08S00354A04U x 5 ULs | PO08S00454A01U x 1 ULs | PO08S00460A01U x 2 ULs
PO08S00368A07U x 2 ULs | PO08S00454A05U x 1 ULs | PO08S00460A02U x 1 ULs
PO08S00377A02U x 1 ULs | PO08S00457A06U x 1 ULs | PO08S00460A03U x 3 ULs
PO08S00378A01U x 2 ULs | PO08S00458A03U x 3 ULs | PO08S00461A01U x 4 ULs
PO08S00453A06U x 2 ULs | PO08S00459A01U x 2 ULs | PO08S00461A02U x 4 ULs
PO08S00453A08U x 3 ULs | PO08S00460A07U x 2 ULs | PO08S00463A01U x 1 ULs

## Slide 59: P43OL1143 Respooling Wire Diameter
Below LSL: 0.002%
Above USL: 0.012%

## Slide 60: P43OL1143 – Cable QC Data Summary
CME:
Residual Twist: 120°
10-stack:
  Qualification: 1.529 mm
  Production tail end: 1.525 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.09 | 0.419 | 18.164 | 1.536
Average | 17.01 | 0.381 | 18.146 | 1.528
Minimum | 16.97 | 0.333 | 18.135 | 1.523
Sigma | 0.02 | 0.019 | 0.007 | 0.003

## Slide 61
Rollers: P-95 (2019 12 02) & P-96 (2019 12 02)

## Slide 62
Rollers: P-95 (2019 12 02) & P-96 (2019 12 02)

## Slide 63
Rollers: P-95 (2019 12 02) & P-96 (2019 12 02)

## Slide 64: P43OL1143 – Braiding
Vector #464342
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.148 | 0.146 | 0.148
LBNL Verification | 0.148 | 0.147 | 0.145 | 0.147
Insulation Thickness (at 5 Mpa)
Fiberglass Lot: #11154
P/I: 18.9 & 18.0
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.

## Slide 65: P43OL1143 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8507 ± 0.001 mm (LBNL)1
Cu ratio a | 54.09% (BOST)
Strand twist pitch a | 18.7mm (BOST)
RRR (RW) a | 339 (BOST)
RRR (15% rolled) a | 214 (BOST)
IC (4.2 K, 15 T) a | 384 A (BOST)
IC (4.2 K, 14 T) a | 480 A (BOST)
IC (4.2 K, 13 T) a | 588 A (BOST)
IC (4.2 K, 12 T) a | 712 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 66: P43OL1143 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 67: P43OL1143 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 68: P43OL1143 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | PO08S00461A01U P43OL1143AE53E | 8 (4) | LRLK200609ALC3 | 353 | 281 | 400 | 413
ID #2 | PO08S00354A04U P43OL1143AE05E | 5 (5) | LRLK200609ALC3 | 391 | 214 | 385 | 392
ID #3 | PO08S00460A03U P43OL1143AE09E | 8 (3) | LRLK200609ALC3 | 364 | 254 | 386 | 379
ID #4 | PO08S00461A02U P43OL1143AE13E | 8 (4) | LRLK200609ALC3 | 368 | 291 | 432 | 417
ID #5 | PO08S00458A03U P43OL1143AE36E | 3 (3) | LRLK200609ALC3 | 349 | 211 | 339 | 349
Vector #464342

## Slide 69: P43OL1143 – Ic, Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00354A04U P43OL1143AE05E | 671 | 557 | 455 | 366
PO08S00354A04U P43OL1143AE06E | 673 | 558 | 456 | 367
PO08S00461A02U P43OL1143AE15E | 683 | 566 | 460 | 370
PO08S00461A02U P43OL1143AE17E | 695 | 575 | 469 | 377

## Slide 70: P43OL1143 – SSL, Qualification Ic