Targetry at 1MW in a Solenoid
Kevin Lynch
CLFV Agora
January 14, 2022

---
Overview
We are here!

---
We have conflicting goals for our production targets
- High particle yields
- Low production of backgrounds
- Long, problem-free operational lifetimes

---
Production targets face a host of severe issues
- Tight alignment tolerances
- High radiation-damage tolerance
  - Active materials research area!
- High temperature tolerance
  - Heat removal systems
- Tolerance to large thermal and stress fluctuations
- Exotic chemistry
- Remote inspection and servicing
- Severe radiological safety issues
- Difficult disposal problems

---
Things can go very bad, very fast
Swelling – JNM 159 (1988) p.114
CERN-HiRadMat – thermal shock

---
This can go very bad, very fast
- Void formation and Embrittlement
- Creep
- Swelling
- Conductivity loss
- Changing moduli
- Fatigue
Effects depend not only on total irradiation, but also rates, temperatures, stresses, irradiating species, etc.

---
It’s not just the targets themselves that are vulnerable, but their enclosures
Horn stripline fatigue failure (FNAL)
Target containment vessel cavitation (ORNL - SNS)
Be window embrittlement (FNAL)

---
Let’s take a look at some of the issues specific to a CLFV production target
- Coherent, neutrinoless muon to electron conversion in the field of a nucleus
- Mu2e (COMET)
  - Under construction
- Mu2e-II
  - Early R&D
- A 1MW ENIGMA program
  - Snowmass discussions

---
Mu2e: Targetry at 8kW
~25m

---
Let’s zoom into the PS
Backward Beam
Heat and Radiation Shield (HRS)
Target
Vacuum end cap
Pbar absorber
Water volume
250 μm Al
\color{red} p
\color{blue} \mu

---
For cost reasons, Mu2e will use a radiation cooled target
- Tight alignment tolerances:
  - 0.25 mm placement
  - 0.25 mm stability
- Maximize muon yield
- High thermal conductivity
- High melting point
- High mechanical integrity
- Operational lifetime of at least 1yr
- Remote replacement
- Low-momentum muons

---
Tens of person-years were required to converge on a solution meeting these requirements
- Bicycle wheel support
- Refractory metal: Tungsten
- Longitudinally segmented cylinder (stress management):
  - 3.15 mm radius
  - 160+60 mm length
- Longitudinal fins (structure and thermal management)
- 1mm tungsten spokes
- ~ 700 W power absorption
- ~ 1500 K temperature

---
Mu2e-II: Targetry at 100kW
- Mu2e-II will largely reuse the Mu2e concept
  - Upgraded detectors
  - Increased beam power from PIP-II
  - New production target system
    - 8MeV/8kW → 800MeV/100kW
    - Same volume target
- Heat extraction and radiation damage are now truly significant challenges!
  - Must be actively cooled
  - Monolithic target probably not feasible due to radiation damage and lifetime concerns

---
Conceptual target design LDRD
- We need an actively cooled target
  - H20, He are typical cooling fluids
  - May need a phase change to extract enough heat (NH3?)
- We need to replace target material regularly (not annually!) to keep ahead of radiation damage
  - Mu2e: < 1 DPA/yr
  - Mu2e-II: > 300 DPA/yr
DPA: Displacements per Atom

---
Conceptual target design LDRD
Conveyor
Rotating cassette
Fixed granular
\color{black} \sim \unit[200]{mm}
material
There are, of course, other potential options of significantly increased complexity that we’ll come back to later…
\color{red} p
\color{red} p
\color{red} p

---
Rotating cassette
- Pros:
  - Radiation damage can be distributed over many rods that are rotated into the beam over time
- Cons:
  - Cooling is difficult
  - Rotation hardware and unused rods consume significant space in the bore
  - Radiation damage is still an issue over 1 year of operation
Alternatively, rotating wheel (great experience at PSI)
\color{red} p

---
Fixed granular
- Pros:
  - Small space requirement
- Cons:
  - Radiation damage extremely high (peak DPA similar to fixed solid target)
  - Gas cooling efficiency is probably poor
\color{red} p

---
Conveyor for spherical target balls
- Pros:
  - Small space requirement
  - Cooling fluid can assist in moving target balls
  - Balls can be swapped during operation to minimize radiation damage
- Cons:
  - Technical complexity!
    - Drive train
    - Drive/cooling marriage
    - Phase change cooling may be required
    - Windows!
material
\color{red} p

---
Conveyor for spherical target balls
- Various materials are good candidates:
  - W
  - WC
  - SiC
  - MoGRCF
  - Graphite
- This is our current leading candidate design, and mechanical prototyping is underway.
material
\color{red} p

---
ENIGMA: Targetry at 1MW
- Initial consideration for 1MW of beam at 800MeV from PIP-II, delivered from proton compressor ring
- Has much in common with Muon Collider target designs
  - Solenoidal capture channel
  - High power, pulsed proton beam
  - Significant power deposition in solenoid shielding
  - Significant power deposition in proton beam stop

---
ENIGMA: Targetry at 1MW
- We already “know” how to do targets at MW scale
  - Nova (~700kW)
  - SNS (~1.4MW)
  - LBNF (~1.2-2.4 MW)
- But these are not compact targets in a solenoid!
  - LBNF: segmented graphite core 16mm x 1.5-1.8 m
- Low duty cycle beams:
  - LBNF: 10μs every 0.7-1.2 s, 120GeV
  - SNS: 695ns at 60Hz, 1GeV

---
ENIGMA: a rough idea of scale
Mu2e Target Core
6.3mm x 220mm x 250kW
LBNF Target core 16mm x 1.5m x 25kW

---
ENIGMA: Targetry at 1MW
- How compact does the target really need to be?
  - Long target could use graphite (or similar) technology we know how to build
  - Shorter target might need radical ideas
    - Liquid metal (Hg? Pb/Ta?)
      - Muon collider R&D on liquid jets
      - Liquid target are difficult to build and operate
      - Liquid jets have been rate limited
    - Granular material
      - Tungsten powder jet prototypes have been tested
    - Rep rates are a problem
- Whatever we do, significant R&D (materials!) will likely be necessary

---
ENIGMA: liquid target challenges
Top: eruption of fluidized tungsten powder
Bottom: disruption of liquid metal jet

---
Other considerations
- Solenoid design
  - Muon Collider designs utilize 10-20T solenoids with forward production
  - Normal or superconducting?
  - Heat and radiation shielding
    - Lifetime?
- Target handling and replacement
- Beam transport
  - Windows!
- Beam stop design
  - Accident conditions!
- Radiological issues
  - Personnel and environmental protection
  - Waste storage and disposal

---
Conclusions
- We think we know how to build a 100kW low momentum muon source
- Target and solenoid design for a 1MW muon facility will go hand in hand and present significant challenges across many fronts
- There is potentially significant synergies with the muon collider community
- Thanks for your interest and attention!