## Slide 1: Targetry and Irradiation Study Requirements of the Fermilab Research Program
Project X Collaboration Mtg – Experimental Opportunities 4/11/12 P. Hurh

## Slide 2: Overview
Need for High Power Target R&D
  Scope of Fermilab Program
  Fermilab Target Experience
  High Power Target Challenges
Identification of targeted R&D
  Cross-cutting HPT R&D
  Niche HPT R&D
Current HPT R&D Activities

## Slide 3: Introduction- Where we are
AD/MS and Pbar and Ext. Beams operates 3 target facilities:
  P-bar Source (off) – 70 kW proton beam on inconel (nickel alloy) target with Be cover (110 kW/mm2)
  NuMI/MINOS – 400 kW proton beam on graphite (carbon) target (14 kW/mm2)
  MiniBooNE – 32 kW proton beam on beryllium target (1 kW/mm2)
Note: Values in red refer to total beam power divided by nominal 3 sigma spot size

## Slide 4: Introduction- What we are working on
Currently have resources working on:
  ANU/NOvA upgrade - 700 kW proton beam on graphite (carbon) target (15 kW/mm2)
  LBNE - 700 kW proton beam on graphite (beryllium?) target (15 kW/mm2)
  Mu2e – 8 kW-8 GeV proton beam on gold (tungsten?) target (0.3 kW/mm2)
  G-2 – 27 kW-8 GeV proton beam on inconel target (??)
  ORKA – 74 kW – 95 GeV proton beam on platinum (??)
Note: Values in red refer to total beam power divided by nominal 3 sigma spot size

## Slide 5: Introduction- Where we are going
Program: | Stage-0: Proton Improvement Plan | Stage-1: 1 GeV CW Linac driving Booster & Muon Campus | Stage-2: Upgrade to 3 GeV CW Linac (MI>70 GeV) | Stage-3: Project X RDR (MI>60GeV) | Stage-4: Beyond RDR: 8 GeV power upgrade to 4MW
MI neutrinos | 470-700 kW** | 515-1200 kW** | 1200 kW | 2300 kW | 2300-4000 kW
8 GeV Neutrinos | 15 kW + 0-50 kW** | 0-40 kW* + 0-90 kW** | 0-40 kW* | 85 kW | 3000 kW
8 GeV Muon program e.g, (g-2), Mu2e-1 | 20 kW | 0-20 kW* | 0-20 kW* | 85 kW | 1000 kW
1-3 GeV Muon program | ----- | 80 kW | 1000 kW | 1000 kW | 1000 kW
Kaon Program | 0-30 kW** (<30% df from MI) | 0-75 kW** (<45% df from MI) | 1100 kW | 1100 kW | 1100 kW
Nuclear edm ISOL program | none | 300 kW | 300 kW | 300 kW | 300 kW
Ultra-cold neutron program | none | 300 kW | 300 kW | 300 kW | 300 kW
Nuclear technology applications | none | 300 kW | 300 kW | 300 kW | 300 kW
# Programs: | 4 | 8 | 8 | 8 | 8
Total* power (mean): | 660 kW | 1950 kW | 4230 kW | 5490 kW | 11300kW
* Operating point in range depends on MI energy for neutrinos.
** Operating point in range is depends on MI injector slow-spill duty factor (df) for kaon program.

## Slide 6: Introduction- Where we are going
 | Energy | Power* | Target material | Power (in target) | Sigma | Power (in target)/3sigma
Beamline (Project X**) | GeV | kW |  | kW | mm | kW/mm^2
Neutrino (LBNE) | 120 | 2300 | graphite (Be?) | 15 | 1.5 | 0.24
Muon | 1-3 | 900 | tungsten?? | 200 | 2 | 1.77
Kaon (Chrg/Ntrl) | 1-3 | 900 | graphite (Ga?) | 4 | 3 | 0.02
Nuclear (ISOL-UCN, EDM) | 1-3 | 900 | Thorium?? | 500 | 10 | 0.18
Nuclear (technology) | 1-3 | 900 | Pb-Bi Eutectic | 900 | 10 | 0.11
*Actual power depends on beam parsing. “Up to” numbers shown here.
**Project X Stage 3 parameters shown here.
Note: Values in red refer to parameters that are in great need of further specification

## Slide 7: Fermilab’s Target Experience
P-bar Target Station and Neutrinos:
  Solid Targets (High Z and Low Z)
  Very high energy deposition per volume
  Pulsed beam (thermal shock)
  Radiation protection and facility operations
Limited Experience in:
  Flowing liquid targets
  High power CW beam
  Radiation damage

## Slide 8: HPT Challenges
Thermal Shock
Heat Removal
Radiation Damage
Oxidation/Radiation Accelerated Corrosion
Physics/target lifetime optimization
Remote Handling

## Slide 9: Thermal Shock
Fast expansion of material surrounded by cooler material creates a sudden local area of compressive stress
Stress waves (not shock waves) move through the target
Plastic deformation or cracking can occur
Ta-rod after irradiation with 6E18 protons in 2.4 s pulses of 3E13 at ISOLDE (photo courtesy of J. Lettry)
Simulation of stress wave propagation in Li lens (pbar source, Fermilab)
Notes: Ta-rod after irradiation with 6E18 protons in 2.4 s pulses of 3E13 at ISOLDE

## Slide 10: Thermal Shock
Methods to overcome thermal shock:
  Material Selection
    High specific heat
    Low coefficient of thermal expansion
    Low modulus of elasticity
    High strength (tensile and fatigue) at elevated temperature
  Segment target length
  Avoid stress concentration prone target shapes
  Pre-load in compression
  Manipulate beam parameters (spot size, intensity)
Must design for accident conditions
  Maximum intensity and smallest spot size
  Mis-steered beam on target

## Slide 11: Thermal Shock in CW and Liquids
Must take thermal shock into account for CW beams:
  Quickly rotating or moving targets create pulse-like loading
Liquid targets also react poorly to pulsed beam
  Contained liquid gives rise to cavitation
  Free liquid may disperse rapidly
  Rapidly flowing targets create pulse-like loading
FRIB Target Test. Rotating graphite wheel (5,000 rpm). Courtesy of G. Bollen, W. Mittig, et al.

## Slide 12: Thermal Shock in CW and Liquids
SNS Liquid Mercury Target Test. B. Reimer, et al.
MERIT Experiment (mercury jet), H. Kirk, et al.

## Slide 13: Radiation Damage
Displacements in metal crystal lattice
  Embrittlement
  Creep
  Swelling
Damage to organics/plastics
  Cross-linking (stiffens, increase properties)
  Scission (disintegrate, decrease properties)
Molecular Damage Simulations of peak damage state in iron cascades at 100K.
R. E. Stoller, ORNL.

## Slide 14: Radiation Damage
Tungsten cylinders irradiated with 800 MeV protons and compressed to 20% strain at RT.
  A) Before irradiation
  B) After 3.2 dpa
  C) After 14.9 dpa
  D) After 23.3 dpa
Data exists for neutron irradiation, less for proton irradiation
  Gas production much higher for high energy particle irradiation
S. A. Malloy, et al., Journal of Nuclear Material, 2005. (LANSCE irradiations)

## Slide 15: Physics/Target Survival Optimization
Physics and Target Survival are generally in opposition
  Beam spot size
  Beam power
  Target dimensions
  Optics considerations
Effects must be understood by both sides
Compromise must be reached in an iterative process

## Slide 16: Physics Optimization
Physics Simulation
(Full optics or reduced set, Figure of Merit)
Energy Deposition Simulation
Target Design
Iterative process makes it difficult to isolate the design efforts
Figure of Merit helps to reduce simulation requirements
Leads to novel target ideas (multiple materials, spherical targets)

## Slide 17: Motivation!

## Slide 18: What future facilities pose which target challenges?
PASI (Proton Accelerators for Science and Industry) High Power Targets and Machine Interface Working Group (Jan, 2012)
  Reviewed target challenges across proposed facilities
  Resulted in identification of:
    Cross-cutting target issues ripe for R&D
    Niche target issues for focused R&D
  Points the way for future HPT R&D program

## Slide 19
The Matrix | Target Technology Issue/Challenge |  |  |  |  |  |  |  |  |  | 
Potential Facility | High Heat Flux Cooling | Thermal "shock” (solid) | Thermal "shock" (liquid, incl. cooling medium) | High Magnetic Field (rad damage to sc cond) | Novel Target/Window Design | Liquid Metals | Radiation Damage and Corrosion | Radiation Protection & Facility Design | Monitoring and Instrumentation |  | "Score" (Avg)
Neutrino (conv, SBL & LBL) | 5 | 8 | 8 |  | 8 |  | 8 | 6 | 5 |  | 6.86
Kaon (LE stopping) | 6 |  |  |  | 3 |  | 7 | 6 | 7 |  | 5.80
Muon (LE stopping) | 6 |  |  | 7 | 3 |  | 7 | 6 | 7 |  | 6.00
Spallation (ISOL) |  |  |  |  |  |  |  |  |  |  | 0.00
Spallation (M&LS, UCN) | 8 | 9 | 10 |  | 4 | 3 | 7 | 4 | 8 |  | 6.63
ADS Demo | 8 |  |  |  | 8 | 7 | 7 | 8 | 8 |  | 7.67
NuFact/Muon Collider | 10 | 10 | 10 | 10 | 5 | 10 | 10 | 10 |  |  | 9.38
Medical Applications |  |  |  |  |  |  |  |  |  |  | 0.00
Security Applications |  |  |  |  |  |  |  |  |  |  | 0.00
"Score" (Avg) | 7.17 | 9.00 | 9.33 | 8.50 | 5.17 | 6.67 | 7.67 | 6.67 | 7.00 |  | 
Count | 6.00 | 3.00 | 3.00 | 2.00 | 6.00 | 3.00 | 6.00 | 6.00 | 5.00 |  | 
Score X Count/6 | 7.17 | 4.50 | 4.67 | 2.83 | 5.17 | 3.33 | 7.67 | 6.67 | 5.83 |  | 
 | 1.667 | 5.31 |  |  |  |  |  |  |  |  | 
Rate 1 through 10 (1 is not difficult, 10 is extremely challenging) |  |  |  |  |  |  |  |  |  |  | 

## Slide 20: Matrix Results
Weighted Averages (least to greatest)
  2.83 High Magnetic Field (SC radiation protection)
  3.33 Liquid Metals (Pumping, Heat exchanger, etc.)
  4.50 Thermal “shock” (solid)
  4.67 Thermal “shock” (liquid)
  5.17 Novel Target/Window Design
  5.83 Monitoring & Instrumentation
  6.67 Radiation Protection and Facility Design
  7.17 High Heat Flux Cooling
  7.67 Radiation Damage

## Slide 21: Matrix Results – “Niche” Impact (con’t)
High Scores for Selected Facilities
  9.00 Thermal “shock” (solid)
    Neutrino (super-beam) (8)
    Spallation (9)
    NuFact/Muon Collider (10)
  9.33 Thermal “shock” (liquid, incl. cooling medium)
    Neutrino (super-beam) (8)
    Spallation (10)
    NuFact/Muon Collider (10)

## Slide 22: Cross-cutting R&D Activities Identified
Radiation Damage
  Correlation of radiation damage effects of LE neutron to HE proton irradiation
    Gas Production
    Dose Rate
    Requires dedicated Material Scientists
    Will require validation testing
  In-beam (>100 MeV proton?) irradiation testing
    Program to support LE to HE damage correlation
    Materials picked from potential target materials
      Low-Zed (graphite, Be)
      Med-Zed (Al, Albemet, Ti alloys)
      High-Zed (Tungsten, Inconel, SS)
    Study Annealing Effect for various materials
    Collect and correlate world data?? Facility?? Funding?? PIE??

## Slide 23: Cross-cutting R&D Activities Identified (con’t)
Radiation Protection and Facility Design
  Participate in conceptual design and review of potential facility design
    Operational experience informing design
    Cradle to Grave mentality
    Largest impact on “up-time” after fundamental design
  Verification/Benchmarking of Simulation Codes
    Residual Radiation
    Complex “gap” geometries
    Tritium migration
  Remote Handling Tools and Methods
    “Shark Cage” Cold Cell
    Volume Reduction Tools
  Novel/Exotic Shielding Materials

## Slide 24: Cross-cutting R&D Activities Identified (con’t)
Novel Target/Window Design
  Development of alternative technologies
    Pebble Bed
    Powder (confined and jet)
    Waterfall

## Slide 25: “Niche” R&D Activities Identified
Thermal “Shock”, Liquid
  Cavitation/Erosion Mitigation
    Bubbles
    Gas Wall
    Coatings/Treatments
  Benefits:
    Neutrino (super-beam) (8)
    Spallation (10)
    NuFact/Muon Collider (10)

## Slide 26: “Niche” R&D Activities Identified
Thermal “Shock”, Solid
  “Single-pulse” Testing
    Simulation validation (elastic-plastic)
    Failure Criteria validation
    Wide parameter space
      Materials
      Temperature
      Load rate
      Irradiated state
  Benefits:
    Neutrino (super-beam) (8)
    Spallation (10)
    NuFact/Muon Collider (10)

## Slide 27: “Niche” R&D Activities Identified
High Magnetic Field (SC Rad Protection)
  Irradiation Testing of SC wire/tape and insulation
    Limits
    Annealing Parameters
  Novel Shielding Materials??
  Benefits:
    Muon (LE stopping) (7)
    NuFact/Muon Collider (10)

## Slide 28: “Niche” R&D Activities Identified
Liquid Metals
  Pumping, Filtering, and Handling
    Erosion Limits
    Material Compatibility (LME, etc)
    Contamination Control
    Freeze-plug mitigation
  Containment/Clean-up
    Technologies and methods
    Reactions and Radiochemistry (Polonium?)

## Slide 29: “Deliverables”
Next 12 months:
  Form an inter-disciplinary team between STFC, Fermilab and allied institutions to foster long term expertise in understanding the response of materials to radiation damage in the high energy proton regime. This represents an excellent opportunity to attract experienced radiation material scientists working with material science post-docs as core members of the team. This expertise is also broadly applicable to developing carbon-free energy technologies, thereby promoting knowledge exchange.
  Participate in conceptual design and review activities of potential facilities (e.g. LBNE, Project X, ISIS Upgrades).
  Design of single pulse tests to explore failure modes for solid target materials at suitable facilities (e.g. HiRadMat at CERN, LANSCE at LANL).

## Slide 30: “Deliverables”
5 Year Goal
  Build a cohesive and coherent target systems team allowing complementarity of facilities and personnel working towards the design of next generation projects. The proposed joint post-doc program between Fermilab and STFC is an excellent opportunity to build critical core competencies.

## Slide 31: Current HPT Activities
Radiation Damage Program Proposal (FNAL/Oxford)
Beryllium Target/Window R&D
  Simulation of LBNE conceptual design (FNAL/RAL)
  Single-pulse failure (thermal shock) testing (FNAL/CERN)
  NOvA beamline (thermal shock) test (PNNL)
Remote Handling/Facility Design for Radiation Protection (FNAL/ORNL/ISIS)
Efforts to Coordinate HPT R&D Efforts as a Program

## Slide 32: Radiation Damage Program Proposal
Collaborative Research into the Response of Materials to Radiation Damage from High Energy Protons
  Conveners of the High Power Particle Production Targets Working Group, PASI 2012: J Thomas (UCL), CJ Densham (STFC RAL), R Tschirhart (FNAL), P Hurh (FNAL)
  Contributing authors: SG Roberts (University of Oxford), C English (NNL), J Hyde (NNL), J Marrow (University of Oxford)
  08 Mar 2012

## Slide 33: Radiation Damage Program Proposal
The following materials have been identified as being of particular interest for targets and beam windows:
  Titanium alloys, e.g. Ti6Al4V, for high pulsed power density beam windows
  Graphite for existing neutrino facility targets
  Beryllium for beam windows and future ‘conventional’ neutrino facility targets
  Tungsten with or without tantalum cladding for spallation neutron source targets and muon production targets
The ultimate ambition is to be able to predict operating lifetimes for as many of the above materials as possible in terms of integrated proton fluence for the high energy proton accelerator parameter space (e.g. temperature, dose rate, duty factor, dynamic stress) while accepting that such predictions are inherently challenging and may not be expected to be applied to safety critical items.

## Slide 34: Radiation Damage Program Proposal
Stage 1: 6 Month Exploratory Phase
  Recruit Materials Science Post-doc
  Review current state of the art considering candidate materials
  Determine further experimental work
Stage 2: 2 Years of Research Activities
  Irradiations
  PIE
  Data Analysis
Stage 3: 1 Year of Results Reporting

## Slide 35: Radiation Damage Program Proposal
LBNE graphite radiation damage testing at BLIP (BNL)
  Low irradiation temperature (140 C)
  Low DPA (0.15)
  Large effects seen (TS, K, CTE)
  Annealing “heals” defects
Proposal for high energy proton radiation damage R&D programme
  Oxford Materials for Fusion and Fission Power
  Beryllium, Graphite, Titanium, Tungsten
  3-1/2 year programme

## Slide 36: In Summary: Coordinated HPT R&D Required
R&D needing test stands
  Radiation Damage Testing
  Thermal Shock (Solid and Liquid)
R&D possibly needing test stands
  Cooling Methods
  Novel Target Designs
R&D that can be done in operating facilities
  Radiation Protection & Facility Design

## Slide 37: In Summary: Coordinated HPT R&D Required
Radiation Damage Testing to establish design properties
  Irradiate samples or identify existing, suitable materials
    > 100 MeV?
      (could be lower for micro-mechanical testing, but need H/He implantation as well)
    0.1 – 10 DPA
  PIE (mechanical and thermal properties)
    Micro-mechanical (take advantage of small, thin samples)
    Bulk-mechanical and thermal
Thermal Shock (Solid)
  “Single pulse” high intensity failure testing
    Validate simulations
    Verify failure criteria
    Energy deposition of 100-400 MJ/m3/pulse
    Relatively short pulses (1-10 microseconds)

## Slide 38: In Summary: Coordinated HPT R&D Required
Past and current HPT R&D efforts have been initiated and funded by individual experiments
  Narrow focus
  Inadequate funding
  Little to no coordination with other efforts
Most of the underlying challenges are very similar.
Coordinate the HPT R&D efforts and possibly fund as separate program
  Build the HPT expertise as a core competency
  Broaden focus of R&D efforts
  More efficient use of funds
  All HPT applications will benefit

## Slide 39: In Summary: Coordinated HPT R&D Required
Targetry requirements (not just targets) must be understood as soon as possible to meet Project X stage 1 goals (beam parameters, materials)
Identify most urgent and mutually beneficial HPT R&D activities
Continue to develop HPT R&D program utilizing complementary resources at collaborating institutions
Build HPT as a core competency at Fermilab to meet the research program’s needs in a timely fashion

## Slide 40: In Summary: Coordinated HPT R&D Required
Looking for input from you:
  Experiment target/beam requirements
  Share target facility experiences
  Recommend future direction for target R&D program
  Identify synergies among laboratories and universities
  Coordinate HPT R&D and conceptual design efforts

## Slide 41: Additional slides, if time…

## Slide 42: LBNE Graphite R&D
Why Graphite?
  Excellent for thermal shock effects (lower CTE, very low E, high strength at high temperatures)
  Not toxic (no mixed waste created)
  Readily available (inexpensively) in many grades and forms
Why not Graphite?
  Rapid oxidation at high temperatures
  Radiation damage

## Slide 43: Graphite R&D: Radiation Damage
Rapid degradation of properties at relatively low levels of DPA
Evidence of complete structural failure at 1e21 p/cm2 (BLIP test)
N. Maruyama and M. Harayama, “Neutron irradiation effect on … graphite materials,” Journal of Nuclear Materials, 195, 44-50 (1992)

## Slide 44: Graphite R&D: Irradiation Testing at BLIP
Working with N. Simos and H. Kirk at BNL to test samples irradiated by 181 MeV proton beam at BLIP
Testing for:
  Tensile properties (YS, UTS, …)
  Coef. of thermal expansion
  Conductivity
Most samples encapsulated in argon filled, stainless steel capsules to isolate from water cooling bath
About 150 samples in total
Tensile samples have gauge width of 3 mm and thickness of 1 mm

## Slide 45: Graphite R&D: Irradiation Testing at BLIP
Material | # Tensile | # CTE | K | Motivation
C-C Comp (3D) | 10 | 8 | ? | First BLIP test showed massive failure
POCO ZXF-5Q | 21 | 6 | .46 | NuMI/NOvA target material
Toyo-Tanso IG 430 | 42 | 6 | .51 | “Nuclear Grade” used for T2K
Carbone-Lorraine 2020 | 21 | 6 | .60 | CNGS target material
SGL R7650 | 21 | 6 | .66 | NuMI/NOvA Baffle material
Saint-Gobain AX05 hBN | 0 | 6 | .80 | Highest K wild card (low flex strength)
K Factor is a thermal shock resistance parameter used by Luca Bruno to evaluate candidate materials for targets/windows
  K=(UTS*Cp)/(E*CTE)

## Slide 46: Graphite R&D: Irradiation Testing at BLIP
Irradiation run complete
Currently finishing testing phase
Preliminary results now available
Additional testing could be done this summer
181 MeV proton beam
Peak integrated flux about 5.9e20 proton/cm2
Corresponds to 0.14 DPA

## Slide 47: Graphite R&D: Irradiation Testing at BLIP
Water immersed c-c samples showed structural damage (as before).
Argon encapsulated c-c and graphite samples showed little damage (not pictured here)

## Slide 48: Graphite R&D: Irradiation Testing at BLIP

## Slide 49: Graphite R&D: Irradiation Testing at BLIP

## Slide 50: Graphite R&D: Irradiation Testing at BLIP
CTE of almost all graphite samples reduced after irradiation (0.07-0.14 DPA) on first thermal cycle to 300 ˚C depending on graphite type
After first cycle CTE is increased to about 10% more than un-irradiated samples, regardless of graphite type
This behavior is consistent with annealing behavior of materials. Interstitial atoms created by the irradiation drop back into the lattice. Any heating above the irradiation temperature will make the interstitials more mobile.
Since, after annealing to 300 C, we still see damage effects, low temperature annealing does not fully “heal” the material. There may be different mobilization temperatures for vacancy defects than for interstitial defects in graphite due to the HCP lattice. This needs further research.

## Slide 51: Graphite R&D: Irradiation Testing at BLIP
Chart: Toyo Tanso IG-430 (T44) at 0.056 DPA

## Slide 52: Beryllium R&D: Conceptual Design Studies at STFC-RAL
Graphite radiation damage issues prompted LBNE to look at Beryllium as an alternative target material for 2+ MW proton beam power
Accord with (STFC) RAL’s Target Engineering Group
  Beryllium target simulations at 2+ MW
  Integrated Be target and horn conceptual design
  Cooling technology R&D (gas, water, water spray)
  Proton beam window conceptual design
  Air cooled Be target for 700 kW
High Power Target Group:
CJ Densham
O Caretta
TR Davenne
MD Fitton
P Loveridge
M Rooney
Focus On:

## Slide 53: Beryllium R&D: Be Target Simulations
Analysis encompasses:
  Physics (FLUKA) – Energy Deposition & Figure of Merit
  Thermal/Structural (ANSYS)
  Dynamic/Stress-wave (Autodyn & ANSYS)
  Off-center beam cases
Beam Parameters:
Proton Beam Energy (GeV) | Protons per Pulse | Repetition Period (sec) | Proton Beam Power (MW) | Beam sigma, radius (mm)
120 | 4.9e13 | 1.33 | 0.7 | 1.5-3.5
60 | 5.6e13 | 0.76 | 0.7 | 1.5-3.5
120 | 1.6e14 | 1.33 | 2.3 | 1.5-3.5
60 | 1.6e14 | .76 | 2 | 1.5-3.5
Pulse Length = 9.78 micro-sec

## Slide 54: Beryllium R&D: Be Target Simulations: Structural
Representative plot of equivalent stress
End of Pulse
120 GeV, 0.7 MW beam
9mm radius Be
Sy~270 MPa at 150 C

## Slide 55: Beryllium R&D: Be Target Simulations: Structural (non-dynamic)
Stresses probably too high for 2 MW cases with 1.5 mm beam sigma radius, but well within reason for 3.5 mm beam sigma radius
Room for optimization (in length as well)!

## Slide 56: Beryllium R&D: Be Target Simulations: Dynamic
2.3 MW
120 GeV
3.5 mm sigma spot
Compare to 88 Mpa for static case (double)
Mainly longitudinal stress- waves

## Slide 57: Beryllium R&D: Be Target Simulations: Dynamic
2.3 MW
120 GeV
3.5 mm sigma spot
50 mm Segments
Peak eqv stress reduced to 109 MPa from 173 MPa

## Slide 58: Beryllium R&D: Be Target Simulations: Off Center Beam
2.3 MW
120 GeV
3.5 mm sigma spot
2 sigma offset
Clearance to Horn Inner Conductor is ~5mm
Bending stress and resonance is a problem
Target will need radial supports

## Slide 59: Beryllium R&D: Be Target Simulations: Spherical

## Slide 60: Beryllium R&D: Be Target Simulations: Spherical
Spherical shape advantages
  Eliminates stress concentrations
  Reduces dynamic stress
  Allows pions to escape
  Allows cooling in target central area

## Slide 61: Summary
Although challenging, critical design issues have been identified for high power, solid targets
Graphite radiation damage testing at BNL
First stage Be target design study by RAL shows promise of Be target for LBNE at 2.3 MW
Future work includes:
  Continuation of graphite sample testing
  Further Be design studies
  Be target testing at new High RadMat Facility (CERN)?

## Slide 62: Thanks to all
N. Simos, J. Misek, H. Kirk, J. O’Conor, C. Densham, T. Davenne, P. Loveridge, M. Fitton, M. Rooney, O. Caretta, J. Hylen, R. Campos, N. Mokhov, T. Grumstrup, R. Zwaska, V. Sidorov, A. Leveling and many others…

## Slide 63: Additional slides, if time…

## Slide 64: Thermal Shock
Work at RAL-Sheffield by R. Bennett and G. Skoro to study solid targets for NuFact
  Pulsed Ta & W wire testing
  Benchmark simulation techniques
  Show promise of solid W at 4 MW
Upcoming Publications:
  G.P. Skoro et al. / Journal of Nuclear Materials 409 (2011) 40–46
  Nuclear Inst. and Methods in Physics Research A, DOI:10.1016/j.nima.2011.03.036

## Slide 65
  Introduction Current pulse – wire tests at RAL
Tantalum wire – weak at high temperatures
  Tungsten – much better!!!
The Finite Element Simulations have been used to calculate equivalent beam power in a real target and to extract the corresponding lifetime.

## Slide 66
Yield strength of tungsten – our results
Combination of visual observation of the wire and LS-DYNA simulations
Stress in
NF target

## Slide 67: Thermal Shock
SNS Hg Target Cavitation problems
J. Haines, B. Riemer, ORNL

## Slide 68: Beryllium R&D: Be Target Simulations: FoM
Figure of Merit
  Provide simple, faster way to gauge effects of target/beam parameter changes on yield of neutrinos of interest
  Proposed by R. Zwaska
Notes: The FoM is calculated using FLUKA to obtain the yield of pions of both signs emerging from the target into the surrounding vacuum. The specific output taken from FLUKA is the plain double differential yield of pions of both signs with respect to the kinetic energy and the transverse momentum of the pions, i.e.where,␣N = number of pions of both signs emerging from the target per primary particle on target ␣E = kinetic energy of the pions [GeV] ␣p = transverse momentum of the pions [GeV/c]We can then obtain the yield of pions per incident proton on target as a function of energy and transverse momentum. To do this a simple numerical integration of the double differential yield is carried out between the following limits :␣kinetic energy from 1.5GeV to 12GeV with 21 discrete intervals of width 0.5GeV ␣transverse momentum between 0 and 0.4GeV/c with a single intervalFigure 3.2.1 shows the resulting pion yield in histogram form. A weighting factor is then calculated for each of the 21 energy intervals which is equal to the energy at the centre of the interval raised to the power 2.5. The energy at the centre of each interval is given by :where for example for the first interval Emin=1.5GeV and Emax=2GeV. The FoM is calculated as the summation of the yield in each energy interval multiplied by the corresponding weighting factor for that interval expressed mathematically as follows.Figure 3.2.2. indicates that the majority of the pions from the target are towards the lower end of the energy range of interest. By integrating over 30intervals in transverse momentum from 0GeV/c to 1.5 GeV/c for three different energy levels the yield as a function of transverse momentum is obtained (Figure 3.2.3).

## Slide 69: Beryllium R&D: Failure Criteria – Simulation versus Reality
Predicted Peak Energy Deposition for LBNE 2.3 MW with 1.5 mm beam sigma radius was 846 J/cc and thought to cause stresses too high for Be to survive
But P-bar Target (FNAL) has a Beryllium cover that regularly sees 1000 J/cc and shows no evidence of damage
ANSYS analysis for similar conditions suggests peak equivalent stresses of 300 Mpa (elastic-plastic, temp-dependent mat’l properties, but not dynamic)
Dynamic stresses could be 30-50% higher

## Slide 70: Beryllium R&D: Failure Criteria – Simulation versus Reality
120 GeV
0.2 mm sigma
Elastic/plastic
Temp Dependent Mat’l Properties
Peak Seqv is 300 MPa
Peak Temp is ~800 C
Be Melting Temp is 1278 C
Be UTS at 600 C is ~150 MPa

## Slide 71: Beryllium R&D: Failure Criteria – Simulation versus Reality
Rotated 17 degrees every pulse
Moved 1 mm vertically every 2e17 protons
Typical beam sigma was 0.195 mm (last 1-2 months of running at 0.15 mm)
Typical ppp was 8E12
This target saw about 5e6 pulses at the time photo was taken
Pbar Target 7 without Be cover. Inconel Target Material is Consumable!

## Slide 72: Beryllium R&D: Failure Criteria – Simulation versus Reality
Possible explanations
  Small areas of deformation not visible
    Analysis indicates about 0.05 mm of plastic deformation on surface in an outward “bump” with diameter of about 1 mm
  Beam profile is not gaussian
    At such small sigma, peak energy deposition would be reduced greatly if profile were flat in center of beam
  Fast energy deposition rate creates high strain rates
    Yield strength of metals increases for high strain rates

## Slide 73: Beryllium R&D: Failure Criteria – Simulation versus Reality
Max strain predicted is 0.01 strain
Pulse length is 1.6 micro-sec
Strain rate is over 6,000 s-1
For LBNE 2.3 MW, 3.5 mm sigma, strain rate=100 s-1
For LBNE 2.3 MW, 1.5 mm sigma, strain rate=340 s-1

## Slide 74: Beryllium R&D: Failure Criteria – Simulation versus Reality
Yield and Ultimate Stresses increase by 25-40% at strain rates greater than 100 s-1
Significant increased hardening as well
F.L. Schierloh and S.G Babcock, Tensile Properties of Beryllium at High Strain Rates and Temperatures, AFML-TR-69-273, General Motors Tech Center, 1969
S200E Be
T Nicholas, et al., Mechanical Properties of Structural Grades of Beryllium at High Strain Rates, AFML-TR-76-168, Air Force Materials Laboratory, Wright Patterson Air Force Base, Ohio, 1976
UTS vs strain rate

## Slide 75: Beryllium R&D: Failure Criteria – Simulation versus Reality
Damage seen on Be Lithium Lens Windows
Just DS of Target
Higher Temperature
Higher Stress (10,000 psi of Li pressure on other side)
Damage observed after 8 months of running at reduced spot size of 0.15 mm sigma and not at larger spot size (0.19 mm sigma)

## Slide 76: Beryllium R&D: Failure Criteria – Simulation versus Reality
More work needs to be done in this area to set limits of Be in high power proton beams
  Effects of irradiation and temperature
  Refined simulation of actual conditions
  In beam validation/benchmarking test
For now, set conservative limits and push the envelope later…