## Slide 1: MQXFA08 SG Data History
L. Garcia Fajardo, D. Cheng, P. Ferracin, G. Vallone
02/17/2022
LBNL

## Slide 2: MQXFA08 SG Gauges Layout
Only HBM gauges are installed.
Shell gauges --- three axial locations:
  Shell gauges (T & Z): on shell 2, 4, & 7
Coil gauges (T & Z): on the axial location of 3989 mm (RE) from LE.
Rod stations are located on the RE
  Each station is full bridge with four individual gauges.
LE
RE
MID
Shell 2
Shell 4
Shell 7
Coil Stations
Coil Stations
RE axial plate assembly
Rod Stations

## Slide 3: MQXFA08 test timeline
1st Thermal Cycle: From 10/28/2021 to 11/22/2021 (1st Cooldown to 1st Warmup)
2nd Thermal Cycle: From 12/04/2021 to 12/20/2021 (2nd Cooldown to 2nd Warmup)
3rd Thermal Cycle: From 01/07/2022 to 02/10/2022 (3rd Cooldown to 3rd Warmup)

## Slide 4: Process History (includes preload, thermal cycles, all quenches and some ramps)

## Slide 5: SG Data History (only quenches and some ramps) – Coils Axial
Quenches at 4.5 K:
12, 17, 18, 32-36, 42-44
Ramps at 20 A/s:
1-12, 15, 19-26, 30, 32, 36, 37, 41, 42, 45

## Slide 6: SG Data History (only quenches and some ramps) – Coils Azimuthal

## Slide 7: SG Data History (only quenches and some ramps) – Rods Axial

## Slide 8: SG Data History (only quenches and some ramps) – Shell07 Azimuthal

## Slide 9: Cooldown (coils’ axial behavior)

## Slide 10: Cooldown – Coils Axial behavior
1st Cooldown
2nd Cooldown
3rd Cooldown

## Slide 11: Quenches 1 and 16 (coils’ azimuthal and axial behavior, and rods’ axial behavior)

## Slide 12: Quenches 1 and 16 – Coils Azimuthal and Axial behavior -- Delta
Quench 1 (20 A/s)
Quench 16 (100 A/s)

## Slide 13: Quenches 1 and 16 – Rods Axial behavior -- Delta
Quench 16 (100 A/s)
Quench 1 (20 A/s)

## Slide 14: MQXFA06, 07 and 08: Coils’ azimuthal stress corrected with averaging up- and down-ramps

## Slide 15: MQXFA06-MQXFA08 Unloading Comparison, corrected Ramps, Deltas
MQXFA07
Ramp to 15500 A
MQXFA06
Ramp to 16530 A
MQXFA08
Ramp to 16530 A

## Slide 16: Appendix Quenches 12, 17 and 18: quenches at 4.5 K during the 1st thermal cycle

## Slide 17: Quenches 12, 17 and 18: quenches at 4.5 K during the 1st thermal cycle
Quench 12
Quench 17
Quench 18

## Slide 18: E.M. Effect is Apparent on Coils and Shell 7 (this example is for magnet 5 but applies to all)
Despite not yet fully processing the files, the gauge readings of the coils and the shell 7 appear to be noisy during current ramps
Similar effects have been observed in earlier magnets
The noise on the signals is most likely from the dI/dt.
LP Filter
Cutoff frequency:0.25 Hz
Clean signal
Clean signal
Noisy signal
(note the different scale from Shells 02 and 04 plots)
Noisy signal

## Slide 19: Reference: MQXFA03 Coil Azimuthal --- over I2
LP Filter
Cutoff frequency:0.25 Hz
C204
C110
C111
C204 ramp up
C204 ramp down
C110 & 111 ramp up
C110 & 111 ramp down
The readings of this part may the combination of actual SG and inductive components
Combined the ramp up and ramp down data, the three coils actually behave identically.
The readings of the “turn around” part are likely to be combined with inductive components;
The “up-warp” on the curves of C110 & 111 may be not mechanical. It is “bended” by the field.
Inorm = 16.47 kA

## Slide 20: MQXFA04 Coil Strain --- over I2
The exact same behavior as seen in MQXFA03 (next slide).
From what we have learned from MQXFA03, there is no issue in the 10 kA ramp tests.
Inorm = 16.47 kA