## Slide 1: Lab 6 Polystyrene Polymer Tests

## Slide 2: Oven Run PS Pellet Casting

## Slide 3: Oven Run Sample Measurements
Measurements performed using: Agilent Cary 60 UV-Vis Spectrophotometer

## Slide 4
Sample Identification: |  |  |  |  |  | 
Sample #: Year (Month) - Gaylord Number/Total Gaylords in Purchase |  |  |  |  |  | 
Oven Run 2/22 |  |  |  |  | Batch/Lot #: | 
OR2-22_1 = 1: 2002 (Aug.) - Box 98 |  |  |  |  | QE13020522 | 
OR2-22_2 = 2: 2003 (Mar.) - Box 48 |  |  |  |  | QE13020522 | 
OR2-22_3 = 3: 2022 (Jan.) - Sample Drum |  |  |  |  | K1101HR101 | 
OR2-22_4 = 4: 2022 (Jan.) - Sample Drum |  |  |  |  | K1101HR101 | 
OR2-22_5 = 5: 2002 (Aug.) - Box 98 |  |  |  |  | QE13020522 | 
OR2-22_6 = 6: 2003 (Mar.) - Box 48 |  |  |  |  | QE13020522 | 
Oven Run 1/22 |  |  |  |  | Batch/Lot #: | 
OR1-22_4 = 4: 2008 (Sep.) - Gaylord 8/26 |  |  |  |  | WH19048L12 | 
OR1-22_5 = 5: 2010 (Jun.) - Gaylord 10/27 |  |  |  |  | XG19048L11 | 
OR1-22_6 = 6: 2013 (Aug.) - Gaylord 18/26 |  |  |  |  | 724809600 | 
OR1-22_8 = 8: 2016 (Nov.) - Gaylord 7/26 |  |  |  |  | E1029HR101 | 
OR1-22_11 = 11: 2018 (Nov.) - Gaylord 2/26 |  |  |  |  | G1014HR101 | 
OR1-22_12 = 12: 2021 (Sept.) - Gaylord 1/25 |  |  |  |  | K0811HR101 | 
*All samples made of pure PS pellets and cut/polished into 7cm lengths |  |  |  |  |  | 

## Slide 5
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized

## Slide 6: Polystyrene %T over Time
 | %Transmittance |  |  |  | 
Wavelength: | 390nm | 405nm | 420nm | 450nm | 500nm
2002 | 61.76795 | 71.93742153 | 78.13495 | 85.35968 | 91.69676
2003 | 60.525 | 70.49690937 | 76.42775 | 83.55524 | 90.4177
2008 | 54.23589 | 70.17348616 | 80.58712 | 89.44572 | 94.48749
2010 | 63.27138 | 74.04961484 | 80.39898 | 87.02418 | 92.02607
2013 | 65.41401 | 78.00700388 | 84.8095 | 90.80903 | 94.82824
2016 | 63.65202 | 77.45036239 | 85.10389 | 91.4707 | 95.31595
2018 | 65.13605 | 76.32921728 | 82.9106 | 89.1824 | 93.57134
2021 | 52.94145 | 67.08357431 | 75.12062 | 82.70656 | 88.20972
2022 | 50.40762 | 64.77253229 | 73.84831 | 82.05732 | 87.74345

## Slide 7
Chart: PS % Transmittance over Time
| 2002 | 2003 | 2008 | 2010 | 2013 | 2016 | 2018
390nm | 61.768 | 60.525 | 54.2359 | 63.2714 | 65.414 | 63.652 | 65.136
405nm | 71.9374 | 70.4969 | 70.1735 | 74.0496 | 78.007 | 77.4504 | 76.3292
420nm | 78.1349 | 76.4278 | 80.5871 | 80.399 | 84.8095 | 85.1039 | 82.9106
450nm | 85.3597 | 83.5552 | 89.4457 | 87.0242 | 90.809 | 91.4707 | 89.1824
500nm | 91.6968 | 90.4177 | 94.4875 | 92.0261 | 94.8282 | 95.3159 | 93.5713

## Slide 8
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized

## Slide 9: Polystyrene %T for Various Lots (“Greying”)
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized

## Slide 10: Upcoming Testing:
Polystyrene Reference from Monomer (Polymerization Run)
INEOS PS Pellets (PS 1200 & PS 153F)