## Slide 1
PIP-II 2nd Technical Workshop, WG#2
Cavity Jacketing Experience at FNAL
Chuck Grimm
Fermilab
12-14 July 2022

## Slide 2: Outline
Background Information
Tooling and Equipment
  Cantilever and Rotation Fixtures
  Glovebox – Gas Distribution System
Cavity and Helium Tank Configurations
  Cavity Beam Flanges
  Fundamental Power Coupler and Field Pickup Flanges
  Helium Tank, Bellow, and Titanium End Caps
Assembly and Tack Welds
  Assembly Setup on Cantilever Fixture
  Tack Welding
Glovebox Welding
  Weld Map and In-Process Weld Examination Forms
  Welding Sequence
  Gas Flows and Internal Cavity Purging
  RF and O2 Monitoring
  Final Frequency Shift and Field Flatness
Pressure Test, Leak Checks, and Traveler
Lessons Learned
Summary

## Slide 3: Background Information
Experienced cavity jacketing teams
  Lead Engineer
  RF Engineer
  Welder
  Support Technicians
Over 60 cavities of various frequencies and beta versions dressed to date
  3.9 GHz
  1.3 GHz
  HB650
  LB650
FNAL jacketed all 6 cavities for the prototype HB650 cryomodule

## Slide 4: Tooling and Equipment
Main Tooling
Rotation Fixture
Cantilever Fixture

## Slide 5: Tooling and Equipment
Glovebox
Gas Distribution System

## Slide 6: Cavity and Helium Tank Configurations
Cavity Flange Configurations
Beam Flanges with RF Feedthroughs
Coupler Flange with VCR Fitting
FP Flange with Valve

## Slide 7: Cavity and Helium Tank Configurations
Helium Tank Configuration
VCR Cap
VCR Purge Line Connection
Foam Plug in Tee Ends (*)
* Foam in Bi-Metal Transition

## Slide 8: Assembly and Tack Welds
Cantilever Fixture Assembly Setup
RRCAT-502
Bellow and Ti Endcap
Helium Tank

## Slide 9: Assembly and Tack Welds
Critical FPC Flange Alignment
FPC Flange Must Rest on Machined Ledge for Proper Cavity Clocking

## Slide 10: Assembly and Tack Welds
Tack Welding
Tack Location
Shielded Cup used for “Open Air” Tack Welding
FPC End Fully Tacked
Tack Location
No Tacks,
Float Location During Welding
FPC End
Pickup End

## Slide 11: Glovebox Welding
Weld Map

## Slide 12: Glovebox Welding
In-Process Weld Examination Forms (J2-J5)

## Slide 13: Glovebox Welding
Bellow Welding – Weld (J2)
Bellow Tack
Bellow Welding

## Slide 14: Glovebox Welding
Tank Integration Welding – Weld (J3)
RF Cable
Completed J3 Weld
Internal Cavity Purge Line
Running 20 CFH Argon
Rotation Fixture

## Slide 15: Glovebox Welding
Tank Integration Welding – Weld (J4)
Completed J4 Weld
Weld Segments
~50mm long
Cavity Internal Purge Vent

## Slide 16: Glovebox Welding
Tank Integration Welding – Weld (J5)
Completed J5 Weld
Weld J5 Location

## Slide 17: Glovebox Welding
RF and O2 Monitoring
Program set to take RF measurements every minute during welding
Cavity RF Monitoring Station
O2 monitor actively displays ppm of O2 during welding
Actual O2 Reading During RRCAT-502 Welding

## Slide 18: Glovebox Welding
Final Frequency Shift and Field Flatness (RRCAT-502)
  All within specifications
Final RF Spectrum
Field Flatness Measurements
Both Graphs Courtesy of Timergali Khabiboulline
Beginning Average: 99.7%
Ending Average: 98.4%
Small loss of only ~1.3%
Beginning Measurement: 649.064 MHz
Ending Measurement: 649.013 MHz
~-50kHz Shift
Modes Separated by only 10 kHz

## Slide 19: Pressure Test and Leak Checks
Helium Vacuum Leak Check Performed Before and After Pressure Test
  Within specification
Performed Pressure Test Stepping up Pressure to 34.5 psig (2.3 bar)
  Passed, maximum pressure held for 10 minutes without loss
  Frequency shift from start to finish was +1 kHz

## Slide 20: Traveler
Assembly, Welding, Leak Checks, and Pressure Test Data Included
  This traveler and any other information regarding cavity jacketing can be shared with the collaboration partners/vendors -

## Slide 21: Lessons Learned
Visited RRCAT in February 2019 to help dress RRCAT-501
  Needed better active cavity cooling during welding to decrease wait times between weld segments – RRCAT wait times were several hours.
  Developed more efficient flow path of Argon on outside surface of cavity within the helium space of the tank.
  Introduced a method to flow cool Argon gas inside of the cavity during welding.
  These steps reduced wait times to 1 hour or less and helped minimize large frequency shifts, especially mode separation which influences the field flatness.
Pictures courtesy of RRCAT

## Slide 22: Lessons Learned
For RRCAT-502 there was a decision to weld the bellow onto the bare cavity first so that we can have the field flatness checked to see the impact of welding so close to the end cell stiffening ring.
  Bead pull measurements indicated that the weld J2 had no impact on frequency or field flatness.
  Future 650 cavities will have all welds performed at the same time

## Slide 23: Summary
Fermilab has a well-established team that has jacketed over 60 cavities of many frequencies and beta versions.
RRCAT-502 cavity jacketing was successful with very minimal frequency and field flatness changes from start to finish. This was true for all seven 650 cavities jacketed at FNAL.
Decision to use an Argon gas flow through the internal cavity surface helped to reduce time between weld segments and helped eliminate further RF drift changes after welding stopped.
All tooling, equipment, and infrastructure developed and validated to jacket 650 MHz cavities. Ready to transfer to industry.

## Slide 24
Thank you!

## Slide 25: Backup Slides
Tee Welding on Helium Vessels
  Some helium tanks will arrive without tee’s welded on
  Tooling was designed to accurately place and weld tee’s
  The precision machined tank bearing lugs are used as a reference point
  The same fixture is used for both HB and LB helium vessels