## Slide 1
Roadmap to determine 800C vs 900C HT
Genfa Wu
PIP-II Technical Meetings
13 July 2022

## Slide 2: Outline
Introduction
Road maps
Current status

## Slide 3: Introduction
Cryoplant capacity – 2,500 W (2K)
PIP-II 650 MHz cavities baseline processing – N-doping + flux expelled.
  HB650 3.3e10 (nominal)
  LB650 2.4e10 (nominal)
N-Doping or Mid-T baking
CW
High Q
Magnetic Hygiene and Flux Expulsion
High Rs sensitivity of trapped magnetic field
Nominal
Flux trapped LB650 at 1.5e10

## Slide 4: Minimize the Magnetic Field Trapping
<=3 mG trapped satisfies Q0 spec, 8 n total Rs .
Magnetic shield and hygiene
  Magnetic field at room temperature for 650 MHz <=5 mG.
Fast cool down
  Thermo-electric current of 8 mG on average.
Niobium capable of flux expulsion with required mechanical strength
  Niobium for 650 MHz requires flux expulsion capability >= 70%

## Slide 5: Road maps
Two parallel paths
  Sample studies
  Cavity studies
    Bare cavity road test with two end supports of the support cage
    Jacketed cavity pressure test and road test

## Slide 6: Road maps – sample studies
Measure YS of PIP-II material after 800C vs 900C
Is YS 900C sample ~ YS 800C sample in both cases?
No
Yes
Is YS at 900C < max stress on cavity, considering de-rating(20 Mpa)??
Yes, in both cases
No, in both cases
Measure YS of half-cell samples w 800C vs 900C
Good confidence that 900C is feasible in LB650s – to be confirmed with test on cavity
900C most likely not feasible in LB650s – to be confirmed with test on cavity since simulations may be affected by large errors
Yes but only in flat samples
Yes but only in half-cell samples
Proceed with YS measured on bended material
Tasks #2,4
Tasks #6
Tasks #13, 14
Courtesy of M. Martinello

## Slide 7
B61C-EZ-103
160um EP + 900C 3h + 2/0 N-doping + 7um EP
No
Transportation test
Jacketing
Pressure Test
Re-HPR
Re-processing
Recommend to not proceed with 900C
Recommend to proceed with B61C-EZ-102 jacketing
If rad. issues
If performance issues
VTS test
Successful ?
Yes
Successful ?
Yes
No
Successful ?
Yes
No
Proceed with 900C on B61C-EZ-102
Task #11
VTS test
Road maps – cavity studies

## Slide 8
B61C-EZ-102
120um EP + 900C 3h +
40 um EP +
2/0 N-doping + 7um EP
No
Transportation test
Jacketing
Pressure Test
Re-HPR + re-test
Re-processing + re-test
Recommend to proceed with 900C on production bare cavities
If rad. issues
If performance issues
VTS test
Successful ?
Yes
Successful ?
Yes
No
Recommend to not proceed with 900C
Contact partner labs to make sure the contract w cavity vendor is modified accordingly
Task #11
Road maps – cavity studies
B61C-EZ-103
Pressure test OK

## Slide 9: Current Status
B61-EZ-103 road test successful (See Jeremiah presentation)
  Additional road tests planned
B61-EZ-102 900C H-bake in progress
B61-EZ-101 and B61-EZ-104 are scheduled to be 800C H-baked tentatively

## Slide 10: Summary
The roadmap was defined
One bare cavity road test is in progress
  Result was promising
Need more data to determine the H-degas temperature.

## Slide 11: Thank You!