## Slide 1: Conductors for HTS Magnets: Why we need both REBCO coated conductors and round wire Bi-2212
David Larbalestier*
Applied Superconductivity Center
National High Magnetic Field Laboratory
Florida State University
Tallahassee, FL 32310 USA
*Opinions formed in many discussions with MagLab, BSCCo, VHFSMC, OI and SuperPower colleagues

## Slide 2: Part 1: What do we need for a secure HTS magnet technology?
A real applications pull that can generate continuous conductor orders
Conductors worth continuous orders
Coils, R&D Test Beds
27T with SuperPower
31T 2212 NHMFL
34 T YBCO NHMFL
HTS Magnet
Systems
32 T
Neutron scattering facilities
SMES + Muon Colliders
NMR
Conductors
YBCO
2212
2223??
Fe-base??

## Slide 3: Part 2. What do we need for a secure HTS magnet technology?
Conductors in length with assured, uniform and predictable performance
Cabled versions of the conductor
Effective thin insulations
Resistance to Lorentz and other coil forces
Quench protection
Affordability
Reliable performance under plausible service conditions

## Slide 4: 3 HTS conductors – so why only consider 2?
REBCO coated conductor tapes
Bi-2212 round wire ~ 1mm dia.
Bi-2223 tapes exhaustively studied for power applications 30-77K: How much more development is possible?
Bi-2223 multifilament tapes
2 mm Ag
20mm Cu
20mm Cu
50mm Hastelloy substrate
1 mm HTS
~ 30 nm LMO
~ 30 nm Homo-epi MgO
~ 10 nm IBAD MgO
< 0.1 mm
SuperPower

## Slide 5: Why not 2223?
Like REBCO it is delivered in the superconducting state ……
Like REBCO it is a high aspect tape, typically 4 mm x 0.2 mm thick
It is available in lengths > 1 km….
The one vendor (SEI) is commercially aggressive, often undercutting REBCO in cost and not losing in performance in the 30-77 K range for low fields
But…
It cannot be cabled to high Je
It appears near its asymptotic development (black box) limit

## Slide 6: Advantages
REBCO CC tape
Ready as delivered
Multiple developers worldwide
Very strong substrate
High Jw feasible – 300-500 A/mm2 in 20T
Could offer 30-60K operation – potentially transformative for magnet technology
Round wire 2212
Round wire form
Multifilament form
Isotropic properties
Easy path to cables
Low cost manufacture compatible with metal superconductor manufacture

## Slide 7: Disadvantages
REBCO CC tape
Single filament tape
Anisotropic shape and Jc with large magnetization
Plated Cu is costly and dimensionally loose
Low perpendicular strength complicates winding, impregnation and insulation
Thin Insulation is difficult
Manufacture is very specific to each process (black box)
Capital and skilled team intensive
Path to cables without loss of Jw not yet clear
Round wire 2212
Long length Je must be raised to best short Je
Filaments within bundle are coupled
Much less strong than REBCO – needs separate strengthener
Complex HT in pure O2 adds complexity at the magnet winder site
Insulations need development
Intrinsic anisotropy will limit use to less than 15 K

## Slide 8
Plot maintained by Peter Lee at: http://magnet.fsu.edu/~lee/plot/plot.htm
Peter Lee’s champion Je plot – HTS is good!

## Slide 9: An alternative view of the plot
REBCO test coils allow an overall Jcu that is unrealistic EXCEPT under circumstances where active quench detection and PROTECTION works and/or loss of the coil is tolerable – defects matter
Peter Lee plot is self-chosen best case plot
  What is typical?
  What is the mission critical result?
Length dependence and process dependence are very different for REBCO and 2212

## Slide 10: Snapshot of 2212 problems
Dedensification is the big problem
It can be controlled – see 2011 papers
See Hellstrom and Shen talks today
Malagoli et al in preparation

## Slide 11
uncorrelated but samples >100 A @77 K
are better than 140A @ LHe @ 14 T B||c
Poor correlation for REBCO between Ic @ 77 K SF and 4.2 K 14 T||c
de-convolution approach
(fitting exp(-T) and exp( –T2 )
weak/strong
shows different pinning
mechanism at low T
Aixia Xu et al, arXiv:1111.1268
140 A
Jaroszynski

## Slide 12
SuperPower production chronology
BZO
no BZO
>100 A @ 77 => > 140 A @ 14 T L He with a few exceptions
4.2 K 14 T ||c
77 K SF
averages over many samples
140 A
BZO
M3
M4
By accident – this is our most heavily characterized conductor
Jaroszynski

## Slide 13
20K anisotropy
Aixia Xu and Dima Abraimov

## Slide 14: Length and variability issues
Both are getting understood
But the process and competitive drivers are very different

## Slide 15: Manufacturing processes are quite different in scale and cost
Powder in tube:
2212 and 2223
Can use standard metal fabrication lines
IBAD-REBCO

## Slide 16: Manufacturing processes are quite different – so what?
Each REBCO process requires its own dedicated team and production line
Each process has its own challenges
Each line costs tens of millions
Each fab line is a black box
REBCO is the ONLY conductor to offer high temperature magnets
2212 uses standard metal fabrication routes
Team needed is much smaller
Scale up is easier (2212 can use ITER scale up route)
2212 could survive on magnet users – is this possible for REBCO?

## Slide 17: Conductor and Coil technologies are intimately linked
Coils, R&D Test Beds
27T with SuperPower
22.5T OI and 31T 2212 NHMFL
34 T YBCO NHMFL
HTS Magnet
Systems
32 T
Neutron scattering facilities
SMES + Muon Colliders
Conductors
YBCO
2212
2223??
Fe-base??
The key challenge of today is to build test or user coils that drive the technology without failure risking black-marking of HTS magnet technology

## Slide 18: A personal take on imminent key technology challenges
Understanding how to safely quench magnets like the recent NIMS-RIKEN 24 T, BNL 15 T and NHMFL 32T magnet
Developing viable cables of REBCO
Bringing bubble formation in 2212 under control so that recent short sample Je values can be obtained in long lengths
Ensuring that insulation technology proceeds in parallel with conductor and magnet technology