## Slide 1: Lab 6 Polystyrene Polymer Tests (cont.)
Brian Leung

## Slide 2: Oven Run PS Pellet Casting

## Slide 3: Oven Run Sample Measurements
Measurements performed using: Agilent Cary 60 UV-Vis Spectrophotometer

## Slide 4: Oven Run Samples
AmSty 665
INEOS 1200
Kumho GP125 – Korea
Hyundai G144 - Korea
LG Chemical 25SPI - Korea
INEOS 153F - Germany

## Slide 5
Oven Run Samples: |  |  |  |  |  | 
Oven Run 4/22 |  |  |  |  |  | 
AmSty 665 |  |  |  |  |  | 
INEOS 1200 |  |  |  |  |  | 
INEOS 153F – Germany |  |  |  |  |  | 
LG Chemicals 25SPI – Korea* |  |  |  |  |  | 
*Sample pellets half the size of other pellets, overflowed during Melt Cycle, only able to cut/polish into 5cm lengths |  |  |  |  |  | 
Oven Run 5/22 |  |  |  |  |  | 
AmSty 665 |  |  |  |  |  | 
Hyundai G144 - Korea |  |  |  |  |  | 
Kumho GP125 - Korea |  |  |  |  |  | 
**Unless noted, samples made of pure PS pellets (no dopants) and cut/polished into 7cm lengths |  |  |  |  |  | 

## Slide 6: LG Chemicals 25SPI vs. AmSty 665

## Slide 7
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
Previous Oven Runs 1/22 & 2/22 – AmSty 665
Older AmSty 665
Newer AmSty 665
*All samples cut to 7cm

## Slide 8
Oven Run 4/22 – AmSty 665, INEOS, LG Chemicals
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
AmSty 665
INEOS 153F
LG Chem 25SPI
*Compared to Newer AmSty 665, all samples cut to 7cm, except LG Chem 25SPI

## Slide 9
Oven Run 5/22 – AmSty 665, Hyundai, Kumho
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
AmSty 665
Kumho GP125
*Compared to Newer AmSty 665, all samples cut to 7cm

## Slide 10
Oven Run 5/22 – AmSty 665, Hyundai, Kumho
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
*Compared to Newer AmSty 665, all samples cut to 7cm

## Slide 11
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
AmSty 665 2021 & 2022 across Oven Runs
*Comparing Newer AmSty 665, all samples cut to 7cm

## Slide 12
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
Various Polystyrene Pellet Brands across Oven Runs
*Compared to Newer AmSty 665, all samples cut to 7cm, except LG Chem 25SPI

## Slide 13
Chart: PS % Transmittance Measurements (Baseline = Air) Normalized
Various Polystyrene Pellet Brands across Oven Runs
*Compared to Newer AmSty 665, all samples cut to 7cm, except LG Chem 25SPI

## Slide 14: Absorption around 500-600nm
Releasing Agents and Lubricants
Antistatics
Antioxidants
Flame Retardants
UV Absorbers
Zinc Stearate – a common releasing agent in Polystyrene

## Slide 15: Upcoming Testing
Additive Testing
Polystyrene Reference from Monomer (Polymerization Run)
Further LG Chemical 25SPI Testing
FTIR Pellet Testing
Additional TiO2 Pellet Casting