## Slide 1: Rotating Foil and Stripping Station Studies
Dave Johnson (APC) and Zhijing Tang (PPD)
May 29, 2012

## Slide 2: Motivation
  Single pass Stripping station
    Beam line (3 GeV H- transport)
      At 3 MW, losses are an issue (Lorentz stripping, black body rad.)
        Currently limited fields (restricted footprint) and Cold beam tube
      Convert to protons w/stripping station eliminates these issues
    1 GeV (1MW) to Nuclear facility
      Potential ADS Technology Demonstration
        Requires protons for vertical orientation
  Multi-pass injection stripping foil
    8 GeV injection into Recycler ( multiple short injections 1mA-4ms x6 inj @ 10 Hz or a single “long pulse” 1 mA-25ms injection)
    1 GeV injection into Booster (CW linac, ≈ 1 ms inj. 15Hz rep)
    Injection into high intensity storage rings
  Why rotating foils
    Spread energy deposition over larger area to reduce peak temperatures
    Does not help with losses due to scattering
  A preliminary estimation for a Project X “long pulse” injection scenario performed by A. Drozhdin, L. Vorobiev, S. Striganov, and I. Rakhno utilizing a moving strip foil indicates a reduction in temperature… to be discussed in next presentations

## Slide 3: Typical H- Stripping Foil Material
Carbon
  Amorphous Carbon (such as Arizona carbon)
  HBC (Hybrid Boron doped Carbon) KEK
  DLC (diamond-like-carbon) Trumph
Aluminum-oxide
More recently polycrystalline (including nano- and ultranano- )diamond foils have been pioneered and utilized by SNS

## Slide 4: UNCD Properties
General material properties
  Young’s modulus: ~ 850 -1100 Gpa
  Large fracture strength: ~ 4 GPa for UNCD
    (free standing sheets are flexible and strong)
  Density: ~3.3 g/cm3
  Poisson ratio: ~0.057+/-0.38
  Mohs hardness: 10
  Dielectric constant: ~5.68
  Electrical resistance ( depends on doping) 10-1 to 10+4 Ω-cm
  Breakdown voltage: ~108 V/m
  Thermal conductivity (depending on grain size) 12-1500 W/m-oK
  Coefficient of linear expansion ~10-6/oC
Not a DLC (amorphous form of carbon) coating or film
Self supporting
Grown in wafers up to 300mm diameter (thickness 0.1 to ~2 mm)
  Can be corrugated, etched, and diced for shaping of final foil geometry
Chemistry (atmosphere), multiple element deposition, grain control impact ultimate thermal, electrical, and mechanical properties

## Slide 5: Approach (1)
Single Pass (want 100% neutralization)
  MARS- for loss distributions/activation
  ANSYS- thermal/mechanical simulations
Multi-turn Injection (typically 98 to 99%)
  Utilize codes such as ORBIT and STRUCT for determination of parasitic hit distribution on foil as a function of
    Ring and injection line lattice
    Painting algorithm
    Injection beam current, injection time, and rep rate
  Losses due to scattering
  Losses due to Stripping of excited states (Stark states)
  ANSYS for thermal and mechanical simulations

## Slide 6: Approach(2)
Develop ANSYS model of rotating foil to investigate thermal and mechanical properties
  Utilize general UNCD properties for initial model (in consultation with CNM) as a starting point
  Utilize existing energy deposition and foil temperature estimations based upon MNCPX and MARS simulations
  Understand physical, thermal, and electrical characteristics requirements due to rotation and beam impact (structural, thermal, electrical, etc) What’s important & and how to specify material properties (strength, uniformity, thermal acoustic, and electrical properties)
  Understand capabilities of CNM (Argonne)/Advanced Diamond Technologies
  Understand the diamond-to-graphite conversion due to ion bombardment
Prototype disk
  Design of rotational system
  Design a disk which meets the physical and thermal requirements
  Plan for temperature and foil dynamics measurement
Beam test (at FNAL) 400 MeV and/or 8 GeV or potentially SNS

## Slide 7: First Example – single pass stripping
Assume 1 mA average linac current at 3 GeV in 162.5 MHz bunch structure  ~4E7 ions/bunch assuming all bunches are filled equally
  Bunch length ~1 ns
  Bunch repetition rate 6.15 ns
  Assume Gaussian beam with s=2mm
Assume foil thickness 2 mm and density 3 g/cm3 (600mg/cm2)
t1
t2
t1 bunch (pulse length),
t2 rep rate
2 micron UNCD film
(surface structure may be required
Si substrate
Copper
6 mm
82 mm
20 mm
H- beam
t = 30 ms
w = 2,000 rpm
w

## Slide 8: Thermal Model
1,
0,
t1
t2
t1 bunch (pulse length),
t2 rep rate
[J-kg/oK]
N is the #ions/bunch
* For now ignore delta electrons
h foil thickness
k thermal conductivity
ANSYS simulation developed by Zhijing Tang
Heat source term

## Slide 9: Preliminary ANSYS Simulations
ANSYS simulation developed by Zhijing Tang
Thermal Analysis
Static solution
Time scale for conduction
Time scale for radiation
For a bunch intensity of 4E7 ions the energy deposition for
single bunch (SI) u ~ 3.2x10-6 J-m2/kg
From NIST tables dE/dx through amorphous carbon (1p-2e) 4.95 MeV-cm2/g
  Neglecting any reduction of energy deposition from delta electrons
Instantaneous power (ruh) into foil ~19W
average power t1/t2P0 ~3W
Consider heat source continuous with time

## Slide 10: Increase Beam power
Outer radius = 8.4 cm, inner radius = 2 cm.
From r = 2 to r = 6 cm, thickness = 100 microns; from r = 6 to r = 8.4 cm, thickness = 2 microns.
Rotation speed = 2000 rpm.
Heating power = 8 W on a spot size = 1x2 mm2 (r = 8 cm).
r = 3 g/cm3, k = 1370 W/m-K, e = 0.5,
Boundary condition is the temperature at r = 2 cm and the enclosure temperature = 300 K.
Use a static solution as initial condition, following is the temperature distribution after 5.6 cycles.
ANSYS simulation developed by Zhijing Tang
Assume hit rate of 5.15E14 proton/mm2
over 30 ms and constant hit rate
Bunch intensity ~1E8
Average heating ~8W

## Slide 11: Mechanical Analysis
ANSYS Mechanical Model (stress for a rotating thin disk)
Stress proportional to square of rotational speed and radius.
All stresses are positive (under tension) when no thermal load
Interested in
stresses in the foil while rotating and with the addition of heat
natural frequencies of oscillation
buckling amplitudes
ANSYS simulation developed by Zhijing Tang
What are the design parameters for a foil to rotate at high speeds?
 ~0.4 MPa for r=8cm and speed 2000rpm
Stress due to centrifugal force
Thermal stress proportional to temperature change
~.13 GPa for temp change of 150oK

## Slide 12: Summary/Next Steps
ANSYS simulations have just began
Start injection simulations
Move forward for beam test of UNCD foil