## Slide 1
09/09/2022
Nano/Micro-fabrication of Josephson junction
Tommaso Bonaccorsi
University of Pisa, Department of physics "E. Fermi"

## Slide 2: Josephson junction theory pt.1

## Slide 3: Josephson junction theory pt.2
If we resolve the Sch. Eq. we obtain

## Slide 4: Josephson junction theory pt. 3
One can infer that the effective inductance of the Josephson junction is :
JJ works as a non-linear inductance without adding dissipation
We can create an anharmonic oscillator with a JJ and a capacitor

## Slide 5
Lift off Process (additive)
Substrate
MMA (8.5) MAA
PMMA
E-beam Expose
Metal Deposition
Develop Resist
Solvent Lift Off
Substrate
Substrate
Substrate
Substrate
Spin Coat Resist
e-beam

## Slide 6: Stack of two resists for junction fabrication
The reason for this choice of resist staking is to achieve a wide undercut which is convenient for clean lift off as depicted in figure. Moreover , the undercut of the lower resist can be used to created suspended resist

## Slide 7: Shadow evaporation technique (ShET)

## Slide 8: New technique to increase the coherence time of the qubit
BEFORE
They used ion milling before the deposition of the JJs on Nb pads to create the electric contact
NOW
During this weeks we have built JJs with a new technique called “patching”

## Slide 9: Electrical contact between Nb pads and JJs with "patching"
Nb pads
Al bandaid
Josephson junction​

## Slide 10: Second experiment with patching
We have deposited JJs between the pads to protect the junction from any charge build-up. In that case the electric contact is established between the parts only at the end.

## Slide 11: Measurements
2° experiment
1° experiment
JJ surface [µm^2]
0.014
0.018
0.023
0.030
0.039
0.050
0.061
0.072
0.090
JJ surface [µm^2]
0.014
0.018
0.023
0.030
0.039
0.050
0.061
0.072
0.090
39.7 | 20.2 | 20.3 | 22 | 19.1
600 | 16.3 | 150 | 400 | 17.7
220 | 600 | 0.12 | 47 | 16
22 | 13.1 | 11.8 | 1.4 | 13.1
600 | 40 | 10.9 | 70 | 0.17
9.3 | 600 | 0.12 | 11 | 10
8.9 | 8.8 | 0.16 | 9.3 | 9.4
7.7 | 8.0 | 7.2 | 500 | 7.4
500 | 13.5 | 600 | 6.78 | 6.26
593 | 590 | 600 | 600 | 600
600 | 600 | 600 | 600 | 600
600 | 600 | 600 | 600 | 600
600 | 600 | 10.4 | 600 | 600
9.35 | 600 | 600 | 600 | 600
600 | 8.34 | 7.64 | 600 | 8.43
6.50 | 600 | 600 | 7.20 | 7.35
5.85 | 6.16 | 5.89 | 600 | 6.03
600 | 4.79 | 4.92 | 4.85 | 600
RESISTENCE [KΩ]
RESISTENCE [KΩ]

## Slide 12: Measurements
JJ ON THE PADS
JJ BETWEEN THE PADS
For small size there is no working junction

## Slide 13: Not working junction

## Slide 14
Thanks for listening