## Slide 1: Lab 6 Polystyrene Polymer Tests – IP2I Extrusion

## Slide 2: IP2I Extrusion
Part Dimensions: 25mm x 5mm w/ 1 hole

## Slide 3: Light Yield Testing
Measurements performed using: Cs-137
K2K Reference
IP2I Extrusion

## Slide 4
Chart: Change in Light Yield IP2I #622 vs Time
| 0 | 8 | 15 | 22
 | 279212 | 277840.6406 | 279250.1867 | 274536.8909

## Slide 5: Future Testing:
Continue monitoring IP2I Extrusion Light Yields over time
Reference with Mackenzie’s TiO2 Reflectance data
Additional Polystyrene Sample tests (various vintages)