## Slide 1: Measured RRR in MQXFA10 magnet
Maria Baldini, Anis Ben Yahia

## Slide 2: MQXFA10 temperature variation during warmup
15 K difference between Lead end and Non lead end of the magnet

## Slide 3: Cold RRR data

## Slide 4: RRR calculation
The resistance value at cold was chosen:
According to the IEC procedure
Same method used for the extracted samples at LBNL
Vendor uses a 20 K criteria for rolled sample

## Slide 5: MQXFA10 cables: RRR estimations
conductor OST 108-127
Both Minor edge extracted sample and rolled samples were used to estimate the best coil ordering based on RRR data
Maximum coil to ground voltage at quench with ordering: 353 V (EDMS 1963398, Us-HiLumi Docdb 879)
COIL | RRR (rolled) | RRR (minor edge)
129 | 222.1 | 263.2
131 | 232.1 | 305.6
132 | 248.5 | 264.2
220 | 208.7 | 246.2
221 | 213.97 | 250.2

## Slide 6: MQXFA10: measured RRR vs estimated RRR
The measured RRR values are in between rolled and the minor edge extracted sample. The use of rolled sample for estimating RRR is conservative

## Slide 7: Summary of all measured RRR