## Slide 1: MQXFA13 Preload Targets
D. Cheng, P. Ferracin, L. Garcia-Fajardo, H. Pan
For the LBNL AUP Team
18-Nov-2022
LBNL

## Slide 2: Outline
Preload targets
Overview of MQXFA03-12 pre-loads achieved
Proposed preload process

## Slide 3: MQXFA SG Layout
HBM gauges and FBG (next slide) are installed
Shell gauges --- three axial locations:
  Shell gauges (T & Z): on shell 2, 4, & 7
Coil gauges (T & Z): on the axial location of 3989 mm (RE) from LE.
Rod stations are located on the RE (see inset)
  Each station is full bridge with four individual gauges.
LE
RE
MID
Shell 2
Shell 4
Shell 7
Coil Stations
Rod Stations
RE axial plate assembly

## Slide 4: MQXFA SG Layout (FBG)
FBG Coil gauges (T & Z): on three axial locations:
  715 mm, 1915 mm, and 3725 mm from LE.
Based on experience with MQXFA09 thru MQXFA11
Only on Upper coils

## Slide 5: MQXFA Preload Specifications
Pole key gap: 0.016” (~400µm) average per side
  New specification wording is now in place
Azimuthal pre-load
  Target coil pre-stress at cold of 100 MPa requires:
    ~80 ± 8 MPa at R.T. after 24 hours
      Assumes 5-10 MPa decrease in 24 hours
  We set as maximum coil stress to 110 MPa during loading
Axial pre-load
  The total force at cold is: 1.0 MN
    ~950 με at R.T
    Equates to total rod force ~0.58 MN at R.T.
These stress targets have remained unchanged for both Pre-Series (MQXFA03-A07) and Series magnets, and are captured in the Series Magnet Specifications Document (US-Hilumi-Doc-4009)

## Slide 6: Preloads Measured for MQXFA Magnets
 |  | Target (MPa) | MQXFA03 | MQXFA04 | MQXFA05 | MQXFA06 | MQXFA07 | MQXFA08 | MQXFA08b | MQXFA09 | MQXFA10 | MQXFA11 | MQXFA12
R.T. | Coil | -80 ± 8 | -79 | -76 | -73 | -80 | -77 | -69 | -76 | -67 | -66 | -70 | -60
 | Shell 7 | 58 ± 6 | 54 | 64 | 62 | 60 | 58 | 52 | 50 | 62 | 56 | 66* | 58
Cold | Coil | -103 | Determined from unloading deltas during powering (see pictures on next slide |  |  |  |  |  |  |  |  |  | 
 | Shell 7 | 110 | 112 | 142 | 144 | 137 | 138 | 134 |  |  | 142 | 132 | 
Coil average delta azimuthal stress during excitation
Coil average delta axial stress during excitation
Maximum stress values of each coil were selected for these plots
In red: Coil quadrants with the highest stress increase
In blue: Coil quadrants with the lowest stress increase

## Slide 7: Preloads Measured for MQXFA Magnets
MQXFA03
Ramp to 16.65 kA
Av. delta stress: 101 MPa
MQXFA04
Ramp to 16.55 kA
Av. delta stress: 115 MPa
MQXFA05
Ramp to 16.46 kA
Av. delta stress: 102 MPa
MQXFA06
Ramp to 16.45 kA
Av. delta stress: 106 MPa
MQXFA07
Ramp to 15.45 kA
Av. delta stress: 107 MPa
MQXFA08
Ramp to 16.50 kA
Av. delta stress: 94 MPa
MQXFA10
Ramp to 16.54 kA
Av. delta stress: 89 MPa
MQXFA11
Ramp to 16.54 kA
Av. delta stress: 106 MPa

## Slide 8: MQFXA10 (Preload 2), MQXFA11 and MQXFA08b Transfer Function Plots
MQXFA10 Achieved a small spread of coil stresses, with average at 72 MPa (within target of 80 +/- 8)
MQXFA11 Achieved a larger spread of coil stresses, with average at 73 MPa
MQXFA08b Achieved a small spread of coil stresses, with average at 76 MPa
MQXFA10
MQXFA11
MQXFA10
MQXFA11
* NOTE: MQXFA09 shell-yoke assembly was unloaded and SG offsets were forced to original pre-A09 preload values before preloading MQXFA11. E.g. shell SG values are likely over-reporting calculated stresses by 2-5 MPa in Shell 7. See appendix.
MQXFA08b
MQXFA08b

## Slide 9: Transfer Function at RT for MQXFA Magnets
* NOTE: MQXFA09 shell-yoke assembly was unloaded and SG offsets were forced to original pre-A09 preload values before preloading MQXFA11. E.g. shell SG values are likely over-reporting calculated stresses by 2-5 MPa in Shell 7. See appendix.

## Slide 10: MQXFA Bladder Pressures
MQXFA10 shimmed coils were smaller, so overall coil pack size was smaller than in other magnets
  Required an additional .025 mm of load key shim to achieve target coil preload (13.82 mm total)
MQXFA11 utilized more midplane shim than A07-A10) due to adjusted measurement reporting
  Larger coil pack required higher pressures at same key shim size
  But required smaller total key size to reach target (13.74 mm total)
Plot of bladder pressures vs target shows correlation between required bladder pressure to achieve preload targets
50% Azimuthal load

## Slide 11: The Load Condition after CD (based on powering)
MXQFA03
MXQFA04
MXQFA05
MXQFA06
MXQFA07
NOTE: axial load values due to cool down SG data is still being examined

## Slide 12: Standard Preload Process
The pre-load sequence:
  Pre-loaded axial rods with average ~50 µε;
  50% azimuthal pre-load (~0.030” shims, or total 13.52 mm)
  50% axial pre-load (~470 µε)
  100% azimuthal pre-load (~.040” shims, or total ~13.8 mm)
  100% axial pre-load (~950 µε)
The pre-load process:
  We preloaded MQXFA05 quadrant by quadrant from the initial 0.010” shims (total 13.01mm) in 0.005” steps, reaching a peak bladder pressure of 4500 psi.
  All subsequent magnets used quadrant by quadrant loading after the 0.015” shims step (total ~13.14 mm)
MQXFA05 Coil 115 slope may have been caused by “locking in” a position too early in the preload process

## Slide 13: Variation of MQXFA13 Pre-Stress due to Coil Variations
Starting with MQXFA08 coils there is now a CMM measurement at the SG location
This location is also the largest per measurements
Shimmed
0.005” on Coil 139
0.005” on 141
0.005” on 227
0.005” on 229
Coil sizes based on CMM and shimmed sizes on midplane
The amount of increased average stress above what is measured at the SG is still below the 120 MPa “hard limit” when staying below the 110 MPa limit during all pressure operations

## Slide 14: Axial Preload for MQXFA
The axial preload targets the same level of MQXFA04 - 11:
MQXFA Target | R.T. | 1.9 K | Nom. Current
Preload | 950 µε ± 95 µε | 1700 µe | 1750 µe
Axial Force (MN) | 0.6 | 1.07 | 1.12
Ratio to the E.M. force at nom. current | 50% | 90% | 93%
Total axial e.m. force is 1.2 MN at nominal current

## Slide 15: Summary
The R.T. preload targets for MQXFA13 remain unchanged and follow the Magnet Specifications:
  Shell Stress: 58 ± 6 MPa
  Coil Stress: -80 ± 8 MPa
  Rod strain: 950 ± 95 µε
Cold powering deltas are used to determine the preload on the coils
Average coil size (arc length) after shimming is within ~±100 µm with respect to average coil size measured at the strain gauge location location (one location slightly small)
The preload process will start quadrant by quadrant loading after the ~13.14 mm load key step
  Intended to prevent “locking in” a position too early

## Slide 16: Additional Slides

## Slide 17: Preload Targets for MQXFA
 | Value
Interference (µm) | 470
Polekey gap (µm/side) | 145
Polekey interception Fpole/Fshell (1.9K) | 0
 | 1.9 K | 16.47 kA | 17.89 kA | 19 kA
Shell Average Von Mises Stress (MPa) | 116 | 121 | 125 | 129
Shell Peak Stress (MPa) | 488 | 481 | 481 | 480
We have kept the same pole-gap since MQXFA03:
  About ≥ 5.5 mil/side: will not fully close at cold

## Slide 18: MQXFA05 &6 Load Key Shimming Summary
From MQXFA05, we reduced number of operations from ~10 steps to 7 steps using a constant 0.005” shim increment
Magnets MQXFA03 to -05 were plotted together
  Shows full-quadrant loading, diametrical loading, and quadrant loading
Load key shims stacks are shown vs. pump pressure required to achieve insertion
  Pressures shown are the highest pressure required (in the case of diametrical and/or quadrant) to complete a full round of shimming

## Slide 19
Analysis of low stress in MQXFA05 coil 115

## Slide 20: MQXFA05 Coils TF
Detailed data points in next slide

## Slide 21: MQXFA05 Coils TF (detailed)
Detailed data points from 20 mil to 30 mil shims

## Slide 22: Individual Coil TF Comparisons
MQXFA03
MQXFA04
MQXFA05
In general, coil stress spreads in MQXFA03 and A06 are much smaller.
MQXFA06

## Slide 23: Previous cases

## Slide 25: MQXFA03 - 06 Shims TF Plots
The correlations of the total load key thickness and the average coil / shell azimuthal stresses are investigated;
The slopes of the linear part of the three magnets are very close.

## Slide 26: Shim TF only for MQXFA05
The average stress of all the shells (shell 2, shell 4 and shell 7) seems linear (red line) ;
The average stress of the shells 2 & 4 seems linear (Dark blue line) ;
The average stress of shell 7 seems to have slope change (green line).
Only MQXFA05

## Slide 27: Individual Shell Shim TF Comparison
Individual shell stress with error bar at each final data point.

## Slide 28: Coil Pack Pole-key Gaps
inch
inch
mm
MQXFA03
MQXFA04
MQXFA05

## Slide 29: Shell ID Measurements
Unit: mm

## Slide 30: Appendix: Possible Polekey Interception in Q4
No Gap
No Gap
Full size 2D model.
The pad is assumed as only iron.
Initial pole key gap is 140 μm / side in quadrant 1 to 3.
No pole key gap in quadrant 4.
No axial loading in the 2D model.
All components are in contact using contact elements
  Contact172
  Target169
  Baseline Friction coefficient is 0.2
2D model Basic Settings:
Apply uy=0 and ux=0 on Y-lock and X-lock, respectively
Apply interference at the loadkey and p-master interface
Boundary conditions:
Q1
Q2
Q3
Q4
Y-lock
X-lock

## Slide 31: Shim TF (with FE simulations)
The slope of average stress of FE is slightly higher than the measurements;
However, the slopes of the simulation results are not different obviously to make a clear comparison with the measurements.
With simulations

## Slide 32: Measurements vs. Simulation
No polekey gap in Q4
Measurements

## Slide 33: TF of the Simulation
No polekey gap in Q4

## Slide 34: Coil stress distribution
No polekey gap in Q4, 8 mil /side gap in the rest quadrants
All quadrants with polekey gap (8 mil /side)
Pa
Pa
Coil Von Mises Stress after preloads:

## Slide 35: Coil stress distribution
Stress (MPa)
No polekey gap in Q4, 8 mil /side gap in the rest quadrants
All quadrants with polekey gap (8 mil /side)
Coil Von Mises Stress on the path (red dash line):
Cooldown
R.T.
Stress (MPa)
0°
90°
180°
270°
Cooldown
R.T.