## Slide 1
Fermilab PAC Meeting, Jan. 2023 1/17/2023
Status of the SQMS Center
Anna Grassellino, SQMS Center Director Jens Koch, SQMS Deputy Director

## Slide 2: Motivation
Quantum Information Science
Quantum Sensing & Metrology
Quantum Computing
Quantum Cryptography
Quantum Communication
Quantum Simulation
Foundations of Quantum Mechanics Physics beyond Standard Model
Dark Matter
…
ħ
ħ
Leveraging quantum technologies
for studying fundamental physics

## Slide 3
10 yr plan to accelerate the development of quantum information science & technology applications.
“ ”
DOE shall establish and operate NQI Science Research Centers to conduct basic research to accelerate scientific breakthroughs in quantum information science
and technology.
5 NQI DOE centers (2020)
National Quantum Initiative Act (2018)
BILL
Quantum
Systems
Accelerator
SUPERCONDUCTING QUANTUM MATERIALS & SYSTEMS CENTER

## Slide 4: DOE NQI Center Requirements (excerpt)
Significant National Impact advance basic research in QIS improve competitiveness of the US catalyze the wider scientific/technical communities serve as national resources and leaders
Major Cross-Cutting Challenge attack a major challenge that warrant a large, multi-institutional, multi-disciplinary effort
S&T Innovation Chain advance science & technology, accelerate progress from discovery to technology/applied research co-design approach
QIS Ecosystem Stewardship: complement existing DOE QIS research leverage other DOE investments in research/facilities create synergies between federal agencies, private sector &academia contribute to QIS workforce development in US
Multi-disciplinary Leadership
Collaborative Management Structure
Well-Structured Plan and Metrics clearly defined near, intermediate, and long-term goals, milestones, deliverables, and metrics of success

## Slide 5
Enable construction and deployment of superior quantum systems for computing and sensing.
Create unique foundry capabilities and quantum testbeds to serve the national QIS ecosystem.
Train next-generation, diverse workforce of quantum scientists, engineers and technicians.
SQMS Mission
Leverage strengths of
national labs, industry & academia
to achieve transformational advances in quantum coherence of superconducting devices.
GOALS

## Slide 6
Impact at a glance
26 SQMS Institutions
420 SQMS headcount
131New hires
143
>200
15 New facilities & testbeds
>210 Companies engaged
115 preprints & publications
$115M Funding 2020-2025
Funded students & postdocs
External students engaged (SQMS schools & internships)

## Slide 7: SQMS Center Organizational Chart

## Slide 8: SQMS Leadership (core management group)
Dr. Anna Grassellino (FNAL) Center Director
Prof. Jens Koch (Northwestern)
Deputy Director
Dr. Matt Reagor
Rigetti PI, CTO
Dr. Matt Kramer
Ames Lab PI, Chief Engineer
Dr. Eleanor Rieffel NASA Ames PI
Chief Computational Scientist
Prof. Jim Sauls,
LSU PI, Chief Theorist
Dr. Alexander Romanenko (FNAL) Technology Thrust Leader
Dr. Silvia Zorzetti (FNAL)
Ecosystem Leader
Dr. Roni Harnik (FNAL)
Science Thrust Leader
Dr. Florent Lecocq
NIST Boulder PI

## Slide 9: SQMS participants
SQMS
…

## Slide 10: SQMS at Fermilab hired > 40 new employees supported by SQMS
SQMS Division (~50) + APSTD, Theory, FQI…

## Slide 11: SQMS participants and research at NU
SQMS
…

## Slide 12: SQMS participants and research at NU
SQMS
- Anna Grassellino
- Alex Romanenko
- Roni Harnik
- Sam Posen
- Silvia Zorzetti
…
- Jens Koch
- Venkat Chandrasekhar
- Michael Bedzyk
- William Halperin
- Mark Hersam
- Peter Voorhees
- James Rondinelli
- Tim Kovachy
- Selim Shahriar
- Vinayak P. Dravid
- Nikolay Zhelev
- David N. Seidman
- Dieter Isheim
- Andrew Geraci
- Matthew Grayson
- Prem Kumar
adjunct NU faculty

## Slide 13: Science & Technology Innovation Chain
Materials
High-coherence devices
Systems integration
New platforms for quantum computing & sensing
Quantum advantage
potential for scientific discovery at every step of the chain

## Slide 14: Center Mission and Co-Design
APPS
OPERATING SYSTEM
INSTRUCTION SET
HARDWARE
algorithms
high-level programming language transpilation/compilation
quantum error correction/mitigation
control & measurement
design of devices … processor
fabrication of devices
materials for devices
vs.

## Slide 15: Progress Assessment
Metrics
Meet/exceed milestones Proposal appendix 13 - project timetable
  - quarterly updates/refinement JIRA/Confluence
  - boost promising research directions
Number, quality, impact of peer-reviewed publications, presentations - ideally DOE/SQMS as lead funding source in acknowledgments - report to FNAL for records
Internal and external evaluations via - SQMS leadership - Advisory Boards and DOE
PI participation in center-wide activities and meetings

## Slide 16
Recent Highlights from SQMS Focus Areas
DEVICES
MATERIALS
ALGORITHMS
PHYSICS & SENSING
WORKFORCE DEVELOPMENT
2022 SQMS Summer Internship
First quantum operation of the SRF-transmon system achieved
Comprehensive material characterization of commercial transmon qubits
VQE for the square-octagonal Kitaev model
Most sensitive search for dark matter-dark photons at specific frequencies

## Slide 17: SQMS Facilities Progress
Material Characterization Facilities
Advanced characterization techniques employed for first time and extended to qubit operational regimes
Foundries New high-flexibility nanofabrication facility at FNAL and NU
Materials testbeds Qubits and materials measurements in the most precise and sensitive environments
Physics Testbeds Platforms enabling new particle searches
Computing Testbeds 2D and 3D-based quantum computer prototypes
Colossus
World’s largest dilution fridge at FNAL

## Slide 18: Technology Thrust
Focus Area 1: Materials
Goal: Understand and mitigate the key mechanisms of decoherence in superconducting qubits and SRF cavities
Deliverables/metrics: achieve at least an order of magnitude improvement in coherence, SRF cavities > 10 seconds, 2D transmons > milliseconds with decrease in performance spread < 20%
Focus Area 2: Devices
Goal: Device performance test, integration and quantum controls development towards high coherence 2D and 3D SC architectures
Deliverables/metrics: develop quantum computer prototypes of 2D/3D architectures, deploy record sized dilution fridge to host the 3D/2D quantum processors
Thrust Leader: Romanenko

## Slide 19: Science Thrust (focus for June PAC)
Focus Area 3: Physics and Sensing
Goal: Exploit the center technological advancements for fundamental physics
Deliverables/metrics: develop and deploy search schemes with detection sensitivity orders of magnitude compared to state-of-the-art
Focus Area 4: Algorithms, Simulations
Goal: Investigate and develop quantum algorithms and simulations enabled by the groundbreaking SQMS 3D and 2D prototypes through co-design principles
Deliverables/metrics: simulations of the dynamics of theories approximating QCD, simulate LHC physics, plasma early universe conditions, quantum materials far from equilibrium, intermediate electron/phonon SC
Thrust Leader: Harnik

## Slide 20: Physics and Sensing 5-year Roadmap (focus for June PAC)
DarkSRF
Multimode Cavity Axion Search
High B-Field Axion Search
Single Particle Penning Trap
Other Quantum Sensing Schemes
Tunable Dark Photon Search
Year 1
Year 2
Year 3
Year 4
Year 5
Measure in LHe, 1st DarkSRF publication
Implement in DR, quantum regime!
Improve Q0 towards 1e12
Phase sensitive readout
2- and 3- mode 1-cavity design
2-cavity multimode design
Evaluate Nb3Sn, NbTi Q0 in high B
Co-design w/ materials & devices
Evaluate search w/ AC B-field
Searches w/ best cavities and qubits
Design high Q cavity geometry
Prototype cavities & squids
1st next gen e- μ/μB measurements
Testing optimized cavities/squids
Evaluate SRF cavities for gravitational wave detection, DM with traps.
Theory study of QIS for dark radiation detection, Quantum Sensor Network,
Nonlinearity studies
2-cavity 1st test
2- and 3- mode 1-cavity 1st test
Design and fabricate cavity
Study heterodyne vs photon counting
Data taking runs
Trial runs, feedback
Notes: Sam

## Slide 21: Quantum control & measurement with SC qubits & cavities
SRF cavity
transmon
circuit

## Slide 22: Quantum control & measurement with SC qubits & cavities
EM mode coupled to transmon
…
Minimal description: Jaynes-Cummings model
oscillator
qubit
3d
2d

## Slide 23: Quantum control & measurement with SC qubits & cavities
EM mode coupled to transmon
…
Encode, manipulate and measure quantum information
in the transmon, using cavity for driving & readout
In the cavity mode using transmon for control & readout

## Slide 24: Role of Materials Science
Slide from 2009:

## Slide 25: Decoherence channels in 2D superconducting qubits: two-level systems, bulk substrate losses, quasiparticles
1. Koch, J. et al. Physical Review A 76, 042319 (2007)
2. Wenner, J. et al. Applied Physics Letters 99, 113513 (2011)
3. Wang et al. Appl. Phys. Lett. 107, 162601 (2015)
4. Calusine, G. et al. Applied Physics Letters 112, 062601 (2018)
Lossy elements with known Estored /Etotal
Other channels
(e.g. radiative decay)
Qubit frequency
Loss tangent
Total decay rate 1,2,3
Each channel bounds T1:
Looking for changes channel-by-channel:
Participation ratio Estored /Etotal
MS: Metal-Substrate | SA: Substrate-Air | MA: Metal-Air | MM: Metal-Metal
Al

## Slide 26: Pushing performance from materials to devices to quantum processors
Material/superconducting analysis of qubits and cavities fragments
Qubits and cavities fabrication processes modifications guided by materials knowledge
Quantum processor of 2D and 3D architectures built with high coherence qubits
Qubits/cavity devices microwave measurements
NbOx
Nb
10nm

## Slide 27: SQMS innovative approaches to QIS materials and devices characterization
β-NMR/μSR
THz Spectroscopy
STM
Magneto-optical
Point-Contact Tunneling
PPMS- AFM/MFM
Dissecting and studying fragments of microwave performance characterized devices
Leveraging DOE and SQMS partners user facilities

## Slide 28
Electron Microscopy
TOF-SIMS
XRR/XRD
XPS
AFM/MFM
APT
Raman

## Slide 29: Possible interface loss structures revealed by electron microscopy
Nb-Oxide interface
There is a ~4-6nm amorphous NbOx layer on Nb metal surface both in the SRF cavity and the Rigetti transmon.
Si-air interface
A Thin amorphous Si-oxide layer (~2nm) is detected between Si/air interface.
side wall
Si
10nm
Nb
NbOx
O
Nb
(a)
10nm
Nb
NbOx
(b)
cavity
Transmon

## Slide 30: Possible interface loss structures revealed by electron microscopy
10 nm
10 nm
Al
Si
Al
Al
a-Al2O3
a-Al2O3
Si
Al
O
(a)
(b)
(c)
(d)
a-SiO2
2 nm
Nb
Si
(a)
(b)
Nb-Si interface
Nb-Si amorphous bi-layers at the Si/Nb interface formed during material deposition.
Josephson junction barrier
The Al/Al2O3/Al interface is wavy.
Existance of amorphous Al2O3 and amorphous SiOx layer at Al/Si interface.

## Slide 31: Discovery of niobium nano-hydride precipitates in superconducting transmon qubits
Scientific achievement
  First ever performed cryogenic microscopy studies of superconducting qubits lead to the discovery of the presence of hydride precipitates in the Rigetti Computing and other transmon qubit devices
Significance and Impact
  Niobium nano-hydrides are poorly superconducting phases that can cause qubit device performance limitations and degradation over time and with subsequent cooldowns
Details
  Cryogenic AFM, electron diffraction and high-resolution transmission electron microscopy (TEM) analyses are performed on the Nb films at room temperature and cryogenic temperature (106 K)
  The results suggest the existence of two possible types of Nb hydride domains in Nb grains: (i) ~5 nm-sized Nb hydride domain with irregular shapes; (ii) 10s~100 of nm-sized distinct Nb hydride domains
Work was performed at Fermi National Accelerator Laboratory material science lab and NUANCE user facility
J. Lee, Z. Sung, A. Murthy, M. Reagor, A. Grassellino, and A. Romanenko; https://arxiv.org/pdf/2108.10385.pdf
Cryogenic TEM, electron diffraction images of Rigetti 2D qubits , revealing the presence of hydrides precipitates in the niobium film at T=100K
Lamellas of superconducting qubits from real Rigetti Computing processors are dissected via FIB-SEM at FNAL and studied for the first time via cryo-TEM
Notes: Notes: Include 200 word highlight summary….

## Slide 32: 3D record coherence cavities as sensitive probes for Nb2O5 (and other) loss tangents
A. Romanenko, R. Pilipenko, S. Zorzetti, D. Frolov, M. Awida, S. Belomestnykh, S. Posen, A. Grassellino, Phys. Rev. Appl. 13, 034032 (2020)
340-450C treatments remove amorphous Nb2O5 hosting TLS
Depth
TOF-SIMS data on cavity cutouts
QIS record
Very large TLS loss in Nb2O5

## Slide 33: High Q cavities to characterize dielectrics loss tangents with very parts per billion accuracy
2.6 GHz materials test-bed has been commissioned to perform silicon loss studies with unprecedented accuracy of parts per billion
Also tunable cavity 5-8 GHz
M. Checchin et al Phys. Rev. Applied 18, 034013 – Published 7 September 2022

## Slide 34: RF Characterization of MSE Sapphire Substrate
Achievement
Finished RF characterization of sapphire substrate used in previous round of qubit fabrication
  C-plane sapphire from MSE
Results:
Preliminary results suggest tanδ ≈ 5e-7
Limits 2-D transmon T1 ~125 us
Next steps:
Making preparations to measure HEMEX sapphire with same setup
T = 100 mK
Notes: Yale estimates: HEMEX limits T1 to 800 us, EFG limits T1 to 1000 us.

## Slide 35: Silicon Sample Exchange with C2QA Collaborator Yale University
Collaborating with Yale University on sample measurement reproducibility (dielectric dipper)
Received previously measured high resistivity, DSP Si sample
Sample installed in new 6 GHz SRF characterization testbed
  Utilizing new, gold-plated O-free cooling setup to ensure adequate cooling to mK
RF Simulations:
  PSi, bulk = 7.4e-4
  Expected Q0,empty = 1E9
  Expected Q0,Si loaded ~ ???
+
=
Notes: DSP: double side polished
Yale has dipper method (in situ actuation of sample via piezo to enable measurements with and without sample). This is a quarter wave stub resonator

## Slide 36: SQMS has launched a Nanofabrication Taskforce across four national qubit foundries
FNAL/Uchicago, NIST, Rigetti, Northwestern foundries capabilities to work together in coordinated study to address material losses
Encapsulation strategies and bulk loss mitigation a priority
UChicago - Pritzker Nanofabrication Facility
NIST - Boulder 2D Nanofabrication Facility
Rigetti - Fab-1 Integrated Circuit Foundry, Fremont CA
Akshay Murthy
Associate Scientist
Mustafa Bal​
Associate Scientist​
Pete Hopkins,
NIST
David Van Zanten​
Associate Scientist
Shaojiang Zhu​​
Associate Scientist​
​
Ivan Nekrashevich​
Associate Scientist​
Florent Lecoq, NIST
Francesco Crisa’, PhD student
Nick Zhelev, NU
Yuvraj Mohan
Rigetti Computing
Northwestern - NUFAB

## Slide 37
Standardized qubit chip
    8 fixed frequency uncoupled transmons ~ 4 – 5 GHz
      4 w/ double capacitive pads (for statistics)
      2 w/ interdigitated capacitive pads (most sensitive)
      2 w/ concentric capacitive pads (most insensitive)
    Anharmonicity ~ 220 MHz
    Readout resonators ~ 6 – 8 GHz
    Frequency multiplexing on single feedline
2D SQMS R&D Qubit Chip and modeling/simulations work to estimate impact of subsystem losses
E-field distribution of different transmon geometries

## Slide 38: First qubit results from FNAL group proving the importance of eliminating the pentoxide and take SQMS at the leading edge of coherence
Studies continue with more materials and passivation schemes under fabrication/evaluation
Goal is to reach world record coherence systematically above milliseconds
Manuscript in preparation

## Slide 39: Round Robin experiment - Launched the first systematic cross-institutional benchmarking study of qubit performance
INFN/Gran Sasso
UColorado/NIST
Rigetti
Fermilab
Paper accepted

## Slide 40: SQMS Devices Integration: research ongoing for 3D architecture

## Slide 41: Progress in 3D architecture
Fermilab SRF group has demonstrated the world’s record photon lifetime in quantum regime with coherence up to 2 seconds
A. Romanenko et al, Phys. Rev. Applied 13, 034032, 2020
SQMS 3D QPU roadmap, courtesy of Tanay Roy
Single photon Fock state generation demonstrated

## Slide 42: Large Cryogenics Facilities for quantum: Colossus
Ambient
80-K (Liquid Nitrogen)
4-K (Liquid Helium)
2-K (Superfluid Helium)
1-K (DR Still)
20-mK (MC 2)
100-mK (MC 1)
2m diameter volume x 1m high
Capitalizing on millions of dollars in previous investments in cryogenic infrastructure, we have launched the design of a record size dilution fridge, capable of hosting thousands of qubits, with the goal to host our first quantum computer prototype at Fermilab, or large networks of quantum sensors for physics experiments

## Slide 43: Larger Cryogenic Facilities – a Concept for a “Quantum Data Center”
The Colossus developments have attracted substantial interest from industry sich as IBM, Rigetti, Form Factor, etc. The use of liquid helium rather than mechanical coolers makes the construction of large individual platforms possible but can also support multiple small cryostats from a central plant.
DISTRIBUTION SYSTEM
Central LHe plant
Image:
Fermilab
Courtesy of M. Hollister

## Slide 44
Carolyn B. Parker first African American woman
to earn a postgraduate degree in physics
Postdoctoral Fellowship
increase representation
and inclusion of URM individuals
SQMS summer internships
SQMS summer schools

## Slide 45: Ecosystem Advisory Board

## Slide 46: Science, Technology and Management Advisory Board

## Slide 47: Playing an important role in the national QIS ecosystem
The National Quantum Centers bridge the gap from blue sky ideas to prototypes to commercial platforms