## Slide 1: News on MQXF magnet assembly
S. Izquierdo, J. Ferradas, P. Quassolo, A. Milanese, N. Lusa, S. Triquet, S. Straarup, M. Guinchard, S. Mugnier, K. Kandemir
… and many more. On behalf of the full MQXF team!
Based on internal report: https://indico.cern.ch/event/1217344/
CERN, 19 January 2023

## Slide 2: CONTENTS
MQXFB:
  MQXFB02 Cold test results (Focus on mechanics)
  Highlights on MQXFBMT4 magnet assembly
MQXFS:
  MQXFS7g magnet assembly.
  MQXFS8 magnet assembly.

## Slide 3: CONTENTS
MQXFB:
  MQXFB02 Cold test results (Focus on mechanics)
  Highlights on MQXFBMT4 magnet assembly
MQXFS:
  MQXFS7g magnet assembly.
  MQXFS8 magnet assembly.

## Slide 4: MQXFB02 – Cold tests
100% of the mechanical instrumentation (Optical for coils and Electrical for rods) is working well at 1.9 K and during the powering phases.
See https://indico.cern.ch/event/1213692/
Larger winding pole unloading in LE and RE measurement locations. Consistent with expectations (larger coil size / pre-load in the middle of the coils).
Target pre-load attained. Unloading at ~ 0.9 – 0.95 Inom
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 5: MQXFB02 – Cold tests
Detailed results:
Strain - Lead End
M. Guinchard, S. Mugnier and K. Kandemir
Noise seems an artifact from the holding current. Kinks may be related to the peak tracking. Under investigation.
Wavy z-signal not understood. Also under investigation.

## Slide 6: MQXFB02 – Cold tests
Detailed results:
Strain - Center
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 7: MQXFB02 – Cold tests
Detailed results:
Strain - Return End
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 8: MQXFB02 – Cold tests
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 9: MQXFB02 – Cold tests
Detailed results:
Stress - Lead End
M. Guinchard, S. Mugnier and K. Kandemir
 | LE |  |  |  | 
 | CR121 | CR123 | CR124 | CR125 | 
Avg | 102 | 120 | 91 | 113 | 
Max | 110 | 128 | 102 | 113 | 
Min | 98 | 112 | 78 | 113 | 
 |  | Avg | 98 |  | 
 |  | Max | 128 |  | 
 |  | Min | 78 |  | 

## Slide 10: MQXFB02 – Cold tests
Detailed results:
Stress - Center
M. Guinchard, S. Mugnier and K. Kandemir
 |  | CE |  |  |  | 
 |  | CR121 | CR123 | CR124 | CR125 | 
 | Avg | 115 | 116 | 111 | 132 | 
 | Max | 128 | 131 | 123 | 142 | 
 | Min | 106 | 107 | 104 | 123 | 
 |  |  | Avg | 115 |  | 
 |  |  | Max | 142 |  | 
 |  |  | Min | 104 |  | 

## Slide 11: MQXFB02 – Cold tests
Detailed results:
Stress - Return End
M. Guinchard, S. Mugnier and K. Kandemir
 | RE |  |  | 
 | CR121 | CR123 | CR124 | CR125
Avg | 87 | 103 | 97 | 100
Max | 98 | 110 | 105 | 117
Min | 75 | 95 | 89 | 92
 |  | Avg | 98 | 
 |  | Max | 117 | 
 |  | Min | 75 | 

## Slide 12: MQXFB02 – Cold tests
Axial rods behaviour at cold in line with MQXFBP3.
Comparison to FE model:
Regarding the magnet cool-down, final rod tension is 15 % lower than expected.
Magnet globally behaves as iron. Rods increase their tension at cold.
What could help to come closer to measurements? Lower friction or lower long. stiffness of the structure.
During energization: larger elongation than predicted by the numerical model. Still, this is very low, in terms of electromagnetic forces we see 5% of Fz during powering vs 2% we expect to see based on ANSYS.
What could help to come closer to measurements? Lower friction or lower long. stiffness of the structure.
 |  | Δ Rod Strain CD | Δ Rod Strain 16.23 kA | Δ Rod Strain CD | Δ Rod Strain 16.23 kA
 |  | FEM | FEM | [µɛ] | [µɛ]
 |  | [µɛ] | [µɛ] |  | 
Magnet | MQXFBP1 | 670 | 35 | 452 | 70
 | MQXFBP2 |  |  | 461 | 55
 | MQXFBP3 |  |  | 517 | 75
 | MQXFB02 |  |  | 571 | ~ 75

## Slide 13: CONTENTS
MQXFB:
  MQXFB02 Cold test results (Focus on mechanics)
  Highlights on MQXFBMT4 magnet assembly
MQXFS:
  MQXFS7g magnet assembly.
  MQXFS8 magnet assembly.

## Slide 14: MQXFBMT4 – Assembly
MQXFBMT4 assembled with 3 (non-virgin) coils from MQXFBP1 and CR127 (Virgin).
Shimming plan defined based on the virgin coil measurements for all coils, targeting for the best geometrical compensation at cryogenic temperature. We assume a consistent decrease in size for the new coil.
G. Vallone, M. Guinchard et al.
Let’s consider it as BP1
After disassembly

## Slide 15: MQXFBMT4 – Assembly
Coilpack centering performed successfully (all operations went smoothly).
Magnet pre-loading (as well) smooth up to the insertion of the 13.7 mm loading keys.
Then, bladder failure occurred at 390 bar, when preparing for the insertion of the last 13.8 mm keys.
  All 13.7 mm keys were in place at the moment of the failure. All bladder circuits were connected ensuring continuity along the magnet longitudinal axis.
  Failure mode indicate that the bladder was out of the masters (not supported). Positioning was checked before starting the loading. A second bladder was replaced preventively for the same reason.

## Slide 16: MQXFBMT4 – Assembly
Fast mechanical transient as a result of the sudden (and local) drop in pressure.
  Increase in comp. az. strain for CR107 and CR104 (diametrically opposite). Inverse effect for CR127 and CR105. Nothing seen on the RE side, covered by a different bladder.
  The strain/spread among coils increases (up to a factor of 2 in the MI station) after the failure.
LE - εθ
MI - εθ
RE - εθ
LE - εz
MI - εz
RE - εz
Bladder failure
M. Guinchard, S. Mugnier, K. Kandemir

## Slide 17: MQXFBMT4 – Assembly
Non-Conformity report for the bladder failure in EDMS 2803022.
Two bladder cycles up to 390 bar performed upon restart of the pre-loading operations. Half of the created imbalance among coils could be recovered (see previous slide).
Loading completed with the insertion of 13.8 mm keys. Magnet is within specifications except for the coil peak stress. The latter happens in CR107, which has already seen larger stress values during MQXFBP1 assembly and cold test.
  Average shell stress (three stations): 58 MPa - Target: +58 ± 6 MPa
  Average coil stress (winding pole, three stations): -71 MPa - Target -70 ± 10 MPa
  Peak coil stress (winding pole, three stations): -107 MPa - Target -100 MPa

## Slide 18: MQXFBMT4 – Assembly
As in MQXFBP1 and MQXFBMT2, a large drift in the FBG strain measurements follows after finishing the magnet pre-load (already seen during the break at lunch time, previous slide).
M. Guinchard, S. Mugnier, K. Kandemir

## Slide 19: MQXFBMT4 – Assembly
In MQXFBMT2 it was proven that such a drift only happened for FBG (SGs, also present, were stable). Once unloaded, the offset remained in the strain readings.
Drift does not happen after bladder failure in short models. Inhomogeneous FBG loading along the length?
Interestingly, both in BP1 and MT4 the strain stabilizes at the same value. To be continued…
M. Guinchard, S. Mugnier, K. Kandemir
MQXFBMT2

## Slide 20: MQXFBMT4 – Assembly
Chart: Pole azimuthal stress , MPa
| MQXFBP1 - LE | MQXFBP1 - MI | MQXFBP1 - RE | MQXFBP2 - LE | MQXFBP2 - MI | MQXFBP2 - RE | MQXFBP3 - LE | MQXFBP3 - MI | MQXFBP3 - RE | MQXFB02 - LE | MQXFB02 - MI | MQXFB02 - RE | MQXFBMT4 - LE | MQXFBMT4- MI | MQXFBMT4 - RE
Warm, > 24 hours after loading | -85 | -98.75 | -77.5 | -101.1679 | -80.8571 | -76.6 | -76.9642 | -83.6775 | -65.7623 | -67.1114 | -63.32 | -59.1304 | -72.3221 | -76.5257 | -62.9014
Max. during bladders | -104.9583 | -128.8421 | -97.7585 | -126.7724 | -98.7439 | -104.2862 | -118.1958 | -107.3778 | -110.2044 | -40.4996 | -26.7932 | -32.2921 | -87.2475 | -86.55 | -65.12

## Slide 21: MQXFBMT4 – Assembly
Coil stress:
Average shell stress (3 stations): 58 MPa
Average coil stress (winding pole, 3 stations): -71 MPa
Peak coil stress (winding pole, 3 stations): -107 MPa

## Slide 22: MQXFBMT4 – Assembly
Improved alignment of the mechanical structure following the lessons learnt from MQXFBP3 (already implemented in MQXFB02 and MQXFBMT3).
View from the top (alignment in the horizontal axis):
CS
NCS
MQXFBMT4
S. Straarup, M. Parent

## Slide 23: CONTENTS
MQXFB:
  MQXFB02 Cold test results (Focus on mechanics)
  Highlights on MQXFBMT4 magnet assembly
MQXFS:
  MQXFS7g magnet assembly.
  MQXFS8 magnet assembly.

## Slide 24: Before MQXFS7g…
Data: Salvador Ferradas Troitino, Franco Mangiarotti
MQXFS7f pre-load at cold ≈ 140 MPa
As expected, increase on pole azimuthal stress of 20 MPa

## Slide 25: MQXFS7g – Assembly
New iteration on MQXFS7, increasing by 0.1 mm the thickness of the loading keys (to 14 mm)
Tubular bladders re-used from MQXFS8 (flattened).
Bladder failure at 400 bar, when inserting the last 14 mm key. Contrary to MQXFBMT4, one key missing all along the magnet length.
Measured peak az. stress ~ 145 MPa. Large coil imbalance upon completion of the pre-load.
NCR for the bladder failure in progress.
Bladder failure
2D FE simulations for the failure case
Peak ~ 145 MPa
Δ ~ 40 MPa
Key
missing
Ref.
(P. M. Quassolo)

## Slide 26: MQXFS7g – Assembly
In this case, the bladder failure mode seems to be related with a potential weakness induced by the re-flattening of already used bladders. Note that bladder stroke in the cooling hole channels is large.
Furthermore, 14 mm keys are obtained by shimming 13.5 mm keys with additional 0.5 mm. Difficult key insertion. Time under pressure was relatively long.
For long MQXFB magnets, bladders are re-used only for disassembly. In this case, they are not re-laminated. Instead, thinner shims are used.
Failure mechanism has been identified for MQXFBMT4 and MQXFS7g. Corrective actions will be adopted to minimize the risk of failure in the future.
Notes: Insertion using the “train”

## Slide 27: CONTENTS
MQXFB:
  MQXFB02 Cold test results (Focus on mechanics)
  Highlights on MQXFBMT4 magnet assembly
MQXFS:
  MQXFS7g magnet assembly.
  MQXFS8 magnet assembly.

## Slide 28: MQXFS8 – Assembly
MQXFS8 assembled with 2 non-virgin and 2 virgin coils.
All new tubular bladders used. Same procedure as MQXFB.
Centering and loading went extremely smoothly.
Pre-loading within specifications (rods not shown for simplicity).

## Slide 29: Thank you for your attention!

## Slide 30: ANNEX

## Slide 31: MQXFB02: Coil Size
Chart: Coil L+R (no ends)
| 400 | 600 | 800 | 1000 | 1200 | 1400 | 1600 | 1800 | 2000 | 2200 | 2400 | 2600 | 2800 | 3000 | 3200 | 3400 | 3600 | 3800 | 4000 | 4200 | 4400 | 4600 | 4800 | 5000 | 5200 | 5400 | 5600 | 5800 | 6000 | 6200 | 6400 | 6600 | 6800 | 7000 | 7200
CR125 | 0.0025 | -0.0155 | -0.061 | -0.098 | -0.1025 | -0.0825 | -0.0325 | -0.0315 | -0.016 | -0.054 | 0.0365 | 0.0785 | 0.103 | 0.0105 | 0.01 | 0.1775 | 0.0715 | 0.0225 | 0.1105 | 0.063 | -0.0145 | -0.0005 | 0.009 | 0.011 | -0.0015 | 0.0035 | -0.0945 | -0.0035 | -0.004 | -0.092 | -0.076 | -0.0455 | -0.017 | -0.031 | -0.0845
CR123 | -0.0075 | -0.0135 | -0.0605 | -0.085 | -0.076 | -0.1055 | -0.062 | -0.085 | -0.062 | -0.058 | 0.0125 | 0.0495 | 0.0535 | -0.0445 | 0.019 | 0.1685 | 0.0675 | 0.047 | 0.0995 | 0.0705 | 0.0505 | -0.0195 | 0.052 | 0.081 | -0.024 | -0.04 | -0.095 | -0.03 | -0.05 | -0.106 | -0.0815 | -0.0395 | -0.031 | -0.019 | -0.119
CR121 | 0.032 | -0.0545 | -0.017 | -0.046 | -0.001 | -0.0465 | 0.0155 | -0.0325 | 0.026 | 0.038 | 0.0925 | 0.175 | 0.14 | 0.1045 | 0.0755 | 0.196 | 0.11 | 0.105 | 0.098 | 0.0245 | 0.022 | -0.0215 | 0.0785 | 0.0675 | 0.02 | -0.0375 | -0.0415 | -0.0105 | 0.004 | -0.0855 | -0.064 | -0.035 | 0.024 | -0.0075 | -0.0125
CR124 | -0.178 | -0.1405 | -0.1445 | -0.169 | -0.1735 | -0.227 | -0.1515 | -0.158 | -0.187 | -0.09 | -0.0795 | -0.028 | -0.024 | -0.041 | -0.0535 | 0.0195 | -0.024 | 0.047 | 0.078 | -0.037 | -0.1045 | -0.026 | -0.035 | -0.015 | -0.0355 | -0.095 | -0.076 | -0.092 | -0.086 | -0.2235 | -0.206 | -0.2165 | -0.1615 | -0.177 | -0.193
 |  | Average (Including ends) | Average (Excluding ends)
Azimuthal excess L+R [µm] | CR125 | -39 | -7 (0)
 | CR123 | -51 | -16 (0)
 | CR121 | -5 | 27 (+50)
 | CR124 | -117 | -100 (-100)
 | Shim
CR125 | 50
CR123 | 50
CR121 | 0
CR124 | 150

## Slide 32: MQXFB02 -250 um shimming plan
Azimuthal size and expected stress variation along the length (w.r.t. average)
Chart: Distance from the LE end, mm
| 400 | 600 | 800 | 1000 | 1200 | 1400 | 1600 | 1800 | 2000 | 2200 | 2400 | 2600 | 2800 | 3000 | 3200 | 3400 | 3600 | 3800 | 4000 | 4200 | 4400 | 4600 | 4800 | 5000 | 5200 | 5400 | 5600 | 5800 | 6000 | 6200 | 6400 | 6600 | 6800 | 7000 | 7200
Average | 0.02475 | 0.0065 | -0.00825 | -0.037 | -0.02575 | -0.052875 | 0.004875 | -0.01425 | 0.00275 | 0.0215 | 0.078 | 0.13125 | 0.13062 | 0.069875 | 0.07525 | 0.20287 | 0.11875 | 0.11788 | 0.159 | 0.09275 | 0.050875 | 0.045625 | 0.088625 | 0.098625 | 0.05225 | 0.02025 | -0.01425 | 0.0285 | 0.0285 | -0.06425 | -0.044375 | -0.021625 | 0.016125 | 0.003875 | -0.03975
Max | 0.0525 | 0.0365 | 0.0055 | -0.019 | -0.001 | -0.0325 | 0.0175 | 0.0185 | 0.034 | 0.06 | 0.0925 | 0.175 | 0.153 | 0.109 | 0.0965 | 0.2275 | 0.126 | 0.197 | 0.228 | 0.1205 | 0.1005 | 0.124 | 0.115 | 0.135 | 0.1145 | 0.055 | 0.074 | 0.058 | 0.064 | -0.042 | -0.026 | 0.0105 | 0.033 | 0.031 | -0.0125
Min | -0.028 | -0.0545 | -0.017 | -0.048 | -0.0525 | -0.077 | -0.012 | -0.035 | -0.037 | -0.008 | 0.0625 | 0.0995 | 0.1035 | 0.0055 | 0.06 | 0.1695 | 0.11 | 0.0725 | 0.098 | 0.0245 | 0.022 | -0.0215 | 0.059 | 0.061 | 0.02 | -0.0375 | -0.045 | -0.0105 | 0 | -0.0855 | -0.064 | -0.0665 | -0.0115 | -0.027 | -0.069
FBG | -5 | 5
FBG | -5 | 5
FBG | -5 | 5

## Slide 33: MQXFBMT4 – Assembly
“Tricky coilpack”. FUJI tests confirmed the expected mechanical contact with the collars:
  Larger contact towards the mid-plane for the virgin coil (CR 127). For the non-virgin coils, contact mostly towards the winding pole.
  The geometry of the new coil is “round”. The three tested coils have the typical “squarish” geometry after test.
After test:
Before test:
*Same behavior observed for MQXFS8 magnet (2 virgin / 2 non-virgin coils)

## Slide 34: MQXFB02 – Cold tests
M. Guinchard, S. Mugnier and K. Kandemir
Noise seems an artifact from the holding current. Kinks may be related to the peak tracking. Under investigation.
Wavy z-signal (See annex) not understood. Also under investigation.

## Slide 35: MQXFB02 – Cold tests
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 36: MQXFB02 – Cold tests
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 37: MQXFB02 – Cold tests
M. Guinchard, S. Mugnier and K. Kandemir

## Slide 38: MQXFB02 – Cold tests
Quick recap: cold-mass welding preparation
Gain in azimuthal pole stress during welding: [0 MPa -5 MPa]
B02

## Slide 39: MQXFB02 – Cold tests
Quick recap: cold-mass welding preparation

## Slide 40: Bladder pressure
Bladder failure
2 bladder cycles up to the same pressure to try to recover the imbalance created by the bladder failure
Non-conform keys.
Thicker than 13.8 mm and shorter in length.
Bladder failure (LE)
When the bladder failed, 13.7 mm keys were placed in all quadrants. We were just creating the necessary gap to introduce 13.8 mm.

## Slide 41: Coil strain
LE - εθ
MI - εθ
RE - εθ
LE - εz
MI - εz
RE - εz
The bladder failure effect (happening in the LE side) is seen in the LE and MI stations.
In these two stations, the failure creates an imbalance among coils. CR127 is the most affected (virgin).
Bladder failure
Strain drift for CR107

## Slide 42: Shell strain
LE - εθ
MI - εθ
RE - εθ
LE - εz
MI - εz
RE - εz

## Slide 43: Coil stress
LE - σθ
MI - σθ
RE - σθ
LE - σz
MI - σz
RE - σz
Transitory peak above 100 MPa for CR107, which saw already larger stress levels during MQXFBP1 assembly.

## Slide 44: Shell stress
LE - σθ
MI - σθ
RE - σθ
LE - σz
MI - σz
RE - σz

## Slide 45: Loading: Bladder bursting
Bladder bursting at 392 bars with 13,7 mm keys inserted
→ Bladder busted on the LE side near the rod A on the left side

## Slide 46: Loading: Coil behavior during bladder bursting
Bladder bursting
Bladder bursting
Bladder bursting
→ Peak strain during bladder bursting: -768 µm/m

## Slide 47: MQXFBMT4 – Assembly
Two bladder cycles up to 390 Bar performed upon restart of the pre-loading operations. Half of the created imbalance among coils could be recovered.
Loading completed with the insertion of 13.8 mm keys. Magnet is within specifications except for the coil peak stress. The latter happens in CR107, which has already seen larger stress values during MQXFBP1 assembly and cold test.
  Average shell stress (three stations): 58 MPa - Target: +58 ± 6 MPa
  Average coil stress (winding pole, three stations): -71 MPa - Target -70 ± 10 MPa
  Peak coil stress (winding pole, three stations): -107 MPa - Target -100 MPa
As in MQXFBP1 and MQXFBMT2, a large drift in the FBG strain measurements follows after finishing the magnet pre-load. Understanding on-going, but drift and absolute strain values are considered non-critical.
  In MQXFBMT2 it was proven that such a drift only happened for FBG (SGs, also present, were stable). Once unloaded, the offset remained in the strain readings.
  Drift does not happen after bladder failure in short models. Inhomogeneous FBG loading along the length?
  Interestingly, both in BP1 and MT4 the strain stabilizes at the same value. To be continued…

## Slide 48: Before MQXFS7g…
Data: Salvador Ferradas Troitino, Franco Mangiarotti
Pre-load at cold ≈ 140 MPa
As expected, increase on pole azimuthal stress of 20 MPa
S7f

## Slide 49: Rods

## Slide 50: MQXFB rods
Rod relative behaviour during powering: Diﬀerence between FEM and measurements is roughly 2.5 fold.
In previous studies, a change of friction coeﬃcient of coil to collar surface from 0.16 to 0.13 led to a change in delta rod stress from 4.4 MPa to 6.9 MPa.
Changing the friction coeﬃcient in the current reference model between 0.2 and 0.3 doesn’t seem to lead to a large change in delta rod stress. A coeﬃcient of 0.16 seems already low (laminated aluminium, polyimide surface).
Instead, a variation of the axial elastic modulus in orthotropic approximation was tried for the laminated yoke. The modulus had to be lowered down to 40% (90 GPa) of the original in order to match the measured values.

## Slide 51: Rods
MQXFB - RODS |  |  |  |  |  |  | MQXFB - RODS COLD |  |  |  |  |  |  | MQXFB - RODS POWERING |  |  |  |  | 
S | XG | YG | ZG | EZ | SZ |  | S | XG | YG | ZG | EZ | SZ |  | S | XG | YG | ZG | EZ | SZ
0.00E+00 | 9.72E-02 | 9.72E-02 | 3.76E+00 | 6.23E-04 | 1.20E+08 |  | 0.00E+00 | 9.72E-02 | 9.72E-02 | 3.76E+00 | 1.36E-03 | 2.86E+08 |  | 0.00E+00 | 9.72E-02 | 9.72E-02 | 3.76E+00 | 1.40E-03 | 2.93E+08
2.48E-02 | 1.22E-01 | 9.72E-02 | 3.76E+00 | 6.05E-04 | 1.17E+08 |  | 2.48E-02 | 1.22E-01 | 9.72E-02 | 3.76E+00 | 1.27E-03 | 2.67E+08 |  | 2.48E-02 | 1.22E-01 | 9.72E-02 | 3.76E+00 | 1.31E-03 | 2.75E+08
4.95E-02 | 1.22E-01 | 1.22E-01 | 3.76E+00 | 5.87E-04 | 1.13E+08 |  | 4.95E-02 | 1.22E-01 | 1.22E-01 | 3.76E+00 | 1.19E-03 | 2.49E+08 |  | 4.95E-02 | 1.22E-01 | 1.22E-01 | 3.76E+00 | 1.22E-03 | 2.56E+08
Average |  |  |  | 6.05E-04 | 1.17E+08 |  | Average |  |  |  | 1.27E-03 | 2.67E+08 |  | Average |  |  |  | 1.31E-03 | 2.75E+08
 |  |  |  | 605 | 117 |  |  |  |  |  | 1273 | 267 |  |  |  |  |  | 1308 | 275
 |  |  |  | µstr | MPa |  |  |  |  |  | µstr | MPa |  |  |  |  |  | µstr | MPa
 |  |  |  |  | DELTA CD |  |  |  |  |  |  | DELTA POWERING |  |  |  |  |  |  | 
 |  |  |  |  | 669 |  |  |  |  |  |  | 35 |  |  |  |  |  |  | 

## Slide 52: MQXFS – Experience from short magnets
As expected from the model, the rods only see 2 % for the electromagnetic forces during powering
Small differences observed in between the two types of structures:
  Structure 1&2 (thick laminations, large gap coil to collar): 1.4 % of Femz in the rods, 0.16 friction coefficient needed to match the measurements
  Structure 3 (thin laminations, small gap coil to collar): 2.2 % of Femz in the rods, 0.13 friction coefficient needed to match the measurements
Measurements confirm that coil elongation is independent of the pre-load level, since it depends on the system stiffness. The effect of the pre-load is to increase the contact pressure coil to pole in the end region.
G. Vallone, et. al., Mechanical analysis of the short model magnets for the Nb3Sn low-beta quadrupole MQXF, IEEE Trans. Appl. Supercond., vol. 26, no. 4, 2016.
Thin laminations, 5*0.125 mm gap between coil and collar, filled with polyimide
Thick laminations, 13*0.125 mm gap between coil and collar, filled with polyimide or G10
5 MPa ≈ 0.1 mm of coil elongation
Eelis Takala