## Slide 1
SSR2 cavities mechanical design and fabrication
Donato Passarelli, Mattia Parise
FNAL-IBS Workshop
March 1-2, 2023
Click to add text

## Slide 2: Outline
PIP-II Project at Fermilab
SSR2 cavities mechanical design
  Structural analyses
  Multiphysics performance
  Cavities fabrication
  SSR Tuners

## Slide 3: PIP-II Project at Fermilab
PIP-II Scope
800 MeV, 2mA H− SRF linac, CW RF Operations
Linac-to-Booster transfer line
Accelerator Complex Upgrades
  Booster
  Recycler
  Main Injector
Conventional Facilities
PIP-II Beam Power
1.2 MW proton beam
Upgradeable to multi-MW
Proton Improvement Plan II (PIP-II) is an upgrade to Fermilab accelerator complex to enable the world’s most intense beam of neutrinos to LBNF/DUNE.
International collaboration

## Slide 4: PIP-II 800 MeV SRF Linac
SRF technology
Cryoplant
2.5kW @ 2K
CDS
Elliptical
LB650 X 9
650 MHz
HWR
162.5 MHz
Single Spoke 2
SSR2 X 7
325 MHz
Elliptical
HB650 X 4
650 MHz
10
PIP-II technology map
Single Spoke 1
SSR1 X 2
325 MHz
Room temperature technology

## Slide 5: PIP-II SRF Cavities
Name (Qty.) | HWR (8) | SSR1 (16) | SSR2 (35) | LB650 (36) | HB650 (24)
Type | Half-Wave | Single Spoke | Single Spoke | Elliptical | Elliptical
 | 0.11 | 0.22 | 0.47 | 0.61 | 0.92
Frequency | 162.5 MHz | 325 MHz | 325 MHz | 650 MHz | 650 MHz
Q0 |  |  |  |  | 
Gradient | 9.7 MV/m | 10 MV/m | 11.5 MV/m | 16.8 MV/m | 18.7 MV/m
Doping | No | No | No | Yes | Yes
Name (Qty.) | HWR (8) | SSR1 (16) | SSR2 (35) | LB650 (36) | HB650 (24)
Type | Half-Wave | Single Spoke | Single Spoke | Elliptical | Elliptical
 | 0.11 | 0.22 | 0.47 | 0.61 | 0.92
Frequency | 162.5 MHz | 325 MHz | 325 MHz | 650 MHz | 650 MHz
Q0 |  |  |  |  | 
Gradient | 9.7 MV/m | 10 MV/m | 11.5 MV/m | 16.8 MV/m | 18.7 MV/m
Doping | No | No | No | Yes | Yes
Prototype validated
Prototype built

## Slide 6
SSR2 cavities mechanical design

## Slide 7: 3D model and materials: bare cavity
Titanium Gr.2
Titanium Gr.5
Niobium
  Nb-Ti alloys will not be employed for the fabrication of the SSR2 cavity
  EB weld development of Ti Gr.2/5 to Nb is ongoing†
  Drawings are released in TC
Ring
end view
Bellows
end view

## Slide 8: 3D model and materials: bare cavity
Ring
end view
Bellows
end view
Titanium Gr.2
Titanium Gr.5
Niobium

## Slide 9: 3D model and materials: bare cavity
Ring
end view
Bellows
end view
13 mm full penetration EBW
Sealing surface is machined after EBW
A step prevents sputtering during flange EBW
Titanium Gr.2
Titanium Gr.5
Niobium

## Slide 10: 3D model and materials: bare cavity
Ring
end view
Bellows
end view
Iris stiffener improve structural performances
Weld grooves improve weld penetration
Minimum penetration on the shell side is 1.4 mm, one side only
Titanium Gr.2
Titanium Gr.5
Niobium

## Slide 11: 3D model and materials: bare cavity
Ring
end view
Bellows
end view
Titanium Gr.2
Titanium Gr.5
Niobium
Required to reduce the stress during the leak check
Weld on the cavity side is continuous, 1 mm penetration both sides

## Slide 12: 3D model and materials: bare cavity
Ring
end view
Bellows
end view
Titanium Gr.2
Titanium Gr.5
Niobium
Spoke ribs improve structural performances, reduce LFD and df/dP

## Slide 13: 3D model and materials: bare cavity
Bellows
end view
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium
3.2 mm thickness facilitate RF compatible EBW from one side only

## Slide 14: Bare cavity – exploded view

## Slide 15: 3D model and materials: jacketed cavity
  He vessel completely fabricated with Ti Gr.2
  The thickness of the He vessel is 4 mm
  Drawings are completed and checking is undergoing
Ring
end view
Bellows
end view

## Slide 16: 3D model and materials: jacketed cavity
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium
Bellows
end view

## Slide 17: 3D model and materials: jacketed cavity
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium
Bellows
end view
Coupling plate and rings reduce LFD, df/dP and improve structural stability

## Slide 18: 3D model and materials: jacketed cavity
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium
Bellows
end view
The tuning ring allows to adjust the position radially and longitudinally †

## Slide 19: 3D model and materials: jacketed cavity
Bellows
end view
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium

## Slide 20: 3D model and materials: jacketed cavity
Bellows
end view
Ring
end view
Titanium Gr.2
Titanium Gr.5
Niobium
The side port adapter and transition allow 3 DOF to compensate for welding distortions during fabrication †

## Slide 21: Jacketed cavity – exploded view

## Slide 22
Structural Analyses

## Slide 23: FEA Outline
Elastic analysis
Elastic-plastic analysis
Bare Cavity
Jacketed Cavity
Leak check
Multiple leak checks
2.05 bar
4.1 bar
2.05 bar + 140 kHz Tuning
4.1 bar + 140 kHz Tuning
MAWP
MAWP + 140 kHz Tuning
Inelastic tuning
Tuning/Stiffness
Room Temperature
Cryogenic Temperature (2K)
VTS

## Slide 24: Materials properties
Materials used:
  RRR grade pure niobium – composition according to ASTM B393-18:
    1000x1000x4.7 mm sheet,
    65 OD x 35 ID x 200 L mm tube,
    65 OD x 35 ID x 100 L mm tube,
    98 OD x 72 ID x 200 L mm tube
  Mechanical properties for FEA:
Property | Values @RT (ED0010117) | Values @2K (ED0371110)
Yield Strength (0.2% offset) | 65 MPa (43 MPa allowable†) | 317 MPa (171 MPa allowable†)
Ultimate tensile strength | 150 MPa | 600 MPa
†According to ASME II, part D, Table 1-100
  Titanium Gr.2 per spec. ASTM B265: He vessel and bare cavity reinforcements
  Mechanical properties:
  Titanium Gr.5 per spec. ASTM B265: cavity flanges due to higher hardness and resistance to wear compared to Titanium gr.2
Property | Values @RT (ASME II-D) | Values @2K (ED0371110)
Yield Strength (0.2% offset) | 275 MPa (98 MPa allowable†) | 834 MPa (319 MPa allowable†)
Ultimate tensile strength | 344 Mpa | 1117 MPa

## Slide 25: FEA Geometry
Ring
end view
Bellows
end view
  Niobium has 3.75 mm uniform thickness: fabrication and processing thickness reductions
  2-phase pipe port and WU/CD line are not included
  Bellows is not included
  Flanges are not included

## Slide 26: Study of the Niobium thickness reduction
Niobium thickness |  | 
Thickness (mm) | Material removed (μm) | Process
4.70 | 670 | Niobium forming process
4.04 | 75 | 3 light BCP (from SSR1 experience)
3.96 | 180 | Bulk BCP on the bare cavity (from SSR1 experience)
3.78 | 10 | Localized BCP before welding
3.77 | 20 | Cleaning of the Niobium sheets when received by the vendor (10 μm per side on each sheet)
3.75 | - | Minimum required Niobium thickness for the bare cavity
Total material removed: 955 μm |  | 

## Slide 27: FEA model
Bare Cavity
Jacketed Cavity
Leak check
2.05 bar
4.1 bar
2.05 bar
140 kHz Tuning
4.1 bar
140 kHz Tuning
Tuning/Stiffness
Room Temperature
Cryogenic Temperature (2K)
Elastic analysis
Mesh
Niobium 5 mm
Titanium 8 mm

## Slide 28: Linear Elastic analyses
Bare Cavity
Leak check
Jacketed Cavity
2.05 bar
4.1 bar
2.05 bar
140 kHz Tuning
4.1 bar
140 kHz Tuning
Tuning/Stiffness
Room Temperature
Cryogenic Temperature (2K)
Stress Classification Lines
Elastic analysis
  Partial penetration and stitch welds are modeled
  Fillet welds are modeled

## Slide 29: Elastic-plastic analysis
Bare Cavity
Multiple leak checks
Results
Jacketed Cavity
Room Temperature
Cryogenic Temperature (2K)
Elastic-plastic analysis
VTS
MAWP
MAWP
140kHz Tuning
Inelastic Tuning
Ring end view
Bellows
end view
Beam pipe BS
Beam pipe RS
Coupler port
Vacuum port
≈ 25 kHz

## Slide 30: ASME compliance
Bare Cavity
Multiple leak checks
Jacketed Cavity
Room Temperature
Cryogenic Temperature (2K)
VTS
MAWP
MAWP
140kHz Tuning
Inelastic Tuning
Elastic-plastic analysis
Boundary conditions
+Tuner displacement (140 kHz)
+ Hydrostatic pressure + Cooldown
Pressure
Gravity

## Slide 31: ASME compliance - MAWP
Bare Cavity
Multiple leak checks
Jacketed Cavity
Room Temperature
Cryogenic Temperature (2K)
VTS
MAWP
MAWP
140kHz Tuning
Inelastic Tuning
Elastic-plastic analysis
Results
MAWP† |  |  | 
RT | P+D | 2.95 > 2.05 bar | 
 | P+D+T1 | 3.37 > 2.05 bar | 
CT | P+D+T1 | 11.95 bar > 4.1 bar | 
 | P+D+T1+T2 | 11.61 >4.1 bar | 
P: pressure D: gravity T1: tuner displacement T2: cooldown
† According to ASME VIII, div.2, part 5

## Slide 32
Multiphysics performance
Thanks to IJCLab (France) for their contributions to the SSR2 cavity design

## Slide 33: Introduction
Minimize Lorentz Force Detuning (LFD)
Minimize sensitivity to He pressure fluctuations (DFDP)
Keep stiffness and tuning sensitivity at suitable level to allow specified tuning range
Estimate the frequency shift during manufacturing, process and test phases
The scope of Multiphysics EM-Mechanical analysis:
TRS Parameter | TRS Value
Sensitivity to LHe pressure fluctuations of dressed cavity, Hz/mbar | < 25
Lorentz Force Detuning coefficient, Hz/(MV/m)2 (Design performance goal optimized for the optional pulsed regime) | < 4
Longitudinal stiffness, kN/mm | < 16
Operating frequency tuning sensitivity, kHz/mm | > 250
Technical Requirements Specification (TRS)

## Slide 34: Tuning sensitivity, longitudinal stiffness
 | TRS | RT | 2 K
Longitudinal stiffness, kN/mm | < 16 | 14.95 | 16.72
Operating frequency tuning sensitivity, kHz/mm | > 250 | 308 | 
Displacement applied on the interface area with the tuner
1 mm
0.042 mm
0.915 mm
Coupler fixed
Deformation due to a 1 mm displacement

## Slide 35: LFD: Sensitivity to Lorentz forces detuning
Electric Field distribution, V/m
Magnetic Field distribution, A/m
[Pa]
PLorentz > 0: pushing pressure for magnetic field
PLorentz < 0: pulling pressure for electric field
Lorentz pressure normalized at 11.4 MV/m:

## Slide 36: LFD: Sensitivity to Lorentz forces detuning
To minimize the sensitivity to the Lorentz Forces Detuning (LFD):
Evaluate the contribution of the different parts of the shell to the LFD
Optimize the cavity stiffeners
-0.55
-0.1
-0.395
-0.066
-0.788
-1.65
The end walls contribute to 70% of the LFD
Lorentz Force Detuning coefficient, Hz/(MV/m)2 |  |  | 
Model | TRS Value | FNAL | IPNO
PDR model with KTuner = 70 kN/mm | < 4 | -3.65 | -3.87

## Slide 37: LFD: Sensitivity to Lorentz forces detuning
[m]
Deformation due to Lorentz pressure normalized at 11.4 MV/m
Tuner stiffness 30 kN/mm
0.96 µm
0.40 µm
Lorentz Force Detuning coefficient, Hz/(MV/m)2 |  | 
Model | TRS Value | FEM
FDR model with KTuner = 30 kN/mm | < 4 | -4.73
  LFD : LFD with infinitely rigid tuner
  : Tuning sensitivity (-308kHz/mm)
  : Reaction force at the interface with
  infinitely rigid tuner (36.8N)
TRS
LFD = -2.9
FEM results
, 2.9 < |LFD| < 8
|LFD| < 4 for KTuner > 63 kN/mm
FDR model

## Slide 38: df/dp: Sensitivity to LHe pressure fluctuations
To minimize the sensitivity to Helium pressure fluctuations (df/dP):
 Find the optimal bellows diameter to achieve DFDP = 0 Hz/mbar
The flexibility of the bellows under pressure generates a resultant force at the bellows connections:
Fbellows reaction = PHe x
As the bellows isn’t included in the FEM, the bellows reaction forces are applied in the mechanical analysis
Assumptions:
Depth of convolution: w = 20 mm
Rint = 158 mm
PHe = 1 bar
Fbellows reaction = 1024 N
R int
R hyd
Rext
PHe
Fbellows_reaction
w

## Slide 39: df/dp: Sensitivity to LHe pressure fluctuations
0.76 (Hz/mbar)/mm
Ktuner = 30 kN/mm
Total deformation due to PHe = 1 bar
Displacements along the beam axis due to PHe = 1 bar
30µm
-8µm
Z
-50µm
-80µm
Tuner stiffness 30 kN/mm
Tuner stiffness 30 kN/mm
NB: with KBellows < 800 N/mm, the bellows elongation produces a negligible reaction force
[m]

## Slide 40: df/dp: Sensitivity to LHe pressure fluctuations
TRS < 25 Hz/mbar
DFDP = -0.27
DFDP = -0.16
  DFDP : DFDP with infinitely rigid tuner
  : Tuning sensitivity (-308kHz/mm)
  : Reaction force at the interface with
  infinitely rigid tuner (12.9N with R=158mm; -86.7N with R=159mm)
For Rint_Bellows = 158 mm,
, -0.5 < DFDP < -0.27
For Rint_Bellows = 159 mm,
, -0.16 < DFDP < 1.4
 | TRS Value | FDR model Rint_Bellows = 158mm & KTuner = 30 kN/mm
Sensitivity to LHe pressure fluctuations of dressed cavity, Hz/mbar | < 25 | -0.35

## Slide 41: Effect of welds and wall thickness on the RF Sensitivity
 | % of penetration ( "-" = full penetration) |  |  |  |  |  |  |  |  |  | 
Weld number | REF | W1 | W3 | W5 | W7 | W9 | W11+W12 | W13+W14 | W15+W16 | W17 | All not full welds
W1 | - | 66 | - | - | - | - | - | - | - | - | 66
W3 | - | - | 30 | - | - | - | - | - | - | - | 30
W5 | - | - | - | 30 | - | - | - | - | - | - | 30
W7 | - | - | - | - | 30 | - | - | - | - | - | 30
W9 | - | - | - | - | - | 30 | - | - | - | - | 30
W11 + W12 | - | - | - | - | - | - | 30 | - | - | - | 30
W13 + W14 | - | - | - | - | - | - | - | 30 | - | - | 30
W15 + W16 | - | - | - | - | - | - | - | - | 30 | - | 30
W17 | - | - | - | - | - | - | - | - | - | 33 | 33
DFDP [Hz/mbar] | -1.90 | -1.90 | -2.44 | -2.08 | -2.19 | -2.00 | -1.83 | -1.70 | -2.04 | -2.04 | -3.12
LFD [Hz/(MV/m)²] | -3.78 | -3.78 | -3.83 | -3.78 | -3.79 | -3.79 | -3.78 | -3.78 | -3.79 | -3.79 | -3.89
DFDP - DFDPREF | 0.00 | -0.01 | -0.54 | -0.18 | -0.30 | -0.10 | 0.07 | 0.19 | -0.15 | -0.14 | -1.23
LFD - LFDREF | 0.00 | 0.00 | -0.05 | -0.01 | -0.01 | -0.01 | -0.01 | 0.00 | -0.02 | -0.01 | -0.12
KCAV @2K [kN/mm] | 16.6 |  |  |  |  |  |  |  |  |  | 16.59
W1
W3
W7
W5
W9
W11
W12
W13
W14
W15
W16
W17
Small worsening of LFD  0.12
Small worsening of DFDP  1.23
No change of tuning sensitivity
No change of cavity stiffness
 The welds have minimal impact on the RF sensitivities
Effect of welds on the RF sensitivity:
Assumption: cavity wall thickness = 3.75 mm; tuner stiffness = 70 kN/mm

## Slide 42: Effect of welds and wall thickness on the RF Sensitivity
Effect of wall thickness on the RF sensitivity:
N° | Area | REF/Welds | Deep drawing | Spin-ning
1 | Spoke bar | 3.75 | 3.75 | 3.75
2 | Cylinder/beam pipes | 3.75 | 4.4 | 4.4
3 | Weld area | 3.75 | 3 | 3
4 | Top endwall | 3.75 | 4.4 | 3.45
5 | Peak endwall | 3.75 | 4.35 | 3.93
6 | Bottom 1 | 3.75 | 4.2 | 3.45
7 | Bottom 2 | 3.75 | 3.4 | 3.45
8 | Bottom 3 | 3.75 | 2.8 | 3.45
9 | Flat area | 3.75 | 3.05 | 3.75
2
1
2
3
4
5
9
7
6
8
FEM with shell elements (different thicknesses)
Thickness decreases from 4.7 mm Niobium sheets due to the fabrication and chemical processing :
Cleaning the sheets + Bulk BCP + Light BCP = 300 µm
Forming process of the endwalls:
  Deep drawing: numerical simulation (M. Parise)
  Metal spinning: extrapolation from measurements of MYRRHA/ESS cavities
Deep drawing:
Metal spinning:
Area with thickness
< 3.75mm
 | REF | All not full welds | Welds+Deep drawing | Welds+Metal spinning
DFDP [Hz/mbar] | -1.90 | -3.12 | -4.13 | -4.26
LFD [Hz/(MV/m)²] | -3.78 | -3.89 | -3.70 | -3.82
DFDL [kHz/mm] | 331 | 331 | 324 | 331
KCAV @2K [kN/mm] | 16.6 | 16.59 | 19.6 | 16.58
Improvement of LFD  0.07/0.2 due to the thickness of the cylinder and top endwalls (>>3.75mm)
Worsening of DFDP  1.1
Slight change of tuning sensitivity
Cavity stiffness  Increasing with deep drawing; no change with spinning
 The variations of the wall thickness have minimal impact on the RF sensitivities.

## Slide 43: Frequency shift during manufacturing, processing & test
Leak check
BCP
H degassing
Fine RF tuning
BCP
L
L
f for 1mm added
Coarse RF tuning
DFDP
f with the cool down 293K  2K
VTS test
f with displacement
LFD
f with vacuum in RF volume
Manufacturing phase
Trimming of Endwalls
Jacketing
EBW Endwalls
Processing phase
Test phase
Frequency shift measured experimentally
Calculable frequency shift

## Slide 44: Trimming operation
L
L
Frequency shift due to trimming (1 mm added on each side): | +289.4 kHz
Trimming operation: 1mm added on each side |  | 
Numbers | Ansys [kHz] | CST [kHz]
2 | +476 | +480
Comparison FEM/ Experimental results on MYRRHA cavities:

## Slide 45: Leak check effect – RF frequency
Frequency shift due to vacuum pumping in the RF volume | -190.5 kHz
 |  | Numbers | Measures [kHz] | Ansys [kHz]
SSR1 | Single Spoke cavity | - | [-250 ; -300] | -305
MYRRHA | Single Spoke cavity | 1 | -125 | -113
ESS | Double Spoke cavity | 1 | -56 | -49
Comparison FEM/ Experimental results on several dressed cavities:
0.48mm
-45µm

## Slide 46: Cool down from 293K to 2K
Frequency shift due to cool down 293K 2K | +456.8 kHz
 |  | Numbers | Measures [kHz] (293K/Patm2K/Vacuum) | Ansys (293K 2K) | r
MYRRHA | Single spoke cavity | 2 | [+576 ; +603] | +500 | +104
ESS | Double spoke cavity | 7 | [+606 ; +628 ] | +501 | +104
Comparison FEM/ Experimental results on some cavities with Titanium helium vessel:
L2 = 277.4mm,
L2 = -0.39mm
L1 = 629mm, L1 = -0.95mm
Calculation:
L1 = - Nb x L1 x (293 – 2)
L1 = -0.906mm
L2 = - Nb x L2 x (293 – 2)
L2 = -0.4mm

## Slide 47: Summary of Multiphysics Analyses
 | TRS Value | FDR model
Sensitivity to LHe pressure fluctuations of dressed cavity, Hz/mbar | < 25 | -0.35
Lorentz Force Detuning coefficient, Hz/(MV/m)2 | < 4 | -4.73
Longitudinal stiffness, kN/mm | < 16 | 16.7
Tuning sensitivity, kHz/mm | > 250 | 308
Leak check, kHz | - | -190.5
Cool down from 293K to 2K, kHz | - | +456.8
Trimming 1mm added on each side, kHz | - | +289.4

## Slide 48
Niobium

## Slide 49: Niobium
Materials ordered for the fabrication of 8 PIP-II SSR2 cavities:
  RRR grade pure niobium – composition according to ASTM B393-18:
    1000x1000x4.7 mm sheet
    98 OD x 72 ID x 200 L mm tube
    65 OD x 35 ID x 200 L mm tube
    65 OD x 35 ID x 100 L mm tube
    1000x1000x4.7 mm
    65OD x 35ID x 100L mm
    65OD x 35ID x 200L mm
    98OD x 72ID x 200L mm
Quantity 22
Quantity 40
Quantity 11
Quantity 11

## Slide 50
SSR cavities fabrication

## Slide 51: Prototype SSR1 cavities
10 prototype SSR1 cavities were designed, fabricated, tested and integrated into a cryomodule.

## Slide 52: Pre-production SSR2 cavities
11 SSR2 cavities are being fabricated. 3 cavities are currently being processed and cold tested. Working to resolve FE limiting performance.

## Slide 53: Production SSR1 and SSR2 cavities
9 production SSR1 cavities are being fabricated. The first one is planned to be cold tested by end of CY2023.
39 production SSR1 cavities will be fabricated in 2024-2025.

## Slide 54
SSR tuners

## Slide 55: SSR tuners
References:

## Slide 56: Thank you for your attention!