## Slide 1: Magnet Fabrication Travelers, Non-Conformities and Resolution
Katherine Ray, Mike Solis, Jennifer Doyle
March 28, 2023 – MQXFA15 Structure and Loading Review

## Slide 2: Overview
State of the Magnet Fabrication Travelers
Non-Conformances on MQXFA15
Structural Components
  Shell
  Yoke laminations and stacks
  Master keys
  Load pad laminations and stacks
  Collar laminations
Assembly

## Slide 3: Magnet Fabrication Travelers Overview
# | Title | Revision | ID
1 | Coil Acceptance WI | C | SU-1011-5294
2 | Coil CMM WI | A | SU-1012-3958
3 | Yoke Pre-Stack WI | C | SU-1008-8072
4 | Yoke Half Stack WI | G | SU-1009-7829
5 | Shell Instrumentation WI | H | SU-1009-3745
6 | Shell-Yoke Assy WI | F | SU-1008-2169
7 | Loadpad Pre-Stack WI | B | SU-1008-8075
8 | Dressed Coil WI | M | SU-1008-8073
9 | Pad-Collar Assy WI | G | SU-1010-1610
10 | Coil Pack Subassy WI | H | SU-1008-8074
11 | Magnet Electrical QA at LBNL | K | SU-1010-1903
12 | Magnetic Measurements | B | SU-1010-2018
13 | Integration and Loading WI | J | SU-1011-5637
14 | Axial Rods Instrumented WI | F | SU-1008-8069
15 | Connectors and Finishing WI | D | SU-1012-5517
16 | Splice Box WI | G | SU-1008-8067
17 | Magnet Shipping WI | E | SU-1011-3284
18 | Disassembly WI | A | SU-1013-8309

## Slide 4: Magnet Fabrication Travelers Overview
# | Title | Revision | ID
1 | Coil Acceptance WI | C | SU-1011-5294
2 | Coil CMM WI | A | SU-1012-3958
3 | Yoke Pre-Stack WI | C | SU-1008-8072
4 | Yoke Half Stack WI | G | SU-1009-7829
5 | Shell Instrumentation WI | H | SU-1009-3745
6 | Shell-Yoke Assy WI | F | SU-1008-2169
7 | Loadpad Pre-Stack WI | B | SU-1008-8075
8 | Dressed Coil WI | M | SU-1008-8073
9 | Pad-Collar Assy WI | G | SU-1010-1610
10 | Coil Pack Subassy WI | H | SU-1008-8074
11 | Magnet Electrical QA at LBNL | K | SU-1010-1903
12 | Magnetic Measurements | B | SU-1010-2018
13 | Integration and Loading WI | J | SU-1011-5637
14 | Axial Rods Instrumented WI | F | SU-1008-8069
15 | Connectors and Finishing WI | D | SU-1012-5517
16 | Splice Box WI | G | SU-1008-8067
17 | Magnet Shipping WI | E | SU-1011-3284
18 | Disassembly WI | A | SU-1013-8309
We continue to update the travelers based on lessons learned.

## Slide 5: Change Records
We are tracking Non-Conformances, Deviations and Engineering Changes in one spreadsheet
These are currently communicated to Fermilab L2 on a monthly basis

## Slide 6: Parts to be used on MQXFA15
The following parts will be used:
Coils:
  127, 220, 226, 233
 | PO #
Shells | 7532740
Yokes | 7532497
Master Keys | 7580674
Load Pads | 7532636
Collars | 7532707

## Slide 7: Introduction

## Slide 8: Shell
Long Shell: SU-1010-1073
Short Shell: SU-1010-1072

## Slide 9: Shell
For the shell ID and OD, the following specifications are set:
The shell ID at 5 evenly spaced rings shall have an average diameter of 556 mm +0.1/-0.0
The shell OD at 5 evenly spaced rings shall have an average diameter of 614 mm +0.1/-0.0
PO 7532740 approved
NCR -0272

## Slide 10: NCR-0272

## Slide 11: NCR-0272 (cont)
 | Short # -0516 | Short # -0517 | Long # -550
ID |  |  | 
OD |  |  | 
Notes: The roundness of these shells are out of tolerance. We were able to accept them because the average diameter is still in spec with the understanding the pre-load will correct the roundness

## Slide 12: Yoke laminations and stacks

## Slide 13: Yoke laminations and stacks

## Slide 14: Yoke laminations and stacks
For the yoke outer radius, the following specifications are set:
The yoke radial profile shall maintain a 0.03 [.001”] tolerance.
For the yoke master key interface, the following specifications are set:
The yoke master key interface profile shall maintain a 0.03 [.001”] tolerance.
For the yoke pre-stacks, the following specifications are set:
588 mm Pre-stacks width shall be 588 mm +/- 0.13 with a Parallelism of 0.03 [.001”]
245 mm Pre-stacks width shall be 245 mm +/- 0.13 with a Parallelism of 0.03 [.001”]
For the yoke half-stacks, the following specifications are set:
Yoke half-stacks width shall be 2281.5 mm +/- 0.25 with a Parallelism of 0.05
PO 7532497 approved
  NCR -0226

## Slide 15: NCR-0226
Notes: The yoke laminations had a profile spec that was out of tolerance in a various places. The maximum profile deviation was .013mm. The small deviance allowed us to accept as-is. The pre and half stacks were in tolerance.

## Slide 16: Master key

## Slide 17: Master key
For the master key outer profile, the following specifications are set:
The master key outer profile scan shall maintain a .05 [.002”] tolerance.
PO 7580674 approved
No NCR

## Slide 18: Load pads laminations

## Slide 19: Load pad pre-stacks

## Slide 20: Load pads laminations and stacks
For the load pad master key interface profile, the following specifications are set:
The Load Pad master key interface profile shall maintain a 0.03 [.001”] tolerance.
For the load pad collar key interface profile, the following specifications are set:
The Load Pad collar interface profile shall maintain a 0.03 [.001”] tolerance.
For the stainless-steel section of the pad pre-stack, the following specifications are set:
On the LE pre-stack, the LE pads shall have a stainless-steel section of 300 ± 0.6 mm and an overall pre-stack length of 1050 ±0.13 mm
On the RE pre-stack, the RE pads shall have a stainless-steel section of 200 ± 0.4 mm and an overall pre-stack length of 1088 ±0.13 mm
The 1100 pre-stack shall have an overall length of 1100 ±0.13
mm
PO 7532636 approved
  NCR -0153

## Slide 21: NCR-0453
Notes: The Load pad laminations had a profile spec that was out of tolerance in a various places. The maximum profile deviation was .006mm. The small deviance allowed us to accept as-is. The pre-stacks were in tolerance.

## Slide 22: Collar laminations

## Slide 23: Collar laminations
For the collar to load pad interface profile, the following specifications are set:
The entire collar to load pad interface profile shall maintain a 0.03 [.001”] tolerance all around.
For the collar to coil interface profile, the following specifications are set:
The collar to coil interface profile shall maintain a 0.03 [.001”] tolerance all around.
PO 7532707 approved
No NCR

## Slide 24: MQXFA15 Change Records
NCRs on A15 thus far include:
  #153 – minor load pad non-conformances
  #226 – minor yoke non-conformances
  #268 – coil 220 PHB01b label missing
  #272 – minor shell non-conformances
  #276 – coil 220 tall pin
  #359 – coil 220 GPI replaced after long storage
  #468 – coil 233 broken strands on lead 31” from LE
  #470 – coil 127 crate, 1 shockwatch tripped
  #472 – coil 127 rubbed NbTi leads due to unprotected leads discovered during in-crate inspection
  #490 – coil 127 some surface anomalies on RE OD, proud spacer in the cable turn region
  #491 – (DEV) make the SG overlap the solder tabs pad in SG prep process
  #494 – (DEV) test out wrapping leads with 0.002” thick 2/3 overlap instead of 0.002” thick 50% overlap
  #495 – coil 226 has proud pin and several proud epoxy plugs
  #497 – three load pad stacks initially placed with RE and LE reversed
  #498 – load pad bushings not fitting, need to be replaced
  #505 – G11 radial layers shifted during glue drying; redone

## Slide 25: NCR #276 Detail
Tall pins trimmed on coil 220
(Done in Oct. 2021, current instructions are to leave the pins)

## Slide 26: NCR #468 Detail
Coil 233, 31” from LE

## Slide 27: NCR #470, 472 Detail
Coil 127, 1 shockwatch tripped, others okay
Coil 127, leads crossed in crate, some discoloration noted
Previous coil for comparison

## Slide 28: NCR #490 Detail
Coil 127, spacer high
To be filed down

## Slide 29: NCR #495 Detail
Coil 226, proud pin at 2167 mm from LE