## Slide 1: MATERIALS & DETECTORS
drhgfdjhngngfmhgmghmghjmghfmf
Valentine NOVOSAD
Argonne National Laboratory
Materials Science Division
Physics Division
High Energy Physics Division
March 20, 2023
novosad@anl.gov
(アルゴンヌへようこそ !)

## Slide 2: MATERIALS SCIENCE DIVISION
SUPERCONDUCTIVITY & MAGNETISM GROUP
SUPERCONDUCTING SENSORS, DETECTORS & DEVICES R&D:
INTERNAL COLLABORATIONS
CNM
On-chip SSNPDs
for QIS
(BES Office)
HEP
Experimental
Cosmology
(HEP Office)
PHYSICS
Particles
& Light
Detectors
(NP Office)
MSD
SC - Magnonic
Hybrids
(BES Office)
MATERIALS DESIGN LABORATORY ENERGY SCIENCE BUILDING

## Slide 3: Talk Outline
INTRO (about thin films synthesis & devices)
1. “LOW Tc” SCs (Tc tuning - key to detectors improvement)
2. DIELECTRIC FILMS (low-loss & tunable optical properties)
3. ”HIGH-Tc” SCs (emerging opportunities for detectors development)
4. NANOFAB & CHARACTERIZATION TOOLS (thin films & novel detectors)
SUMMARY

## Slide 4
Credit: HEP detectors microfab team
hep journey of Silicon wafer

## Slide 5: MAGNETRON SPUTTERING
Reproducible process:
  Widely employed in industry.
Versatile:
  Allows for the synthesis of elemental materials, alloys, and layered structures.
Controllable growth of thin films:
  By adjustment the plasma parameters, substrate temperature and bias.
Metals & insulators can be grown:
  Reactive sputtering processes.
Why it matters:
- Uniquely suited process for detector R&D and device fabrication

## Slide 6: LOW Transition temp. SUPERCONDUCTORS
UHV grade
5 sputtering guns
DC/RF/Impulse + RF bias
800C sample stage
(MSD lab # ESB/A013)
Ir/Pt bilayers:
- Proximity effect - Dep. temp. effect
Why it matters:
- New low Tc superconductors for ultra-low noise TES devices
Credit: Vlad Yefremenko, HEP
G
Ptot
TB
Tc
Al: 1.2 K
Mo: 0.9 K
Ti: 0.5K
Ru: 0.5 K
Zr: 0.5 K
Ir: 0.15K
Transition temp. Tc (mK)
Ir/Pt
80nm/20nm
Deposition temp., C
Transition temp. Tc (mK)
Ir: 100nm
Pt thickness, nm
Resistivity, ohms
Stage Temperature, K
CMB-3G design

## Slide 7: Connections
For superconducting detectors, noise and threshold scale with Tc.
Materials enables lowering detector threshold
TES detector
Low Tc Dark Matter detectors (Credit: Gensheng Wang, HEP)
Low Tc MKIDs
Credit: Zhaodi Pan, HEP
Low Tc detectors for NLDB searches

## Slide 8: THIN FILM DIELECTRICS
Why it matters:
low-loss dielectrics for RF circuits
tunable optical properties
tunneling barriers
Chart: Si target + Ar/N2
| 0 | 1.5 | 3 | 6 | 9
 | 3.85 | 2.77 | 2.14 | 2.09 | 2.08
Stochiometric
Si and Si3N4
Ar flow, sccm
400 500 600 700 800 900 1000
Wavelength, nm
1.0
0.9
0.8
0.7
0.6
0.5
0.4
0.3
0.2
0.1
0.0
bare Si wafer AR-coated Si
Reflectivity
Optical constant, n
Sputtering of SiO2 (SiO2 target)
200C + RF-bias
SiO2
Nb
Nb
Sputtering of Si3N4 (Si target, RT)
UHV grade
DC/RF + RF bias
Cryo pumping
700C sample stage
Direct sputtering
5 sputtering guns
(MSD lab # MDL/H109)

## Slide 9: Connections
Resolving power of mm-wave on-chip spectrometers limited by microstrip materials loss
Future mm-wave detectors require low loss microstrip
Filter banks
OMT probe
Feedline
On-chip mm-wave spectrometers
Credit: Zhaodi Pan, HEP

## Slide 10: “HIGH-Tc” SUPERCONDUCTORS: NITRIDES via REACTIVE SPUTTERING
UHV grade
6” wafer process
Class 1000 CR
5 sputtering guns
DC/RF + RF bias
700C sample stage
Turbo + Cryo pumping
(MSD lab # MDL/H109)
Example of NbN
Why it matters:
Superconductivity fine-tuning via nitrogen content adjustment
Synthesis of new superconductors
Passivation & diffusion barrier layers
@ 250C + RF-bias
F. Carter, et al., Appl. Phys. Lett. 115, 092602 (2019)
“Bulk” Tc:~16K

## Slide 11: Connections
Hybrid Superconducting – Magnonic Devices
Remote coupling of distant magnetic resonator
Credit: Yi Li, MSD
magnon1
magnon2
YIG sphere1
YIG sphere2
Time-domain
Rabi-like oscillation
Low-loss SC circuit (NbN)
(YIG: Y3Fe5O12)
Why it matters:
On-chip coherent information trunsduction
From RF to Microwave frequency (microwave-to-optical is a possibility to)
Low-temperature operation
Magnetic field tenability
An emerging opportunity for novel dark matter particle candidates?

## Slide 12: “HIGH-Tc” SUPERCONDUCTORS: NITRIDES ION-BEAM ASSITED SPUTTERING
Conventional process
Si
N+
e-
Nb
Nb
N2
Si
IBAS process
T Polakovic, et al.,
Appl. Phys. Lett, - Materials, 6(7) 076107 (2018)
+ heating
heating
Example of NbN
UHV grade
Auto-loader / five wafers
Class 1000 CR
5 sputtering guns
Low voltage ion gun
700C sample stage
E-beam evaporator
Tiltable stage
Oversized Cryo pump
(MSD lab # MDL/H109)
Why it matters:
Synthesis of nitrides/oxides @ RT
Surface preparation + in-situ interfaces control

## Slide 13: NANO-FABRICATION FACILITIES: from SUB-MICRON TO wafer-scale
Example: superconducting nanowire single photon detector
Why it matters:
- Fast turn-around devices prototyping
High-resolution e-beam writer
Class 1000 Clean Room
Resist processing CR lab nearby
Closed-loop x-y-z stage
30 kV, sub-10nm e-beam
Earth magnetic field compensator
Vibration isolation
Multi-apertures for pattering & SEM
(MSD lab # MDL/A051)
Ion-milling tool
Titled stage
Liquid N2-cooled
From ~0.1-1kV (Ar+)
(MSD lab # ESB/H109)
Credit:
Tomas Polakovic, PHY

## Slide 14
SNSPDs are an emerging high-impact superconducting technology
  Fast timing, no dark count, high efficiency at IR
  QIS science enabling technology
Growing program at Argonne
  for DOE-BES QIS
  for DOE-NP
  for DOE-HP
The inter-divisional partnership the key to enable the success of future SNSPD-related programs
Connections
Single Photon / Single Particles Detection

## Slide 15: LOW Temperature TRANSPORT
Examples:
Measurements of R(T), Jc & in time domain
Why it matters:
- Fast samples screening & characterization
Liquid He cryostat w/ 7T magnet
300 K – 1.7K
QO four channels SNSPD readout
Commercial inserts for R(T) measurements
Ultra-fast real-time oscilloscope
(MSD lab # ESB/A013)
Commercial device
Our device
Credit:
Tomas Polakovic, PHY

## Slide 16: Particles detection
Novel application of SNSPDs:
- a particles detection
Source activity: 10 μCi
Limited by noise/interference at low bias currents → working to improve the SNR in this region
Should be able to detect ɑ particles down low Ib/Ic < 0.2
Credit:
Whit Armstrong, PHY

## Slide 17: Particles detection
Novel application of SNSPDs:
- 120 GeV protons at Fermilab
Particle | Energy | Approximate Energy loss in |  | Detected
 |  | 100 μm silicon | 15 nm NbN | 
photon | 0.1 - 2 eV | all | all | ✔
alpha | 5 MeV | 5 MeV | 9.1 keV | ✔
beta | 1 MeV | 15 keV | 15.8 eV | ✔
electron | 100 MeV | 100 keV | ~100 eV | ?
proton | 120 GeV | 40 keV | 24 eV | ✔
pion /muon | 10 GeV | 30-45 keV | ~20 eV | ?
Preliminary results show 120 GeV proton detection with superconducting nanowires.
This is a key demonstration for applications at the EIC.
nanowire signal (red)
scintillation counters (blue)
Need to scale up detector area with larger pixel arrays
Cryogenic readout electronics also needed for high channel counts
Credit:
Whit Armstrong, PHY

## Slide 18: MATERIALS R&D is foundational for Complex devices
Low Tc materials
High Tc materials
Dielectrics
Nano-patterning
Mm-wave imagers and spectrometers:
  CMB, LIM, early universe cosmology
Low threshold detectors:
  dark matter, neutrinos, NLDBD
Nano-strip devices:
  Particle detection, Quantum sensing
Materials & Devices
IN SUMMARY:
どうも ありがとう ございます !