## Slide 1
Status Update – Mar, 2023

## Slide 2: SSR2 Cavity
Cavity Component Forming
  Forming of all copper components Completed
  CMM Measurement completed and results send to FNAL
    Awaiting Approval
EBW Trials
  Trials completed; Acceptable parameters achieved for all weld types
  WPS, PQR completed for 3.2 mm Nb-Nb, 4.0 mm, 4.7mm Nb-Nb
  Weld coupon EB weld completed for 4.0 mm Nb-Ti Grade 2; Testing u/p.
  Weld coupon EB weld u/p for 13mm Nb-Ti Grade 5.
Nb Components
  Machining Completed
  Seam Weld u/p
Weld Fixture scheme and Drawing completed
  Manufacturing Under Progress

## Slide 3: SSR2 Tuner
Procurement of Standard Components
  Bellows received at BARC
  G10 has been sourced
Manufacturing under progress

## Slide 4: SSR2 Cryomodule
Charges to be addressed for PDR determined.
  Document containing details received from FNAL
TRS Requirements that will be addressed in PDR has been identified.
TRS Requirements that will be later addressed by FDR has been identified.
Document listing changes in parts to be prepared