## Slide 1
Cryogenic (and Other) Detectors for Dark Sector Searches
Dr. Rupak Mahapatra
Texas A&M University
0


## Slide 2: Cryogenic Detector Technology Developed for SuperCDMS
iZIP Detector with ionization and phonon sensors for ER/NR discrimination (>keV)
First SNOLAB Ge iZIP (fabricated at TAMU)
https://arxiv.org/pdf/1610.00006.pdf
High Voltage Detector with NTL gain. Give up discrimination in favor of low threshold (~100eV).
First SNOLAB Si HV (fabricated at TAMU)
Phonon
Ionization
7mK base temp

## Slide 3: Phonon Sensors
R0
R
T
T0
Phonons are collected by superconducting Al fins (=~meV), creating quasi particles that are then trapped by the W Transition Edge Sensors (TES), held in equilibrium between Normal and Super Conducting temp. SQUIDs measure small change in current through sharp R/T
Al
Al Collector
W Transition Edge Sensor (TES)
Ge or Si
phonons
Cooper Pair
1 m TES

## Slide 4: gm-kg scale Phonon Detectors for DM/
Ge, Si, Al2O3, SiO2, GaAs
0V, LV (few V), HV (400V)
Smallest – 10 gm Si
Largest – 1.5 kg Ge

## Slide 5: Dedicated Fab and Testing @ TAMU. 1st SNOLAB Tower Done
Polish
Deposition
Photo Coat
Circuit Mask Exposure
Chemical Etch
Multi-step process repeatable for high quality detectors
XRD
Inspect and Package

## Slide 6: Single-e Sensitive HV Detectors
100-gm single-e sensitive Contact Free Si HV Detector for MINER. Signal amplification observed without increase in leakage up to 300 V using laser
Initial demo with 250 gm Ge with =7 eV
https://doi.org/10.1016/j.nima.2017.02.032
Single-e/h pair 100 gm Si :
https://inspirehep.net/literature/1828158
SuperCDMS Collaboration 10.1103/PhysRevLett.121.051301
gm-scale Si HV @ 100V bias- resolves single e-h. Strong validation at NEXUS@FNAL

## Slide 7: Low-Threshold Sapphire Detector with No Lindhard Suppression
~5 times better (A+B+C+D) resolution than Si detector with same mask (~120eV in Si HV at 0V)
Calibrated based on 13.9KeV line.
~100 gm 3”x 4mm sapphire detector shown
~200 gm 3”x1cm sapphire detector tested
TES sensors will be optimized for the faster timing
Calibration: Internal 55Fe, 241Am and external 57Co, 252Cf, AmBe.
https://linkinghub.elsevier.com/retrieve/pii/S0168900222009263

## Slide 8: Dark Aspects of Dark Sector Searches
Background
Recoil energy in eV
Integrated rate/kg-year
Background-limited Discovery Potential? All detector technologies see similar exponential rise in “unknown” background at low energies. The DM/CENS community working to understand

## Slide 9: Hybrid HV Detector
Main idea: Monolithic detector with a LV and a HV side – LV to measure primary phonons like iZIP and HV to measure NTL phonons. Do it without significant NTL pollution from HV to LV. ~100gm
https://www.sciencedirect.com/science/article/abs/pii/S0168900222002467
Discrimination improves at low energies due to Lindhard suppression of ionization

## Slide 10: ALP Search @ Reactor/Beam
PRL: https://journals.aps.org/prl/abstract/10.1103/PhysRevLett.124.211804

## Slide 11
CsI(Tl) Single Scatter Event Selection (Active Veto)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
CsI(Tl)
Signal: Unvetoed Single-scatter event
5x5 vs 3x3 Background

## Slide 12
Trigger on E1 and Search for missing E2
PRD:https://journals.aps.org/prd/abstract/10.1103/PhysRevD.105.015030
Same MINER CsI setup is used for this experiment. Moving to LANL this summer for beam-based and source-based searches as a CCM sister experiment
ALP Search Using Nuclear Gamma Cascades

## Slide 13: Sensitivity to Dark Sector
Credit: Wei-Chih, Dutta
10eV-100 keV: Ge electron recoil
(100-kg scale G2 experiment, Can go to ton-scale for PIP2)
10 keV-100MeV: CsI Inelastic
(20-ton scale experiment)
1023 POT

## Slide 14: Searches for Lightly Ionizing Particles
Sensitivity to smallest charge directly related to Eth
  Low-threshold (10eV) detectors can search beyond -e
For modest (keV-scale threshold) charge sensitivity, large (20-ton) CsI-cube is ideal for PIP2 – ability to use tracking in segmented detector system to strongly reject background
SuperCDMS: 10.1103/PhysRevLett.127.081802

## Slide 15: Conclusion
Two strong detector technologies available for world-leading dark sector searches at PIP2
  Low-threshold phonon-mediated cryogenic Ge/Si/Sapphire detectors with sub-100 eV threshold (~10 eV for smaller dets.)
  Higher-threshold CsI(Tl) detectors that can be scaled to 20-ton scale with keV-MeV scale dynamic range
These detector technologies are already in use or soon to be used in SuperCDMS SNOLAB Dark Matter Search, MINER CENS search, CsI-Cube ALP search using reactor and missing-gamma experiments.