## Slide 1
W Pellico
Vertical Drift Photon Detector
Power over Fiber PoF
NuFact 2022 Meeting

## Slide 2: Today
PoF has moved beyond a concept – It has been successfully demonstrated
PoF has proven itself in VD PD but also industry
PoF will play a role in HEP detectors which require power delivery that offers low noise, isolation and long term viability

## Slide 3: Thanks
People that made this effort successful
  Broadcom (Led by Jan Werthen with more than 40 years of expertise)
  UIUC (Led by Professor Larry Lee and Student Bora Kim)
  MH GoPower ( Led by John Wu and MHG (president and owner))
  NASA ( Space Systems – JPL)
  FNAL (Led by Andrew Feld, Ken Koch and William Pellico)
  SDSM ( Led by David Martinez, Students Diana Leon, Alex Heindel
  Many in the field who have help test, poke and prod our PoF systems

## Slide 4: -How did we get here -
Almost a year ago we did our first PoF
  First PoF system based upon Si optical photovoltaic cells (OPC)
  Operating at wavelengths of 971 nm
  Lasers power between 2 and 3 W
  Efficiencies between 16 and 23 percent
  20 systems were built and operated
  After multiple cathode removals, cryo cycling and system connections/disconnection – not a single OPC or laser system failure or even any issue found.
  Si PoF based system met all the requirements of power, noise, and existing in the VD high voltage environment

## Slide 5: Path to Present Desire to deliver a more cost effective, lower loss PoF system
Si was successful and delivered as expected
  Si has known limitations at cold temperatures (well document over 30 years)
    Si is not well suited for space applications
    Si OPCs semiconductor design has efficiency limitations at any temperatures
  Si popularity is due to cost
  Si Vendor (GoPower) was/is extremely helpful and suppurative of expanding use.
    Chief scientist/engineers visited FNAL twice
    Vendor did initial testing of products in liquid nitrogen at their facility before shipping
From the start, options were available, but the rapid VD PD time scale required we first demonstrate the PoF concept before we could test and implement a more ideal solution.
  GaAS and similar semiconductors

## Slide 6: GaAs
Two GaAs products were available that looked to meet the needs of VD PoF
  Both vendors were contacted, and we started an extended period of discussions.
  Vendor One
    Deals exclusively in space use PoF and related technology
    Low voltage options geared to digital use in space missions (heat applied to boost efficiency)
    Limited desire to collaborate and develop cryo temp usage ( not part of business model)
  Vendor Two
    Broadcom has been a leader in communications for some time and had purchased a leader in developing of PoF technology
      New uses of PoF has made technology desirable – bought a company with 30+ years of experience
      Most importantly – they kept the original scientists who were still interested in further development
      FNAL Purchased several PoF units – tested and characterized at FNAL in argon and nitrogen
      Vendor lead PoF scientist (several visits with various tech people) is very interested in development
        Vendor has provided over 30k in free lasers and PoF modules for FNAL evaluation
        FNAL provided insight into operations and some modeling of devices

## Slide 7: GaAs
During the development of the GaAs cryo use – additional R&D was/is desired.
  A one year contract with University of Illinois school of engineering was started
    GaAs potential at cryo temps was not fully investigated
      Carrier freeze out was evident
      Tunnel junctions at cold temp became more resistive
    Build units that meet VD PD specification
      Extreme low temp ops with efficiencies of room temp devices
      No contaminants
      Use of approved material – namely epoxies/sealants
In the end a partnership between FNAL, Broadcom, UIUC and GoPower

## Slide 8: GaAs
UIUC has led the modeling –
Broadcom has led the rapid improvement of their product to meet our initial needs and longer-term product development/distribution.
GoPower has supplied all the fibers and OPC packaging options
FNAL has done most of the testing and guided the partnership to meet the VD PD needs.
Products being tested today are twice as efficient
We are moving up the power (I-V) curve meeting our needs and aligning to theoretical predictions
  Final product run is expected by the end of the year (approx. 2 dozen units)
    Power > 1 W with efficiency above 65% (expect about 72%)
    All known materials and processes -
  SOME PICTURES PLEASE

## Slide 9: GaAs Lasers now at CERN CB, FNAL TS, Italy, SDSM,UIUC
Two types of lasers
Civilaser
  Lots of functionality
    Precise temp regulation
    Modulation capable
      DUNE doesn’t need (looking to get basic system)
      Could send power and control
  Cost effective
Broadcom compact unit
  2 W capability
  25+ years CW operations
  20 units have been tested
  Housing and controls developed
  Shipped to several DUNE partners
  I adapted controls for our use – (Vendor gave all drawings)
    To allow safe commissioning
    To allow for OPC full range testing
    Last step is DUNE housing/layout

## Slide 10: Moving from R&D (Mostly) to Certification Testing
Certification of Hardware
  Fibers: Two Viable Candidates which have been used for years in PoF systems
    Bending, Installment constraints (SDSM)
    Splices (SDSM)
    Light leakage (FNAL)
  Laser,
    Two Viable Candidates (SDSM, FNAL, Italy, UIUC, Broadcom)
    Laser safety concepts/layout now in development for implementation at farsite.
  Connectors
    Lots of options (SDSM)
  OPCs
    Units currently being tested are ready to purchase
    Units meet the DUNE needs
    Next version are pin for pin compatible and will be delivered by EOY
      Hope to exploit the higher performance – requiring fewer units/less heat loss/fully modeled
      This does not impact DUNE installation plans

## Slide 11: Fiber Testing (DUNE and for Others)
Where has all the light gone?
We wanted to know about the optical power
How was it distributed
What happened at the OPC unit
What about leakage
Using a ‘bare’ fiber – you can see with IR the points of interest
Fiber light is largely contained in the core
Some OPA leakage on backend
Backscatter at fiber to OPA
Not able to see this is a jacketed fiber
But using SiPM or similar device can isolate loss points.
Backend is simply due to clear epoxy where GaAs cell is inserted.
Jacket type and thickness removes fiber leakage.
Connection point requires a slightly thicker jacket.
Fiber down select completed
Good understanding of principles at work for PoF use
Placing large bulk orders to distribute to test teams

## Slide 12: SDSM Team – Testing fibers, connectors, lasers Installation and long-term viability minded

## Slide 13
Aspects expected to be improved
Low RS enabled by thick, n+-InGaP
Suppressed majority carrier blocking
Low Rsheet (33-35 ohm/sq)
EQE enhancement by DLARC
UIUC New LPC Design to Lower Series Resistance (RS)
Design
600nm p-GaAs substrate
400nm p-GaAs buffer, p=7e18
100nm p-GaAs BSF,
p=7e18  1e17
2um p-GaAs base, p=1e17
80nm n-GaAs emitter, n=1e18
500nm n-InGaP window, n=8e18
n-GaAs
contact
TiO2/SiO2 DLARC
Au/Ti
Au/Cr
600nm p-GaAs substrate
200nm p-GaAs buffer, p=7e18
50nm p-InGaP BSF, p=1e18
2um p-GaAs base, p=1e17
50nm n-GaAs emitter, n=1e18
20nm n-AlInP window, n=1e18
n-GaAs
contact
Au/Ti
Au/Cr
50nm p-GaAs base I, p=2e18
#1
#3
-
+
h+ barrier
e-
Emitter
Window
Contact

## Slide 14
EQE boost with optimized ARC
Simply, with optimum ARC, efficiency at 190˚C will be ↑ to -54%.
(* expected values)
p+Al0.1GaAs BSF
Diffusion length ↑, barrier for minority carrier
 suppress decrease in EQE at low T
Near-Term Roadmap for >60% Efficiency GaAs LPC at Low T
ID | R808 nm at RT | EQE808 nm at RT | EQE808 nm at -190˚C
#3 | 7.0% | 75.4% | 62.2%
#3 with optimum ARC | 0.2% | 80.9%* | 66.8%*
808 nm

## Slide 15: Summary
From black board to a product that will impact DUNE and others.
PoF has worked and delivered the clean power as expected to the VD cathode plane.
Industry has already taken notice of this development
The PoF system demonstrated about a year ago it’s capability. The system installed has operated without any failures or faults. Not a single Si laser module or OPC has had to be replaced. The recently GaAs system will show improved performance and reliability.
The PoF system not only works, but it will also most certainly be expanded to others in HEP and industry.

## Slide 16: Backup –Reliability Examples (More from JPL)
I was recently told by Siemens, one of the first to deploy PoF in the late 90’s that an HVDC installation between Australia and Tasmania has been running non-stop without any component failure, incl OPC, laser and fiber, for more than 23 years. Likewise, even earlier installations by ABB in the north of Sweden have been, and still are, running non-stop since 1997. In fact, at one point I was there to replace all lasers which had been sourced from ……. The problem was that on very cold nights (-35C), the current sensing system had stopped working. It turned out that using 850nm lasers with OPCs optimized for 808nm meant that at the cold temperatures for the OPCs, they no longer responded to 850nm light. At least not as long as the lasers were comfortably located inside a control room at room temperature….; after switching all the lasers to 808nm, the problem disappeared. Little did I know back then that fast-forward 25 years, we’d be pushing the OPC to longer wavelengths for ostensibly the same reason albeit lowering the operating temperature by another 150 K.
Best regards
Jan
Chief Photonics Scientist, Broadcom
We did conduct some reliability tests over the 62.5um black fiber in the past. The fibers are installed in an outdoor high voltage (22.4kV) environment, one end was secured on the high voltage busbar and the other end on the ground. In this test setup, the fibers were exposed to high voltage, high humidity (with rain falls), and UV from the sun. Over 3 years of testing, we did not see any problem with the fibers.
Regards,
John Wu
VP, System Engineering Dept.

## Slide 17: Full set of tests for each OPC unit Power, Efficiency, Leakage (I-V curves across loads)
We have been putting together a testing and assembly standards.
Each laser, fiber and OPC will have a traveler that provides information on assembly and test performance.

## Slide 18: R&D for DUNE and Others (State of the art laser lab)
We are building a more practical fiber feedthrough:
One that does not require fibers be inserted before termination
One that can be adjusted to the fiber dimensions and count.